Polymer Laboratory Weekly Meeting Summary – 03.07.2025

- General information:

- FO and Roland visited Herzog for the design review of winding and braiding machines; design completed.

- Welcome to the two newcomers Daphnée and Filip who started this week.

- Operation & Services:

- 10-stack falcon D, and 10-stack MQXF desized are ready for impregnation, will be performed this Friday with POLAB mix.

- BORIS tube is being prepared for impregnation in the coming weeks, the gaps will be filled with 2 half-shell 3D-printed parts in Accura 48.

- Moulding of parts in silicone for leak detection (vacuum section).

- Silicone ropes to produce for 180.

- FSI heads for BE HPA in progress, 114 out of 156 produced.

- 8 PU parts to produce for electrical insulation.

- Glueing of 100 thermocouples for TE HSD.

- KSW magnet impregnated with Araldite F + dolomite for SY ABT, one left.

- 3D-printed spacers for Falcon D to complete.

- ULTEM 1010 parts to 3D-print for 180.

- Covers for electrical insulation for BE HPA to 3D-print in Accura 25.

- 20 filters holders for HSE ENV to 3D print in ABS, then 40 more.

- Projects (R&D):

- Wax impregnation: 10-stack has been de-moulded and has been cut with diamond wire for SEM examination. Samples have been dropped off at MME for analysis.

- ITER collaboration: Surface resistance measurement of Glyptal paint at room temperature and 77 K tests are completed for ITER (TF coil). Measurements at 4K will begin Friday.

- ITER collaboration: 2 to 1 design for HV wire repair completed and validated by ITER, production of 5 moulds and tests to be completed in summer (electrical tests, thermal cycles, tensile tests).

- POLAB BOX: Tooling and cable are going through Nb3Sn reaction cycle for electrical testing of insulation.

- Ceramic binder and fibres study: Qualitative tests of Rescor 901 ceramic binder with thinner completed with S2-glass interlayer configuration.

- BOND ceramic interlayer study: Ceramic prepreg plate samples going through a Nb3Sn reaction cycle to quantify the effects of the cycle on the composite.

- De-sizing study: N2-H2 plasma-desized MQXF 10-stack will be impregnated on Friday. 12-Tesla 10-stack with N2-H2 and Air plasma desizing has gone through reaction cycle and will be instrumented in the coming days before impregnation.