## Slide 1
Nb-Ti Hybrid Block Coil Designs
- From concepts to BOND-H -
Ariel Haziot
HFM Forum
October 9th, 2025

## Slide 2
Context
In high field magnets (above 12 T) wound with high amounts of Nb3Sn, the cost is mostly driven by the price of the conductor, thus impacting significantly the cost of future accelerator using this technology.
Material grading is the concept of replacing an expensive conductor by a cheaper one in lower field regions where the performances of the original conductor are not required.
Nb-Ti is a good candidate to replace Nb3Sn in field region below 8.5 T. It can carry up to 1500 A/mm2 at 10.5 T for a price 7-10 times lower than Nb3Sn.

## Slide 3
Outline
The BOND Case – Recap from last HFM Forum
BOND-H(ybrid)
Short Model Coil Validation

## Slide 4
2. The BOND Case
Hybrid Concepts for Block Coil 14 T Dipole Magnets
Presented at MT29, July 2025
A. Haziot, end E. Todesco, Nb3Sn/Nb-Ti Hybrid Concepts in Block for High Field Dipole Magnets, IEEE Trans. Appl. Supercond., Accepted

## Slide 5
The BOND Case
BOND: Baseline with Nb3Sn
The block coil design used for this case study is the BOND double aperture magnet:
Double aperture of 50 mm
2 double layers Nb3Sn coils per aperture
14 T bore field with 20% margin at 1.9 K
Overall Parameters |  | 
Aperture | (mm) | 50
Field | (T) | 14.0
Number of apertures | (adim) | 2
Distance between apertures | (mm) | 250
Yoke outer diameter | (mm) | 700
Coil design |  | 
Insulated cable surface (one aperture) | (mm2) | 12746
Equivalent coil width | (mm) | 56.9
Coil efficiency | (T mm / A) | 0.00077
N. layers | (adim) | 2
N. turns/pole | (adim) | 52
Operational parameters |  | 
Current (Inom) | (kA) | 19.34
Peak Field | (T) | 14.81
Short sample current @ 1.9 K | (kA) | 23.66
Short sample current @ 4.2 K | (kA) | 21.20
Short sample field @ 1.9 K | (T) | 17.8
Short sample field @ 4.2 K | (T) | 16.0
j overall | (A/mm2) | 348
j strand | (A/mm2) | 509
j superconductor | (A/mm2) | 967
j copper | (A/mm2) | 1074
Loadline fraction @ 1.9 K | (%) | 81.7
Loadline fraction @ 4.5 K | (%) | 91.2
Stored energy/m | (MJ/m) | 2.064
Inductance/m | (mH/m) | 10.24
J.C. Perez et al., Conceptual Design of BOND: A 14 T Dipole for FCC-hh, IEEE Trans. Appl. Supercond. 35, 4002506 (2025)

## Slide 6
The BOND Case
Conductor choice
Conductor parameters |  | Nb3Sn |  | Nb-Ti
Strand diameter | (mm) | 1.10 |  | 1.10
Layout |  | RRP 162/169 |  | 
Effective filament diameter | (µm) | 64 |  | 7
Jc at 4.2 K and 16 T | (A/mm2) | 1200 |  | 
Cu/NonCu ratio |  | 0.9 |  | 1.0
No. of strands in cable |  | 40 |  | 40
Bare cable width | (mm) | 23.045 |  | 23.275
Bare cable thickness | (mm) | 1.98 |  | 2.0
Bare cable width (reacted) | (mm) | 23.275 |  | 
Bare cable thickness (reacted) | (mm) | 2.06 |  | 
Insulation thickness | (mm) | 0.150 |  | 0.150
Insulated cable width (reacted) | (mm) | 23.575 |  | 23.575
Insulated cable thickness (reacted) | (mm) | 2.36 |  | 2.3
A strand | (mm2) | 0.950 |  | 0.950
A sc | (mm2) | 0.500 |  | 0.475
A cu | (mm2) | 0.450 |  | 0.475
The Nb3Sn cable in BOND is made of 40 DEM-1.1 strands of 1.1 mm.
For this conceptual study, a hypothetical Nb-Ti conductor was considered:
  1.1 mm strand
  cable identical to the BOND cable
A more realistic conductor using LHC 01 strands (1.065 mm) will be considered in the next part.

## Slide 7
20%
The BOND Case
The Low Field Region – Criteria for Nb-Ti
Same current as in BOND: 19.34 kA
Field region suitable for using Nb-Ti with 20% margin on the loadline.
20% margin seems a suitable value for impregnated Nb-Ti, but a discussion on this criteria should be addressed.
Critical surfaces are defined in the references below.
19.34 kA
B, Auchmann, et al. “High Field Magnet Programme – European Strategy Input”, arXiv:2504.16885 (2025)
L. Bottura., A Practical Fit for the Critical Surface of NbTi, IEEE Trans. Appl. Supercond. 10, 1054 (2000)

## Slide 8
The BOND Case
2 options for the Nb-Ti blocks
Easier for fabrication
Less Nb-Ti turns
Optimal use of the low field region
More Nb-Ti turns
Flat coil
Stepped coil

## Slide 9
The BOND Case
14 T Flat version
Nb3Sn |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 17.8
SS current at 1.9 K | [kA] | 23.65
Loadline fraction | (%) | 81.8
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 9.9
SS current at 1.9 K | [kA] | 31.65
Loadline fraction | (%) | 61.1
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 10.8
SS current at 1.9 K | [kA] | 24.03
Loadline fraction | (%) | 80.5
Nb3Sn: 26 turns (10+16)
Nb-Ti: 26 turns (13+13)
Nb3Sn ratio: 50 %
At nominal, loadline fractions are:
  81.8% on the Nb3Sn
  80.5% on the Nb-Ti
Limited by the Nb3Sn at 23.65 kA
Magnetic Field
Margin on the loadline

## Slide 10
The BOND Case
14 T Stepped version
Nb3Sn |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 17.8
SS current at 1.9 K | [kA] | 23.63
Loadline fraction | (%) | 81.9
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 10.7
SS current at 1.9 K | [kA] | 24.79
Loadline fraction | (%) | 78.0
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 10.8
SS current at 1.9 K | [kA] | 23.99
Loadline fraction | (%) | 80.6
Nb3Sn: 23 turns (7+16)
Nb-Ti: 29 turns (16+13)
Nb3Sn ratio: 44 %
At nominal, loadline fractions are:
  81.8% on the Nb3Sn
  80.6% on the Nb-Ti
Limited by the Nb3Sn at 23.65 kA
Magnetic Field
Margin on the loadline

## Slide 11
The BOND Case
12 T Flat version
Nb3Sn |  | 
Nominal current | [kA] | 19.92
SS field at 1.9 K | [T] | 17.1
SS current at 1.9 K | [kA] | 27.27
Loadline fraction | (%) | 73.0
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 19.92
SS field at 1.9 K | [T] | 10.6
SS current at 1.9 K | [kA] | 25.38
Loadline fraction | (%) | 78.5
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 19.92
SS field at 1.9 K | [T] | 10.7
SS current at 1.9 K | [kA] | 24.91
Loadline fraction | (%) | 80.0
Magnetic Field
Margin on the loadline
Nb3Sn: 14 turns (4+10)
Nb-Ti: 26 turns (13+13)
Nb3Sn ratio: 35 %
At nominal, loadline fractions are:
  73.0% on the Nb3Sn
  80.0% on the Nb-Ti
Limited by the Nb-Ti at 24.91 kA

## Slide 12
The BOND Case
12 T Stepped version at 4.5 K
Nb3Sn |  | 
Nominal current | [kA] | 16.20
SS field at 4.5 K | [T] | 16.0
SS current at 4.5 K | [kA] | 21.02
Loadline fraction | (%) | 77.1
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 16.20
SS field at 4.5 K | [T] | 7.9
SS current at 4.5 K | [kA] | 18.95
Loadline fraction | (%) | 85.5
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 16.20
SS field at 4.5 K | [T] | 7.9
SS current at 4.5 K | [kA] | 18.43
Loadline fraction | (%) | 87.9
Magnetic Field
Margin on the loadline
Nb3Sn: 24 turns (8+18)
Nb-Ti: 26 turns (15+11)
Nb3Sn ratio: 50 %
At nominal, loadline fractions are:
  77.1% on the Nb3Sn
  87.9% on the Nb-Ti
Limited by the Nb-Ti at 18.43 kA

## Slide 13
The BOND Case
AC-losses considerations
AC-losses are calculated over a typical current cycle in the LHC:
  Ramp down from nominal to reset (100 A) of 10 A/s
  Injection plateau of 20 min at 1 kA
  Ramp up to nominal of 10 A/s
Calculation is done over the second cycle to account for magnetization.
Today the target in HFM for the loss during this cycle is 10 kJ/m.
Collision
Reset
current
Beam dump
Injection
Calculation interval
B, Auchmann, et al. “High Field Magnet Programme – European Strategy Input”, arXiv:2504.16885 (2025)

## Slide 14
 |  | BOND | Hybrid 14 T Flat | Hybrid 14 T Stepped | Hybrid 12 T Flat | Hybrid 12 T at 4.5 K
Persistent current losses | [kJ/m] | 24.216 | 14.879 | 13.485 | 8.147 | 14.058
Interfilament coupling current losses | [kJ/m] | 0.009 | 0.007 | 0.006 | 0.003 | 0.005
Interstrand coupling current losses | [kJ/m] | 0.343 | 0.352 | 0.351 | 0.182 | 0.244
Total cable losses | [kJ/m] | 24.569 | 15.238 | 13.842 | 8.332 | 14.308
The BOND Case
AC-losses considerations
Strand parameters |  | Nb3Sn | Nb-Ti
Strand diameter | [mm] | 1.10 | 1.10
Strand twist pitch | [mm] | 121 | 115
Effective filament diameter | [µm] | 64 | 7
Filament twist pitch | [mm] | 19 | 15
Crossover resistance (Rc) | [µΩ] | 30 | 30
Adjacent resistance (Ra) | [µΩ] | 0.3 | 0.3
Filling factor in strand | [mm] | 0.5 | 0.5
Results from the simulations

## Slide 15
Coil design |  | BOND | Hybrid 14 T Flat | Hybrid 14 T Stepped | Hybrid 12 T Flat | Hybrid 12 T at 4.5K
Nb3sn Insulated cable surface (one aperture) | (mm2) | 11 572 | 5 786 | 5 119 | 3 116 | 5 786
NbTi Insulated cable surface (one aperture) | (mm2) | 0 | 5 394 | 6 016 | 5 394 | 5 394
Nb3sn ratio to BOND | (%) | 100 | 50 | 44 | 27 | 50
Operational parameters |  |  |  |  |  | 
Current | (kA) | 19.34 | 19.34 | 19.34 | 19.92 | 16.20
Peak Field on Nb3Sn | (T) | 14.8 | 14.8 | 14.8 | 13.0 | 12.7
Short sample current @ 1.9 K on Nb3Sn | (kA) | 23.66 | 23.65 | 23.63 | 27.27 | 21.02
Short sample field @ 1.9 K on Nb3Sn | (T) | 17.8 | 17.8 | 17.8 | 17.1 | 16.0
Loadline fraction @1.9 K on Nb3Sn | (%) | 81.7 | 81.8 | 81.9 | 73.0 | 77.1
Peak Field on NbTi 1st layer | (T) |  | 6.8 | 8.7 | 8.7 | 7.0
Short sample current @ 1.9 K on NbTi 1st layer | (kA) |  | 31.65 | 24.79 | 25.38 | 18.95
Short sample field @ 1.9 K on NbTi 1st layer | (T) |  | 9.9 | 10.7 | 10.6 | 7.9
Loadline fraction @1.9 K on NbTi 1st layer | (%) |  | 61.1 | 78.0 | 78.5 | 85.5
Peak Field on on NbTi 2nd layer | (T) |  | 8.8 | 8.8 | 8.9 | 7.0
Short sample current @ 1.9 K on NbTi 2nd layer | (kA) |  | 24.04 | 23.99 | 24.91 | 18.43
Short sample field @ 1.9 K on NbTi 2nd layer | (T) |  | 10.8 | 10.8 | 10.7 | 7.9
Loadline fraction @1.9 K on NbTi 2nd layer | (%) |  | 80.5 | 80.6 | 80.0 | 87.9
AC-losses over a full cycle | (kJ/m) | 24.6 | 15.2 | 13.8 | 8.3 | 14.3
AC-losses ratio | (%) | 100 | 62 | 56 | 34 | 58
Loadline at 4.5 K
The BOND Case
Summary table
16
13
16
13
10
13
18
11
10
13
7
16
13
4
8
15
Nb3Sn
Nb3Sn
Nb3Sn
Nb3Sn
Nb-Ti
Nb-Ti
Nb-Ti
Nb-Ti

## Slide 16
3. BOND-H
A Realistic Case with the LHC 01 Strand

## Slide 17
BOND-H
LHC 01: an “on the shelf” conductor
Conductor parameters |  | Nb3Sn DEM-1.1 |  | Nb-Ti LHC 01
Strand diameter | (mm) | 1.10 |  | 1.065
Layout |  | RRP 162/169 |  | 
Effective filament diameter | (µm) | 64 |  | 7
Jc at 4.2 K and 16 T | (A/mm2) | 1200 |  | 
Cu/NonCu ratio |  | 0.9 |  | 1.6
No. of strands in cable |  | 40 |  | 42
Bare cable width | (mm) | 23.045 |  | 22.650
Bare cable thickness | (mm) | 1.98 |  | 1.90
Bare cable width (reacted) | (mm) | 23.275 |  | 
Bare cable thickness (reacted) | (mm) | 2.06 |  | 
Insulation thickness | (mm) | 0.150 |  | 0.150
Insulated cable width (reacted) | (mm) | 23.575 |  | 22.950
Insulated cable thickness (reacted) | (mm) | 2.36 |  | 2.2
A strand | (mm2) | 0.950 |  | 0.891
A sc | (mm2) | 0.500 |  | 0.343
A cu | (mm2) | 0.450 |  | 0.548
The Nb3Sn cable in BOND is made of 40 DEM-1.1 strands of 1.1 mm.
For the Nb-Ti, we consider using a cable of 42 LHC 01 strand:
  1.065 mm strand
  1.6 Cu/NonCu ratio
The high amount of copper in the Nb-Ti dramatically increases the current density in the superconductor.

## Slide 18
BOND-H
14 T flat version with LHC 01
Nb3Sn |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 17.8
SS current at 1.9 K | [kA] | 23.65
Loadline fraction | [%] | 81.8
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 9.1
SS current at 1.9 K | [kA] | 28.56
Loadline fraction | [%] | 67.6
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 10.0
SS current at 1.9 K | [kA] | 22.22
Loadline fraction | [%] | 86.8
Nb3Sn: 28 turns (11+17)
Nb-Ti: 26 turns (13+13)
Nb3Sn ratio: 50 %
At nominal, loadline fraction are:
  81.8% on the Nb3Sn
  86.8% on the Nb-Ti
Limited by the Nb-Ti at 22.22 kA
Magnetic Field
Margin on the loadline
13
13
16
10

## Slide 19
BOND-H
Gaining margin on the Nb-Ti
Tools to reduce the peak field on the upper Nb-Ti layer:
Optimization of the shape of the yoke to force the flux lines in the iron away from the Nb-Ti upper block.
gain 1-2% on the loadline
Reduce the number of Nb-Ti turns.
gain ~2% per turn
We are limited by the field target of 14 T and the field homogeneity in the aperture.

## Slide 20
BOND-H
Optimized LHC 01 version
Nb3Sn |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 17.8
SS current at 1.9 K | [kA] | 23.65
Loadline fraction | [%] | 81.8
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 8.5
SS current at 1.9 K | [kA] | 33.52
Loadline fraction | [%] | 57.6
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 9.8
SS current at 1.9 K | [kA] | 23.58
Loadline fraction | [%] | 81.8
Magnetic Field
Margin on the loadline
11
11
18
12
Optimization: iron pockets and 2 turns less
Nb3Sn: 30 turns (12+18)
Nb-Ti: 22 turns (11+11)
Nb3Sn ratio: 58%
At nominal, loadline fractions are:
  81.8% SS on both Nb3Sn and Nb-Ti
Limited by the Nb-Ti at 23.58 kA

## Slide 21
BOND-H
Hot-spot simulations
Based on the “14 T flat” non optimized design.
Hot spot calculation has been performed for a 14.3 m long magnet as a function of the copper amount in the Nb3Sn and the Nb-Ti.
In this design, hot spot reaches ~240 K.
A Nb-Ti strand with less copper should allow to gain 10-20 K.
Courtesy of E. Ravaioli
LHC 01 version
Ideal version

## Slide 22
The BOND Case
14T – Ideal version
Nb3Sn |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 17.8
SS current at 1.9 K | [kA] | 23.65
Loadline fraction | [%] | 81.8
Nb-Ti layer 1 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 10.2
SS current at 1.9 K | [kA] | 29.48
Loadline fraction | [%] | 65.6
Nb-Ti layer 2 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 10.9
SS current at 1.9 K | [kA] | 24.15
Loadline fraction | [%] | 80.1
Magnetic Field
Margin on the loadline
14
14
15
9
Nb3Sn: 24 turns (9+15)
Nb-Ti: 28 turns (14+14)
Nb3Sn ratio: 46%
At nominal, loadline fraction are:
  81.8% on the Nb3Sn
  80.1% on the Nb-Ti
Limited by the Nb3Sn at 23.65 kA

## Slide 23
BOND-H
Summary table
Conductor parameters |  | Nb3Sn DEM-1.1 |  | Nb-Ti Ideal | Nb-Ti LHC 01
Strand diameter | (mm) | 1.10 |  | 1.10 | 1.065
Layout |  | RRP 162/169 |  |  | 
Effective filament diameter | (µm) | 64 |  | 7 | 7
Cu/NonCu ratio |  | 0.9 |  | 1.0 | 1.6
No. of strands in cable |  | 40 |  | 40 | 42
Bare cable width (r) | (mm) | 23.275 |  | 23.275 | 22.650
Bare cable thickness (r) | (mm) | 2.06 |  | 2.06 | 1.90
Insulation thickness | (mm) | 0.150 |  | 0.150 | 0.150
Insulated cable width | (mm) | 23.575 |  | 23.575 | 22.950
Insulated cable thickness | (mm) | 2.36 |  | 2.36 | 2.2
A strand | (mm2) | 0.950 |  | 0.950 | 0.891
A sc | (mm2) | 0.500 |  | 0.475 | 0.343
A cu | (mm2) | 0.450 |  | 0.475 | 0.548
Coil design |  | LHC 01 version |  |  | Ideal version | 
 |  | Nb3Sn | Nb-Ti |  | Nb3Sn | Nb-Ti
Insulated cable surface / aperture | (mm2) | 5341 | 6073 |  | 6676 | 4443
Nb3sn ratio to BOND | (%) | 58 |  |  | 46 | 
Operational parameters |  |  |  |  |  | 
Current (Inom) | (kA) | 19.34 |  |  | 19.34 | 
Peak Field | (T) | 14.8 | 8.2 |  | 14.8 | 8.9
Short sample current @ 1.9 K | (kA) | 23.65 | 23.58 |  | 23.65 | 24.15
Short sample field @ 1.9 K | (T) | 17.8 | 9.8 |  | 17.8 | 10.9
j overall | (A/mm2) | 348 | 383 |  | 348 | 348
j strand | (A/mm2) | 509 | 517 |  | 509 | 509
j superconductor | (A/mm2) | 967 | 1323 |  | 967 | 1018
j copper | (A/mm2) | 1074 | 840 |  | 1074 | 1018
Loadline fraction @ 1.9 K | (%) | 81.7 | 82.0 |  | 81.7 | 80.1
Nb3Sn
Nb-Ti
15
14
9
14
Ideal version
Nb3Sn
Nb-Ti
18
11
12
11
LHC 01 version

## Slide 24
3. Short Model Coil Validation

## Slide 25
Short Model Coil Validation
Hybrid racetrack coil
Conductor parameters |  | Nb3Sn |  | Nb-Ti
Strand diameter | (mm) | 0.850 |  | 0.825
Layout |  | RRP 108/125 |  | 
Effective filament diameter | (µm) | 55 |  | 7
Cu/NonCu ratio |  | 1.2 |  | 1.9
No. of strands in cable |  | 32 |  | 35
Bare cable width | (mm) | 14.7 |  | 14.75
Bare cable thickness | (mm) | 1.525 |  | 1.48
Bare cable width (reacted) | (mm) | 14.88 |  | 
Bare cable thickness (reacted) | (mm) | 1.59 |  | 
Insulation thickness | (mm) | 0.150 |  | 0.150
Insulated cable width (reacted) | (mm) | 15.18 |  | 15.05
Insulated cable thickness (reacted) | (mm) | 1.89 |  | 1.78
A strand | (mm2) | 0.567 |  | 0.535
A sc | (mm2) | 0.258 |  | 0.184
A cu | (mm2) | 0.310 |  | 0.350
The Short Model Coil (SMC) assembly has been designed as a test bench for short racetrack coils wound with Nb3Sn cable.
SMC MQXF uses a cable made of 32 MQXF strands in a double pancake racetrack coil of 31 turns.
A similar cable made of 35 LHC 02 strands could be used to make a hybrid version with:
  Nb3Sn coil of 15 turns
  Nb-Ti coil of 15 turns
SMC-H
SMC MQXF
15
16
30

## Slide 26
SMC-H is always limited by the Nb-Ti due to higher filed on the last turns.
The Nb3sn operates at 90% when the Nb-Ti is at short sample limit, limited at 17 kA.
The hybrid SMC includes 48% of Nb3Sn.
Short Model Coil Validation
Magnetic design
Coil design |  | SMC MQXF | SMC H
Nb3sn Insulated cable surface (one aperture) | (mm2) | 3558 | 1725
Nb-Ti Insulated cable surface (one aperture) | (mm2) | 0 | 1714
Nb3sn ratio | (%) | 100 | 48
Operational parameters |  |  | 
Current | (kA) | 18.93 | 17.00
Short sample current @ 1.9 K on Nb3Sn | (kA) | 18.93 | 18.93
Short sample field @ 1.9 K on Nb3Sn | (T) | 14.0 | 14.0
Loadline fraction @1.9 K on Nb3Sn | (%) | 100 | 90.0
Short sample current @ 1.9 K on Nb-Ti | (kA) |  | 17.00
Short sample field @ 1.9 K on Nb-Ti | (T) |  | 8.7
Loadline fraction @1.9 K on Nb-Ti | (%) |  | 100
SMC-H
SMC MQXF
15
16
31

## Slide 27
Short Model Coil Validation
Engineering of SMC-H
Engineering design for the coil is already advanced.
After winding and reacting the Nb3Sn coil, an internal splice allows the connection to the Nb-Ti cable.
The head spacers are diluting the peak fields in the turn and allocate the internal splice.
A mock-up is manufactured to test and develop this specific splice.
After splicing, the Nb-Ti wound around the Nb3Sn coil, and the coil is fully impregnated.
A mechanical model should validate this structure.
Courtesy of T. Poszwa

## Slide 28
Conclusion
Material grading is a great way to reduce conductor cost in high field magnets by replacing the Nb3Sn by Nb-Ti in the low field regions of the coils.
The case study of BOND generating 14 T at 1.9 K, shows that 50 % or more of the Nb3Sn could be replaced by Nb-Ti in this block coil design, improving Ac-losses as well.
A realistic design is proposed based on the available LHC 01 strand with 58% Nb3Sn.
A hybrid short model racetrack magnet with internal splices is under development with an engineering design on-going.

## Slide 30
BOND-H
Optimizing the yoke
original
10/10
20/20
40/40
30/30

## Slide 31
original
40/40
40/10
40/20
BOND-H
Optimizing the yoke

## Slide 32
original
40/20
40/20
removing 1 Nb-Ti turn
40/20
removing 2 Nb-Ti turn
BOND-H
Removing turns

## Slide 33
BOND-H
Ideal version
original
Iron optimized
adding 1 Nb-Ti turn

## Slide 34
The BOND Case
14T – LHC 01 version 12-turns
Nb3Sn |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 17.8
SS current at 1.9 K | [kA] | 23.65
Loadline fraction | (%) | 81.8
NbTi layer 1 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 8.8
SS current at 1.9 K | [kA] | 31.00
Loadline fraction | (%) | 62.4
NbTi layer 2 |  | 
Nominal current | [kA] | 19.34
SS field at 1.9 K | [T] | 9.9
SS current at 1.9 K | [kA] | 23.10
Loadline fraction | (%) | 83.7
Nb3Sn: 28 turns (11+17)
NbTi: 26 turns (12+12)
Nb3Sn ratio: 54 %
Loadline at 1.9 K: below 82 %, limited by the Nb3Sn coil.
Magnetic Field
Margin on the loadline
12
12
17
11