## Slide 1: First large-scale production of MgB2 round wire: the Superconducting Links for the HL-LHC Project at CERN
17th European Conference on Applied Superconductivity
21-25 September 2025, Porto
Amalia Ballarino1, Gianni Grasso2, Simon Hopkins1, Matteo Tropeano2 Christian Barth1, Algirdas Baskys1
1 CERN, 2ASG Superconductors
Amalia Ballarino, CERN
Invited oral presentation at EUCAS 2025

## Slide 2: HL-LHC: Extending the Physics Reach of LHC
HL-LHC is a technology driver
High Luminosity LHC (HL-LHC) physics goals:
  Increase integrated luminosity by a factor of 10 beyond LHC design value
  Extend the LHC lifetime by 15+ years

## Slide 3: LHC Underground
New underground galleries and surface buildings for technical infrastructure finished

## Slide 4: Superconducting Transmission
70 m long
120 kA DC
120 m long
40 kA DC
8+2 Systems
Two types

## Slide 5: MgB2 for Superconducting Transmission
Nb-Ti challenging – small temperature margin, constraints in vertical path cooling
MgB2: affordable cost for large procurement. Low field (< 1 T) application. Advantages:
  Operating conditions: up to  25 K with helium gas cooling, offering > 5 K temperature margin
  Conductor: round wire – not yet industrialized. React & Wind technology
  System benefits: simplified cryostats and cryogenic control, higher heat loads acceptable, lower cryogenic cost
System capability: up to 120 kA DC
with < 5.5. g/s helium gas flow

## Slide 6: The HL-LHC Superconducting Link Configuration
  90 mm
120 kA DC
Bending radius  2 m

## Slide 7: Targets for Development of MgB2 wire
Layout, composition
and dimensions
Mechanical properties
Unit lengths
Electrical properties
Targets defined according to the estimated requirements
of the HL-LHC Cold Powering Systems
* Ic degradation < 3 %

## Slide 8: MgB2 Conductor for HL-LHC
Early CERN studies of MgB2 wire for HL-LHC electrical transmission systems: ex-situ MgB₂ available only as tape; used by ASG in MRI cryogen-free magnets. In-situ wire availability was also investigated
R&D conductor focus: round ex-situ MgB₂ wire enabling adoption of React & Wind technology; multiple iterations → final design
Industrialization: wire layout/composition chosen → pilot run at ASG → large-scale production at ASG
2008-2016
R&D & Industrialization ~ 150 km
2017-2019
Pilot Production ~ 400 km
2020-2021
Series Production ~ 1000 km
2018: Adoption of MgB2
technology for HL-LHC
TOT  1550 km
2016: HL-LHC approved by the CERN Council

## Slide 9: R&D Phase: Key Developments
Development of round wire layouts, definition/reduction of filament size, introduction of twisting of filaments
Reduction of thickness of Monel 400 matrix
  Increasing filling factor
  Reducing splice resistance
  Study on the impact on wire workability and mechanical properties
  Improvement of Jc
    Optimizing powder packing density
    Enhancing grain boundary pinning ( 1 T)
    Increasing purity of B powder
    Introducing Nb barrier
  Implementation of copper stabilizer
  Definition and implementation of copper coating
  Scale up of billet volume by a factor  10 to enable industrial scale production (series billet  13 km of wire)

## Slide 10: Evolution of Wire Layout
MgB2 ex-situ tape available before launching the R&D for HL-LHC
High powder density achieved through uniaxial pressure and flat rolling. 12 filaments in Ni matrix and Fe/Cu core
Intermediate MgB2 ex-situ wire layouts
Octagonal wire: Ni matrix, Cu stabilizer at the centre (a)
Quasi-square wires: Monel® matrix, Ni barrier around the filaments (b)
Round wire: Monel® matrix, Ni barrier (c)
Final multi-filamentary MgB2 ex-situ wire
Alternating wire drawing and groove rolling to increase powder packing density, improve microstructure, and obtain regular multifilament cross-sections. Explored 12, 19, 30 and 37 filament configurations with twist pitches ranging from 30 to 300 mm.
Final wire:  = 0.995 ± 0.02 mm, 37 filaments (eq ≤ 60 m)
Twist pitch: 85  15 mm
b)
b)
a)
c)
c)

## Slide 11: Wire Composition
Ni barrier separated from MgB2 with Nb. Intermetallic compounds (MgNi2, Mg2Ni, and MgB2Ni2.5) formed during heat treatment lead to the formation of microcracks compromising mechanical properties and electrical resistance of splices. Nb final thickness  10 m
Cu stabilizer around the Monel: reduces hot-spot temperature and facilitates electrical splices. Electrochemical deposition used as “post-processing” method. In-line process depositing
 30 m of pure Cu (RRR ≥ 100)
Electrochemical deposition of Sn-Ag alloy (Stay-Brite , 96% Sn and 4% Ag) onto the copper to avoid oxidation and ensure long term stability of inter-strand resistance in cables. Resilience to oxidation and good solderability – it facilitates electrical splices. Final thickness:  3 m
The thin ( 2 m) reaction layer at the Nb-Ni interface did not show brittleness
Porosity and detachments in between MgB2-Ni reaction layers
Nb barrier vs Ni

## Slide 12: Reduction of Monel Thickness
Initial thickness
-9%
-16%
-35%
Produced MgB2 wires with Monel thickness reduced from the original  115 m to  78 m. Further thickness reduction ( 50 %) resulted in mechanical degradation of the wire during the fabrication process
Final Monel thickness: compromise with mechanical properties
Filling factor was increased from 16 % to 20 %
Splice resistance was reduced by 35 %. This is an important optimization in view of the high current (up to 18 kA) splices in the MgB2 cables of the Cold Powering System

## Slide 13: Optimization of Boron Powder (1/2)
Initially used typical amorphous B powder with a purity level of  95 wt%. Oxide impurities (mainly B₂O₃) are largely responsible for MgO formation during MgB₂ reaction
Implemented a high purity (99 wt% class range) amorphous boron powder to improve grain boundary connectivity. Main goal: reduce MgO formation, which tends to form an insulating layer at the MgB2 grain surface, resulting in a limitation of current flow and reduction of transport properties
By using high purity boron powder, MgO content was reduced to a level below what is detectable by XRD (< 1–3 wt %)
Critical current density (Jc) improved by up to 30 %. Microstructural analysis revealed the absence of large agglomerates that may destroy the Nb barriers locally, like for lower purity powder. Je of the wire increased from 750 A/mm2 to 1150 A/mm2 at 4.3 K and 1 T
High purity B was adopted for the series wire
Carbon doped powders were prepared and used to manufacture 37 filament MgB2 round wires. The process was however not implemented in the series wire because not effective in the relevant operating field range (< 1 T)

## Slide 14: Optimization of Boron Powder (2/2)
Longitudinal cross section
Transverse cross section
Ex-situ 2: homogeneous microstructure
with smaller pore, consistently sized and distributed. Pores form a uniform network with a consistent microstructure – suggesting an isotropic distribution
Comparison of microstructure and porosity
Pore size <0.2–0.3 µm
Pore size  0.5–1 µm
Notes: Ex-situ 2: smaller pores, more
homogeneously sized and distributed

## Slide 15: Filament Size and Twist Pitch
R&D wires: Φeq up to  130 μm. A 37-filament layout with Φeq = 60 μm was developed to meet mechanical and electrical requirements. Smaller eq were not investigated
Twist pitch (Tw) introduced during wire drawing to reduce AC losses during fast magnet discharge. Wires were produced with twist pitches ranging from 30 mm to 300 mm: 300 mm, 150 mm, 75 mm and 30 mm. No significant degradation (<20 % for the 30 mm pitch and not measurable for the other twist pitches) was observed over this wide range. The CERN specification 85  15 mm was selected for the series production
SEM of MgB2 wire with 1 mm diameter and 37 filaments
Tw = 150 mm
Tw = 75 mm
Tw = 30 mm
Measured twist pitch of
series wire: 80 mm - 85 mm

## Slide 16: Mechanical Qualification (1/2)
M. Sugano et al.,
IEEE Trans. Appl. Supercond. 22 (3) 4801004 (2015)
EMgB2 filaments  97 GPa
K. Konstantopoulou et al., Supercond. Sci. Technol. 29 084005 (2016)
Tensile tests at RT
Room Temperature
Axial Tensile Tests on MgB2 Wires
3 T, 4.2 K
Room Temperature
 | Ic/Ic0
0.35% | 0.05

## Slide 17: Mechanical Qualification (2/2)
Specified Rb  100 mm
t = Tensile strain in MgB2 filaments
Rb = Bending radius of the MgB2 wire
K. Konstantopoulou et al., Supercond. Sci. Technol. 29 084005 (2016)
Industrialisation
Pilot production
Series
production
All unit lengths
Shipment average
Degradation of Ic on bending

## Slide 18: Specification for Procurement of Series Wire
Parameter | Value
Diameter of MgB2 wire | (0.995 ± 0.020) mm
Ovality of MgB2 wire | ≤ 0.015 mm
Diameter of superconducting filaments | ≤ 60 µm
Filament twist pitch | (85 ± 15) mm
Filament twist direction | Right-handed screw
Critical current at 25 K and 0.9 T | ≥ 186 A
Critical current at 25 K and 0.5 T | ≥ 320 A
Critical current at 20 K and 0.5 T | ≥ 480 A
Bending radius (after final heat treatment) | ≤ 100 mm
Critical tensile strain at room temperature | ≥ 0.28 %
Copper fraction of the wire total cross section | ≥ 12 %
Stay Brite® on copper | (30 ± 5) µm
RRR of copper stabilizer (293 K and 40 K) | ≥ 100
n-value @ 25 K and 0.9 T | ≥ 20

## Slide 19: QA and QC at ASG
Geometrical
Electrical
Micro-structure
Eddy currents
+ Test methods/procedures
+ Certificates of conformity of raw materials and traceability of raw materials in billets
Critical current
25 K, 0.9 T (B)
25 K, 0.5 T (B)
20 K, 0.5 T (B)

## Slide 20: Tests at ASG (1/2)
Requirement | Test Frequency
Minimum and maximum filament diameter | SEM images on one sample extracted from each extremity of every billet
Copper fraction | By an imaging method Measurement of one sample extracted from each extremity of every billet
Wire diameter | Continuous laser micrometer measurements
Wire twist direction | One sample from each wire unit length or billet (depending on the stage at which the twist is applied)
Wire twist pitch | Value verified after the setting of the twisting machine One sample extracted from each extremity of every unit length or billet (depending on the stage at which the twist is applied)
Bend test | SEM images on one sample extracted from each extremity of every billet
Wire surface condition | Contractor Quality Assurance Plan

## Slide 21: Tests at ASG (2/2)
Requirement | Test Frequency
Wire critical current | Measurement of one sample extracted from the point of every wire unit length
Wire critical current after bending and straightening | Critical current measurement of one sample per unit length taken adjacent to the sample for critical current
Wire tensile strain | Critical current measurement of one sample per billet recommended
Residual Resistance Ratio | Measurement of one sample extracted from one extremity of each unit length before and after copper plating
Eddy current | Continuous control on each wire unit length

## Slide 22: QC at CERN
Visual inspection
Critical current at 4.30.1 K and parallel fields:
  Ic(4.3 K,1.5 T)  550 A
  Ic(4.3 K, 2 T)  402 A
  Ic(4.3 K, 3 T)  216 A
Frequency of Ic measurements – per unit length:
  2 straight samples
  3 samples after bending (100 mm)
10 straight samples per cool-down

## Slide 23: Production Overview: Quantity and Unit Length
Industrialisation
Pilot production
Series production
Cumulative wire deliveries
Trend in average
unit length
Average unit length advanced from ~1 km on industrialisation
to ~2.5 km in series production

## Slide 24: Production Overview: Quantity and Unit Length
Distribution of unit lengths during series production

## Slide 25: Production Overview: Critical Current
Consistent performance of accepted series unit lengths
  Average Ic 18 % above minimum requirement (at 4.3 K 1.5 T)
  Average variability of Ic within billet ± 2.8 % (standard deviation/mean)
Pilot production
Series production
Performance distribution within each delivered batch (unit lengths from different billets)
Measurements at CERN at 4.3 K and 1.5 T

## Slide 26: Production Overview: Critical Current
Data supplied by ASG match the trends of data collected at CERN, despite different testing conditions:
  Average Ic 22 % above minimum requirement (at 25 K 0.9 T)
  Average variability of Ic within billet ±3.4 % (standard deviation/mean)
Performance distribution within each delivered batch (unit lengths from different billets)
Measurements at ASG at 25 K and 0.9 T
Series production

## Slide 27: Production Overview: Bending Degradation
Distribution of Ic degradation on bending during series production
ASG Measurements
  Average degradation on bending -0.87 %
  Average degradation on bending 0.49 %
Distribution of Ic degradation on bending during series production
CERN Measurements
Each data represents a delivered batch (unit lengths from different billets)

## Slide 28: Non-Conformities Identified at CERN (1/2)
Surface staining/oxidation identified upon receipt on two spools
Identified causes:
  Spool 1 (3.1 km): accidental contamination of the wire, after spooling, by an oxidizing agent (H2SO4) from the galvanic line  reviewed procedure
  Spool 2 (2.98 km): discoloration of the wire on the second layer of the spool. Attributed to a contaminated cloth used during the final cleaning  reviewed procedure
Non-conformities identified during visual inspection
In total, only  3 % of the series wire was identified as non-conform
Spooling problems identified upon receipt on four spools
Identified causes:
  Spools 1, 2 and 3. Overlapping turns were generated during the final spooling process. Local plastic deformations (1 or 2 per spool) were identified and cut out  spooling procedure reviewed
  Spool 4. A wire extremity opened during transport and several turns ( 30 m of wire) were loose and overlapping  packing procedure reviewed

## Slide 29: Non-Conformities Identified at CERN (2/2)
Critical current measured at CERN below specification
Identified causes:
Three spools from two different billets experienced excessive tension on the wire during re-spooling. It was adopted a new re-spooling line suitable for tape more than round wire
One spool underwent overheating during production process
One spool experienced degradation during handling at one extremity
Three spools from the same billet had systematically low Ic
Non-conformities identified during Ic measurements
C3355

## Slide 30
Advanced techniques for:
Incoming materials inspection
Real time monitoring (SCADA alerts)
Post-production statistical analysis
Eddy current detector and visual systems to check integrity of wires
ASG Superconductors Proprietary & Confidential
4 camera visual inspection
to check surface appearance
Dimensional Measurement
& Acquisition System
and statistical analysis
QA at ASG: Full Process Control
Image analysis
QA Procedures defined and implemented to ensure full process control
from raw material to final wire

## Slide 31
Each batch of Nb tubes inspected according to the following control plan:
Integrity and adequacy of packaging
Presence of Certify 3.1 according to UNI EN10204 and correspondence of the values declared to the supply specification
Visual aspect 100% of the tubes (absence of internal and external imperfections, burrs, oxides, grease, oil, lubricants)
Statistical check on 2% of the tubes of the batch of:
Outer Diameter, measured with gauge: 21.70 ± 0.13mm
  Thickness, measured with gauge: 2.4 ± 0.24mm
  Length, measured with meter: 900 -0 + 3mm
Hardness 100% of the tubes: average of 5 measures each tube
Tensile tests on a tube representative of the batch (external laboratory)
Chemical composition 100% of the tubes using an XRF analyzer: 45 analyses for each tube (15 x 3 Axis)
QA at ASG – Inspection of Nb Tubes

## Slide 32: The Superconducting Link
  90 mm,  25 kg/m

## Slide 33
System Assembly

## Slide 34: Transport and Installation
1-LO-IS, this conference

## Slide 35: Validation of the Superconducting Link System
Bending radius  2 m
Construction and qualification at CERN

## Slide 36: Validation of the Superconducting Link
Bending radius  2 m
DFX SOTON
Construction and qualification at CERN

## Slide 37: Validation of the Superconducting Link (2/2)
REBCO to MgB2, GHe @ 20 K
MgB2 to Nb-Ti, LHe @ 4.5 K
High Current Splices
94 kA,  5 g/s
All splices within expected resistance range
Results confirm design
Validated at up to 94 kA* (maximum current delivered by power converters) with a He gas mass flow < 5 g/s. All splices are within expected range
* 15% above HL-LHC nominal current
Scientific Reports volume 15, Article number: 20428 (2025)

## Slide 38
Run3 operation
Approval of
HL-LHC Project
EU funded HiLumi
Design Study
HL-LHC Operation
We are here
Long Shutdown 3 will start in less than 1 year
Installation of Cold Powering Systems is from Q2 2028 to Q3 2029

## Slide 39: Conclusions
A total quantity of 1550 km of MgB2 wire was produced at ASG for the HL-LHC Superconducting Link at CERN. R&D was instrumental for developing a wire meeting the specified requirements. The R&D wire ( 550 km) was used by CERN for developing and studying prototype system components (high current cables and Superconducting Links). Short length cables ( 20 m) were produced at CERN. Series cabling was industrialized by CERN at ICAS
Series production ( 1000 km) was completed during  2 years (partially during the COVID period and associated restrictions). Average wire unit lengths of 2.5 km were produced, with maximum unit lengths of up to 4 km. Critical current values consistently above specification
Two Superconducting Link Systems for HL-LHC have been produced and successfully qualified at CERN. Other two are planned to be completed by end of 2025, with full production finishing in 2027
Installation of the Superconducting Link Systems in the HL-LHC underground is scheduled for Q2 2028. Commissioning of HL-LHC in Q1 2030

## Slide 40: Thanks for your attention !
Acknowledgments: the ASG technical team, B. Bordini, the CERN technical team and in particular J. Hurte and P. Jacquot, CERN students and fellows, the CERN HL-LHC and ATS/TE management