## Slide 1
IV – Conclusions
As part of the High Field Magnet programme (HFM) at CERN, the Nb3Sn block coil configuration is a candidate for the main dipole in future large hadron collider as FCC-hh. To reduce the cost, the use of material grading in the block coils is explored by using Nb-Ti conductor instead of Nb3Sn in the external low field regions. Different designs are being investigated for dipoles with a target nominal field of 14 T and 12 T. The gain in conductor as well as in AC-losses are reported, together with consideration on operational
temperature (1.9 K vs. 4.5 K). Finally, the preliminary design of a Nb3Sn/Nb-Ti Short Model Coil (SMC) is presented as a first proof of such a concept of hybrid technology in block coils.
Presentation ID: Thu-Af-Po.01-02
Ariel Haziot, and Ezio Todesco
Nb3Sn/Nb-Ti Hybrid Concept in Block Coils
for High Field Dipole Magnets
CERN, European Organization for Nuclear Research, Switzerland
I – Introduction
III – SMC-Hybrid
II – The BOND Case
Material grading is an interesting way to reduce conductor cost in high field magnets replacing the Nb3Sn by Nb-Ti in the low field regions of the coils.
The study of BOND (14 T at 1.9 K), shows that 50 % or more of the Nb3Sn could be replaced thus practically reducing the cost of the conductor by 40 %.
The AC-losses per cycle due to the smaller filaments of Nb-Ti is also significantly reduced by 40 % approaching the HFM target.
More drastic options are considered at 14 T, 12 T, and 4.5 K with even less Nb3Sn.
The implementation of a hybrid in the magnet platform SMC is presented along with technical choices of impregnating or not the Nb-Ti coil.
C. Wang et al., “Electromagnetic design, fabrication, and test of LPF1: A 10.2-T common-coil dipole magnet with graded coil configuration”, IEEE Trans. Appl. Supercond. 29, 4003807 (2019)
C. Wang et al., “Mechanical Design, Assembly, and Test of LPF1: A 10.2 T Nb3Sn Common-Coil Dipole Magnet with Graded Coil Configuration”, IEEE Trans. Appl. Supercond. 29, 4000108 (2019)
C. Wang et al., “Development of superconducting model dipole magnets beyond 12 T with a combined common-coil configuration”, IEEE Trans. Appl. Supercond. 34, 065006 (2023)
LPF1 at IHEP (2017-2023)
LFP1: Hybrid common coil with 2 Nb3Sn and 4 Nb-Ti layers (Nb3Sn ratio: ~25 %) :
  10.2 T in a 10 mm aperture at 4.2 K (72% ISS)
  Quenches in Nb-Ti outer coils
LFP1-S: LFP1 with higher pre-load,
  10.7 T in a 12 mm aperture at 4.2 K (77% ISS)
  Quenches in 1 Nb3Sn coil, HF region
LFP1-U: New cables, new coils
  12.5 T in a 14 mm aperture at 4.2 K (90% ISS)
  Quenches in 1 Nb3Sn coil, on a localized defect
14 T stepped version
12 T flat version
12 T stepped version
at 4.5 K
14 T flat version
“BOND-H”
Nb-Ti accessible region
Same operating current as BOND (19.34 kA)
Operating loadline margin of 20 % for the Nb-Ti
Flat: Nb-Ti start at the same position on both layers
Stepped: more Nb-Ti turns on the lower layer
The stepped coil makes a more optimized use of the low field region with more Nb-Ti turns but introduces manufacturing complexity.
BOND
AC-losses considerations
Reducing Nb3Sn content also lowers AC-losses during magnet operation:
  smaller effective filament diameters (6 µm / 64 µm)
  tighter filament twist pitch (4 mm / 19 mm)
We assume identical interstrand contact resistances for both cables—using LHC 01 Nb-Ti values, since no measured data exist for the Nb3Sn cable.
AC-losses are calculated over a typical current cycle in the LHC:
    Ramp down from nominal to reset (100 A) of 10 A/s
    Injection plateau of 20 min at 1 kA
    Ramp up to nominal of 10 A/s
The target in HFM for the loss during a cycle is 10 kJ/m.
The Short Model Coil (SMC) assembly has been designed as a test bench for short racetrack coils wound with Nb3Sn cable.
SMC MQXF uses a 32-strand cable from MQXF strands in a double pancake racetrack coil of 31 turns.
A similar cable made of 35 Nb-Ti strands (LHC 02) is considered for the hybrid, SMC-H.
SMC-H
SMC MQXF
15
16
Assembly option 1: Impregnated Nb-Ti
Better and simpler for mechanics
Careful winding: Nb-Ti is wound on reacted but not impregnated Nb3Sn coil
Assembly option 2: Non-impregnated Nb-Ti
Allows a helium permeable insulation
Mechanically challenging: a harder Nb-Ti coil is required to limit the movements of Nb3Sn
Magnetic design of SMC-H
SMC-H is always limited by the Nb-Ti due to higher filed on the last turns.
We target a configuration for which the Nb3sn operates at 90% when the Nb-Ti is at short sample limit: 15 (Nb3Sn) / 16 (Nb-Ti) turns.
E. Todesco et al., “Dipoles for high-energy LHC”, IEEE Trans. Appl. Supercond. 24, 4004306 (2014)
Grading
Grading the current density, i.e. using larger current densities in the lower field region of dipole coils, is a design that has been used in several accelerator magnets with Nb-Ti (LHC dipoles) and Nb3Sn (CERN-ELIN, MSUT, D20,…)
Assuming 50 % of the coil is at higher current density, this technique allows to reduce the mass of the conductor by 10 % with respect to a case that would use the same current density, and additional conductor to reach the same short sample field.
Material Grading
For magnets requiring the use of Nb3Sn (< 10 T), the use of Nb-Ti in accessible regions with adequate margin (< 8 T at 1.9 K) brings substantial saving.
The cheaper the material, the higher the interest so the current density should not be pushed too much.
For the HE-LHC a 15 T dipole using Nb-Ti in part of the coil was proposed. Since Nb3Sn is 5 to 10 times more expensive than Nb-Ti, this design can reduce the conductor cost by 50 %.
Limits of Nb-Ti
One can assume a critical surface at 1500 A/mm2 and at 10.5 T for the Nb-Ti (LHC conductor).
It corresponds to a use of Nb-Ti with 1200 A/mm2 at fields up to 8.5 T, keeping at 80 % loadline fraction.
More conservative condition than in the LHC dipoles (8.6 T peak field at 86 % of loadline fraction).
D19H at LBNL (1997)
Built from D19A, Nb-Ti cos-θ dipole generating 7.6 T at 4.35 K and 10 T at 1.8 K in a 50 mm bore
The Nb-Ti inner layer was replaced by Nb3Sn (Nb3Sn ratio: 42 %)
At 4.35 K: 7.56 T bore field (7360 A)
  All quenches in the Nb-Ti coil
At 1.7 K: 8.99T (9092 A) bore field
  Long training (40 quenches) limited by the Nb-Ti
  Insufficient pre-loading on the Nb-Ti coil
S. Caspi et al., “Design and Construction of a Hybrid Nb3Sn Nb-Ti Dipole Magnet”, IEEE Trans. Appl. Supercond. 7, 547 (1997)
A. Lietzke et al., “Test Results on Nb3Sn Dipole Magnets”, IEEE Trans. Appl. Supercond. 7, 739 (1997)
J.C. Perez et al., “Conceptual Design of BOND: A 14 T Dipole for FCC-hh”, IEEE Trans. Appl. Supercond. 35, 4002506 (2025)
Coil design | Unit | BOND | 14 T flat version | 14 T stepped version | 12 T flat version | 12 T stepped at 4.5 K
Nb3sn Insulated cable surface (1 aperture) | (mm2) | 11 572 | 5 786 | 5 119 | 3 116 | 5 786
Nb-Ti Insulated cable surface (1 aperture) | (mm2) | 0 | 5 394 | 6 016 | 5 394 | 5 394
Nb3Sn savings to BOND | (%) | 0 | 50 | 66 | 73 | 50
Operational parameters |  |  |  |  |  | 
Current | (kA) | 19.34 | 19.34 | 19.34 | 19.92 | 16.20
Peak field on Nb3Sn | (T) | 14.8 | 14.8 | 14.8 | 13.0 | 12.7
Short sample current on Nb3Sn | (kA) | 23.66 | 23.66 | 23.66 | 27.27 | 21.02
Short sample field on Nb3Sn | (T) | 17.8 | 17.8 | 17.8 | 17.1 | 16.0
Loadline fraction on Nb3Sn | (%) | 81.7 | 81.7 | 81.7 | 73.0 | 77.1
Peak field on Nb-Ti 1st layer | (T) | - | 6.8 | 8.7 | 8.7 | 7.0
Short sample current on Nb-Ti 1st layer | (kA) | - | 31.65 | 24.79 | 25.38 | 18.95
Short sample field on Nb-Ti 1st layer | (T) | - | 9.9 | 10.7 | 10.6 | 7.9
Loadline fraction on Nb-Ti 1st layer | (%) | - | 61.1 | 78.0 | 78.5 | 85.5
Peak field on Nb-Ti 2nd layer | (T) | - | 8.8 | 8.8 | 8.9 | 7.0
Short sample current on Nb-Ti 2nd layer | (kA) | - | 24.04 | 24.04 | 24.91 | 18.43
Short sample field on Nb-Ti 2nd layer | (T) | - | 10.8 | 10.8 | 10.7 | 7.9
Loadline fraction on Nb-Ti 2nd layer | (%) | - | 80.5 | 80.5 | 80.0 | 87.9
AC-losses over a full cycle | (kJ/m) | 24.6 | 15.2 | 13.8 | 8.3 | 14.3
AC-losses gain to BOND | (%) | 100 | 38 | 44 | 66 | 42
BOND Conductor Parameters | Nb3Sn | Nb-Ti
Strand layout | RRP 162/169 | Custom
Strand diameter | 1.1 mm | 1.1 mm
Effective filament diameter | 64 µm | 7 µm
Filament twist pitch | 19 mm | 15 mm
Crossover resistance | 30 µΩ | 30 µΩ
Adjacent resistance | 0.3 µΩ | 0.3 µΩ
Cu/Non-Cu ratio | 0.9 | 1.6
Number of strands in a cable | 40 | 40
Strand twist pitch | 121 mm | 115 mm
Bare cable thickness (reacted) | 2.06 | 2.06
Bare cable width (reacted) | 23.275 | 23.275
Insulation thickness | 150 µm | 150 µm
BOND Magnet Parameters | Unit | BOND
Aperture diameter | (mm) | 50
Intra-beam distance | mm) | 250
Number of turns per quadrant | - | 23 / 29
Insulated cable surface per aperture | (mm2) | 11572
Nominal current | (kA) | 19.34
Overall current density | (A/mm2) | 348
Bore field at Inom | (T) | 14.0
Peak field at Inom | (T) | 14.8
Loadline fraction at 1.9 K | (%) | 81.7
Short sample current at 1.9 K | (kA) | 23.66
Short sample peak field at 1.9 K | (T) | 17.8
Short sample current at 4.5 K | (kA) | 21.20
SMC Conductor Parameters | Nb3Sn | Nb-Ti
Strand layout | RRP 162/169 | LHC 02
Strand diameter | 0.850 mm | 0.825 mm
Effective filament diameter | 55 µm | 7 µm
Cu/Non-Cu ratio | 1.2 | 1.9
Number of strands in a cable | 32 | 35
Bare cable thickness (reacted) | 1.59 | 1.48
Bare cable width (reacted) | 14.88 | 14.75
Insulation thickness | 150 µm | 150 µm
Coil design | Unit | SMC MQXF | SMC-H
Number of turns (Nb-Ti/Nb3Sn) | - | 31 | 15 / 16
Nb3sn insulated cable surface | (mm2) | 3 564 | 1 725
Nb-Ti insulated cable surface | (mm2) | 0 | 1 714
Nb3sn ratio to SMC MQXF | (%) | 100 | 48
Operational parameters |  |  | 
Short sample current on Nb3Sn | (kA) | 18.9 | 18.9
Short sample field on Nb3Sn | (T) | 14.0 | 14.0
Short sample current on Nb-Ti | (kA) | - | 17.0
Short sample field on Nb-Ti | (T) | - | 8.1
Nb3Sn
Nb-Ti
Nb3Sn
Nb-Ti
Nb3Sn
Nb-Ti
Nb3Sn
Nb-Ti