## Slide 2
High Field Magnets news, actions and special topics
Ezio Todesco
On behalf of HFM collaboration
Thanks to B. Auchmann, A. Milanese

## Slide 3: Contents
Recall of mandate, structure and ESPP documents
Revised targets for FCC-hh in Nb3Sn, options, and some special topics
Outlook on HTS

## Slide 4: Mandate of HFM
Mandate of HFM was revised in January 2024 towards a more directed R&D for FCC-hh
  In particular the concept of “finding the limit” is removed – impossible to make a TDR without a baseline, but with ranges – on the other hand, we are ready to change the baseline if needed
2024
Develop an Nb3Sn accelerator dipole with 14 T operational field for FCC-hh, giving an energy of 85 TeV c.o.m., with a focus on sustainability, cost versus performance, and large scale production
Explore the HTS magnet technologies for accelerator applications in the range from 14 T up to 20 T
Promote the required developments for superconductors
Highlight the innovative of high field magnets developments, both for particle physics instruments different from FCC, and for societal applications
2023
Design and demonstrate a full-size Nb3Sn accelerator magnet to proof the maturity of the most advanced technologies today, based on the HL-LHC design, i.e., 12 T magnets, and applying all the lessons learned from the US LHC Accelerator Research programme (LARP), the US High-Luminosity LHC Accelerator Upgrade project (AUP) and the HL-LHC project
Explore the limitations of the LTS state-of-the-art technology and push Nb3Sn magnet technology to its practical limits in terms of ultimate performance, towards the 16 T target targeted by the FCC-hh
Explore the capabilities and limitations of state-of-the-art HTS

## Slide 5
11 collaborating institutes
33 workpackages, half from CERN
HFM forum
HFM WG
www.cern.ch/hfm
Five RD lines
  Nb3Sn conductor
  Nb3Sn magnets
  HTS
  Integration & sust.
  Infrastructures
  Plus societal impact
Each collaboration has a CERN technical coordinator

## Slide 6: Budget
Budget is of the order of 180 MCHF (CERN material) for the 2021-2035
  This is used for CERN WPs to pay material and M4P (fellow, students, associates, FSU)
  This is used for collaboration WPs to pay material for collaborations, and monetary contribution
This is complemented by 40 MCHF of in kind from collaborations
  Note that only active collaborations are estimated, therefore this number is expected to grow with time
See talk of G. Riddone

## Slide 7: The ESPP documents
European Strategy Update was anticipated by one year, and 2025 has seen a major effort to prepare the documents
  We contributed to the FCC document with the revised baseline for FCC-hh ESSP document 247 page 533-546
  We wrote a specific document for the HFM program ESPP document
  Both presented in Venice, 2025 and published
A Physics Briefing Book summarizing all documents has been published
  It contains two sections concerning HFM in the chapter accelerator technology
  The baseline for FCC-hh (pp. 171-183)
  A dedicated section on the magnets (pp. 179-181)
  https://cds.cern.ch/record/2944678

## Slide 8: Contents
Mandate, structure and ESPP documents
Revised targets for FCC-hh in Nb3Sn, options, and some special topics
Outlook on HTS

## Slide 9: Main novelties of the strategy update: baseline
Baseline for FCC-hh: from 100 Tev - 16 T, to 85 TeV - 14 T
  1.9 K and Nb3Sn are kept as baseline
Main advantages
  The magnet is at 80% of short sample with HL-LHC conductor
  Stress limits <150 MPa rather than <200 MPa
  Conductor is available 1200 A/mm2 at 16 T and 4.2 K
  Synchrotron radiation scales with E4: so 15% less energy gives 50% less synchrotron radiation
Another relevant element is that we made a clarification between baseline (this slide) and options (see next slide for Nb3Sn)
  The HTS option has a 14 T target, but with possibilities of going up to 20 T
    This would give 120 T, i.e. four times the synchrotron radiation – however we keep it as a long term strategic target
Finally, we updated the timelines without the constraint of having operation in 2070 (see slides 16 and 21)
  It is very difficult to make a R&D program with 2070 as target date …
FCC-hh parameters | CDR 2019 | 2024-Nb3Sn
Dipole field (T) | 16.0 | 14.0
Temperature (K) | 1.9 | 1.9
Tunnel length (km) | 100 | 90.7
Arc length (km) | 82.0 | 76.9
Arc filling factor (adim) | 0.80 | 0.83
Energy c.o.m (TeV) | 100 | 85
Non Cu jc 16 T 4.2 K | 1500 | 1200
Loadline margin | 86% | 80%

## Slide 10: Main novelties of the strategy update: options
If in the future Nb3Sn can achieve 1500 A/mm2 (original target of FCC-hh), with same price, we can reduce the conductor mass by 30%
  Conductor is a driving factor of the dipole cost (order of 50% under some hypothesis)
  This option can be injected in the designs that are presently developed at any time
  This option has been introduced in 2024, when the target for the conductor has been lowered
We could use Nb-Ti in the low field area (nb-Ti / Nb3Sn hybrid option)
  This can reduce the Nb3Sn conductor mass by 50% (more in the next slides)
  This option has been proposed/rediscovered in 2024 by CIEMAT
We could consider 4.5 K operation with the same design for 1.9 K
  This reduce the total energy consumption by 30%, but this would exclude the hybrid Nb-Ti/Nb3Sn and strongly reduce the margin (more in the next slides)
  This option has been proposed in 2024, after seeing that MQXFB always reach operational current also at 4.5 K
We could consider 12 T operational field to reduce the conductor mass, cost and challenges
  This would reduce the magnet cost by 20%
  Several demonstrators are being built as intermediate step
  This option has been proposed in 2020

## Slide 11: HFM Nb3Sn zoo
Block 14 T
current grading
Block 14 T
Cosq 12 T
option
Cosq 12 T
option
Stress managed
Common coil 14 T
Common coil
14 T
Common coil
Demonstrator
(12 T)
Block demonstrators
(12 T)
SMCC demonstrator
(5 T)
Block demonstrators
(>14 T)
Done
Done
Done
2025
2025
2026
2026

## Slide 12: HFM Nb3Sn zoo
We rearranged the global view of the designs separating
Demonstrators (magnet without all features needed for operation)
short models (magnet that if scaled to long lengths can satisfy all operation requirements

## Slide 13: The 4.5 K option
The 4.5 K option is challenging but offers some opportunities
  Lower consumption of the magnet (total reduction of energy consumption of about 30%) – and a factor two less on the magnet consuption
Challenges
  The temperature margin is reduced by a factor two (4.5 K to about 2 K)
  Having a variation of temperature along the machine of the order of 0.5 K, the margin could be too small
Moreover, the option considers a conduction cooled forced flow “dry magnet” (see P. Borges de Sousa at HFM forum https://indico.cern.ch/event/1449712/ )
  This would reduce He inventory from 800 to 400 tons and reduce the logistics
  Challenge: magnet insulation becomes more complex
PSI is manufacturing a SubSMACC to be tested in 2026 to be cooled via conduction (22 mm aperture)
Conclusion: we carefully study this option but it looks challenging
  Note also that 400 tons of He cost is order of 50 MCHF, so neglibile
  One could consider also 4.5 K with a magnet immersed in LHe
Magnet immersed in LHE (right) and cooled via forced flow (left)
P. Borges de Sousa
SubSMACC cooled via forced flow
D. Araujo et al.

## Slide 14: Nb3Sn/Nb-Ti hybrid option
Nb-Ti/Nb3Sn were proposed for HE-LHC 15 and 20 T conceptual design and long time ago E. Todesco et al, IEEE TAS 24 (2014)
Nb-Ti/Nb3Sn were used in LPF3 by the IHEP colleagues, reaching 12.5 T in a common coil demonstrator C. Wang et al., SUST 36 (2023)
For the 14 T case, half of the coil can be in Nb-Ti !
  See F. Toral (DAISY) at ASC 24: IEEE TAS 35 (2025) https://ieeexplore.ieee.org/document/10859164
  See A. Haziot at HFM forum (BONDh), https://indico.cern.ch/event/1524821/
  See D. Araujo at HFM forum (SMACC), https://indico.cern.ch/event/1581999/
Moreover, the finer filaments of Nb-Ti give lower losses (30% reduction in hysteresis losses)
  If operate at 4.5 K, the reduction of Nb3Sn is only 1/5
  If we go at 4.5 K and 12 T, the reduction of Nb3Sn is 1/3
CERN plans to explore this technology in a SMC
  Conceptual design ongoing, first test in 2026
Hybrid Nb3Sn / Nb-Ti BONDh 14 T dipole [A. Haziot, et al.]
NbTi
Nb3Sn
Hybrid Nb3Sn / Nb-Ti DAISY 12 T dipole
[F. Toral, et al.]

## Slide 15: Nb3Sn/Nb-Ti hybrid option
We had a brainstorming about the present hybrid designs of CIEMAT, PSI and CERN https://indico.cern.ch/event/1595880/
  INFN is also considering a 4 layers with Nb-Ti in the outer
Designs are quite similar, with a 350 A/mm2 overall current density
  PSI is considering a grading also in current, reaching 500 A/mm2
CEA keeps the baseline of the Nb3Sn grading

## Slide 16: Too many designs ? And when going long ?
In March we had an LDG review on the program
  Reviewers: H. ten Kate and Ph. Lebrun
Two main comments for Nb3Sn
  The requirement of down-selection now it is not wise, collaboration are manufacturing magnets: we have to wait for the results
  The requirement on accelerating demonstration of full-length magnets has been addressed
CERN is launching a 4-m-long block coil to be tested vertically to prove the scaling of block coil to intermediate lengths
CERN could also launch a 4-m-long racetrack for common coil
LDG REVIEW Nb3Sn COMMENTS
Down-select 12-14 T Nb3Sn dipole designs now and engage coordinated development of the baseline design with the collaborating labs
Accelerate the demonstration of full-length magnets
5-m-long block dipole BONDM
[J. Ferradas, et al.]
The block coil with flared ends, based on HD2 concept [J. C. Perez, et al.]
CERN winding tests with portal winding machine for long block coils.

## Slide 17: Another new element: the timeline for Nb3Sn
Now-2035: select a magnet design and launch a demonstrator program to scale up to 4 m, check reproducibility, performance, …
2035-2042: scaling to 15 m with industry involvement and preseries magnets
2042-2050: production and installation
Nb3Sn accelerated timeline for FCC-hh [ESPP document]
15 m long prototypes (>5 each type)
Ongoing
12 T and 14 T short models
(7 designs, 1 or 2 of each type)
Short model program on two selected designs
(>5 each type)
Selection of final design
to start long magnets
`25
`26
`27
`28
`29
`30
`31
`32
`33
`34
`35
`36
`37
`38
`39
`40
`41
RunIII
HL-LHC RunIV
HL-LHC RunV
5-m-long prototypes
(>5 each type)
`42
`43
`44
`45
`46
`47
`48
`49
`50
`51
Industrialization (pre-series magnets)
Production and test
Installation and commissioning
`52
`53
`54
Tender
for the series
First selection
of design
4-m-long demonstrators
(block and racetrack)

## Slide 18: Too many designs ?
Coming back on the point of too many designs
Main part of mastering Nb3Sn is coil manufacturing
  A key to the success to the FCC-hh is that several laboratories master Nb3Sn technology
  CERN is mastering this with several programs (up to 14-16 T)
  CEA has mastered the full manufacturing cycle via two SMC (11 T) and R2D2 (test soon)
  PSI has mastered the full manufacturing via a CCT (10 T) and a stress managed magnet (6 T)
  ASG/INFN is starting now and should complete in 2026
  CIEMAT will produce coils in 2026
Ideas are circulating and being exchanged
  Asymmetric common coil proposed by PSI, and adopted by CIEMAT
  Hybrid design proposed by CIEMAT (and IHEP …), and adopted by CERN and PSI
This is a very important exchange that is within the guideline of the program
  To avoid that HFM is just distributing money and requirements, but to produce a global coordinated effort in R&D
The R2D2 coil (E. Rochepault, et al.)

## Slide 19: Another development: wax impregnation
Wax impregnation has been proved to reduce (eliminate) training in stress managed magnets as CCT
Proof in PSI A. Brem et al., IEEE TAS 34 (2024) 7700105, doi: 10.1109/TASC.2023.3338588.
Recent proof in LBNL: CCT5-w
CERN is building the first non stress managed magnet (SMC) wax impregnated
  Test will be in November
  Will it have the same effect ?
wax
CTD 101K
11 T
10 T
9 T
8 T
7 T
CCT5w in LBNL (D. Arbaleaz, at HFM forum)

## Slide 20: Contents
Mandate, structure and ESPP documents
Revised targets for FCC-hh in Nb3Sn, options, and some special topics
Outlook on HTS

## Slide 21: The HTS path
HFM also includes as a R&D target dipoles based on HTS in the 14 -20 T range, that could operate at higher temperatures and at fields >15 T
  HTS has a huge potential and a large momentum from the fusion community
  Even though high field solenoids have been successfully built, many challenges have still to be solved for the applications to high field dipoles, protection above all
    Is the 20 T target still valid for FCC-hh? 120 TeV means 4 times more synchrotron radiation w.r.t. 85 TeV (with same beam parameters), and power consumption now is critical
FCC-hh parameters | 2024-Nb3Sn | 2024-HTS
Dipole field (T) | 14.0 | 14-20
Temperature (K) | 1.9 | 4.5-20
Tunnel length (km) | 90.7 | 90.7
Energy c.o.m (TeV) | 85 | 85-120
Non Cu jc 16 T 4.2 K | 1200 | TBD
Loadline margin | 80% | TBD
HTS tape developed in ARIES and Bruker
MI racetrack coil [T. Lecrevisse, et al. ]
ReBCO racetracks [A. Ballarino, et al.]

## Slide 22: Timeline for HTS
Target: by 2035 a proof of a short model dipole with all features for FCC
  Aperture, field ≥14T, field quality, protection, …
  Ten years look a lot, but if you look back …
This timeline, if all proofs are positive, could give FCC-hh operation in 2060
CONSTRUCTION (ends 2060)
CANAVASSING
Demonstrators to select cable
and design
SCOPING
Short model ≥14 T
Selection of cable and
insulation technology
`25
`26
`27
`28
`29
`30
`31
`32
`33
`34
`35
`36
`37
`38
`39
`40
`41
RunIII
HL-LHC RunIV
HL-LHC RunV
FEASIBILITY
Reproducibility and first scaling in length
`42
`43
`44
`45
`46
`47
`48
`49
`50
`51
FINAL PROTOTYPES
PRE_SERIES AND INDUSTRIALZATION
`52
`53
`54
Proof of short model
with all requirements
Proof of reproducibility
and first long magnets
HTS timeline for FCC-hh [August 2023, B. Auchmann, et al.]

## Slide 23: HTS for accelerator dipoles: advancement in the last ten years
Apertures
  C1, C2, C3: 65 mm
  Feather2, cosq: 40 mm
  IHEP: 20 mm
Cables
  Bin5 (BSCCO): Rutherford
  Feather2, Cosq: Roebel
  IHEP, CERN 2025: tapes
  CEA 2025: MI tapes
Design
  Feather2: aligned block
  C1, C2, C3, Bin5: CCT
  IHEP: racetracks with gap

## Slide 24: HTS program: hybrid LTS/HTS or all HTS ?
Both IHEP and US-MDP have a program that is relying on hybrid Nb3Sn and HTS
  IHEP present target: 11 T in Nb3Sn, 7 in HTS
    They recently achieved the target on both HTS and LTS separately, but when powering together the HTS degraded
  US MDP target: 20 T with stress managed designs
    5 T reached with ReBCO C3 CCT dipole, and test in Nb3Sn outsert is coming soon
HFM strategy is to go for a all HTS, ramping up in field
  Approximate steps 5 T, 9 T, 14 T
  Common coil geometry is strongly preferred by all labs
Hybrid design for 20 T magnet
[P. Ferracin, et al, IEEE TAS 33 (2023) 4002007
and 4LOr1B-01]
Hybrid design for 20 T magnet
[Q. Xu, et al, CEPC design report, pg 749]

## Slide 25: HTS program: tapes
Roebel cable was the Eucard2 workhorse, but it has been abandoned
  Today, the community is working with tapes, or with cables with a circular geometry (CORC® or CORC like)
HFM is mainly investing on ReBCO
    We carefully follow BSSCO development and advancement in the US (talk at HFM forum of T. Shen, https://indico.cern.ch/event/1510468/ )
    We have a WP on IBS (CNR SPIN), and we follow the advancements in China
Three different paths are being taken by CEA, CERN and PSI for the first demonstrators
  CEA: metal insulated tapes – wide experience of CEA with this technology, an impressive literature has been produced – the program has reached >5 T in racetrack (no aperture), and is going to test 600 mm long coils (Narsil)
  CERN: insulated tapes, with Cu – the program has reached >5 T in racetrack, and is ramping towards 9 T soon
  PSI: soldered stacks of tapes, with stress managed common coil platform also used for Nb3Sn

## Slide 26: HTS program: synergies
HTS today is a more difficult environment to apply the collaborative paradigm
  Lot of emphasis coming from fusion, with private investements, start-ups … this field is growing very very rapidly with a lot of expectations
HFM management is encouraging sharing of results and strategies in a early stage – this is the way of accelerating the R&D (HL-LHC/LARP/AUP paradigm)
  I wish to organize a brainstorming on the dimensions of the coils that we are manufacturing today
  And the path in field/length/ aperture that is planned, in PSI, at CERN and in CEA
180 mm long MI racetrack coil [T. Lecrevisse, et al. ]
100 mm long ReBCO racetracks [A. Ballarino, et al.]
600 mm long MI racetrack coil
[T. Lecrevisse, et al. ]
LDG REVIEW HTS COMMENTS
Set up a task force to accelerate the R&D on ReBCO, aiming at demonstrating principle solutions for a 10-20 kA accelerator magnet conductor and quench protection of long HTS coils

## Slide 27: Some questions about physics
How to make the scale up of the demonstrators to short models ?
  Several parameters: field, aperture, length …
How about cable geometries
  Can we exclude that simple tapes cannot be used to manufacture a accelerator magnet ?
Protection seems today the main critical aspect
  What is the driving parameter ?
    Stored energy ? (hard to believe to me – it should be an intensive quantity, not an extensive)
    Field square , i.e. magnetic pressure ?
    Energy density on the coil ?

## Slide 28: Conclusions
The new baseline for FCC-hh is more compatible with all constraints
  85 TeV is a good bargain: 15% less energy, bringing 50% less synchrotron radiation, plus ..
  … a 14 T Nb3Sn magnet feasible with HL-LHC conductor, and 150 MPa stress rather than 200 MPa
  … and at 14 T half of the coil can be in Nb-Ti ! Considerable cost reduction – we just need 30% reduction of present HL-LHC strand cost to fit the FCC targets
Options are being considered
  Hybrid Nb-Ti/Nb3Sn to reduce cost, 4.5 K to bring energy saving, 12 T to reduce costs
Several designs for Nb3Sn are being explored (block, cosq, common coil, stresss managed) and first results will come in 2026
HTS efforts are focussed on ReBCO, and all-HTS; first results are available on racetracks
  Common coil design is the workhorse for the moment, but other designs are being explored

## Slide 30: Some references
Talks at FCC week
    E. Todesco, Overview of LTS HFM magnet and conductor activities. indico.cern.ch/event/1549746
    A. Ballarino Progress towards HTS HFM magnet and conductor strategy indico.cern.ch/event/1408515/contributions/6513891
    A. Verweij Protection of LTS and HTS magnets and circuits for FCC-hh. indico.cern.ch/event/1408515/contributions/6513888
    Q. Xu HTS magnet R&D for next-generation accelerators at IHEP
    P. Ferracin Status of US MDP indico.cern.ch/event/1408515/contributions/6513892
    E. Rochepault Status of HFM development at CEA indico.cern.ch/event/1408515/contributions/6513893
    F. Toral Status of HFM development at CIEMAT indico.cern.ch/event/1408515/contributions/6513896
    A. Pampaloni Status of HFM development at INFN indico.cern.ch/event/1408515/contributions/6513894
    B. Auchmann Status of HFM development at PSI indico.cern.ch/event/1408515/contributions/6513895
    L. Delprat FCC-hh cryogenics update for 1.9 K and 4.5 K options indico.cern.ch/event/1408515/contributions/6499564
    P. Tavares Coutinho Borges De Sousa Cryogenic baseline and advancements on the 4.5 K option for FCC-hh using Nb3Sn magnets indico.cern.ch/event/1408515/contributions/6513882
HFM forum: https://hfm.web.cern.ch/hfm-forum
HFM talks at conferences and meetings: https://indico.cern.ch/category/19189/
For the updated baseline of FCC-hh, my plenary at ASC 10.1109/TASC.2025.3558196

## Slide 31: Timeline for HL-LHC
All development and production in labs (4 different ones: BNL, FNAL, LBNL, CERN)
MQXFA
prototypes
(2 each type)
HL-LHC
project
MQXFB production and test (10 magnets)
Demonstrators (TQ, HQ, LQ) including scaling to 4 m, plus first MQXF in the US
Selection of aperture
and cable
`00
`01
`02
`03
`04
`05
06
`07
`08
`09
`10
`11
`12
`13
`14
`15
`16
LHC RunI
LHC RunII
LHC RunIII
MQXFB
prototypes
(2 each type)
MQXF short models (7) ……..
`17
`18
`19
`20
`21
`22
`23
`24
`25
`26
MQXFA production and test (20 magnets)
`27
`28
`29
LARP
approval
Design study HiLumi

## Slide 32: Timeline for LHC
Initial development in industry and institutes (mature technology) - approval based on a 10 m long magnet
Reduction of field from initial 10 T to 8.3 T
Short model at CERN from 1995
Design changes up to the very end of prototypes
Scaling to 10 m in industry (6 magnets)
Field reduction:
8.65 T to 8.33 T
LHC approved
Production
(1200)
Final prototypes
(6 magnets)
SSC canceled
`79
`80
`81
`82
`83
`84
85
`86
`87
`88
`89
`90
`91
`92
`93
`94
`95
LEP operation
Scaling to 10 m in industry
56 mm aperture (5 magnets)
CERN final short models (30)
`96
`97
`98
`99
`00
`01
`02
`03
`04
`05
Preserie
(30)
`06
`07
`08
LHC in the LEP tunnel first proposal:
8 TeV, 10 T
Field reduction:
10 T to 8.6 T
Aperture increase:
50 mm to 56 mm
Installation
Collar material change:
Al to SS
Short models
Thanks to L. Rossi for comments