## Slide 1: e-cloud in SPS
Present situation of the development of mitigation methods
-MD 2011 results (clearing electrodes, half coated chambers, Q20/Q26)
-Carbon coating of dipoles
-Plans
Taborelli Mauro. LIU Day, 25/11/2011

## Slide 2: Summary of previous measurements of electron cloud monitors (ECM) in SPS MD for various SEY (StSt, a-C, DLC..)
Chart: SEY
| 2.25 | 1.8 | 0.95000000000000062 | 1.750000000000008 | 1.45 | 1 | 1.1399999999999877 | 0.92 | 0.97000000000000064 | 0.95000000000000062
25 ns | 1.1482 | 0.4 | 7.9433e-05 | 0.17 | 0.1 | 3e-05 | 0.0003 | 5e-05 | 0.0004
50 ns | 0.15 | 0.06 | 0.015 | 1.5e-05 | 3e-05 | 3e-05

## Slide 3: ECM for MD in 2011: two configurations in SPS
Carbon coated
3y in SPS
StSt8
Clearing
electrode
(StSt)
Carbon/StSt
Half coated H
StSt 9
Carbon coated
hollow cathode
MD w19
MD w21
MD w33
MD w35
Would it be sufficient to coat half of the pipe or insert a coated “gutter” ?
Do clearing electrodes work up to nominal B-fields ?
Carbon/StSt
Half coated V
Carbon coated
3y in SPS

## Slide 4: 25 ns, half carbon-coated vs StSt
At 25 ns the half coated has only 10 times lower current (500 times lower for 50 ns) than StSt, whereas a full carbon coating has at least 1000 times lower current
Conditioning has a similar slope for both (6.5 hours, 3 batches x 72b)
Half coated V
StSt9
Int e-cloud/int BCT
MD
Half coated V

## Slide 5: Half-coated vertical : predicted effect by simulations of G.Rumolo (uncoated part δmax=1.8)
G.Rumolo
1.8
1.6
1.4
1.2
1
0.8
0 500 1000 1500 2000 Energy[eV]
StSt liner extracted from SPS:
1.8 is realistic
The result from the MD fits with the prediction of the simulation if we assume an SEY around 1 and a reflection or a zero energy reflection above 0.5
SEY

## Slide 6: Clearing electrode (StSt)
2011 , StSt
alumina plasma spray, to be tested in 2012
From KEK (Y. Suetsugu) to CERN
Al2O3
W

## Slide 7: Clearing electrodes: as a function of voltage for different B fields, 25 ns
o 1.1A
o 2.5A
o 5A
* 25A
* 40A
+ -25A
o 25A
+ 25A, 450Gev
26GeV
3 batches
Int e-cloud/int FBCT
0 20 40 60 80 100 120 140 160 180 200
Voltage on the electrode [V]
◊Effective suppression at all tested B fields with low voltage <100V
◊NB: the effect on pressure is almost invisible (the electrode is short 0.4 m) compared to the conductance of the pipe

## Slide 8: Comparison of e-cloud in Q20/Q26 settings in e-cloud monitor
50 ns
3 batches Q26 + 2 batches Q20
Int e-cloud/int BCT
Int e-cloud/int BCT
0
-0.05
-0.1
-0.15
-0.2
-0.25
-0.3
-0.35
-0.4
25 ns
2 batches Q26 + 2 batches Q20
1.885 1.89 1.895 1.90 1.905 1.91 1.915 1.92 1.925
super cycle number
No significant difference in the measured e-cloud current between the two settings neither at 50 ns nor at 25 ns

## Slide 9: Emittance effect on e-cloud: 50 ns, StSt ECM
1x36
2x36
3x36
4x36
1.35p/b
Inj Eh= 1.6-1.7
Inj Ev=1.6-1.8
4x36
1.6p/b
Inj Eh= 2
Inj Ev=1.9
1.4p/b
Inj Eh= 3
Inj Ev=2.6
4x36
From G.Rumolo
Lower emittance at equal intensity leads to larger e-cloud current
- Should we redo it by disentangling vertical and horizontal emittance effect?

## Slide 10: Coatings of SPS dipole chambers
MBB chambers (disassembling/assembling the dipole-yoke):
We have the technology to coat 7m chambers in “magnetron” (new cathode being rebuilt), 3 dipoles already in SPS since 1 year
MBA chambers (disassembling/assembling the dipole-yoke):
-Same technology as MBB, 1 prototype in MBA in progress (next week)
NB: at present we do not have a technique for
magnetic measurements in coated pipes, which
avoids damaging the coating!

## Slide 11: Coatings in dipole
MBB in dipole (without disassembling):
We have the technology to coat 7m chambers in “hollow cathode” (2 prototype tubes)
MBA in dipole (without disassembling):
Same technology as MBB, cathode under construction (March 2012)

## Slide 12: Direct measurement of e-cloud and pressure in dipoles
20 mm
40 mm
grid for RF screening
20 mm+1mm
Insert a screened pick-up electrode directly in the dipole by drilling a hole in the yoke: local measurement of e-cloud and pressure
Calculations (J.Bauche) confirm that the effect of two symmetric holes on the magnetic length can be compensated by shims

## Slide 13: Diagnostics in the lab: Multipactor in StSt dipole
RF diagnostics: reflected power
Pressure rise diagnostics: RGA signal
M.Holz
M.Holz
Power in
reflected
pressure
Time

## Slide 14: Planning
Plan for winter 2011-12 TS
Insert in SPS a half cell (or part of it) with carbon coated chambers in magnetron
Clearing electrode in alumina plasma-spray
By mid 2012
Complete the half-cell and add a second half-cell coated in “hollow cathode”
Equip it with more detailed pressure diagnostics
Insert pick-up diagnostics in dipoles (1 coated + 1 uncoated)
Plan for LS1
- Insert 2 cells with coating

## Slide 15: All this would not have been possible without the contributions of :
J.Bauche
P.Costa Pinto,
F.Caspers,
P.Edwards,
M.Holz,
D.Holzer,
M.Jimenez,
L.Leggiero,
M.Mensi,
H.Neupert,
G.Rumolo,
E.Shaposhnikova,
C.Yin-Vallgren
…….

## Slide 16
proton
beam
e-cloud current
48 strips spaced 1.5 mm
magnet chamber
Coated liner
B-field (0.12 T = field of SPS at injection)
Measurements of currents in electron cloud monitors

## Slide 17: Pressure calculation
Coated
dipoles
without
dyn. outgassing
Entire layout: 6 full cells
Measured p
Assumptions:
only StSt dipole have dynamic outgassing
pumping speed of ion pumps is the nomimal one
Result of the analytical calculation:
The dynamic pressure rise in the coated dipoles is between 3 and 5 times lower than in StSt
We never observed this!
D.Holzer

## Slide 18: Pressure measurements between coated/uncoated MBB dipoles
1 and 2 batches, 25 ns, 2011
Uncoated
carbon coated

## Slide 19: Residual gas analyser installed in SPS (MD May 2011) close to ECM
Chart: Time[hh:mm:ss]
Beam on: 25 ns, 3 batches, 72bunches, 450 GeV
Gas ratios typical for particle induced desorption: no change for water and p dominated by CO and H2. (approximate calibration of RGA)