## Slide 1
Surface effects in double-sided silicon 3D sensors fabricated
at FBK
Gian-Franco Dalla Bettaa, M. Povolia, A. Bagolinib,
M. Boscardinb, G. Giacominib,F.Mattedib, E.Vianellob, N. Zorzib
a INFN and University of Trento, 38123 Povo di Trento, Italy
b Fondazione Bruno Kessler (FBK-irst), 38123 Povo di Trento, Italy
Work supported by PAT, project MEMS2, INFN CSN V, projects TREDI (2005-2008)
and TRIDEAS (2009-2012), and INFN CSN I, project ATLAS

## Slide 2: Outline
Overview of FBK 3D technology
Aim of this work
Devices under test
Experimental results and TCAD simulations
Conclusion

## Slide 3: 3D sensor technology at FBK
- Double side process - Passing through columns.
- P-spray on both sides - Contacts on surface implants
E. Vianello et al., IEEE NSS11, Valencia, Paper N10-6

## Slide 4: Process evolution
ATLAS07: bad currents and low breakdown (p-spray dose too high)
ATLAS08: better current (less mechanical stress), low breakdown (same p-spray)
ATLAS09: good currents and higher breakdown (p-spray dose adjusted)
With higher breakdown, some layout dependent features have shown up …

## Slide 5: Aim of this work
Gain insight into the device electrical behavior using TCAD simulations
Tests performed on 3D diodes:
  two terminal devices, easy to measure
  ~10mm2 area, low defect density  intrinsic behavior
Measured technological parameters (lifetimes,…) and doping profiles (SIMS) implemented in the simulations
Attempt to disentangle the effects of each “component” of the device on the electrical characteristics

## Slide 6: FE-I4 like diode with field plate
Front-side
Back-side

## Slide 7: Other available 3D diodes
Different shapes, sizes and column configurations
Different distances between n+ and p+ regions
With and without field-plate

## Slide 8: I-V curves at different temperatures

## Slide 9: Breakdown voltage vs temperature
T coeff. in good agreement with typical values for avalanche breakdown

## Slide 10: Leakage current vs temperature
Avalanche contribution easily distinguished from SRH at 30V

## Slide 11: TCAD simulations
Structure parameters
1/4 of elementary cell (exploiting symmetry)
Exact layouts implemented
FBK technology parameters
Measured (SIMS) doping profiles
Models and simulation
Mobility: Doping Dependent, High Field Saturation
Generation/Recombination: SRH, Avalanche
Data analysis
Monitor electrical quantities in different regions
Understand where the breakdown occurs:
2D slices at different depths
1D cut extraction from 2D slices

## Slide 12: Exp. vs Sim. I-V curves (@RT)
Good agreement on leakage current at low voltage and breakdown voltage values
Agreement not so good as of the curve slope (work in progress)
Experimental Simulated

## Slide 13: Exp. vs Sim. Comparison Part 1: static parameters

## Slide 14: Simulations of FE-I4 diode @ -35V
Electrostatic potential Electric field
Electrostatic potential
P+ column brings the bias
voltage directly on the
p-spray on both sides
Electric Field
Highest fields at the
junctions between
N+ and p-spray:
Front 2.65e5 V/cm
Back 2.48e5 V/cm
High E-field also under
the front side metal
(vertical and horizontal
metal connections)

## Slide 15: Simulations of FE-I4 FP diode @ -35V
Electrostatic potential Electric field
Electrostatic potential
The field-plate helps depleting the p-spray close to the N+ diffusion
The potential of the p-spray now drops on a wider region
Electric Field
Highest fields at the
junctions between
N+ and p-spray:
Front 2.11e5 V/cm
Back 2.53e5 V/cm
But the field-plate helps in redistributing and lowering
the E-field on the front side (higher breakdown voltage, probably
on the back side)

## Slide 16: Electric field peak comparison

## Slide 17: FE-I4 FP diode C-V curves: exp. vs sim.
Column contribution ~50pF (less than 50% …)
Important increase due to p-spray
Back-side layers contribution negligible
Front-side N+ diffusion and field plate cause a large increase at low voltage, then reduced as p-spray is depleted

## Slide 18: Exp. vs Sim. Comparison Part 2: capacitance
Discrepancies between experimental and simulated capacitance at high voltage are mainly due to edge effects (not accounted for in the simulations)

## Slide 19: Conclusion
We have studied the electrical behavior of different 3D diodes fabricated at FBK
The layout has been found to impact on both the I-V and C-V curves of the devices.
A good agreement was found between measurements and simulations, confirming that TCAD is a reliable tool for device analysis and design (3D simulation compulsory)
This study will then continue with irradiated devices, with the aim of optimizing the layout accounting for both pre-irradiation and post-irradiation conditions.

## Slide 20: Acknowledgements
We would like to thank all members of the Processing Group within the ATLAS 3D Sensor Collaboration for many fruitful discussions

## Slide 21: Back-Up: Details of different diodes