## Slide 1
Development of
n-in-p planar pixel sensors
with active edge
for the ATLAS High-Luminosity Upgrade
L. Bosisio*
Università degli Studi di Trieste &
INFN – Trieste, Italy
*visiting professor @ Université
Pierre et Marie Curie
7th “Trento” Workshop on Advanced Silicon Radiation Detectors (3D and p-type Technologies)
Ljubljana, March 1st 2012
M.Bomben, G. Calderini,
J. Chauveau, G. Marchiori
LPNHE, Paris, France
A. Bagolini, M. Boscardin ,
G. Giacomini, N. Zorzi
Fondazione Bruno Kessler, Trento, Italy
A. La Rosa
DPNC, Université de Genève (CH)

## Slide 2
FBK (Trento)
Design
Process
Laboratoire de Physique Nucléaire et des Hautes Energies
(LPNHE)-Paris
Project leader
Simulations
Test

## Slide 3: Outline
What is this sensor for?
Trench Tech @ FBK
Layout
Simulations
Test Plans

## Slide 4: ATLAS Pixel Sensor
Dead edge
R&D for ATLAS upgrade
  a) Rad-hard for ~ 1e16 neq/cm2 (high luminosity LHC)
  b) Highly segmented to cope with high-event rate
   pixel sensor
  c) Minimize dead area (no z-overlap)
   Active Edge
  d) Low material budget
   Thin substrates (200 mm)
  e) Signal mainly due to electrons
   n-on-p technology
  (n-on-n is double-side, not compatible with Active Edge)
Active edge pixel sensor can be a choice

## Slide 5: Active Edge Sensor Structure
oxide
oxide
Support wafer
Field plate
p-substrate
Substrate contact
Trench
p-spray
p-stop
n-pixel

## Slide 6
n-on-p needs pixel insulation
We will use both p-spray and p-stop.
Process splittings concern the dose of such implants: e.g.
Splitting # | p-spray dose (cm-2) | p-stop dose (cm-2)
1 | 0 | 3e12
2 | 1e12 | 5e12
3 | 3e12 | 3e12
4 | 2e12 | 5e12
FBK has experience on planar n-on-p
the edgeless technology is different due to the presence of high temperature steps required for trench doping

## Slide 7: InterPixel Capacitance vs p-spray dose
Pixel capacitance should be minimized.
We want Field Plate (FP) for higher BD Voltage
p-spray must deplete under the FP or there’ll be a large interpixel capacitance
 Low p-spray dose
Field Plate, High dose p-spray
No FP, High dose p-spray
FP, Low dose p-spray
Interpixel Capacitance
fF/mm
Substrate Voltage (V)

## Slide 8
10mm wide
220mm deep
polysilicon filled
A.Bagolini, “Development of planar active-edge technology at FBK”, 6th Trento workshop 2011
poly
Clean Si surface
Trench experience @ FBK (1)

## Slide 9
Povoli et al., “Development of planar detectors with active edge” NIM A658 (2011) p. 103
Trench experience @ FBK (2)
Planar strip sensor (p-on-n)

## Slide 10: Wafer Layout
Space for
Hg probe
9 FE-I4
  0, 1, 2, 3, 5, 10 GRs
  Different n+trench distances
4 FE-I3
  1 or 2 GRs
  2/4 are PT biased
DC Strip Sensors
  0, 1, 2 GRs
  Different n+ trench distances
OmegaPix
  1 or 2 GRs
  2/4 are PT biased
TestPixels/Pad
  0, 1, 2, 3, 5, 10 GRs
  Different n+trench distances
FE-I4
FE-I3
OmegaPix
Planar
Test Strip
Test Pad
Pro SIMS
n+, p+, p-spray, p-stop

## Slide 11
Planar Test Structures
2 MOS (one over p-spray and one over p-spray + p-stop)
Gated diode
1-D Diode
Van der Pauw and contact resistance of every implant
Capacitors

## Slide 12: Test Pixel Sensors
trench
Short-circuited
FE-I4 pixel
Bias Tab:
back-side in not accessible until support wafer is removed
 ohmic (p) contact from front-side
IV Measurement: Break-down Voltage vs n+ trench distance
  Layout splittings
  0, 1, 2, 3, 5, 10 GRs
  Different n+trench distances
  Full-size FE-I4 sensors should behave exactly as these baby sensors
Scribeline:
useful if support wafer is not removed
its position does not affect the electrical characteristics

## Slide 13: DC-strip sensor
3-mm long strips
Same design as pixels, only length
is changed
In a group, 3 design variants
(36 strips each)
(0 GR, 1 GR, 2 GRs)
  wire-bondable to a 128 ch ASIC
Many groups, differing by
strip  trench distance
(50, 75, 100, 150 mm)
scribeline
Designed for measuring efficiency and signal collection in the edge region vs. design parameters (distance to trench, # of GRs)
Bias tab
trench
0 GR
1 GR
2 GRs
50 mm

## Slide 14
FE-I3 and Omega-Pix
n+  trench distance = 100 mm
~ 1.7 mm
 | PT biased | ROC biased
1 GR | OK | OK
2 GRs | OK | OK
PT-biased
Biased only by ROC
trench
Bias Tab
100 mm
100 mm

## Slide 15
Sensors with FE-I4 Layout
FE-I4 ROC is the newest of ATLAS and is available.
We can profit from the large experience on 3D and n-on-n read-out by FE-I4.
1 X 0 GR (100 mm)
1 X 1 GR (100 mm)
1 X 2 GR (100 mm)
2 X 3 GR (200 mm)
2 X 3 GR (bis) (200 mm)
1 X 5 GR (300 mm)
1 X 10 GR (400 mm)
trench
Bias tab
100 mm
250mm
50mm

## Slide 16
FE-I4 sensors: temporary metal
An additional metal contacts the pixel in the regions of passivation openings.
Automatic measurements on pixel sensors are possible.
Temporary metal is removed after measurements.
Temporary metal stripes (over the passivation), connecting all pixels in one row
100 mm
trench

## Slide 17: Simulations
Mainly dedicated to BreakDown Voltage (BDV) analysis.
Varied parameters are:
# of GRs
distance n+  trench
Design covers many layout options
 BDV can be measured on test diodes and compared with simulations
After validation with measured data, simulations can be used to improve the design,
Simulations/measurements done before & after irradiation

## Slide 18: Simulation Example (n+  trench distance = 100 μm)
BEFORE IRRADIATION
Vdepletion
O GR
1 GR
2 GRs
BDV >> Vdepl, also for short n+ trench distance

## Slide 19: Outlook
ready to start the fabrication:
  4-inch p-type 200-mm thick wafers have been bond-annealed at SINTEF
  Final layout done! masks ready
  ~ 4 months for processing
Electrical characterization
  pixel sensors, at wafer level, making use of temporary metal (automatic measurements)
  test structures ( diode, strip,..) before and after irradiations (manual measurements)
Late 2012: bump bonding
2013: beam tests

## Slide 20
Back-up

## Slide 21: Status
20 p-type 4” 200-mm thick wafers have been bond-annealed at SINTEF
Microscope inspection and IR images show no particular problems
4”

## Slide 22
Read-out chip FE-I4
sensor