## Slide 1: Exchange coupled donor dimers in nanocrystal quantum dots
A. J. Almeida1, R. N. Pereira1, A. R. Stegner2, M. S. Brandt2, H. Wiggers3
1 Institute of Nanostructures, Nanomodeling and Nanofabrication, University of Aveiro, 3810-193 Aveiro, Portugal 2 Walter Schottky Institut, Technische Universität München, Am Coulombwall 3, 85748 Garching, Germany 3 Institut für Verbrenung und Gasdynamik, Universität Duisburg-Essen, 47048 Duisburg, Germany
WALTER SCHOTTKY INSTITUT
MAP-fis PhD Research Conference – January 2012, Braga
University
of Aveiro

## Slide 2
Photoluminescence for dNC < 5 nm
High surface/volume ratio;
Tunable bandgap;
Intra- vs. interparticle physics.
Printable electronics;
Thermoelectric power devices;
[Lechner et al. Phys. Stat. Sol. (RRL) 1, 262 (2007)]
Solar cells;
[Lui et al., Nano Lett. 9, 449 (2009)]
Lighting;
[Cheng et al., Nano Lett. 11, 1952 (2011)]
Interesting properties:
Applications:
Understanding and control of doping is crucial for many of the applications!
MAP-fis PhD Research Conference - 2012
1/16
CB
VB
Motivation

## Slide 3: Motivation
Exchange interaction of many dopants
Properties of dopants in the bulk cannot be transposed to NCs:
[P]>3.7x1018 cm-3
Impurity
subband
Exchange interaction between few dopants
Impurity subband model unsuitable!
Confinement and
Isolation
CB
VB
MAP-fis PhD Research Conference - 2012
2/16
[P]>3.7x1018 cm-3

## Slide 4: Outline
Synthesis and basic properties of P doped Si NCs ensembles
  Characteristics of our P doped Si NCs ensemble
  Only NCs with single donor electrons or dimers are statistically relevant
Theoretical framework for exchange coupled donor dimers in NCs
  Prediction of EPR spectra from electronic structure of single donor electrons and dimers
  Prediction of the variation of the EPR signal due to dimers
Conclusions
Probing P doping of Si NCs via low-temperature Q-band electron paramagnetic resonance (EPR) spectroscopy
MAP-fis PhD Research Conference - 2012
3/16
Signal from surface defects, which displays Curie paramagnetism ( )
At low T, signal at g=1.998 due to exchange coupled dimers deviates
from

## Slide 5: Donors in NCs
Growth of Si NCs in a low pressure microwave plasma reactor;
Powder of isolated Si nanoparticles;
Lognormal size distribution with a standard deviation of ≈1.3;
A natural oxide shell is formed upon exposure to air (oxide thickness ≈ 1.5 nm) ;
Synthesis and basic properties of measured P doped Si NCs:
MAP-fis PhD Research Conference - 2012
A. R. Stegner, R. N. Pereira et al., Phys. Rev. B 80, 165326 (2009)
c-Si
core
SiO2
shell
Donors incorporated during growth (substitutional doping) with efficiency ≈100%;
Segregation – 95% of the incorporated donors segregate to surface, which oxidizes;
Compensation – Some donor electrons in NCs core become trapped in surface defects;
Segregation
SiO2 shell
P donor
Compensation
4/16
J. Knipping, H. Wiggers et al., J Nanoscience and Nanotechnology 4, 1039 (2004)
surface defects
(Si-dbs)

## Slide 6: Donors in NCs
Measured P doped Si NCs:
Macroscopic amount of NC powder (NCs ensemble)
Mean NC diameter dNC=3.9 nm
Ensemble density of surface defects [Si-dbs]=1.8x1011 cm-3 (as previously measured by EPR)
MAP-fis PhD Research Conference - 2012
Segregation
Segregation
Compensation
[P]NOM≈ 5x1020 cm-3
[e–] ≈1.4x1019 cm-3
Ensemble density
of donor electrons
[P]CORE ≈ 2.5x1019 cm-3
Nominal doping
concentration
Ensemble density of P donors in NC cores
How are these donor electrons distributed in our P doped Si NCs?
5/16
A. R. Stegner, R. N. Pereira et al., Phys. Rev. B 80, 165326 (2009)

## Slide 7: Donors in NCs
Measured P doped Si NCs:
MAP-fis PhD Research Conference - 2012
Segregation
Segregation
Compensation
[P]NOM≈ 5x1020 cm-3
[e–] ≈1.4x1019 cm-3
Ensemble density
of donor electrons
[P]CORE ≈ 2.5x1019 cm-3
Nominal doping
concentration
Ensemble density of P donors in NC cores
How are these donor electrons distributed in our P doped Si NCs?
5/16
Macroscopic amount of NC powder (NCs ensemble)
Mean NC diameter dNC=3.9 nm
Ensemble density of surface defects [Si-dbs]=1.8x1011 cm-3 (as previously measured by EPR)
A. R. Stegner, R. N. Pereira et al., Phys. Rev. B 80, 165326 (2009)

## Slide 8: Donors in NCs
Measured P doped Si NCs:
MAP-fis PhD Research Conference - 2012
Segregation
Segregation
Compensation
[P]NOM≈ 5x1020 cm-3
[e–] ≈1.4x1019 cm-3
Ensemble density
of donor electrons
[P]CORE ≈ 2.5x1019 cm-3
Nominal doping
concentration
Ensemble density of P donors in NC cores
How are these donor electrons distributed in our P doped Si NCs?
A. R. Stegner, R. N. Pereira et al., Phys. Rev. B 80, 165326 (2009)
5/16
Macroscopic amount of NC powder (NCs ensemble)
Mean NC diameter dNC=3.9 nm
Ensemble density of surface defects [Si-dbs]=1.8x1011 cm-3 (as previously measured by EPR)

## Slide 9: Donors in NCs
Ensemble concentration of NCs containing a cluster of n donor e–:
MAP-fis PhD Research Conference - 2012
NNC – number NC lattice sites
– relative density of donor e-
W – binomial distribution
dNC=3.9nm
Statistically, most P doped NCs in our NCs ensemble contain:
Single donor e- (n=1)
Donor dimers (n=2)
How are these donor electrons distributed in our P doped Si NCs?
We calculate the probability of one donor e– being in a NC core with n donor e-:
6/16

## Slide 10: Donors in NCs
Ensemble concentration of donor e– clusters with n e–:
MAP-fis PhD Research Conference - 2012
NNC – number NC lattice sites
– relative density of donor e-
W – binomial distribution
dNC=3.9nm
Statistically, most P doped NCs in our NCs ensemble contain:
Single donor e- (n=1)
Donor dimers (n=2)
How are these donor electrons distributed in our P doped Si NCs?
We calculate the probability of one donor e– being in a NC core with n donor e-:
6/16

## Slide 11: Outline
MAP-fis PhD Research Conference - 2012
7/16
Synthesis and basic properties of P doped Si NCs ensembles
  Characteristics of our P doped Si NCs ensemble
  Only NCs with single donor electrons or dimers are statistically relevant
Theoretical framework for exchange coupled donor dimers in NCs
  Prediction of EPR spectra from electronic structure of single donor electrons and dimers
  Prediction of the variation of the EPR signal due to dimers
Conclusions
Probing P doping of Si NCs via low-temperature Q-band electron paramagnetic resonance (EPR) spectroscopy
Signal from surface defects, which displays Curie paramagnetism ( )
At low T, signal at g=1.998 due to exchange coupled dimers deviates
from

## Slide 12: Principle of EPR spectroscopy
Applied magnetic field B lifts the degeneracy
Splitting of electronic levels ΔU=gμBB
Microwave radiation hν is applied
When ΔU=hν we have a resonant situation  EPR signal centered at Br
System with S=1/2
J. A. Weil, J. R. Bolton. Electron Paramagnetic Resonance: Elementary Theory and Pratical Applications. Wiley, 2nd edition, 2007
MAP-fis PhD Research Conference - 2012
Spectra acquired as first derivative
Microwave power below threshold for saturation
Ground state degeneracy equal to 2S+1=2
8/16

## Slide 13: Donors in NCs: Q-band EPR spectroscopy
Low microwave power EPR spectra of P doped Si NCs:
ganis
g
g
MAP-fis PhD Research Conference - 2012
Displays Curie paramagnetism
( )
Signal used as calibration constant for the measurement of the number of P donor states in Si NCs
High microwave power EPR spectra
of P doped Si NCs:
Broad absorption band – saturated signal from Si-dbs
g=1.998
9/16
Signal due to surface defects in NCs
Resonance at g=1.998
  Asymmetric at low T

## Slide 14: Donors in NCs: Q-band EPR spectroscopy
MAP-fis PhD Research Conference - 2012
High microwave power EPR spectra
of P doped Si NCs:
At low T, signal due to dimers deviates from Curie paramagnetism
Density of detected donor electrons decreases with T
g=1.998
Broad absorption band – saturated signal from Si-dbs
10/16
Resonance at g=1.998
  Asymmetric at low T

## Slide 15: Donors in NCs: Q-band EPR spectroscopy
MAP-fis PhD Research Conference - 2012
High microwave power EPR spectra
of P doped Si NCs:
g=1.998
Broad absorption band – saturated signal from Si-dbs
Resonance at g=1.998
  Asymmetric at low T
To understand these spectra, we must unravel the electronic structure of dimers in NCs
10/16
As we have seen before from our statistical analysis, donors in our NCs are present mostly as isolated donors and donor dimers

## Slide 16: Outline
Signal from surface defects, which displays Curie paramagnetism ( )
At low T, signal at g=1.998 due to exchange coupled dimers deviates
from
MAP-fis PhD Research Conference - 2012
11/16
Theoretical framework for exchange coupled dimers in NCs
  Prediction of EPR spectra from electronic structure of single donor electrons and dimers
  Prediction of the variation of the EPR signal due to dimers in P doped Si NCS
Conclusions
Synthesis and basic properties of P doped Si NCs ensembles
  Characteristics of our P doped Si NCs ensemble
  Only NCs with single donor electrons or dimers are statistically relevant
Conclusions
Probing P doping of Si NCs via low-temperature Q-band electron paramagnetic resonance (EPR) spectroscopy

## Slide 17: Donors in NCs: theoretical framework
Single donors
EPR signal: (a) and (b) – doublet with hyperfine splitting ANC
Zeeman effect
Hyperfine interaction
Absent in measured spectra! Why:
Broadening and quenching of single donor signal in conventional EPR
MAP-fis PhD Research Conference - 2012
12/16
Our P doped Si NCs show lognormal size distribution
R. N. Pereira, A. R. Stegner et al., Phys. Rev. B, 79, 161304 (R) (2009)
ANC is size dependent:

## Slide 18: Donors in NCs: theoretical framework
Donor dimers
Zeeman effect
Hyperfine interaction
Exchange
coupling
Singlet (S=0) and triplet (S=1) states separated by J
Only dimers in triplet states are EPR-active
(these states are thermally populated)
EPR signal: (a) and (b) – hyperfine doublet separated by ANC
(c) and (d) –
MAP-fis PhD Research Conference - 2012
13/16

## Slide 19: Donors in NCs: theoretical framework
Donor dimers
For J>>ANC, c and d are degenerate and centered at g=1.998
Resonance at g=1.998 should be due to transitions (c) and (d)
To confirm this assignment, we need to calculate J
MAP-fis PhD Research Conference - 2012
g=1.998
13/16

## Slide 20: Donor dimers: theoretical framework
To calculate J we use this expression
Each donor wave function is described by the hydrogenic model –> effective mass theory
Computational implementation
MAP-fis PhD Research Conference - 2012
P. R. Cullis, J. R. Marcus, Phys. Rev. B 1, 632 (1970)
N(J) spans over three orders of magnitude
    angular dependence
    donor separation dependence
Most J>105 MHz
From N(J), we will estimate IEPR(T)
14/16

## Slide 21: Donor dimers: theoretical framework
Each donor wave function is described by the hydrogenic model –> effective mass theory
Computational implementation
MAP-fis PhD Research Conference - 2012
N(J) spans over three orders of magnitude
    angular dependence
    donor separation dependence
Most J>105 MHz
From N(J), we will estimate IEPR(T)
14/16
P. R. Cullis, J. R. Marcus, Phys. Rev. B 1, 632 (1970)
To calculate J we use this expression

## Slide 22: Donor dimers: theoretical framework
Each donor wave function is described by the hydrogenic model –> effective mass theory
Computational implementation
MAP-fis PhD Research Conference - 2012
N(J) spans over three orders of magnitude
    angular dependence
    donor separation dependence
Most J>105 MHz, we confirm that J>>ANC
From N(J), we will estimate IEPR(T)
14/16
P. R. Cullis, J. R. Marcus, Phys. Rev. B 1, 632 (1970)
To calculate J we use this expression

## Slide 23: Donor dimers: theoretical framework
EPR intensity
calibration
Number of dimers in sample (fitting parameter)
MAP-fis PhD Research Conference - 2012
15/16
This model considers:
average value of exchange energy, <J>
average radius of NCs in ensemble, δd0,dNC
N(J) gives dominant contribution to this deviation
From ND we obtain [e-]≈1x1019 cm-3 and confirm that in this regime clusters with n>2 are negligible

## Slide 24: Donor dimers: theoretical framework
EPR intensity
calibration
MAP-fis PhD Research Conference - 2012
Number of dimers in sample (fitting parameter)
This model considers:
distribution of J in our NCs ensemble, N(J)
average radius of NCs in ensemble, δd0,dNC
15/16
N(J) gives dominant contribution to this deviation
From ND we obtain [e-]≈1x1019 cm-3 and confirm that in this regime clusters with n>2 are negligible

## Slide 25: Donor dimers: theoretical framework
EPR intensity
calibration
MAP-fis PhD Research Conference - 2012
Number of dimers in sample (fitting parameter)
15/16
This model considers:
distribution of J in our NCs ensemble, N(J)
lognormal size distribution of NCs, Ld0,σ(dNC)
N(J) gives dominant contribution to this deviation
From ND we obtain [e-]≈1x1019 cm-3 and confirm that in this regime clusters with n>2 are negligible

## Slide 26: Conclusions
Doping in NCs is quite different from the bulk:
  Confinement and isolation of donors
  Statistical distribution of donors in NCs
Exchange coupled donors in NCs can be probed via T-dependent EPR spectroscopy (yield line at g=1.998)
Deviation of IEPR from Curie behavior due depopulation of triplet state of dimers at low T
Exchange coupling of donors dimers in NCs is well described by effective mass theory
Distribution of J in NCs ensembles gives major contribution to the variation of the IEPR
MAP-fis PhD Research Conference - 2012
Only few-dopant exchange coupling is statistically relevant
16/16
For further details, see R. N. Pereira, A. J. Almeida, A. R. Stegner, M. S. Brandt, H. Wiggers. Exchange coupled donor dimers in nanocrystal quantum dots. Phys. Rev. Lett. (2012) in press.

## Slide 27: Thank you for your attention!
MAP-fis PhD Research Conference – January 2012, Braga

## Slide 28: g=1.998 line asymmetry at T=15 K
Nfrozen
Nsplitting
For T = 15K:
Percentage of donor dimers yielding sizable splitting (ΔB(c),(d)>0.1 mT):
For T = 230K:
MAP-fis PhD Research Conference - 2012
sizable splitting is expected for lower J
at lower T, more dimers with large J are frozen in singlet state and so contribution of dimers inducing splitting is greater
Nfrozen – dimers in the singlet state (EPR inactive)
Nsplitting – dimers yielding ΔB(c),(d)>0.1 mT
Nactive= Ntotal – Nfrozen

## Slide 29
Nfrozen – dimers in the singlet state (EPR inactive)
Nsplitting
Nsplitting – dimers yielding ΔB(c),(d)>0.1 mT
Nactive= Ntotal – Nfrozen
For T = 15K:
For T = 230K:
sizable splitting is expected for lower J
at lower T, more dimers with large J are frozen in singlet state and so contribution of dimers with lower J is greater
MAP-fis PhD Research Conference - 2012
Nfrozen
g=1.998 line asymmetry at T=230 K
Percentage of donor dimers yielding sizable splitting (ΔB(c),(d)>0.1 mT):

## Slide 30: Angular dependence of J
4
8
12
(x103)
16
0
[1 1 1] is the most common dimer orientation
For each orientation, J depends on the distance between donors
θ
θ
θ
J1
<
J2
<
J3
Number of dimers
MAP-fis PhD Research Conference - 2012