## Slide 1: Emission Mössbauer spectroscopy of advanced materials for opto- and nano-electronics
Spokepersons: Haraldur Páll Gunnlaugsson Sveinn Ólafsson
Contact person: Karl Johnston
Addendum of the IS501 experiment
Outline
The IS501 experiment
Mössbauer spectroscopy
Paramagnetic relaxation in compound semiconductors
Vacancy diffusion in group IV semiconductors
Experimental plan and beam request

## Slide 2: IS 501 experiment INTC-P-275
Paramagnetic relaxation in compound semiconductors
Vacancy diffusion in group IV semiconductors
Doping of Si-nano-particles
Investigation of phase change mechanisms in chalcogenides.
57Mn, 57Co, 119In, 119mSn, 119Sb
Calibration
Proposal
Opportunistic/contingency
Requested 22 shifts
Awarded 15 + 3 IS443
shifts = 18 shifts
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 3: Mössbauer spectroscopy + ISOLDE
Dilution (< 10-4 at.%) not possible with conventional MS (>10-1 at.%), interactions set in at 10-2 at.%
Site selective doping with different parents:
Make use of ”special” properties - Recoil to create interstitials (57Mn, 119In) - Observe meta-stable electronic states (57Co)
57Co (271 d)
119mSn (290 d)
119Sb (38 h)
119Sn
119In (2.1 m)
57Fe
57Mn (1.5 m)
PAC
Use in home
laboratories
Off-line at
ISOLDE
Recoil
 interstitials
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 4: Mössbauer spectroscopy
Valence(/spin) state of probe atom (Fen+, Snn+)
Symmetry of lattice site (Vzz)
Diffusion of probe atoms (few jumps ~100 ns)
Debye-Waller factors
Magnetic interactions
Paramagnetic relaxation of Fe3+
Paramagnetic relaxation rates (~107-108 Hz)
Can usually detect and distinguish up to 5-6 spectral components (substitutional, interstitial, damage, vacancy-defects,…)
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 5: Paramagnetic relaxation in compound semiconductors
Method to distinguish between slow paramagn. relaxation and defect(-induced) ferromagnetism
  Applied to ZnO, MgO, a-Al2O3, SrTiO3, TiO2,…
Methods to determine spin-lattice relaxation rates
  Applied to ZnO, MgO, a-Al2O3, SrTiO3, TiO2,…
Absence of major defect magnetism verified by using implantation of 119In→119Sn
  ”Strange” (and interesting) results
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 6: Paramagnetic relaxation in compound semiconductors
”Abnormal” behaviour observed for spin-lattice relaxation of Fe3+ in ZnO
Experimental (Mølholt et al., 2012)
Theory
 T2
 T9
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 7: Paramagnetic relaxation in compound semiconductors
Lattice location of 119In →119Sn in oxide semiconductors
In ZnO (MgO, a-Al2O3), Sn4+ is found to be stable and hence it is not Sn2+ replacing the metal ion
Possibly due to a charge compensating defect as Sn is too big to enter ”normal” lattice site
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 8: Paramagnetic relaxation in compound semiconductors
111In is a PAC probe, often assumed to enter regular lattice sites upon implantation and annealing
Positive results obtained on p-type doping in ZnO by co-doping of N and In
Implant the same (new) type of samples as used for 57Mn with 119In and 119mSn
  57Fe gives the annealing reactions and lattice properties,
  119mSn gives information on whether this is a chemical effect or whether annealing procedures are possible
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 9: Paramagnetic relaxation in compound semiconductors
Need Fe concentration < 10-2 at.% to avoid spin-spin relaxation (out of reach of other techniques)  ISOLDE
  Extend the list of oxides: SrO, BaO, BaTiO3, (Zn, Cd)(S, Se, Te)) – 2 57Mn shifts (5 samples)
Follow up on lattice location of In results
  119In: 1.6 shifts (complementary to 57Mn data)
  119mSn: 3 shifts
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 10: Vacancy diffusion in group IV semiconductors
Disputed nature and diffusivity of the monovacancy in silicon
Data from Watkins et al., (T < 200 K) coincides with growth data from Voronkov and Falster, suggesting Ea = 0.45 eV at all T’s
Bracht et al., found high Ea’s at elevated T’s
Current interpretation of our ISOLDE data supports low diffusivity at high T’s
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 11: Vacancy diffusion in group IV semiconductors
Current picture (T > 400 K):
MnS
MnI - V
MS + EC
data
57Mn→57Fe
ER = 40 eV
FeS
FeI
+
V
~600 K
FeI - V
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 12: Vacancy diffusion in group IV semiconductors
Unique method to monitor the mono-vacancy in silicon due to the recoil in 57Mn→57Fe
Current data suggest ”slow” vacancy
Still more data needed to support these conclusions
  EC on 57Mn: 3 shifts
  57Mn for Mössbauer spectrsoscopy: 4 shifts
  Supporting 119Sn MES: 119In (1 shift) 119mSn (0.75 shift)
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 13: Experimental plan
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request

## Slide 14: Formal beam request
1. The IS501 experiment | 2. Mössbauer spectroscopy | 3. Paramagnetic relaxation | 4. Vacancy diffusion in Si (+..) | 5. Exp. plan and beam request