## Slide 1: For the RD50 Simulation Group
Mercedes Miñano
mercedes.minano@ific.uv.es
IFIC - Valencia
Electric Field Modeling by simulations with ISE-TCAD

## Slide 2: Outline
2D Pad Sensor simulated by ISE-TCAD
  2Defects radiation model
Full Depletion Voltage
Electric Field Distribution @ 1015 cm-2
Temperature Effects
Electric Field Distribution vs. Fluence
Leakage Current
  Single level radiation model
Summary and next steps

## Slide 3: 2D Pad Detector
Radiation induced deep levels
DOPING PROFILES
[p+] = 3 x 1017 cm-3
[n-bulk] = 6 x 1011 cm-3
[n+] = 1 x 1019 cm-3
Detector thickness ---- d=0.03 cm
Simulations by Synopsys ISE-TCAD
Version D-2010.03 of a pad sensor has been carried out with the next characteristics:
Backplane
p+ implant
n bulk
As proposed from the RD50 Detector Simulation Group :
N+

## Slide 4
Electrode {
{Name="nplus" Voltage=0.0 Material="Aluminum"}
{Name="pimplant" Voltage=0.0}
}
Physics {
Temperature=@<Temperature>@
Mobility( DopingDep CarrierCarrierScattering HighFieldSaturation Enormal)
Recombination(SRH(DopingDep) SurfaceSRH)
EffectiveIntrinsicDensity(Slotboom) }
Physics (material="Silicon") {
#if @<Fluence==0>@ ## No Traps
#else
Traps (
(Acceptor Level fromValBand Conc=@<Fluence>@ EnergyMid=0.595
eXsection=1.0E-15 hXsection=1.0E-15 )
(Donor Level fromValBand Conc=@<Fluence>@ EnergyMid=0.48
eXsection=1.0E-15 hXsection=1.0E-15 )
)
#endif }
Physics(MaterialInterface="Oxide/Silicon") {
#if @<Fluence==0>@
Charge(Conc=4e11)
#else
Charge(Conc=1e12)
Recombination(surfaceSRH)
#endif }
ISE-TCAD Code used for simulations
Standard physics model for a sensor with no radiation damage
Radiation model for traps
Oxide charge
Parameters:
Bias Voltage, temperature and fluence

## Slide 5
Full Depletion Voltage
T=290K
The n-type bulk is inverted to p-type with irradiation at 1013 cm-2
Fluence [cm-2] | Vfd [V]
0 | 48
1e12 | 41
1e13 | 7
1e14 | 285
3e14 | 955
1e15 | 3245
3e15 | 10086

## Slide 6
Electric Field Distribution @ 1015 cm-2
Inverted sensor
NP bulk
The electric field grows from the sensor backplane
T=260K
T=290K

## Slide 7: T=290K φ = 1 x 1015 cm-2
Electric Field Distribution through sensor depth
The peak at front contact does not depend on bias voltage
Backplane
Front plane (p+)

## Slide 8: T=260K φ = 1 x 1015 cm-2
Electric Field Distribution through sensor depth
Backplane
Front plane (p+)

## Slide 9
@500V and irradiated at 1015 cm-2
Temperature Effects
The peak at p+ contact decreases as temperature increases, whereas a double junction effect is more evident.
P+
N+
backplane
P+

## Slide 10: T=290K Bias=300V
Electric Field Distribution
As intrinsic silicon
Higher with dose after SCSI

## Slide 11: Leakage Current
Bulk generated current calculated from a single level model:
T [K] | α [x10-17 A/cm]
290 | 4
260 | 0.2
V = 100 μm2 x 300μm
Moll’s Thesis 
Current related damage rate

## Slide 12: Summary
Following the Vladimir’s proposals, simulations with ISE-TCAD have been carried out in order to perform a cross-test of the software.
The results are focused in Electric Field distribution in irradiated sensors (2 midgap level model) and some conclusions can be extracted:
  After bulk inversion an asymmetric double peak is seen at both sides of the sensor.
  The peak at p+ contact seems to depend on:
    Temperature
    Irradiation dose
Full depletion voltage and leakage current (single level model) characteristics are also presented.

## Slide 13: Next Steps
Charge collection efficiency
Implementation of avalanche effect
Trap configuration
Geometrical dependence
…
…
Any suggestion is wellcome

## Slide 14: Back Up

## Slide 15: Physics Models
Poisson Equation
Transport Equations
Shockley-Read-Hall Model

## Slide 17: Electric Field 500V – 1015 cm-2

## Slide 18: Leakage Current
T=260K
T=290K