## Slide 1
Operational conditions
for enhancement of collected charge
via avalanche multiplication
in n-on-p Si strip detectors
E. Verbitskaya, V. Eremin, A. Zabrodskii, B. Ermolaev
Ioffe Physical-Technical Institute of Russian Academy of Sciences
St. Petersburg, Russia
20 RD50 Workshop
Bari, May 30 - June 1, 2012

## Slide 2
Outline
♦ Goal
♦ Background
♦ E(x) and Qc(V) vs. T dependences
♦ E(x) and Qc vs. V and F dependences
♦ Influence of detector geometry
♦ Comparison with experimental results
♦ Considerations on defect energy levels
♦ Impact of avalanche multiplication on S/N
Conclusions
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 3
 Simulation of Qc enhancement:
extension of quantitative PTI model
 Finding the conditions for observation of enhanced collected charge in n-on-p Si strip detectors
 Comparison with experimental data
Goal
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 4
Recent results on collected charge enhancement: main references
1. I. Mandić, V. Cindro, G. Kramberger, M. Mikuž, NIM A 603 (2009) 263
2. I. Mandić, A. Gorišek, G. Kramberger, M. Zavrtanik, NIM A 612 (2010) 474
3. A. Affolder, P. P. Allport, G. Casse, Nucl. Instrum. Meth. A 612 (2010) 470
4. G. Casse, NIM A 612 (2010) 464
5. G. Casse, et al., NIM A 624 (2010) 401
6. M. Mikuž, V. Cindro, G. Kramberger, I. Mandić, M. Zavrtanik, NIM A 636
(2011) 550
7. G. Casse, A. Affolder, P. P. Allport, H. Brown, I. McLeod, M. Wormald,
NIM A 636 (2011) 556
8. I. Mandić, V. Cindro, G. Kramberger, M. Mikuž, NIM A 629 (2011) 101.
9. A. Dierlamm, NIM A 624 (2010) 395
10. J. Lange, et al., NIM A 622 (2010) 49 (epi-Si)
11. A. Affolder, et al., NIM A 658 (2011) 11 (3D)
12. I. Mandić, et al., JINST (2011) doi:10.1088/1748-0221/6/11/P11008
13. V. Eremin, E. Verbitskaya, A. Zabrodskii, Z. Li, J. Härkönen, NIM A 658 (2011) 145
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 5
G. Casse, et al., NIM A 636 (2011) 556.
♦ N-on-p microstrip detectors processed by Micron
♦ Neutron irradiation
I. Mandić, et al., NIM A 612 (2010) 474.
Experimental results
-20C (and -40C for 1x1016 cm-2)
-25C
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 6
Simulation of Qc enhancement
www.cern.ch/rd50:
V. Eremin, E. Verbitskaya, Z. Li, J. Härkönen, 14 RD50 workshop, June 3-5, 2009, Freiburg
V. Eremin, E. Verbitskaya, A. Zabrodskii, 15 RD50 workshop, Nov 16-18, 2009, Geneva, CERN
V. Eremin, E. Verbitskaya, A. Zabrodskii, Z. Li, J. Härkönen, NIM A 658 (2011) 145.
The PTI model considers:
competition of Qc reduction due to carrier trapping to radiation induced deep level (DL) defects and charge increase arisen from avalanche multiplication;
 formation of Double Peak electric field profile E(x);
 focusing of the electric field and current near the collecting strips;
 avalanche hole generation near the strips, the hole injection into the detector bulk, and the hole trapping to radiation induced deep levels defects
 gives rise to the negative feedback, which stabilizes the avalanche multiplication
and total detector performance
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
Most probable – carrier avalanche multiplication in high E of n+-p junction

## Slide 7
PTI model of Qc enhancement
via avalanche multiplication
Processes considered:
formation of a steady-state E(x) distribution by considering the generation of equilibrium carriers (bulk generation current), avalanche generated carriers near the n+ strips, and carrier trapping by the radiation induced DLs;
 charge collection in the detector bulk with a calculated E(x) profile
Procedure and main parameters
♦ Poisson equation combined with the rate equation
♦ one-dimensional approach for detector geometry
♦ Deep levels: DA Ec – 0.53 eV; DD Ev + 0.48 eV
♦ 1/te,h = be,hFeq; be = 3.2x10-16 cm2s-1, bh = 3.5x10-16 cm2s-1 [2]
♦ A and B from B. J. Baliga, Modern Power Devices, Hoboken, NJ; Wiley, 1987
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
Extension in this study: variable parameters
♦ detector bias voltage V,
♦ temperature T in the LHC range,
♦ irradiation fluence F,
♦ strip detector geometry (strip width,
detector thickness)
Starting point – fit to the curve with maximal Qc [2]: F = 3x1015 neq/cm2,
T = -20C
 gives KDA = 2, KDD = 0.07

## Slide 8
E(x) and Qc vs. T dependences
n-on-p strip detector; d = 300 mm; pitch/strip width 80/20 (mm) F = 3x1015 neq/cm2
No avalanche multiplication
Avalanche multiplication is considered
x = 0 at p+ contact
E at n+
is stable
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
E(x) vs. T – changes of DL occupancy due to tdetr  as T

## Slide 9
E(x) and Qc(V) dependences at different F
T = 253K
Avalanche multiplication
500 V
1000 V
1800 V
Qc
Qc rise correlates
with appearance
of DP E(x)
Minimum V – 500 V
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 10
Dependence of Qc(F) on V
T = 253K
♦ competition of carrier trapping
and avalanche multiplication
 non-monotonic behavior with a bump;
♦ at F ~ 1015 cm-2 and 1800 V
Qc is close to 25 ke-;
♦ at V≥1500 V Qc_max is above 24 ke-;
♦ maximum Qc of 34 ke- at F  2x1015 cm-2
and 1800 V
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 11
Influence of detector geometry
1. Strip width → 20, 10, 6 mm
Focusing of the electric field and current – special parameters vs. strip width
E (x) vs. strip width
Qc(F) vs. strip width
♦ Rise of the maximum Qc due to focusing with strip width reduction
 the scale of the effect is rather small;
♦ Main effect - shift of Qc enhancement towards lower F
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 12
Influence of detector geometry
2. Different detector thickness → 300, 100 mm
300 mm
100 mm
1000 V, 253K
1000 V
1000 V
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
In thin detector
DP E(x) and Qc_max are shifted to higher F
DP
uniform

## Slide 13
Influence of detector thickness on CCE
1000 V, 253K
♦ Low electric field base region damps avalanche effect in 300 mm detector
♦ Reduction of the wafer thickness increases the collected charge more effectively than the electric field focusing at the strip with a smaller width
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 14
Analysis of experimental data
In legend:
1 - [2]; 1.6x1015 cm-2; -40C
2 - [1]; 3x1015 cm-2; -20C
3 - [2]; 1x1016 cm-2; -40C
4 - [7]; 1x1015 cm-2; -25C
5 - [7]; 3x1015 cm-2; -25C
6 - [7]; 1.5x1016 cm-2; -25C
Neutron irradiation
 Nice agreement at 3x1015 cm-2
 Qc enhancement is larger at lower T (as in the model)
 Agreement between experiment and simulation
 Dominant contribution of multiplied holes to Qc
F = 3x1015 n/cm2
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 15
Very abnormal Qc enhancement
Experiment
PTI model
300 mm
100 mm
protons 26 MeV
140 mm; -25°C:
Qc-max = 20 ke
Kenh = 1.75 [5]
300 mm:
Qc-max= 40 ke
Kenh = 1.7 [8]
300 mm:
Qc-max= 35 ke
Kenh = 1.45
100 mm:
Qc-max= 15 ke
Kenh = 1.9
-20°C
Kenh = Qc-max/Qmip
-20°C
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
3D detectors:
Qc-max = 42 ke
Kenh  2
V = 200 V [11]

## Slide 16
Consideration on trapping centers
PTI model: DD Ev + 0.48 eV; DA Ec – 0.53 eV
M. Bruzzi, IEEE Trans. NS-48 (2001) 960-971
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
TCT:
Ec – 0.52 eV – electron trap
Ev + 0.51 eV – hole trap
E. Fretwurst, V. Eremin, et al., NIM A 388 (1997) 356;
Z.Li, C.J.Li, V.Eremin, E.Verbitskaya, NIM A 388 (1997) 297
TSC:
Ev + 0.48 eV (0.46) – hole trap
U. Biggeri, E. Borchi, et al., NIM A 409 (1998) 176;
M. Moll, Ph.D. dissertation, Univ. of Hamburg, Hamburg, Germany, 1999

## Slide 17
Alternative traps
D. Pennicard, et al., NIM A 592 (2008) 16
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
Perugia traps
Agreement with experiment are
obtained with midgap levels only

## Slide 18
Signal to noise ratio
Achieving of good performance  S/N should be above 8
N  1000 ENC - strip detectors 320 mm thickness, 6 cm length and 75 mm pitch irradiated to (1-5)x1015 neqcm-2 and connected to SCT128A readout ASIC [8]
S/N  8 can be realized
at F = (1-5)x1015 neqcm-2 - in avalanche mode at V≥1500 V since Qc > 11 ke-
F  1x1016 neqcm-2 - the S/N ratio may go down
Conversely, with shorter strips and better electronics, an adequate S/N should be achievable at lower voltage
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 19
Conclusions
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
In avalanche multiplication mode:
Qc enhancement occurs when E(x) distribution transforms to a DP profile and results in self-stabilization of the electric field at the n+ strip at 300 kV/cm regardless of T and F
 Minimal bias voltage at which Qc rise starts is 500 V (at F = 3x1015 cm-2)
 Maximal Qc is above the charge collected in nonirradiated detector!
PTI model gives an adequate description of the experimental results
Main results were presented at PSD9, Sept 2011
and are published: E.Verbitskaya, V. Eremin, A. Zabrodskii, 2012, J. Instrum., v.7, 2 ArtNo: #C02061

## Slide 20
Acknowledgments
This work was made in the framework of RD50 collaboration
and supported in part by:
Fundamental Program of Russian Academy of Sciences
on collaboration with CERN,
RF President Grant # SS-3008.2012.2
Thank you for attention!
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012