## Slide 1: Progress on investigation of dynamic vacuum (RF structures only)
Sergio Calatroni
With Cedric Garion, Irene Martini, Chiara Pasquino, Pedro Costa Pinto, Mauro Taborelli

## Slide 2: Requirements from beam dynamics
The vacuum threshold for preventing fast ion beam instability (essentially due to direct field ionization and not the usual impact ionization) :
  Main beam linac requirements :
  total p  few 10-9 Torr each for CO, N2 and/or H2O.
  H2 is not harmful (p  few10-8)
True for practically all the main LINAC length, also inside the RF accelerating structures
For details see:
  G. Rumolo, A Oeftiger http://cdsweb.cern.ch/record/1406050?ln=en
  C. Garion https://edms.cern.ch/document/1095288/1

## Slide 3: The problem
Static vacuum: not discussed here
Dynamic vacuum
  Breakdowns
  Dark current

## Slide 4: Dynamic vacuum – Breakdown I
2.1012 H2 or CO molecules released during breakdown (in a baked system)
Data measured in DC “spark test” reported in PRST-AB12, 092001 (2009)
FE code model
Pumping surfaces

## Slide 5: Dynamic vacuum – Breakdown II
Calculated with thermal analogy model (and Monte-Carlo model)
Four manifolds
Longitudinal pressure distribution in the cells:
Uniform after ~3 ms
Calculated with Monte-Carlo and thermal analogy model
Maximum pressure vs time:
20 ms to reach 10-9 mbar for H2
20 ms to reach 5x10-8 mbar for CO
(Note: CLIC repetition rate = 50 Hz
Duty cycle = 20 msec)
Chart: H2
MC | 3.4167e-05 | 2.3082e-05 | 7.3235e-06 | 3.9198e-06 | 2.9749e-07 | 1.3999e-07 | 1.4874e-07 | 7.8747e-08 | 5.2498e-08 | 4.3748e-08
Monte-Carlo

## Slide 6: Dynamic vacuum - Dark currents
Dark-current electrons are field-emitted, impact on surfaces and desorb gas
Dynamic vacuum by ESD: desorbed molecules fill the whole cell volume
No pumping
e- current ~ 10-4-3 A during pulse
Need e- distribution and energy + ESD coefficients at high energy
e- on faraday cup
How are e- distributed inside the cell? Structure?
e- on faraday cup

## Slide 7: ESD data
Work of C. Pasquino & I. Martini for master thesis:
New ESD measurement system at high-voltage.
Several surface treatments being studied
Notes: Dose per pulse few 10E8. Ten days for 1E16, 100 Days for 1E17

## Slide 8: Dynamic vacuum I – Results
Pressure goes to < 10-9 mbar in less than 1 msec !
This is faster than the sampling time of common vacuum gauges...
Same plot as for dynamic vacuum due to breakdowns (2x1012 molecules released)
Extrapolating to 1000 less molecules released due to ESD
Chart: H2
MC | 3.4167e-05 | 2.3082e-05 | 7.3235e-06 | 3.9198e-06 | 2.9749e-07 | 1.3999e-07 | 1.4874e-07 | 7.8747e-08 | 5.2498e-08 | 4.3748e-08
Molecules released per pulse ~ few 107 both for H2 and CO, resulting in pressure bursts of few 10-8 mbar locally

## Slide 9: Outlook 1
Static vacuum achieved but only marginally with present design
  Need more precise data on water re-adsorption (sticking probability depends on coverage)
Dynamic vacuum due to breakdowns seem to be under control (recovery time ≤ pulse repetition)
  However, data from RF tests are needed for further cross-checking

## Slide 10: Outlook 2
Dynamic vacuum due to dark currents: still open question
Experimental programme:
  ESD data on unbaked copper at high e- energy from CERN 
  Dark current simulations from SLAC – ACE3P
  Introduce these into MC+FEM models and get gas distribution
  Direct measurements should be attempted in 12 GHz test bench
    Feasibility should be demonstrated
    Collaborations ?

## Slide 12: Molecule speed
 | Atomic mass | Molecule speed @ 300 K [m/s] | Molecule displacement in RF pulse [mm]
H2 | 2 | 1579 | 3.16E-01
H2O | 18 | 526 | 1.05E-01
CO | 28 | 422 | 8.44E-02
CO2 | 44 | 336 | 6.73E-02
Assuming a molecular speed of 300 K = 0.026 eV

## Slide 13: Data
Total e- current [A] | Pulse duration [ns] | Total charge [C] | Number of electrons | Solid angle (one cell, one side) | Total electrons on copper | Dose per pulse (e- /cm2)
1.00E-04 | 200 | 2.00E-11 | 1.25E+08 | 0.027439024 | 4.56E+09 | 4.42E+08
ESD coefficient for H2 (unbaked copper) | Total H2 molecules per RF pulse | Equivalent pressure at RT (total volume) |  |  |  | 
2.00E-01 | 9.11E+08 | 1.12E-08 |  |  |  | 
ESD coefficient for CO2 (unbaked copper) | Total CO2 molecules per RF pulse |  |  |  |  | 
6.00E-02 | 2.73E+08 | 3.37E-09 |  |  |  | 
ESD coefficient for H2 (copper baked 250 C) | Total H2 molecules per RF pulse |  |  |  |  | 
1.30E-02 | 5.92E+07 | 7.29E-10 |  |  |  | 
ESD coefficient for CO2 (copper baked 250 C) | Total CO2 molecules per RF pulse |  |  |  |  | 
6.00E-03 | 2.73E+07 | 3.37E-10 |  |  |  | 
ESD coefficient for H2 (copper baked 300 C) | Total H2 molecules per RF pulse |  |  |  |  | 
3.00E-03 | 1.37E+07 | 1.68E-10 |  |  |  | 
ESD coefficient for CO2 (copper baked 300 C) | Total CO2 molecules per RF pulse |  |  |  |  | 
1.60E-03 | 7.29E+06 | 8.98E-11 |  |  |  | 
107 pulses to start conditioning
(~2 days at 50 Hz)
109 pulses for 10 ESD reduction
(200 days at 50 Hz)
10 times maximum allowed
3 times maximum allowed
For the dynamic vacuum of breakdowns we were considering 2x1012 molecules.
G. Vorlaufer CERN-Thesis (2002)
Benvenuti et al LEP2 94-21
MathewsonJVSTA 15 (1997) 3093