## Slide 1
Zr-V NEG coatings studied by ESD

## Slide 2: Overview
Introduction
  NEG coatings
  Aim of project
  Characterization methods
Coating process
Scanning Electron Microscopy / X-ray Photoelectron Spectroscopy results
Calibrated leaks method
Electron stimulated desorption
Results: Sticking factor and ΔP
Conclusion – Future work

## Slide 3: Introduction
NEG coatings are already used in LHC (6 km long section parts)
Important to continue the research and development of the NEG coatings
NEG coatings will be used to the new
Extra Low Energy Antiproton Ring (ELENA)

## Slide 4: Introduction
Aim:
To study the effect of excluding Ti from the coating, on the sticking probability and the surface cleanliness
To evaluate the optimum ZrV composition in terms of sticking probability and the surface cleanliness
30%,30%,40%
In this study were used/made:
10 different cathodes
: R>0.5
: R<0.5
(after 200oC for 1hr)
Quality composition map of TiZrV films by AES

## Slide 5: Introduction
Characterization methods:
Electron Stimulated Desorption (ESD)
Sticking Factor Evaluation using the
calibrated leaks (H2 & CO)
X-ray Photoelectron Spectroscopy (XPS)
  Activation temperature evaluation
Scanning Electron Microscopy (SEM)
  Morphology
  Thickness
  Composition
Cathodes
Special thanks to the team of M.Taborelli and S. Sgobba for the XPS and SEM analysis of the samples

## Slide 6: Coating Process
e-
B
Kr
E
Parameters
Est. Thickness: 1μm
Substrate: SS tube
Tsubstrate: 100 oC
Pressure range:
4x10-3 to 9x10-3 mbar
Average coating
duration: 9 hours
Magnetic field:
225 Gauss

## Slide 7: Results: SEM (EDX)
30%,30%,40%

## Slide 8: Thickness-Morphology-XPS Results
The estimated thickness for all the coatings was 1μm.
The average measured thickness was between 0.6μm and 2 μm.
The XPS analysis of the samples is confirming the results from the ESD and sticking factor measurements.

## Slide 9: Calibrated leaks method
Calibrated leaks(H2&CO)
At 120oC (no Pumping)
Seff = Q / ΔP(120oC)
R = ΔP(120oC) / ΔP(xoC)
ΔP(120oC) = P120(inj)-P120(res)
ΔP(xoC) = Px(inj)-Px(res)
R
Sticking factor
Q=2,31E-7 Torr·l/s
Q=3.192E-6 Torr·l/s
H2
CO
Monte Carlo simulation

## Slide 10: Electron Stimulated Desorption
Tungsten filament
-100V
+50V
+550V
e -
ΔP = P(100sec) - P(res)
Bombardment of the tube for 100 sec at 1mA

## Slide 11: Results from each coating
ΔP (Torr)
Heating Temperature [oC] (for 2 hours)
Sticking probability
Heating Temperature [oC] (for 2 hours)
H2
CO
S.F by calibrated leaks
ΔP by ESD

## Slide 12: Results: Sticking Factor for H2
Sticking probability
Heating for 2 Hr at 200 oC
% Vanadium
Zr
V
TiZrV
Ti(5%)ZrV

## Slide 13: Results: Sticking Factor for CO
Sticking probability
% Vanadium
Zr
V
Heating for 2 Hr at 200 oC
Ti(5%)ZrV
TiZrV

## Slide 14: Results: ΔP for H2
ΔP (Torr)
Effective Desorption Yield
[molecules/electron]
% Vanadium
Zr
V
Heating for 2 Hr at 200 oC
Ti(5%)ZrV
TiZrV

## Slide 15: Results: ΔP for CH4
ΔP (Torr)
Effective Desorption Yield
[molecules/electron]
% Vanadium
Zr
V
Heating for 2 Hr at 200 oC
Ti(5%)ZrV
TiZrV

## Slide 16: Results: ΔP for CO
Effective Desorption Yield
[molecules/electron]
ΔP (Torr)
% Vanadium
Zr
V
Heating for 2 Hr at 200 oC
Ti(5%)ZrV
TiZrV

## Slide 17: Results: Δp Total
ΔP (Torr)
% Vanadium
Zr
V
Heating for 2 Hr at 200 oC
Ti(5%)ZrV
TiZrV

## Slide 18: Conclusions - Future work
To introduce new materials (Hf, Y) for NEG coatings
To make more functional measurements (pumping speed, ageing, etc) for the best ZrV composition (30-40%V)
TiZrV may not be the best composition
Necessary to continue the R&D for NEGs

## Slide 19
Thank you for
your attention!
Thanks:
to the people working in the lab for their help