## Slide 1: Electropolishing of Niobium cavities SPL R&D work frame

## Slide 2: Outline
SPL R&D work frame
Electropolishing
Main parameters
Polishing Plant
Cathode design
Feedback

## Slide 3: SPL R&D work frame
SPL (Superconducting Proton Linac)
“Conceptual design of the SPL II: A high-power superconducting H- linac at CERN” Baylac et al.
Eacc↑ -> Surface treatment needed
Most promising technique: Electropolishing
Roughness < 0,1 μm
Eacc up to 45 MV/m
First SPL Collaboration Meeting 11-12 December, 2008 – CERN, R. Garoby
Nb SRF cavities
β-1 (25 MV/m)
β-0.65

## Slide 4: Electropolishing
H2SO4 (96% m/m): 90 % v/v
HF (40% m/m): 10 % v/v
DC Power supply
Cathode (Cu)
Anode
(Nb)
A
V
+
-

## Slide 5: Electropolishing
DC Power supply
Cathode (Cu)
Anode
(Nb)
A
V
1 µm

## Slide 6: Electropolishing
HF reacts with Niobium oxide under anodic potential and forms soluble products
Thin viscous layer rapidly forms at the anode surface transforming a charge controlled into a mass control process. Under these conditions, the removal rate of metal is higher on “peaks” and lower on “valleys”.
The imposed anodic potential allows the water molecule to break into Hydrogen and Oxygen and enhances the diffusion of Oxygen to form Niobium Oxide.
Cathodic reaction: 2 H+(aq) + 2 e- → H2(g)
Anodic reaction: 2 Nb(s) + 5 H2O(l) → Nb2O5(s) + 10 H+(aq) + 10 e-
Nb2O5 + 14 HF → 2 H6NbO2F7 + H2O
Nb2O5 + 12 HF → 2 HNbF6 + 5 H2O
Nb2O5 + 10 HF → 2 H2NbOF5 + 3 H2O
Nb2O5 + 10 HF → 2 NbF5 + 5 H2O

## Slide 7: Main Parameters
Chart: Overpotential (V)
Cathode
R
R
Primary current distribution
Secondary current distribution
J = f(η(Overpotential))
J = f( T, Qv, Sc/Sa, [F-], [H2O])
Quite straightforward?
~ 400 mm diameter
~ 1400 mm in length
Current density (A/m2)
Overpotential (V)
Temperature
Bath flow rate
Sc/Sa
[HF]
[H2O]
Notes: Different parameters to take into account
Not so simple if the geometry is complex:
shape, internal surface, agitation, cooling, power input...

## Slide 8: The Polishing Plant
Horizontal
+ flexible in terms of working parameters
+ complex setup (axial rotary motion)
Electrical contact
Rotary sealed Interfaces
Pivot motion
+ Surface needed
Axial motion
“On/Off” EP
+ EP time (same parameters)
Proven setup
SRF WP 5.1.1.4 : “Electropolishing of Niobium : best EP Parameters” F. Eozénou , A. Aspart, C. Antoine, B. Malki
or
Vertical
Notes: Main design parameter for the setup.
Define an installation for high performance but simple.
Installations performing well at DESY and KEK

## Slide 9: The Polishing Plant
- Flexible in terms of working parameters
- complex setup ( without axial rotary motion)
No pivot motion
- Surface needed
Continuous EP
Cathode geometry and working parameters must be well defined
- EP time (same parameters)
Horizontal
Vertical
+ flexible in terms of working parameters
+ complex setup (axial rotary motion)
Electrical contact
Rotary sealed Interfaces
Pivot motion
+ Surface needed
Axial motion
“On/Off” EP
+ EP time (same parameters)
Proven setup
Notes: Vertical because:
Let’s make it simpler and better
Approach for an industrial setup: cheaper and easy to operate
Fermilab already did it
Saclay has one vertical setup as well

## Slide 10: The Polishing Plant
Where:
Chemicals compatible building/room;
Services:
  Air extraction;
  Air washers;
  Waste water recovery/processing;
  Chemicals storage facility;
  Demineralised water;
  Compressed air;
  Power connections.
- and enough space available;
B.102
B.118
B.254

## Slide 11: The Polishing Plant
Where:
Here!

## Slide 12: The Polishing Plant
Where:
Make space: Removal and disposal of unused Nb BCP plant

## Slide 13: The Polishing Plant
Equipment:
Materials
Cavity geometrie
Working parameters
PVDF
PFA
FPM
Surface
Volume
Procedure
Type of bath
Processing time
Power input
Flow
Air Washers
Retention
Confined working space
PTFE

## Slide 14: The Polishing Plant
Equipment:
Materials
Cavity geometrie
Working parameters
PVDF
PFA
FPM
Surface
Volume
Procedure
Type of bath
Processing time
Power input
Flow
Storage tank
Heat exchanger
Cathode
Pumps
PTFE

## Slide 15: The Polishing Plant
Paper work:
Budget:
~ 260 kCHF (Material)
Purchasing procedures (DO, specifications,...)
Safety file:
https://edms.cern.ch/document/1178723/1
Safety:
Exposition monitoring:
Manpower: ...
https://edms.cern.ch/document/1240840/1

## Slide 16: Cathode Geometry
Cathode geometry optimisation:
Geometry constraints
80 mm diameter
129 mm diameter

## Slide 17: Cathode Geometry
Cathode geometry optimisation:
Even current density distribution on the cavity surface
9 November, 2012
TE-VSC
17
Anodic current distribution within 1% difference

## Slide 18: Cathode Geometry
Cathode geometry optimisation:
Minimum power input
R
R
Cathode
Distance between cathode and anode
Ratio Scathode / Sanode
Chart: Overpotential (V)
Minimum potential for even current density distribution

## Slide 19: Cathode Geometry
Cathode geometry optimisation:
Bath flow dynamics
TE-VSC
19
Chart: Cavity Length (mm)
v = 0.8 * V_mean
Maximum Flow Rate:
20lpm
Minimum Flow Rate: 1lpm

## Slide 20: Feedback
Data from operation:
20
Assembly | Cavity | Qv/ l.min-1 | T/°C | E/V | I / A | Duration/h
1 | ASH b0.65 | 8 | 11 | 16 | 26 | 1.5
2 | ASH b0.65 | 21 | 10 | 16 | 28 | 1.5
3 | ASH b0.65 | 21 | 11 | 16 | 29 | 0.3
4 | SPL m b1 | 20 | 12 | 12 | 37 | 7
5 | SPL m b1 | 20 | 10 | 12 | 33 | 7.2
6 | SPL m b1 | 15 | 12 | 12 | 37 | 5
 |  |  |  |  |  | 22.5 hours

## Slide 21: Feedback
First Results:
ASH Nb cavity beta 0.65
BCP polished (before EP)
After < 20 microns EP
25 MV/m @ Q0= 1E+10
Processing equipement is performing well:
HPWR & EP
1st time EP on beta < 1 sucessfully electropolished
21
To be confirmed

## Slide 22: Feedback
First Results:
SPL mono cell beta 1
As received
After < 100 microns EP
13 MV/m @ Q0= 8 E+09
22

## Slide 23: Thank You Questions?

## Slide 24: Theory
A | Cross Sectional Area (cm2) | n | Number of Electrons Transferred (-)
Co | Concentration (mol/cm3) | vr | r component of velocity (cm/s)
Do | Diffusion Coefficient (cm/s) | vy | y component of velocity (cm/s)
F | Faraday Constant (C/mol) | yh | Boundary layer thickness (cm)
il,c | Levich Current (A) | ν | Kinematic Viscosity (cm2/s)
j | Current Density (A/m2) | ω | Angular Velocity (s-1)
Chart: ω½
| 10 | 31.622776601683793 | 44.721359549995796 | 0
 | 214.9581 | 487.3185 | 756.3127 | 0
Notes: Identified laboratory paramaters  characterised  actual cavity 