## Slide 1: WP6.4 - Status of energy deposition studies.
Effect of isotopic composition of B in MgB2
F.Broggi (INFN)
2nd Joint HiLumi LHC-LARP Annual Meeting
Frascati 14-16 November 2012

## Slide 2: Outline
Cold Powering via Superconducting Links
Possible Material Solutions
Progress since last meeting (June/July 2011)
Expected particle fluences (neutrons) from LHC 7+7 TeV p-p collision
Nuclear reactions and effects of neutrons on MgB2. Is it worth considering the isotopic separation on B for MgB2 ?
Conclusion and future perspectives

## Slide 3: Cold Powering via Superconducting Links
P7L
P7R
Betatron cleaning Insertion
Advantages of remote powering:
Safer long-term operation of powering
equipment (power converters, current leads
and associate auxiliary devices) located in a
radiation-free environment;
Safer access of personnel to equipment for maintenance, repair, diagnostic and routine tests interventions;
Reduced time of interventions on power converters, current leads and DFBs if the powering equipment is located outside of the tunnel areas – gain in machine availability ;
- Free space in the beam areas which becomes available for other equipment.
Courtesy of Amalia Ballarino

## Slide 4: Possible Material Solutions
Superconducting lines are mandatory because of the length
HTC Superconductors (Experience on the LHC current leads)
MgB2, BSCO, YBCO …

## Slide 5: What do we know about HTC SC
Cryogenic and magnetic characteristics are well established (CERN experience in LHC Current leads)
Radiation effects ????
Some MgB2 and YBCO irradiation data
But, in general, there is a lack in data on HTS (R.Flukiger Wamsdo 2011)

## Slide 6
Magnets: Nb3Sn
Bi-2212 (strong progress needed)
Current leads (Link): (NbTi): Tc too low, small T reserve
MgB2 : Top = 10 K (under investigation)
R.E.BCuO: Top = 77K (under investigation)
The critical current density of the superconducting wire or tape
as a function of fluence and energy:
neutrons most known data ≤ 14 MeV
protons few data on Nb3Sn ≤ 2 MeV
pions unknown
electrons superconductor: small effects expected*)
photons superconductor: small effects expected*)
*) OK for ≤ 2 MeV. Unknown for 100 MeV
From R. Flukiger WAMSDO 2011 addressing

## Slide 7: Today status
• Create the material library (MgB2, BSCCO, YBCCO etc) with the correct isotopic composition etc. etc…… IN PROGRESS
• Create the FLUKA geometry for the SC links (waiting for input from CERN)
A tentative layout is necessary
• Academic exercise of evaluating a n beam effect on MgB2 with 10B, 11B and natB IN PROGRESS (B10 data already presented at the June meeting see next slides)
Yesterday status
As presented at HiLumi LHC Extended Steering Committee CERN 23rd July 2012

## Slide 8: Today status
• Create the material library (MgB2, BSCCO, YBCCO etc) with the correct isotopic composition etc. etc…… STILL IN PROGRESS
• Create the FLUKA geometry for the SC links (Received input from CERN : IN PROGRESS )
A tentative layout is necessary : IN PROGRESS
• Academic exercise of evaluating a n beam effect on MgB2 with 10B, 11B and natB DONE (results in the next slides)

## Slide 9: Neutrons on MgB2
Neutrons
Neutron spectra in the coil of the insertion quadrupole for different apertures (F.Cerutti)
For the problem of the SC links, the neutron spectra where the links will be located (Iron Yoke and outside the magnets) most of the neutrons are thermal

## Slide 10
Concerns of Neutrons on MgB2
B natural isotopic composition is : 80% 11B - 20% 10B
10B has a very high thermal neutron
capture cross section for 10B(n,a)7Li
Thermal
1 MeV
Data from National Nuclear Data Center http://www.nndc.bnl.gov/
Mg natural isotopic composition is : 78.99% 24Mg – 10% 25Mg - 11.01% 26Mg

## Slide 11
Reactions occurring
sterm (b) | s1MeV (b)
5.7E-2 | 3.3E-4
2.2E-1 | 3E-4
4.3E-2 | 3.7E-4
4.2E3 | 2.2E-1
6.4E-4 | 9.6E-4
5.8E-1 | //
6.1E-3 | 2.2E-6
Data from National Nuclear Data Center http://www.nndc.bnl.gov/
27Mg  27Al + b- + n
27Mg t1/2= 9.5 min
27Be t1/2= 1.39 x106 y
10Be  10B + b- + n
12B  12C + b- + n
12B t1/2= 20.2 ms

## Slide 12: Neutrons on MgB2
Cases studied
TARGET (2x2x1 cm3)
MgB2 with only 10B
MgB2 with only 11B
MgB2 with natural composition of B (80% 11B – 20% 10B)
BEAM
Thermal Neutrons – 1MeV Neutrons
Neutron beam spot : 2 cm ; Fluence2x109 n/s x 1 d

## Slide 13: Energy Deposition
10B
11B
Bnat
1 MeV
Thermal n
Effect of the high neutron capture

## Slide 14: Neutron Fluence
10B
11B
Bnat
1 MeV
Thermal n
Effect of the high neutron capture

## Slide 15: Activation (at t=0)
10B
11B
Bnat
1 MeV
Thermal n
Effect of the high neutron capture
(occurring at the surface of the target)

## Slide 16: Activation (at t=3600 s)
10B
11B
Bnat
1 MeV
Thermal n
About a factor 100 less

## Slide 17: Residual Nuclei (at t=0 s)
10B
11B
Bnat
1 MeV
Thermal n
Protons from

## Slide 18: Displacement Per Atom
10B
11B
Bnat
1 MeV
Thermal n
Effect of the high neutron capture
(occurring at the surface of the target)

## Slide 19: B consumption
Assuming 200 days/year x 10 years of operation x 10 (Luminosity increasing) a 0.00072% consumption can be espected
Day consumption
Day consumption

## Slide 20: Conclusions
MgB2 neutron damage is not a concern about the performance of the SC Links, so no isotopic separation is necessary.
The energy deposition and “damage” are studied in a conservative case of collimated beam on target matching the beam geometry
What informations can be inferred from DPA values ?
How DPA are correlated to SC performance ?
Anyway it is the only parameter we have (R.Flukiger)

## Slide 21: Perspectives
Continue the work on MgB2 by studying the proton , pion and combined n, p, p effects
BSCO, YBCO …
Irradiation tests, code benchmarking and correlations with DPA
LHC Layout and geometry in FLUKA

## Slide 22: Acknowledgment
Thank You for Your attention
F.Cerutti , LS Esposito (CERN FLUKA Team)
A Bignami (POLIMI)