## Slide 1: Measurement of the noise of irradiated sensors CMS Preshower D. Barney, A. Honma, A. Peisert, Y-M. (Jacky) Tzeng
Preshower sensors
Noise of non-irradiated sensors
Noise of irradiated sensors
Model
Radiation field
Conclusions

## Slide 2: The CMS Preshower: part of the end cap el. calorimeter
Preshower + ECAL
2 layers of lead absorbers
each followed by Si sensors
and digital electronics
Z = ± 304, ± 309 cm
45 cm < R <121 cm
Si sensors, p-on-n , DC coupled, 63×63×0.32 mm3
32 strips 1.8 mm wide at a pitch of 1.9 mm
4288 total, 1072/absorber
Sensors mounted on Al tiles and
assembled into “ladders” of 6 to 10 tiles
Load capacitance dominated by the back plane:
Cbackplane ~ 40 pF
Cint ~ 6 pF
ladder
digital electronics

## Slide 3: Noise of non-irradiated sensors
Noise ~ Cdetector ~ 1/√V
Can be used to:
Verify that the sensor is biased
Estimate the full depletion voltage
Single strips noise vs. voltage
Vnoise – Vcapa (V)

## Slide 4: Noise vs. radius at 5.86 fb-1, no bias voltage
Average noise
of fully depleted
sensors

## Slide 5: Noise vs. radius, no bias voltage
0.066 fb-1, April 2011
5.86 fb-1, March 2012

## Slide 6: Model
Observed that for f ≥ 1012 n/cm2 the junction capacitance assumes the value of the detector geometry capacitance at f > 105 Hz, independent of voltage
Frequency dependence of the deviation of the C-V characteristics is strongly dependent on the ratio of the defect density, Nt, to the effective doping concentration, Nd
Developed a two-trap-level model which predicts this effect as Nt/ Nd → 1
* http://ieeexplore.ieee.org/ielx4/531/3487/00693473.pdf?tp=&arnumber=693473&isnumber=3487&tag=1
Developed by Zheng Li and H.W. Kraner* (1990):
“Studies of Frequency Dependent C-V Characteristics of Neutron Irradiated
P+-n Silicon Detectors”
Chart: R (cm)
| 42.5 | 45 | 47.5 | 50 | 52.5 | 55 | 57.5 | 60 | 62.5 | 65 | 67.5 | 70 | 72.5 | 75 | 77.5 | 80 | 82.5 | 85 | 87.5 | 90 | 92.5 | 95 | 97.5 | 100 | 102.5 | 105 | 107.5 | 110 | 112.5 | 115 | 117.5 | 120 | 122.5
 | 2789911165041 | 2859648068277 | 2888962885809 | 2.7315e+12 | 2597715744624 | 2474783804493 | 2.3253e+12 | 2.1905e+12 | 2.0357e+12 | 1823276068614 | 1.6482e+12 | 1598058374913 | 1473124616964 | 1.3478e+12 | 1.245e+12 | 1.125e+12 | 1.0188e+12 | 961614556402.5 | 918286077208.5 | 853694673331.5 | 810512761558.5 | 751937347161 | 701335960825.5 | 683699631615 | 626602116640.5 | 592900123315.5 | 530650293673.5 | 505202296599 | 447519452029.6499 | 433352324755.3499 | 370348336858.5 | 350722751979.6 | 329905904328
Fluence vs. distance from beam at 5.85 fb-1

## Slide 7: Conclusion
Preshower sensors capacitance dominated by the backplane capacitance
Independent of bias voltage at frequencies ~ 105 Hz after irradiation to f ≥ 1012 n/cm2
Noise, measured at 40 MHz, can not be used to evaluate the full depletion
Vfd can only be measured from the signal