## Slide 1
Karl Johnston
ISOLDE/CERN
karl.johnston@cern.ch
Solid State and bio-physics at ISOLDE
FPRIB2012, Kolkata

## Slide 2: Outline
Overview of the community
Introduction to techniques used in nuclear solid state physics
Techniques used at ISOLDE
Focus on some recent results in solid state and biophysics.

## Slide 3
SSP @ ISOLDE: Diverse community
Solid State physics: Semiconductors, Metals
Materials scientists: High Tc Superconductors, Multiferroic materials
Biophysics: structural properties & role of heavy metals in proteins, DNA.
Running experiments/letters of intent | 24
Participating countries | 26
Scientists | 160
SSP collaborations

## Slide 4
Radioactive isotopes for solid state physics? Why & How??
Nothing is more easy to detect with high sensitivity than nuclear radiation, i.e. very low concentrations of radioactive impurity atoms in a material can be detected.
The radioactive isotopes (“probes”) act as “spies” transmitting information with atomic resolution via their decay.
Crucially: what information do you get?????
Adds extra dimension to “normal spectroscopies” e.g. optical / electrical characterisation of semiconductors
Provides extremely local probe which is applied to variety of systems
You need
A facility providing a large variety of radioactive isotope (if possible, isotopically clean)
You have to introduce the isotopes into the semiconductor
by ion implantation
by diffusion
during crystal growth
by nuclear reaction with one of the constituents of the solid

## Slide 5: Techniques used at ISOLDE
Nuclear
Physics
Solid state physics
Applications in use at ISOLDE
Radioactive
Nuclei
 g, a, b
Muons
 ß+
Positrons
Neutrons
Ions
Hyperfine
Interaction
Coulomb
Interaction
Scattering,
Diffraction
Nuclear
Reaction
Mößbauer effect
gg angular correlation
Nuclear Magnetic resonance
Nuclear orientation
Radioactive
decay
DLTS
Photoluminescence
Tracer Diffusion
Emission Channeling
Ion Channeling
Backscattering
Elastic Recoil
Resonant Scattering
Neutron Scattering
Nuclear Reaction Analysis
Positron Annihilation
Positron Angular Distribution
Positron Energy Distribution
ß+-e-
Interaction
Nuclear probes
Interactions
Methods

## Slide 6: Techniques & facilities available
Hyperfine Interactions:
PAC (See Prof Das’ talk)
  9 g-g machines on-site
  4 detectors; 6 detectors: analogue and digital.
  Online UHV beamline for surface physics
Mossbauer Effect: 3 online chambers available.
b-NMR including novel system developed for biophysics.
Lattice location using emission channelling: 3 offiline and 1 online setup
Radiotracer diffusion: online and offline systems
Semiconductor spectroscopy: full PL and DLTS characterisation labs
Dedicated suite of offline labs for sample preparation, treatment and measurement.

## Slide 7
Experimental techniques used with radioactive isotopes at ISOLDE

## Slide 8
Nuclear SSP Elements produced at ISOLDE
low energies & high multipolarities  highly converted cascades  e-g PAC
e-g
RED  g-g PAC BLUE g-e PAC
e-e

## Slide 9
ISOLDE table of elements
Isotopes of this element used for solid state physics or life science
Ni
Co
Cr
Pt

## Slide 10
Magnetic semiconductors studied using Mossbauer spectroscopy
Development of 57Mn beam in late 1990s (with laser ionisation) brought about a new era in Mossbauer experiments at ISOLDE.
Very clean, intense beam of 57Mn (>3e8 ions sec-1)
Allows collection of single Mossbauer spectrum in ~ 3 mins.
Able to collect many hundreds over course of a 3 day run.
Allows low concentrations of probe atoms to be used (~10-4At%)

## Slide 11
Experimental setup
On-line measurements
High statistical spectrum
Incoming 40-60 keV 57Mn+ beam Intensity: ~2108 57Mn+/cm2
Implantation chamber
Mössbauer drive with resonance detector
Sample

## Slide 12
ZnO: a ferromagnetic semiconductor?
Observation of 6 fold spectrum: characteristic of magnetic structure (at room temperature!!!).
Time to celebrate?
Not quite.
Further reults in an external magnetic field show that the spectrum shown to be a slowly relaxing paramagnetic system .
Gunnlaugsson et al (APL 97 142501 2010)

## Slide 13
After high-dose implantations, precipitates of Fe-III are formed. These form clusters yielding misleading information about the nature of magnetism in ZnO (as reported by many groups over the last number of years).
More on ZnO
Gunnlaugsson et al (APL 100 042109 2012)

## Slide 14
Described as first-order dielectric phase transition below Tco
A.M.L. Lopes et al., Phys. Rev. Lett. 100, 155702 (2008)
Results: Electric susceptibility / spontaneous polarization below TC
x=0.35 ->TEDO=206 K, x=0.4 ->TEDO=218 K,
x=0.85 -> TEDO=112 K
PAC results: Local Probe Studies / Pr1-xCaxMnO3 system

## Slide 15
Emission channelling: locating impurity atoms in the lattice
Channelling of charged particle in crystal, channels along high symmetry directions.

## Slide 16
Emission channelling: locating impurity atoms in the lattice
Since 2009, online system available, able to measure isotopes with half-lives of ~1min.
Position sensitive detectors produced at CERN (Medipix project).

## Slide 17
Pereira et al APL 98 201905 (2011)
Spintronics: Location of Mn in Ga1-xMnxAs
GaAs: a dilute magnetic semiconductor, not yet at room temperature.
Emission channelling results showed that Mn is surprisingly stable at interstitial sites in GaAs (400C).
Results that have consequences for “defect engineering” of this material.

## Slide 18
PL Characterisation of Semiconductors
One of the principal techniques in semiconductor research.
High Spectral resolution
Non-destructive
No need for contacts
Very sensitive (can probe ppb)
Relatively flexible and straightforward
Can be extended to include external perturbations.
Not quantitative
Low concentrations may be more optically efficient
Lack of chemical information (except for some rare cases where isotope shifts are observed)

## Slide 19
PL + L-DLTS apparatus at ISOLDE
Monochromator
Focus: 0,75 m
Gratings: 150 – 1800 l/mm
Detectors
CCD-camera (1,1 - 6,2 eV)
Ge-Diode (0,7 - 1,5 eV)
LASER
HeCd (3,8 eV)
Nd:YAG (2,3 nm)
Diode (1,9 nm)
Cryostat
He-Bathcryostat (1,5 – 300 K)
Closed cycle

## Slide 20
(1)
(2)
(3)
(1)
Fundamental properties of donors in ZnO

## Slide 21
Time
I8 feature decays as Ga decays; So does the weak I1 line; DD2 grows as Ge is produced.
First chemical identification of Ga and Ge in ZnO, (PRB 73, 165212 (2006)) and PRB 83 125205 (2011))
I8
DD2
I1

## Slide 22
Diffusion: experimental procedure
1...30 µm
CdTe:111Ag
Tdiff = 570 K
tdiff = 30 min
CdTe
Ø = 6 mm
d = 800 µm
111Ag
111Ag Implantation
CdTe
thermal
treatment
550 … 900 K

## Slide 23
Diffusion: Ag in CdTe
Tdiff = 825 K
tdiff = 60 min
Shapes of diffusion profiles strongly depend on external vapor pressure
H. Wolf, F. Wagner, Th. Wichert, and ISOLDE Collaboration, Phys. Rev. Lett. 94, 125901, 2005

## Slide 24
Implantation
Diffusion annealing up to 1800 °C
Sample sectioning by ion sputtering
Catching the sputtered ions by a tape system
In situ activity measurement
Remote control
Online Diffusion

## Slide 25
Biophysics at ISOLDE: Radioisotopes for Probing Biomolecular Functionality in Living Matter
PAC isotopes used for biophysics at ISOLDE:
Hemmingsen et al. Chem. Rev., 2004, 104: 4027
No implantations: collect ativity in ice  chemistry

## Slide 26
ωQ and η
BASIL model
QM calculations
6·180º spectra and 24·90º spectra
Least χ2 analysis
Fourier transform
compare experiment to model
In practice….

## Slide 27
C A B
Matzapetakis et al. J. Am. Chem. Soc. 2002, 124: 8042; Lee et al.
Angew. Chem., 2006, 45: 2864; Peacock et al. Proc. Nat. Acad. Sci. 2008, 105: 16566
111mCd-PAC
113Cd-NMR
Metal Ion Binding Site Structure:
Fast inter-conversion between species
A
B
C
B
C
A

## Slide 28
Temp [ºC] | t1 [ns] | t-1 [ns]
1 | 52 | 48
20 | 42 | 36
35 | 28 | 20
50 | 19 | 12
De novo designed heavy metal
Ion binding proteins: ns dynamics
Stachura et al. Manuscript in preparation
50 ºC
35 ºC
20 ºC
1 ºC
1 ºC
-20 ºC
-196 ºC
111mCd-PAC

## Slide 29
In vivo experiments
Hg(II) binding to barley
Whole barley plant
Homogenised barley leaves
Adolph et al. Chem. Eur. J., 2009, 15, 7350 – 7358
5-7 days-old plants
Plant inserted into test tube.
Fast uptake of Hg(II) (<1h)
Bound to large molecules, similarities to HgS2 compounds
Notes: 29

## Slide 30
Beta-NMR applied to biophysics
Beta-NMR
Cu, Zn, Mg, Mn, Fe, Ni
Measurement of electric field gradient
  Cu(I) is “invisible” in most (except X-ray and nuclear) spectroscopic techniques because it is a closed shell ion
  Cu(I)/Cu(II) are essential in many redox processes and electron transport in biology

## Slide 31
Advantages and Limitations of PAC Spectroscopy for biophysics
Advantages:
Characterisation of structure
and dynamics at the PAC
probe site (including rotational
correlation times)‏
High sensitivity to structural
changes
Small amount of PAC probe needed
(in principle about 1 pmol)‏
Different physical states
(crystals, surfaces, solutions, in vivo...)‏
Mechanically stable, allowing for
stirring, flow, ...
Limitations:
Suitable PAC isotopes do not exist for
all elements
PAC isotope must bind strongly to
the molecule of interest
Spectral parameters do not uniquely
determine structure
After effects can cause problems (in
particular for EC). (111In)‏
Production of PAC-isotopes
Hemmingsen et al. Chem. Rev., 2004, 104: 4027; Hemmingsen and Butz, in "Application of Physical
Methods to Inorganic and Bioinorganic Chemistry" 2007, Ed. R.A. Scott, Wiley
Notes: 31

## Slide 32
Funding and Acknowledgements
Manfred Deicher, Herbert Wolf, University of Saarlandes, Germany
Guilherme Correia, Uli Wahl ITN, Lisbon, Portugal
Ligia Amorim, KU, Leuven, Belgium
Martin Henry, Dublin City university, Ireland
Haraldur Gunnlaugsson, University of Arhus, Denmark
Torben Molholt, University of Iceland, Iceland
Monika Stachura, University of Copenhagen, Denmark
Krish Bharuth-Ram, iThemba Labs, South Africa

## Slide 33
Summary
Solid state physics/biophysics: a very active experimental programme at ISOLDE
Radioactive measurements complement work at home laboratories
Unique information – be it chemical or local – which is only achievable using radioactive implantations/probes.
Synergy between groups e.g. extension of biophysics methods for studying graphene and fullerenes (Prof Das).
Ability to profit from the huge range of beams available at ISOLDE (especially now with online and offline setups).
Many new developments under preparation e.g. b-NMR for biophysics
Much more info at:
Cern.ch/ssp or follow us on

## Slide 34
Splitting of features
Mossbauer sextet indicates magnetism at the Fe site