## Slide 1: Development of new FFAG RF Cavity at KURRI
Fukui University
Tomoya Minamikawa

## Slide 2: Contents
・Background
・Introduction
・Flow of my work
・considering shape
・the processing new magnetic core
・Experiment
・Summary

## Slide 3: Background
・Analyze properties of materials using neutron beam
・Accelerator Driven Subcritical Reactor
・(Cancer therapy with neutron beam)
FFAG at KURRI
Ion source
Linac
FFAG
(Main Ring)
RFCavity
Extract the Proton Beam
For cancer therapy
ADSR
Proton Beam strikes the neutron target
→Neutron breaks out
ADSR
・Stop reactor safely
・Recycle spent nuclear fuel by radiation of neutron beams.
・Disposal of long life radio nuclide.
Notes: １、開発が進めば、小型で大強度な中性子源として期待できる。
２、実際に、げんざいはこのような用途で使われている
３、加速器はこんな感じ、私はRFをやってるよ
４、じゃあRFってどんな物なのか説明します。

## Slide 4: Typical of the RF Cavity
Magnetic
Field
Magnetic
Field
Capacitor
Amp.
Amp.
Electric
Field
Troidal Core
Troidal Core
Beam duct
Capacitor resonates with Toroidal Core
It can apply acceleration Gap
to Voltage efficiency.
・Impedance depends
mostly on Magnetic Alloy
Installing Troidal Core,
standing wave length
become shorter.
Installing Troidal Core,
・We don’t use any capacitor.
・We deal with the gap and the plate
as a capacitor.
Notes: １、ビームが通過
２、電場（加速電圧）を感じて加速
３、外側から、電流を送ってる 磁性体が電流を感じて磁場を発生。LCの共振構造。
４、空胴の性能はほとんど磁性体で決まり、インピーダンスが高いほど加速電圧を大きく出来る。
５、加速電圧が大きくなるとどういうメリットがあるのか、見て行きます。

## Slide 5: Introduction
We try to get High power Beam
reusing J-PARC RCS Core .
We should Install another cavity.
Present spec
Energy (MeV) | 100
Accelerating Voltage (KV/turn) | 4
Repetition rate (Hz) | 20
Cavity Impedance (Ω) | 500
Number of cores | 2
We want to get more acceleration voltage to get High power beam.
If the acceleration voltage is more higher, we can increase repetition rate.
It means,
・we can increase Average output beam current
・The beam can avoid the foil quickly. Beam doesn’t lost particles.
Horizontal aperture is not enough.
BUT

## Slide 6: Flow of my work
Install New Cavity
Making ”Ribbon Core”.
Determine the Impedance to confirm the boundary
(put it in the New cavity)
Input high power and do the thermal test
Construct New Cavity
To determine the Impedance.
verify the effect of the cutting Core.
Investigate the property of the Core
Process the Core
Consider the shape
Examination of the shape.
Notes: １、加速電圧を高く出来ると短時間でこうエネルギーまで加速可能になります。
２、だから、空胴の性能を左右する磁性体の開発が必要です、
３、（フローの説明）

## Slide 7: Consider the shape(1)
Beam duct
Beam
Accelerating
electric field
RF Cavity has rectangular beam duct.
▷We should make
the large aperture core.
Present core
If the new core can be made from RCS core,
We don’t have to use a large oven.
It is too hard to make.
We need too much cost.
It is useful technique
to make the core from piece.

## Slide 8: Consider the shape(2)
Flower core
Ribbon core
Outer circumference(mm) : 3238.68
Inner circumference(mm) : 1758.13
ln(OC/IC) :0.265
Compare with RCS L0 :0.74
Outer circumference(mm) : 3656.79
Inner circumference(mm) : 2164.53
ln(OC/IC) :0.227
Compare with RCS L0 : 0.57
:The factor depends on the shape of MA core
×density
N2

## Slide 9: Consider the shape(2)
Flower core
Ribbon core
Outer circumference(mm) : 3238.68
Inner circumference(mm) : 1758.13
ln(OC/IC) :0.265
Compare with RCS L0 :0.74
Outer circumference(mm) : 3656.79
Inner circumference(mm) : 2164.53
ln(OC/IC) :0.227
Compare with RCS L0 : 0.57
:The factor depends on the shape of MA core
×density
N2

## Slide 10: Cutting core
How to make Ribbon Core
Cut troidal core
Manage how to cut
using Diamond cutter
Polish the cut surface
and shape the flower cavity
Notes: これが花弁型コアだよ
制作費が浮く
次に、カットした事による影響について考えます

## Slide 11: Exp1-Impedance
Change the gap of the cut surface : 0mm , 1mm
Cut surface
Network Analyzer

## Slide 12: Result - Exp1,：Impedance-
・The form of the Impedance doesn’t change almost.
・RCS Inductance is larger than Flower core’s.
・”Flower Core 0mm L” is larger than “Flower Core 1mm L”.
▷Inductance depends on the gap of the cut surface.
Decreasing Inductance means
Impedance may not be so broad(Q is higher) → should check if it can be used on the whole frequency range
*L,R of the J-parcRCS are normalized by L,R of Flower Core
Flower Core 0mm
Flower Core 1mm
Chart: Freq vs L*
Chart: Freq vs R*

## Slide 13: Result - Exp1,：Impedance-
・The form of the Impedance doesn’t change almost.
・RCS Inductance is larger than Flower core’s.
・”Flower Core 0mm L” is larger than “Flower Core 1mm L”.
▷Inductance depends on the gap of the cut surface.
Decreasing Inductance means
Impedance may not be so broad(Q is higher) → should check if it can be used on the whole frequency range
*L,R of the J-parcRCS are normalized by L,R of Flower Core
Flower Core 0mm
Flower Core 1mm
Chart: Freq vs L*
Chart: Freq vs R*

## Slide 14: Result - Exp1,：Impedance-
・The form of the Impedance doesn’t change almost.
・RCS Inductance is larger than Flower core’s.
・”Flower Core 0mm L” is larger than “Flower Core 1mm L”.
▷Inductance depends on the gap of the cut surface.
Decreasing Inductance means
Impedance may not be so broad(Q is higher) → should check if it can be used on the whole frequency range
*L,R of the J-parcRCS are normalized by L,R of Flower Core
Flower Core 0mm
Flower Core 1mm
Chart: Freq vs L*
Chart: Freq vs R*

## Slide 15: Result - Exp1,：Impedance-
Chart: Freq vs L*
Decrease about
3.0×10-6 (H)
If we make the gap 1mm,
▷Inductance decrease
about 3.0×10-6(H)
▷Qblue is 1.6 times Qgreen .
If the core has more large gap, Q value is increased quickly.
I must not to make the gap as possible.

## Slide 16: Exp2-Impedance with Capacitor
Set the resonance point at ２MHz using capacitor (1,200pF)

## Slide 17: Result - Exp2,：Impedance with Capacitor-
Impedance is broad. We can get High Accelerating voltage constantly.
Set the resonance point at
２MHz using capacitor
Accelerating Freq：
1.5MHz ~ 4.4MHz
Chart: Frequency vs R
100MeV Extraction 4MHz
150MeV Extraction 4.4MHz

## Slide 18: Result - Exp2,：Impedance with Capacitor-
Impedance par a core(Ω) | How many cores can we install | Aim of the Acc Vol ”VRF”(kV) | Input Power we need (kW)
130〜140 | 4 | 4kV | 14~15
We can get the Impedance 130~140 Ω at whole frequency range.
If we install 4 cores on the new RF cavity and input *14~15 kW,
we can get 4kV per turn.
We will be able to make The New Cavity Reusing RCS Cores.

## Slide 19: Summary
【Summary】 We will Install New RF Cavity to get high power beam
・Cut J-PARC RCS core and make new core “Ribbon core”
・Measure the Impedance R and Inductance L”
which concern performance of the cavity.
・Effect of the cut surface
Impedance almost doesn’t change, Inductance decreased
→Impedance may not be so broad(Q is higher)
・Impedance with Capacitor
Broadband Impedance
On the cavity, we install 4 cores and input 15kW.
▷Get 4kV of the Accelerating Voltage.
【Future plan】
・Put the core in the new cavity and measure the Impedance.
・Input high power
・Thermal test
・Effect of the L0
Flower Core is 0.57 times the RCS Core

## Slide 20
Thank you for your attention

## Slide 21: Impedance
Effect of the Flower cavity
①Shape(Form factor : L0）
Impedance：
:The factor depends on the shape of MA core
×density
N2
Ribbon Core is 0.57 times the RCS Core
②Effect of the cut surface
Decrease Magnetic field at cut surface → Decrease L
▷We may not get the Impedance which is broadband.
*Input Power is
Notes: １、形状因子の話
Aとbで決まる、サイズに起因するよ
２、測定器側では、インピーダンスのデータはこのように（RとX）アウトプットしてくれます。
３、変換計算して指標RpLpを出します。
では実験方法について見て行きます。