## Slide 1: DS Dipole MBHSP01 Design, Fabrication, & Lessons Learned
Fred Nobrega
11 T Collaboration Review
September 26, 2012

## Slide 2: Cold Mass Stress Analysis
Stress analysis for:
  a) collaring
  b) assembly
  c) cool-down
  d) maximum design field
a)
b)
c)
d)
The mechanical design maintains coil compression up to 12 T.
Collar structure is aligned & supported by the yoke and shell.
Maximum stress during assembly ~130 MPa
The mechanical structure is optimized to keep the coil stress below 165 MPa.
EDMS no: 1107424
Parameter and performance specification for the 11 T Dipole demonstrator model magnet

## Slide 3: Demonstrator Dipole As Built Cold Mass Parameters
Parameter | Specification | As Built | 
Yoke ID, mm | 160..200 | 174.5 | 
Yoke OD, mm | 400 |  | 
Yoke length, mm | 1700 | 1980 | 
Number of alignment keys | 2 |  | 
Alignment keys material | bronze |  | 
Clamps material | Al | 7075-T6 | 
End fillers material | 316L |  | 
Total end filler length, mm | 330 | 355 | 
Skin material | 304L |  | 
Skin thickness, mm | 12 | 12.7 | 
Cold mass length, mm | 1970 | 2154 | 
End plate material | 316LN | 304L | 
End plate thickness, mm | 50 |  | 
Skin
Clamp
Alignment Keys
Yoke
Collar
Fiducial

## Slide 4: Coil Parameters
The coil has:
  56 total turns, 22 inner, 34 outer
  3 wedges in Layer 1
  1 wedge in Layer 2
  Splice-less layer jump transitions between the inner and outer coils.
  Cable insulation double butt lap by 75 mm thick E-glass
Alignment notch in L2 pole pieces
Nb3Sn cable expansion due to the phase transformation ~ 3% in thickness & ~1% in width

## Slide 5: Ground Insulation & Quench Heaters
MBHSP01 used a 60 mΩ external dump resistor.
Stainless steel quench heaters 25 mm thick were placed in 2 different locations within each coil’s ground insulation as part of a quench heater study.
One set of SS heaters had one layer of 127 mm Kapton next to the coil. Another set had two layers of 127 mm Kapton.
2x 127 mm Kapton between coil and heater
25 mm
SS Heater
1x 127 mm
Kapton
between coil and heater
25 mm
SS Heater
1x 127 mm
Kapton
between coil and heater
2x 127 mm Kapton between coil and heater
Parameter | Value
Number of layers | 5
Insulation material | Kapton
Layer thickness, mm | 0.127
Number of heaters/coil | 8
Heater material | 316
Heater width, mm | 27.8
Heater thickness, mm | 0.025

## Slide 6: Collar Design
Parameter | Specification | As Built
Protection shoe thickness, mm | 0.5 | 
Protection shoe material | 304 | 
Collar material | 316LN | Nirosta high-Manganese SS
Collar width, mm | 20..40 | 15.2
Lamination thickness, mm | 1.5 | 1.8
Collar pack length, mm | 50 | 
Number of keys | 4 | 
Key height, mm | 6 | 8
Key thickness avg, mm | 5 | 5.4
Key material | Bronze/SS | Phosphor Bronze

## Slide 7: Yoke, Shell, and End Plate Design
Parameter | Spec | As Built
Yoke thickness, mm | - | 25
Yoke material | - | SAE 1045
Clamp material | Al | Al 7075-T6
Skin material | 304L | 
Skin thickness, mm | 12 | 12.7
End plate material | 316LN | 304L
End plate thickness, mm | 50 | 

## Slide 8: Coil Technology
Reaction cycle is in an argon atmosphere and at 210° C for 72 hours, 400° C for 48 hours and 640° C for 48 hours. The heat treatment lasts about 9 days including ramp up and cool down.
Cure cycle is 150° C for 30 min. at ~27MPa.
Coil is compressed with 1 mm curing shim. Shim size is approximate sum of cable expansion during reaction and used to pre-compress insulation with binder.
Impregnation is with CTD101K and is done in the IB2 vacuum oven at 30-50 mm Hg with epoxy temperature of 60° C.
Curing is done in a different oven at 125° C for 21 hours.
Coil winding tensions is ~156 N.
Pole gap is maintained during winding and curing. Stored coil winding tension is near zero prior to reaction.
CTD-1202X ceramic binder used during winding of end turns to support cable to help prevent popped strands and cable collapse. Binder applied to entire coil prior to curing.

## Slide 9: PC00, Cu Coil Winding
RE, Cu coil
LE, Cu coil
End parts designed & provided by CERN
  Laser sintered (SLS)
  2 designs being evaluated, upright, minimum strain
End parts large and stiff
  Hand modification to most parts prior to use
LE, Cu coil
RE, Cu coil

## Slide 10: Practice Coil, PC01
PC01 was used for the mechanical model
  Cable insulation was 2 layers butt lap E-glass
  Added more slits to end parts for flexibility.
Cold mass MBHSP01 used coils MBH02 & 03 with a single layer nominal half lap E-glass cable insulation.

## Slide 11: Coil Fabrication, MBH02
MBH02 LE
MBH02 RE
L2 After Reaction
L2 Before Curing

## Slide 12: Coil Fabrication, MBH02
L1 inner coil after reaction
MBH02 LE
MBH02 RE
L1 outer surface before curing

## Slide 13: Coil Fabrication, MBH02
Gaps between cable and end parts filled with S2-glass.

## Slide 14: Coil Fabrication
MBH04 (2m) with 3mm gap, used end stopper during reaction, spacer not modified
MBH05 (1m) Spacer legs shortened, saddles modified (1 mm removed from inner saddle parting plane, 1.5 mm from outer saddle), no reaction end stopper.
MBH04
MBH05

## Slide 15: MBH04 Damage
L2 LE saddle out of tolerance
  Outside diameter large by 37 mm
  Mid-plane gap for cable lead small by 60 mm
Insulation between cable lead and saddle too thick by at least 127 mm
Retrospective view of coils 2 and 3 in MBHSP01

## Slide 16: Coil Size Data
MBH02
445 mm from RE
MBH03
1165 mm from RE
MBH03
435 mm from RE
MBH02
1165 mm from RE
MBH01 (PC)
1165 mm from RE
MBH01 (PC)
455 mm from RE
(1 box = 101.6 mm)

## Slide 17: Coil Fabrication Lessons Learned
QC
  End part inspection
Add ceramic binder each end turn for added cable stability.
Remove material from mid-plane of saddles for coil curing. Shim saddles at mid-plane as required for reaction and impregnation process.
Leg length of selected end parts modified
Match cable final turn angle with end part
  Balance between cable hard way bend and torsion

## Slide 18: Collar Fabrication
Collars fabricated via laser cutter
Material provided by CERN
  Issues with surface cracks in coil material and with making sheets for the laser cutter.
Average part tolerance from vendor +/- 26 mm with standard deviation of 16.6 mm.
  Several iterations with vendor needed to improve part tolerance to the reported levels.
Collar packs:
  Use 127 mm shim between laminations.
  Are welded longitudinally along the pole and on the O.D. above the pole.
  Have 2 pins each welded at the ends.
1 Box = 25.4 mm

## Slide 19: MBHSP01 Coil Shim Plan
223.3 mm mid-plane shim
(not tapered at the ends)
MBHSP01 Shim Plan

## Slide 20: Mechanical Model #3
Radial shim 101.6 mm
Mid-plane shim 152.4 mm
Average SG readings
  -40 MPa mid-plane
  -4 MPa Pole
Pressure sensitive film
  High pressure used on mid-plane, max = 130 MPa
  Medium pressure used on coil surface, max = 49 MPa
POLE
POLE
Mid-plane

## Slide 21: Mechanical Model #4
Half of collar packs rotated 180° (collar witness mark)
Radial shim 127 mm (added 25.4 mm)
Mid-plane shim 152.4 mm
Average SG readings
  -61 MPa mid-plane
  -5 MPa Pole
POLE
POLE

## Slide 22: Collar Deflection & Coil Stress After Collaring
Collar Deflection | MM#6 |  | Magnet |  | FEA
Horizontal radius change (mm) | 43 |  | 52 |  | 20
Vertical radius change (mm) | 52 |  | 72 |  | 86
Coil Stress Average (MPa) | LE | RE | LE | RE | -
Mid-plane coil A | -59 | -83 | -42 | -54 | -93
Mid-plane coil B | -55 | -67 | -67 | -59 | 
Pole coil A | -1 | -12 | -13 | -9 | -33
Pole coil B | -3 | -13 | -10 | -47 | 
Coil SG locations, pole & mid-plane
After Collaring

## Slide 23: End Mechanical Model
Coil sections were positioned such that the upper and lower saddles were in the same position as they would be in the magnet. The cable splice leads were not studied in the MM.
Results from MM#7 Body are from coil ends which include a portion of the straight section. Ecoil = 20 GPa
Collar Deflection | MM#6 | MM#7 | MM#7 | Magnet |  | FEA
 | Body | Body | Ends | Body | Ends | Body
Horizontal radius change (mm) | 43 | 62 | 24 | 52 | 2 | 12
Vertical radius change (mm) | 52 | 71 | 33 | 73 | 1 | 74

## Slide 24: Collared Coil Stress Summary
Same collar keys used for all mechanical models.
Many mechanical models built with same coils. Coil modulus assumed at 20 GPa.
Pressure sensitive film used to identify high stress areas and uniform loading.
MM#5 had a double layer of pressure sensitive film by mistake.
Average Collar Deflection Radius Change (mm) |  |  |  |  |  | 
 | MM#3 | MM#4 | MM#5 | MM#6 | Magnet | FEA
Horizontal (R) | - | 7 | 67 | 43 | 52 | 12
Vertical (R) | - | 58 | 79 | 52 | 73 | 74
Collared Average Coil Stress (MPa) at SG Location |  |  |  |  |  | 
 | MM#3 | MM#4 | MM#5 | MM#6 | Magnet | FEA
Mid-plane | -40 | -61 | -74 | -66 | -56 | -77
Pole coil | -4 | -5 | -3 | -7 | -20 | -13

## Slide 25: Coil Assembly & MM
Coil assembly process developed with mechanical model
Upper and lower collar packs are shifted to interlock all collar packs together
Iron on Kapton used for ground insulation
Silicone O-rings used to hold collars together prior to the keying operation.

## Slide 26: Collared Coil Lessons Learned
Fuji film between saddles indicated low pressure in keyed collar assembly – use tapered mid-plane shim as precaution
Fabrication technique cost and schedule tradeoffs
  Laser cutting
  Wire cutting
  Stamping
Choose 2 of the 3
  Fast
  Cheap
  Accurate

## Slide 27: MM Clamped Yoke
2 iterations used to determine the collar to yoke shim.
Clamped Yoke Average Coil Stress (MPa) |  |  |  | 
 | MM#6-1 | MM#6-2 | Magnet | FEA
Mid-plane | -60 | -39 | -38 | -64
Pole coil | -15 | -21 | -56 | -59
Coil SG locations, pole & mid-plane

## Slide 28: Magnet Shell Welding
Nominal gap between alignment key and shell 0.7mm. Actual gap ~3 mm  large weld shrinkage
  Higher coil stress
  Local yielding of end yoke laminations
New weld carriage system not completely debugged prior to use.  weld process not well controlled
Approximately half of coil stress increase came from the fusion weld passes.
End yoke lamination with apparent local yielding
Gaps
Gap

## Slide 29: Shell Welding Stress
High shell welding stress due to bending
Step increase in shell stress after fill pass 2 was a result of poor visibility due to camera support issues
Chart: Shell Stress at ±30°, Lead & Return End
| in press | fusion-skip 100 mm | final fusion-skip 100 mm | 1 filler | next day | 2 filler | 3 filler | next day | 4 filler | 5 filler | 6 filler | next day
30ALE | 0 | 46.8164 | 72.0209 | 71.8751 | 74.1999 | 65.7764 | 143.7273 | 143.5775 | 185.7197 | 217.9851 | 231.8955 | 235.6079
30ARE | 0 | 34.638 | 62.746 | 35.2971 | 36.9128 | -4.3779 | 245.8676 | 251.1244 | 330.8232 | 406.9422 | 470.1097 | 473.8056
30BLE | 0 | 49.1594 | 88.645 | 128.8093 | 135.3926 | 193.3867 | 275.4283 | 277.9331 | 352.9487 | 420.6889 | 479.1629 | 479.4638
30BRE | 0 | 41.3804 | 87.0968 | 119.1534 | 128.4953 | 122.7881 | 278.1472 | 282.174 | 383.453 | 446.4268 | 514.0751 | 517.9311
30CLE | 0 | 66.3382 | 100.4671 | 121.8876 | 129.1493 | 163.5835 | 303.4664 | 304.3855 | 352.6783 | 381.4232 | 410.0571 | 410.7959
30CRE | 0 | 63.1936 | 94.3861 | 111.0436 | 115.0568 | 121.7794 | 281.3963 | 282.8224 | 360.9963 | 456.4805 | 534.3689 | 539.9592
30DLE | 0 | 27.253 | 88.5399 | 170.7949 | 177.0807 | 244.5532 | 328.2624 | 331.4674 | 401.864 | 462.8922 | 524.7011 | 527.4053
30DRE | 0 | 2.3015 | 71.1087 | 137.0749 | 153.7658 | 155.5826 | 276.6995 | 278.5094 | 350.2821 | 398.7851 | 451.5214 | 453.2847
Chart: Shell Stress at ±60°, Lead & Return End
| in press | fusion-skip 100 mm | final fusion-skip 100 mm | 1 filler | next day | 2 filler | 3 filler | next day | 4 filler | 5 filler | 6 filler | next day
60ALE | 0 | 132.4652 | 184.5079 | 200.6835 | 204.7982 | 260.454 | 330.5738 | 339.1588 | 378.3033 | 406.7642 | 433.625 | 443.3731
60ARE | 0 | 143.8035 | 198.3023 | 219.0072 | 221.3304 | 239.0749 | 342.0159 | 347.3569 | 399.9892 | 445.2166 | 482.2591 | 488.2023
60BLE | 0 | 116.8728 | 155.9539 | 175.0465 | 184.4299 | 224.5186 | 279.2319 | 283.6164 | 330.25 | 363.1608 | 389.9929 | 393.7005
60BRE | 0 | 81.3522 | 125.7253 | 156.5483 | 163.5269 | 174.4045 | 267.4211 | 272.7027 | 322.6947 | 359.2341 | 389.0284 | 394.7546
60CLE | 0 | 115.305 | 152.6564 | 171.3303 | 178.2914 | 206.1985 | 279.6104 | 284.324 | 318.3545 | 338.2272 | 362.0663 | 367.7897
60CRE | 0 | 40.3091 | 76.0835 | 97.3358 | 104.4444 | 116.1055 | 202.1208 | 203.845 | 247.9781 | 292.271 | 333.5115 | 338.3103
60DLE | 0 | 105.5512 | 139.5312 | 167.3468 | 175.8876 | 213.1472 | 265.9842 | 270.2099 | 310.0871 | 337.2329 | 366.8678 | 368.8545
60DRE | 0 | 30.4632 | 68.8091 | 99.8052 | 109.6153 | 122.567 | 194.7902 | 200.3885 | 242.9087 | 278.1919 | 313.1065 | 318.571

## Slide 30: Coil Stress During Shell Welding
Chart: Coil SG Average
| 0 | Pres | skip-fuse 0.1 m | Press | final skip-fuse 0.1 m | 1 filler | next day | 2 filler | 3 filler | next day | 4 filler | 5 filler
02 Pole Average | -59.345 | -60.3171 | -61.8297 | -61.5886 | -63.4442 | -65.2034 | -63.3525 | -66.2278 | -67.9863 | -66.7817 | -68.3209 | -69.0203
02 PP Average | -41.0659 | -40.5999 | -41.9302 | -41.6526 | -44.5609 | -45.9913 | -44.1438 | -46.5805 | -49.7363 | -47.9066 | -50.2371 | -50.9583
03 Pole Average | -52.35 | -52.8979 | -54.484 | -54.3551 | -55.4491 | -56.1275 | -54.2063 | -56.3246 | -58.0862 | -56.8769 | -57.8802 | -58.3839
03 PP Average | -34.444 | -34.155 | -34.7868 | -34.4054 | -35.9684 | -36.2528 | -34.3154 | -37.0938 | -38.68 | -36.8358 | -38.5377 | -39.1064
Shell Welding Average Coil Stress (MPa) |  |  | 
 | Before Weld | Final Weld | FEA
Mid-plane | -38 | -42 | -39
Pole coil | -56 | -62 | -110
Coil SG locations, pole & mid-plane
After Skin Welding

## Slide 31: Final Assembly
50 mm thick end plate
4 bullets with strain gauges preloaded to 4.4 kN each.
Assuming 25% of Lorentz load, end plate deflection calculated to be 159 mm with 81 MPa max stress in the weld area.

## Slide 32: Instrumentation
Coil strain gauges (14) on coil pole, mid-plane, and key
Voltage taps (44)
End bullet load strain gauges (8)
Shell strain gauges (16) at 30° and 60° from shell weld

## Slide 33: Clamped Yoke & Final Assy Lessons Learned
Bolted skin for R&D magnets has advantages over welded skin assemblies
  Shim iterations
  Fast turn around of assembly
  Cost
No coil over compression in the straight section from shell welding but can’t exclude coil end damage because of end yoke yielding. Using tapered mid-plane shim can help mitigate unexpected over compression from welding.

## Slide 34: Discrepancy Reports
DR’s are written when there is any non conformance with respect to the traveler.
  Written description
  Cause of non conformance
  Disposition
  Corrective action to prevent recurrence
Coil Fabrication Discrepancy Reports |  | 
 | Coil Winding | Reaction & Epoxy Impregnation
MBH02 | 7 | 2
MBH03 | 2 | 1
MBH04 | 2 | 1
MBH05 | 0 | 0*
MBH06 | 1 | 
MBH07 | 0 | 0*
* Coil is or will be in fabrication |  | 

## Slide 35: Lessons Learned
Implemented
  Double butt lap of 75 mm E-glass changed to single half lap cable wrap due to difficulty controlling placement second layer of the wrap to cover gap of 1st layer.
  End part quality control
  End part design revisions, cable lay angle, part length, saddle mid-plane
  Collar manufactures to hold print tolerances
To be implemented
  Less end part modifications by technicians prior to use.
  Shell welding tooling refinement and process improvement before next magnet weldment.
Observation
  Coil degradation appears to be an aggregate effect beginning with and perhaps dominated by the end saddle design.
    Over compression of cable during reaction
    Over compression from shell welding in ends  yoke lamination yield
  Next steps
    Autopsy of MPHSP01 coil inspection
    Redesign of saddles
    Bolt on shell
    Demonstrate shell welding well understood prior to use
    Tapered mid-plane shim
    Test MBH02 in Jan 2013 with these steps incorporated.

## Slide 36: MBHSP01 Schedule
Coil 02 impregnation: Hole miss match 50 mm vs 2 inches wrt impregnation & reaction tooling delayed coil transfer from one set of tooling to the other
Impregnation base plate out of tolerance, part rejected & fabricated again at the same time needed for impregnation
Coil longer than design modify impregnation base plate.
Input from PC01 CMM  changed impregnation radial materials for coil 02
Impregnation curing oven out of service
Coil 03 reaction delay  furnace CPU defective
Collar delay
Yoke delay
 | Actual days | Planned days
coil 02 wind | 42 | 22
coil 02 react | 28 | 29
coil 02 impreg | 64 | 19
coil 03 wind | 39 | 22
coil 03 react | 71 | 29
coil 03 impreg | 19 | 19
coil assy | 6 | 14
collar assy | 9 | 28
yoke assy | 5 | 6
shell welding | 14 | 14
final assy | 18 | 18
days including w/e weeks months | 315 45.0 10.5 | 220 31.4 7.3

## Slide 37: Review questions/answers
Phase 1
  Was any problem encountered during construction or final testing understood? Are such problems addressed properly in view of the next steps?
  Was the instrumentation sufficient to evaluate fabrication procedure, validate mechanical and magnetic models and demonstrate that the magnet met specifications?
Yes
Yes



## Slide 38: Backup

## Slide 39: Key Strain Gauges
Strain gauges near edge of part have higher strain.
RE L1 Key
MBH03
LE L1 Key
MBH03
Chart: Key Strain Gauge Values
| 0 | Pres Pressure | skip-fuse 0.1 m | next day | final skip-fuse | 1 filler | next day | 2 filler | 3 filler | next day | 4 filler | 5 filler
02KYRE | -109.489 | -114.4412 | -117.7679 | -122.0422 | -126.6369 | -132.5239 | -130.2899 | -135.0583 | -138.0153 | -140.7153 | -144.7997 | -145.1489
02KYLE | -159.1011 | -172.1517 | -180.1567 | -180.0428 | -194.3197 | -201.8269 | -195.7544 | -209.6282 | -216.1829 | -214.8973 | -221.9483 | -223.8119
03KYRE | -88.4916 | -93.6497 | -96.1386 | -98.8338 | -101.3099 | -102.9561 | -102.2119 | -106.0479 | -105.9888 | -107.8471 | -109.2249 | -109.032
03KYLE | -185.1322 | -196.6237 | -207.4343 | -207.4309 | -220.6115 | -225.186 | -217.6155 | -237.9995 | -240.0574 | -235.7225 | -244.912 | -249.4117

## Slide 40: MBHSP01 Schedule
 | Start | Finish | Actual days | Planned days
coil 02 wind | 9/16/2011 | 10/28/2011 | 42 | 22
coil 02 react | 11/7/2011 | 12/5/2011 | 28 | 29
coil 02 impreg | 12/6/2011 | 2/8/2012 | 64 | 19
coil 03 wind | 10/29/2011 | 12/7/2011 | 39 | 22
coil 03 react | 12/8/2011 | 2/17/2012 | 71 | 29
coil 03 impreg | 2/18/2012 | 3/8/2012 | 19 | 19
coil assy | 3/20/2012 | 3/26/2012 | 6 | 14
collar assy | 3/27/2012 | 4/5/2012 | 9 | 28
yoke assy | 4/13/2012 | 4/18/2012 | 5 | 6
shell welding | 4/19/2012 | 5/3/2012 | 14 | 14
final assy | 5/4/2012 | 5/22/2012 | 18 | 18
days including w/e weeks months |  |  | 315 45.0 10.5 | 220 31.4 7.3