## Slide 1: CERN 2-in-1 Demonstrator Design, Construction and Test Plan M. Karppinen on behalf of CERN-FNAL collaboration
“Demonstrate the feasibility of an accelerator quality 2-m-long 2-in-1 dipole providing > 11 T with an adequate margin and being scalable up to 5.5 m”

## Slide 2: Contributions & Acknowledgements
FNAL:
N, Andreev, G. Apollinari, E. Bartzi, R. Bossert, G. Chlachidze,
F. Nobrega, I. Novitski, G. Wilson, A. Zlobin,...
CERN:
B. Auchmann, A. Ballarino, A. Bonasia, S. Bermudez,
N. Bourcey, A. Cherif, S. Clement, A. Gerardin, M. Guinchard, L. Bottura, C. Kokkinos, B. Favrat, L. Favre, C. Fernandes, P. Fessia, R. Gauthier, B. Holzer, G. Kirby, F. Lackner, G. Maury, J. Mazet, N. Mena, R. Moron-Ballester, J-M. Mucher,
J. Murtomaki, L. Oberli, J-C. Perez, L. Rossi, T. Sahner,
F. Savary, J.-M. Scigliutto, L. Remandet, S. Russenschuck,
S. Sgobba, E. Todesco, D. Tsirigkas,...

## Slide 3: Outline
2-in-1 Demonstrator Parameters
CERN 2-in-1 demonstrator design concept
Magnet assembly process
Structural analysis: straight section
Mechanical model
Structural analysis: end region
Mechanical concepts pros-cons
Magnet design status
Procurement status
QC and documentation
Milestones
Some R&D Topics
Summary
Review questions (Phase 2b) and answers

## Slide 4: 2-in-1 Demonstrator Parameters

## Slide 5: Mechanical Design Features
Separate collared coils
  Most of the coil pre-stress obtained by collaring
  Symmetric loading
  Better control of pre-stress
  Testing of collared coils in 1-in-1 structure
Vertically split yoke
  Assembly process less influenced by friction (vs. horizontal split)
  Closed gap at RT and up to 12 T to provide rigid support for the collared coil
  Better controlled (collared) coil deformation
Welded stainless steel skin

## Slide 6: Pole Loading Concept
Pole wedge
Shim
Filler
wedge
Loading plate

## Slide 7: Pole Loading Concept: Lead End Winding
Ceramic filler piece
Filler wedge
Layer-jump region with cable removed
Outer layer winding pole
Inner layer winding pole

## Slide 8: Pole Loading Concept: Coil
Loading plate
(t = 2 mm)
Vacuum impregnated coil
Filler wedge

## Slide 9: Collared Coil Assembly

## Slide 10: Coil Fabrication

## Slide 11: Coil Assembly

## Slide 12: Coil Assembly

## Slide 13: Coil Assembly
Notes: All on order,

## Slide 14: Coil Assembly

## Slide 15: Coil Assembly

## Slide 16: Coil Assembly

## Slide 17: Coil Assembly

## Slide 18: Coil Assembly

## Slide 19: Collaring

## Slide 20: Collaring

## Slide 21: Collaring

## Slide 22: Collaring

## Slide 23: Collaring

## Slide 24: Collaring

## Slide 25: Collaring

## Slide 26: Collaring
Notes: Recommissioning of the monster press to do.
Load cells being studied.

## Slide 27: Collaring

## Slide 28: CERN 1-in-1 Cold-mass

## Slide 29: CERN 1-in-1 Cold-mass

## Slide 30: CERN 2-in-1 Cold-mass

## Slide 31: CERN 2-in-1 Cold-mass Assembly

## Slide 32: CERN 2-in-1 Cold-mass Assembly

## Slide 33: CERN 2-in-1 Cold-mass Assembly

## Slide 34: CERN 2-in-1 Cold-mass Assembly

## Slide 35: CERN 2-in-1 Cold-mass Assembly

## Slide 36: CERN 2-in-1 Cold-mass Assembly

## Slide 37: CERN 2-in-1 Cold-mass Assembly

## Slide 38: CERN 2-in-1 Cold-mass Assembly

## Slide 39: 1-in-1 with Pole-Loading
Design features:
  Pole shim
  Collar/yoke shim
  Pole adjustment shim
  Gap closing @ room temperature remaining closed to 12 T.
  Stainless-steel shell
(3) is an optional knob.
(2) and (4) must be controlled in order to close gap at RT.
1.
2.
3.
4.

## Slide 40: 2-in-1 with Pole-Loading
Design features:
  Pole shim
  Collar/yoke shim
  Pole adjustment shim
  Gap closing @ room temperature remaining closed to 12 T.
  Stainless-steel shell
(3) is an optional knob.
(2) and (4) must be controlled in order to close gap at RT.
1.
2.
3.
4.
5.

## Slide 41: Pole Loading Concept: 2-in-1 FEA
After CM assembly
at 293 K
At 1.9 K, I = 0 A
B0 = 12 T
Under collaring
press
After collaring
-138 MPa
-138 MPa
-140
0

## Slide 42: Mechanical model
Validate assembly parameters
Feed-back to FEA

## Slide 43: CERN 2-in-1 End Support

## Slide 44: Structural Analysis of End Region

## Slide 45: Pole loading pros and cons
Direct transfer of collaring force into the coils
Allows using different pole for un-reacted/reacted coils
More “knobs” for tuning the pre-load (poles & mid-plane)
Majority of the pre-stress by collaring
Less sensitive to yoke-collar interface
Smaller spring back after collaring
Closed yoke gap at warm and at cold up to 12 T
Easier to adapt for azim. coil size variations
Top shims allows varying coil stress by 50 Mpa
Less sensitive to friction thanks to the closed gap at RT
Easier to instrument
Transition from transverse to axial loading in the ends
Coil fabrication with temporary pole pieces

## Slide 46: Integrated pole pros and cons
Coils more robust to handle
Coils fabrication process easier
“Monoblock” end region
High coil stress during collaring
Majority of the pre-stress by yoke assembly
More complex yoke-collar interface
Larger stress gradients in the coils (bending)
Open yoke gap at warm

## Slide 47: Magnet Design Status
1-in-1 (2 m) magnet assembly and fabrication drawings being completed.
2-in-1 (2 m) magnet fabrication design being completed
Tooling design:
  Coil fabrication tooling competed
  Coil assembly tooling completed
  Collaring tooling completed
  Yoke stacking tooling completed
  Cold mass assembly tooling in progress
5.5 m long tooling design in progress

## Slide 48: Procurement Status
St. steel end spacers made by SLS
ODS copper alloy based wedges (Discup C3/30 material) expected October
Collar laminations (EDM) for the aperture #1 delivered and in QC. Order for fine-blanking collars for aperture #2 to #5 being raised.
1-in-1 yoke laminations delivered, order for 2-in-1 yoke laminations to raise once FNAL design completed
Order for the outer shells raised
Winding and curing tooling operational
Reaction tooling delivered
Reaction furnace commissioning early October
Vacuum impregnation tooling expected early October
Vacuum impregnation system commissioning early October
All handling and collaring tooling expected by Mid-October

## Slide 49: QC & Documentation
FNAL Vector traveller system was implemented at CERN
Procedures and travellers are being written
We currently rely on CERN central metrology services
Dimensional control systems for Nb3Sn coils are being investigated

## Slide 50: CERN Milestones
Practice coils (2 m)
  Practice coils #1-#2 (Cu) Jun..Sep-12
  Practice coil #3 (cored ITER Nb3Sn) Oct..Nov-12
  Practice coil #4 (cored LARP RRP 54/61) Nov..Jan-12
  Mirror test @FNAL (TBC) Feb-12
2-in-1 Demonstrator (2 m)
  Coils for aperture-1 (cored RRP 108/127) Jan..Apr-13
  1-in-1 assembly and test Q2-13
  Coils for aperture-2 (cored PIT) May..Jul-13
  1-in-1 assembly and test Q3-13
  2-in-1 assembly and test Q4-13
  Eventual coil design update (?) Q4-13..Q1-14
5.5 m prototype magnet (Preliminary)
  Selection of mechanical concept Q1-14
  Tooling commissioning Q4-13..Q1-14
  Practice coil (Cu) Q1-14
  Practice coil (Nb3Sn) Q2-14
  Coils for aperture-1 & mirror tests Q4-14
  Collared coil Q1-15
  2-in-1 cold-mass and cryo-magnet Q3-15
  Cold test Q4-15

## Slide 51: Some R&D Topics
Analysis tools (Quench and persistent currents)
Strand
Cored cable
Cable insulation
End spacers
Wedge material
Inter-layer heater
Internal splice
Notes: Move to CERN 2in1

## Slide 52: Summary
Pole loading concept provides several important engineering features:
  Efficient transfer of the collaring force into the coils.
  Good control and easy adjustment of the assembly parameters
  Minimal bending of the coils
Coil technology transfer from FNAL well in progress
  Very fast tooling design phase
  Very much shortened “trial-and-error” period
  Existing procedures based on US HFM projects experience
  Very open communication and sharing of information in both ways
Coil fabrication is in progress at CERN
All key components and tooling for the 2 m model magnet construction in procurement
Construction and test plan has been established

## Slide 53: Answers to Charge
Has technology transfer from FNAL to CERN started in earnest?
  Yes: Coil fabrication technology, traveller system
b. Have the lessons learned in the Phase 1 been used?
  Coil fabrication tooling concept same as at FNAL
  End spacer iterations
  Cable development jointly between CERN and FNAL
c. Have plans been made for development and decision making process of any possible alternative design for coils and/or mechanical structure?
  We first have to build and successfully test both FNAL and CERN 2-in-1 demonstrators. Topic of the 2-in-1 review.
d. Are plans ready for CERN to proceed with coils and cold masses material procurement, construction and testing?
  All tooling and key components in procurement,
  practice coils in progress
  See milestones...

## Slide 54: FEA: Material Data
Structure | Material | Thermal contraction (300-2 K) mm/m | E modulus Gpa warm | E modulus Gpa cold
Coil | impregnated Nb3Sn | 3.3/2.9 (rad./azi.) | 27 | 30
Wedge pole loading | ODS Cu-alloy, Discup | 3.3 | 130 | 130
Wedge inte- grated pole | 316L | 2.9 | 195 | 215
Central post | Ti-6Al-4V | 1.7 | 115 | 125
Collar | YUS 130S | 2.9 | 195 | 215
Keys | Nitronic 40 | 2.64 | 190 | 210
Yoke | Soft iron | 2.05 | 210 | 225
Shell | 304L/316L | 2.9 | 195 | 215

## Slide 55: FEA Model Under the Collaring Press
Integrated pole concept Pole-loading concept

## Slide 56: Press Displacement, Coil Stress
Shim thickness:
  0.1 mm on mid-plane
  0.05 mm radially
Press displacement:
  – 0.025 mm
Peak stress under press:
  148 MPa
  (0.21 mm on pole-wedge)
  0.015 mm pole azimuthal
  0.075 mm still ok
  110 MPa
148 MPa
110 MPa
65 MPa
95 MPa
Integrated pole concept Pole-loading concept

## Slide 57: Collared Coil - Spring Back
Collared-coil deformation:
Prestress after collaring
55 MPa
87 MPa
default 0.2 mm
111 MPa
0.4 mm
62 MPa
0.0 mm
0.09 mm
0.04 mm
0.03 mm
0.11 mm
Integrated pole concept Pole-loading concept

## Slide 58: Coil Stress Evolution 1/2
Yoke assembly @ room temp.
Cryogenic temp.
12 T
-150 MPa

## Slide 59: Coil Stress Evolution 2/2
Minimal azimuthal coil stress:
FEA shows that both designs allow for +/- 0.05 mm adjustment of the collar size.
 | Integrated pole |  |  |  | Pole loading |  |  | 
 | P1 | P2 | M1 | M2 | P1 | P2 | M1 | M2
Under press | -65 | -80 | -148 | -80 | -110 | -65 | -95 | -82
Spring-back | -55 | -55 | -103 | -55 | -87 | -45 | -45 | -73
Yoke assy. | -102 | -57 | -70 | -70 | -137 | -48 | -60 | -110
Cool down | -129 | -35 | -70 | -70 | -111 | -44 | -55 | -90
12 T | -4 | -14 | -147 | -100 | -10 | -37 | -126 | -139
-150 MPa
P1
P2
M1
M2

## Slide 60: Azimutal stress vs. von Mises Stress
Coil stress after yoke assembly at room temperature, pole-loading concept.
Left: von Mises stress, Right: Azimutal stress

## Slide 61: Sensitivity to Coil Material Data
Sensitivity to coil material by using uniform coil modulus (including wedges) instead of Nb3Sn estimate.
Structure | Material | Thermal contraction (300-2 K) mm/m | E modulus Gpa warm | E modulus Gpa cold
Coil approx. | impregnated Nb3Sn | 3.3/2.9 (rad/azi) | 27 | 30
Coil incl. wedge | impregnated Nb3Sn, SS | 3.3/2.9 | 44 | 50
 | Integrated pole |  |  | Pole loading |  |  | 
 | P1 | P2 | M1 | P1 | P2 | M1 | M2
Under press | -65 | -90 | -206 | -122 | -80 | -145 | -95
Spring-back | -60 | -65 | -121 | -99 | -47 | -40 | -85
Yoke assy. | -115 | -70 | -70 | -162 | -70 | -66 | -124
Cool down | -148 | -36 | -70 | -133 | -65 | -60 | -105
12 T | -22 | -2 | -172 | -24 | -6 | -130 | -156
27/30 GPa
44/50 GPa
 | Integrated pole |  |  | Pole loading |  |  | 
 | P1 | P2 | M1 | P1 | P2 | M1 | M2
Under press | -65 | -80 | -148 | -110 | -65 | -95 | -82
Spring-back | -55 | -55 | -103 | -87 | -45 | -45 | -73
Yoke assy. | -102 | -57 | -70 | -137 | -48 | -60 | -110
Cool down | -129 | -35 | -70 | -111 | -44 | -55 | -90
12 T | -4 | -14 | -147 | -10 | -37 | -126 | -139

## Slide 62: Impact of Over-Compression
Impact of over-compression by additional 0.05 mm collaring press displacement.
Values for default displacement
 | Integrated pole |  |  | Pole loading |  |  | 
 | P1 | P2 | M1 | P1 | P2 | M1 | M2
Under press | -65 | -80 | -148 | -110 | -65 | -95 | -82
-205 MPa
-145 MPa
Integrated pole concept Pole-loading concept

## Slide 63: Shape Evolution
Coil deformation
Pole loading, coil inner-contour ellipticity f = b/a
We may review the room-temperature beam separation of 2 x 97.194 mm.
 | Coil ellipticity |  | Coil center shift | 
 | Integrated pole | Pole loading | Integrated pole | Pole loading
Yoke assy. | 0.6% vert. | 0.2% vert. | -0.11 mm | 0.02 mm
Cool down | 0.6% vert. | 0.1% hor. | -0.65 mm | -0.39 mm
12 T | 0.1% vert. | 0.6% hor. | -0.57 mm | -0.3 mm
f = 1.002
f = 0.999
f = 0.994
Δx = 0.39
Δx = 0.3
b
a

## Slide 64: Shape Evolution
Coil deformation
Integrated pole, coil inner-contour ellipticity f = b/a
We may review the room-temperature beam separation of 2 x 97.194 mm.
 | Coil ellipticity |  | Coil center shift | 
 | Integrated pole | Pole loading | Integrated pole | Pole loading
Yoke assy. | 0.6% vert. | 0.2% vert. | -0.11 mm | 0.02 mm
Cool down | 0.6% vert. | 0.1% hor. | -0.65 mm | -0.39 mm
12 T | 0.1% vert. | 0.6% hor. | -0.57 mm | -0.3 mm
f = 1.006
f = 1.006
f = 1.001
Δx = 0.65
Δx = 0.57
b
a
Δx = 0.11

## Slide 65: Collar Stress
Under press
Yoke assembly RT
12 T
Collared Coil
Cryogenic temp.

## Slide 66: Shell Stress, Yoke Gap
Room temp.
weld shrinkage 0.65 mm
weld shrinkage 0.4 mm
shell thickness 10 mm
shell thickness 10 mm
Cryogenic temp.
12 T