## Slide 1: Modeling of Metallic Micro-Protrusions on the surface of High Gradient Structures
A study of coupled thermal and electrical effects giving rise to dark current and thermal breakdown.
Aydin C. Keser
Dr. Gregory Nusinovich
Prof. Thomas Antonsen
IREAP UMD

## Slide 2: Motivation
Micron sized structures on the surface are a source of dark current.
Dark current causes performance loss and breakdown.
Local heating of these structures may affect the emission leading to phase transitions and runaway scenarios
Connection to current accelerator science is already pointed out by previous speakers

## Slide 3: Outline
Point Charge Model and geometry, field enhancement calculations
General Thermal Field Equation and comparison with Fowler Nordheim emission
A simple Space Charge model
Inside the metal E-field calculation
Solution of heat equation
Possible other effects and discussion

## Slide 4: Assumptions
A single cylindrically symmetric, micron sized object with a sharp tip will be simulated.
‘The protrusion’ is made of the same material as the surface. A metal like Cu.
Electrical relaxation times () are very short compared to pulse duration (). Therefore background is essentially static. The surface field is typically around 100-300 MV/m
We will skip the analysis of the evolution or root cause of these protrusions.

## Slide 5: The Point Charge Model
We need to describe the geometry in order to simulate
An image charge model called PCM is a simple and efficient analytical tool to produce arbitrary protrusion geometries.
Experimental measurements of dark current can be reproduced by using this image charge model.
Image charges stacked upon each other with decreasing strength will be considered.

## Slide 6: PCM
Protrusion models can be constructed using the PCM
We build a potential function of the form:
As an image charge potential this describes the potential outside.
identifies the protrusion profile constructed by using an n charge PCM model.
The sharp tip amplifies the background electric field by a factor of ranging from 10 to 100.
Jensen and Lau and O’shea Electron emission contributions to dark current and its relation
to microscopic field enhancement and heating in accelerator structures. PHYS.REV. ST - ACCELERATORS AND BEAMS11, 081001 (2008)

## Slide 7: The Protrusion Geometry
For and we have:

## Slide 8: The Protrusion Geometry
As the number of
charges increase sharper
protrusions are obtained.
We will show that
there exists such
that are
destroyed due to extreme
E-field and temperature
conditions at the tip.
A: n=4; B: n=6 C: n=12;

## Slide 9: The Protrusion Geometry
The ratio of two
successive charges is the
other input parameter in
this model.
I: r=0.69; II: r=0.8; III:r=0.9

## Slide 10: The Boundary Conditions
We solve the Laplace
equation in the shaded
region with the specified
boundary conditions.
The boundary condition for the
surface of the protrusion is
determined by the current density
flowing through the boundary.
The region includes a chunk
from the rest of the surface for a
more realistic calculation
= 0
= 0
= 0
= 0

## Slide 11: The Surface Current
The current in question is due firstly, to the intense electric field amplified at the sharp tip of the structure. This is called Field electron emission and quantified by the Fowler-Nordheim formula.
Secondly, to the high temperatures occurring via a combination of Joule and resistive heating. This is called thermionic emission and described by the Richardson-Laue-Dushman formula.
Although their domains of validity do not overlap, both of these formulas are deduced from the same expression:

## Slide 12: The Surface Current
Here f is the supply function:
And D is the transition probability. A WKB type approximation provides a formula:
Where is the complex momentum of bound state and are the zeros of .

## Slide 13: The Barrier Potential
𝜁
0
-
x
V(x)
0

## Slide 14: Range of E field
We can calculate as
So an electron at Fermi level sees a barrier of
height .
was lower than the Fermi level, there would be no bound electron which is not physical.
So we should avoid this case, by restricting the E field.
For a work function of 4.7 eV, the field should be less then
15 GV/m.
For a background surface field of 300 MV/m, the amplification factor 𝛽 must be less than 50.

## Slide 15: Transition Probability

## Slide 16: Current Density Comparison
Current is mostly
concentrated at the tip,
sharper tips emit
exponentially higher
current.
Our aim is to calculate
E-field inside. At the tip we
expect:
=
which is for
and .
where
Hence should be around

## Slide 17: Current Density Profile

## Slide 18: Space Charge Effects
Barbour et. al. predicts space charge effects should be relevant above 0.4 A/𝜇m².
We need to model space charge effects and incorporate it to our results.
Exact modeling requires PIC codes which is beyond the scope of this study
Feng et. al. studied the transition from FN to space charge limited emission in an 2006 paper.
We will describe our own simpler model.

## Slide 19: Modified Child-Langmuir Model.
Two major concerns:
  There is no definite anode unlike in the CL model.
  There is a 3D emitter with non-trivial geometry
The current is concentrated at the tip
As me move away from the emitting tip, electron density drops very fast due to the 3D geometry.
Therefore the tip radius serves as a good scale over which the space charges are spread.
The tip is assumed to be a planar cathode
Typical range is 20 nm to 300 nm.
Instead of an anode we will use a Neumann Boundary condition.

## Slide 20: Space Charge Model
=0

## Slide 21: Space Charge reduced Electric Field

## Slide 22: Space Charge Reduced Electric Field

## Slide 23: Onset of Space Charge Effect as Current Density grows
Although the space charge effect is not prominent till
very high
current
densities;
consistent
solution of
space
Charge
equations
reduced the
current emission
by up to 3 to 7 fold.

## Slide 24: Simulation Results

## Slide 25: Simulation Results

## Slide 26: Heating
The Heat Equation is
solved subject to the
following initial and
boundary conditions.
For Cu:
As it seems, heat dissipation
takes place predominantly at the
tip and ultimately depends on the
sharpness of the protrusion
i.e. number of charges in PCM.
= 0
=
= 0

## Slide 27: Simulation Results Tip 𝛽=48, Pulse duration 1𝜇s

## Slide 28: Evolution of Temperature at the tip

## Slide 29: Stability and phase transition

## Slide 30: Summary
We have considered a coupled thermal and electrical simulation, including the following effects:
  Space Charge
  General Thermal Field Emission
  Hans Grüneisen effect on the conductivity.
  Joule Heating
  Thermopower is negligible due to small temperature gradient
More on the way:
  Nottingham Heating/cooling
  Better models for space charge and plasma sheath phenomena

## Slide 31: Future Work
Phase transition and mixed phase simulations
  Taylor cones, EM Stress analysis
Thermo mechanical stress is ruled out due to almost harmonic temperature field, but worth revisiting.
Explosive Emission, destroyed tip and micron sized particles in the tube.
Finally tie up everything to observed break down stats.
Acknowledgements:
This work is supported by the DoE