## Slide 1
Anna Macchiolo
L. Andricek, M. Beimforde, H.G. Moser, R. Nisius, R.H. Richter, P. Weigell
Max-Planck-Institut für Physik & MPI Halbleiterlabor (HLL)
Munich
Update on the measurements of the FE-I3 modules interconnected with SLID
In collaboration with
Second TIPP Conference on ….
Anna Macchiolo
3D Integration activities at MPP
AIDA General Meeting 10 April 2013
© Fraunhofer EMFT / Bernd Mueller
L. Andricek, H.G. Moser, R. Nisius, R.H. Richter, S. Terzo, P. Weigell
Max-Planck-Institut für Physik & MPI Semiconductor Laboratory, Munich
In collaboration with

## Slide 2
R&D towards a 3D integrated demonstrator module
R&D towards a fully 3D integrated demonstrator pixel assembly allowing for a minimized inactive area:
from the present ATLAS pixel module design ...
... to a 3D integrated assembly with thin sensors (75-150 mm range) interconnected with the Solid Liquid Interdiffusion technique, SLID, to thin chips (down to 60 mm thickness)
Inter Chip Vias (ICVs) etched in the read-out chip on the front-side on the positions of the original wire bonding pads to route signal and services to the ASIC backside
Production of active edge sensors to achieve a fully four-side buttable module, in collaboration with VTT (Finland)

## Slide 3
MPP 3D R&D Program: demonstrator module
Step I:
  ATLAS FE-I3 ASIC thinned to 200 µm
  n-in-p pixel sensors of 75 mm active thickness
  thin sensors / ASIC interconnection using SLID
  No ICV, integrated fan-out on sensor for service connection
Step II:
  ICV etched in the read-out chip on the front-side on every wire bonding pad to route signal and services to the ASIC backside
  ASIC thinned to 60 µm
  thin sensors /ASIC interconnection using SLID

## Slide 4
MPP 3D R&D Program: demonstrator module
Step I:
  ATLAS FE-I3 ASIC thinned to 200 µm
  n-in-p pixel sensors of 75 mm active thickness
  thin sensors / ASIC interconnection using SLID
  No ICV , integrated fan-out on sensor for service connection
Step II:
  ICV etched in the read-out chip on the front-side on every wire bonding pad to route signal and services to the ASIC backside
  ASIC thinned to 60 µm
  thin sensors /ASIC interconnection using SLID
ICV

## Slide 5
Thin pixel technology at MPP-HLL
n-in-p 6“ wafers with ATLAS FE-I3 compatible sensors
75 mm thick sensors interconnected with SLID to FE-I3 chips, thinned down to 200 mm, at EMFT
n-in-p 6“ wafers with ATLAS FE-I4 sensors (pitch 50 mm x250 mm)
IBL compatible GR  450 mm dead edge
Interconnected to FE-I4 chips with bump-bonding at IZM
FE-I4 modules
75μm and 150μm active thickness
150μm active thickness

## Slide 6
Post irradiation characterization of SLID FE-I3 modules
SLID interconnection is radiation hard and withstands thermal cycling
Good Charge Collection efficiency after irradiation up to 1016 neq/cm2
Number of unconnected channels stable after irradiation and multiple thermal cycles ( +20oC  -50oC)
F=2x1015 neq/cm2
2x1015 neq/cm2
All channels connected
5x1015 neq/cm2
MPV = 4.8 ke
Vbias=600V

## Slide 7
Comparison of CC for n-in-p pixels of different thickness
Higher charge with 150 mm thick sensors up to a fluence of F=(4-5)x1015 neq cm-2  next run of interconnection to FE-I3 chips with ICVs will be performed with wafer of 150 mm active thickness
At higher fluences the charge of thin and thicker sensors tends to equalize
150 mm data still missing
F=(4-5) x1015 neq cm-2
F= 2 x1015 neq cm-2
F= 1016 neq cm-2

## Slide 8
ICV etched in the read-out chip on the front-side on every wire bonding pad of the FE-I3 chip to route signal and services to the ASIC backside
  ASIC thinned to 60 µm
  thin sensors /ASIC interconnection using SLID
Inter Chip Vias on FE-I3 chips
Processing sequence:
Via- and trench etching in Bosch-process, TSV cross-section of 3x10 mm2
insulation with TEOS (low T)
filling of vias with Tungsten
attachment to handle-wafer on the top side and thinning to desired thickness of chip ~ 60 mm
redistribution layer on the backside
SLID-interconnection to sensor wafer.

## Slide 9
Design concept of ICVs on the backside
Backside
Front-side
Process steps:

## Slide 10
Process steps:
Thin with CMP until the opening of the trenches
Design concept of ICVs on the backside
Backside
Front-side

## Slide 11
Process steps:
Thin with CMP until the opening of the trenches
Etch silicon down to the oxide of the ICV
Design concept of ICVs on the backside
Backside
Front-side

## Slide 12
19.02.2013
TSV preparation from back side
  High selectivity of silicon etch doesn’t touch isolation oxide of TSV
TSV preparation from back side shows different etch depths between TSVs and trench (due to bowed shape of trench). This results in specific topology:
Trench height is about 3 µm higher (deeper) than TSV height (TSV height: < 1.0 µm)
Status of ICVs on the backside

## Slide 13
TSV preparation from back side
   Additional CMP process necessary to cut down isolation trench
TSV preparation results in specific topology due to CMP selectivity:
trench height: 375 nm
TSV height: < 1.0 µm
Status of ICVs on the backside

## Slide 14
Process steps:
Thin with CMP until the opening of the trenches
Etch silicon down to the oxide of the ICV
Additional layer of isolation oxide including opening within trenches
Design concept of ICVs on the backside
Backside
Front-side

## Slide 15
Process steps:
Thin with CMP until the opening of the trenches
Etch silicon down to the oxide of the ICV
Additional layer of isolation oxide including opening within trenches
Access to metallic core of TSV by dry etching (if not already done by the dry etch of oxide before)
Metallization including lithography, aluminium etch and resist strip
Backside
Front-side
Design concept of ICVs on the backside
Steps 3-5 have still to be achieved

## Slide 16
ICVs on the FE-I4 chip
  Difficult to apply the ICV process developed for the FE-I3 chip : in the FE-I4 chip a stack of different metal layers and filling structures for many metal layers are present all over the wire bonding pads
  EMFT is setting up a process to etch ICVs from the back-side, still with a reduced cross-section, around 10x30 mm2. The total FE-I4 wafer thickness will be below 150 mm. An aggressive thinning will be performed only locally, below the wire bonding pad.
Metal stack on the FE-I4 wire bonding pad
M1 has to be contacted through the ICV from the backside

## Slide 17
Polysilicon layer
ICVs on the FE-I4 chip
TSV have to be placed between the opening of the poly-silicon layer
Most difficoult step is the etching of the silicon oxide beneath M1 through the ICV

## Slide 18
FE-I4 chip wafer availability
4 FE-I4B wafers ordered by MPP within the common IBL-ATLAS R&D order
  2 or 3 reserved for TSV trials at EMFT, shipment has already started after testing

## Slide 19
Sensors for FE-I4 modules with SLID and ICVs
  SLID interconnection of FE-I4 chips with n-in-p pixel sensors with standard thickness and reduced inactive edges (~450 mm)
  Successive run to interconnect FE-I4 chips with ICV using SLID to active edge n-in-p sensors produced at ADVACAM (spin-off company of VTT)
450 mm

## Slide 20
Active edges with planar n-in-p sensors
FE-I3
50 mm edge
Vbias=15 V
Measurements with radioactive sources: edge pixels show the same charge collection properties as the central ones
Active edge sensors produced at VTT and connected with bump-bonding to FE-I3 and FE-I4 chips

## Slide 21
Charge Collection Efficiency after irradiation
Edge Tracking Efficiency in Beam Tests
F=1 e15
F=2 e15
Active edges with planar n-in-p sensors
99-100% hit efficiency on the area of the pixel implant of the edge column
84% efficiency in the last 50 mm of the sensor edge, beyond last pixel implant

## Slide 22
Conclusions and Outlook
Development of hybrid pixel modules with reduced inactive edge is carried out in collaboration between MPI für Physik and Fraunhofer EMFT
SLID interconnected FE-I3 modules have been characterized before and after irradiation: good mechanical strength and radiation hardness of the SLID interconnection
Thin sensors have shown good charge collection properties after heavy level of radiation
ICVs on FE-I3 chips with very narrow cross-section and high aspect ratio are almost completed
Next step: develop ICVs for the FE-I4 chip etching from the back-side  process under development
Plan to interconnect FE-I4 with ICVs to active edge sensors as demonstrator towards a four-side buttable module

## Slide 23
Back-up slides

## Slide 24
Chip to wafer SLID interconnection (with handle wafer)
For R&D purposes difficult to have same pattern on sensor and chip wafers  a chip to wafer approach is needed. Problems encountered due to the misalignment of chips in the handle wafer with respect to the nominal positions.
Change of pick and place machine (switching to Panasonic FCB3 ) should improve this step for the next interconnection runs

## Slide 25
SLID Interconnection efficiency
Low interconnection efficiency at the center of the wafer  not due to the SLID technology but to the missing opening in the BCB passivation layer used to isolate and planarize the surface of the sensor wafer
Solvable by descum process with SF6 of the remaining wafers for next interconnection runs with ICVs
connected
not connected
Electrically not functional
Insufficiently opened passivation layer
perfectly opened passivation layer

## Slide 26
Connected channel
Unconnected channel
Overview of SLID interconnection efficiency
10
09
08
07
06
90Sr scan
Unconnected
Chip | Unconn. Pixels | Efficiency [%]
3 | 0 | 100
6 | 731 | 70
7 | 713 | 71
8 | 274 | 89
9 | 134 | 94
10 | 0 | 100
Dead columns
03
A. Macchiolo et al, “SLID-ICV Vertical Integration Technology for the ATLAS Pixel Upgrades”, arXiv:1202.6497

## Slide 27
Problem with contact opening in BCB passivation
Badly defined BCB contact openings observed in 2 sensor wafers not yet electroplated  pattern fully compatible with the distribution of unconnected channels in the modules
SLID 10
Good opening in BCB
SLID 6
Bad opening in BCB
BCB (BenzoCycloButhene) passivation deposited to planarize the sensor surface before Cu and Sn electroplating
Unconnected channels are not an intrinsic SLID problem!
Problem cured for the remaining wafers with a descum process of BCB using a SF6 plasma at IZM

## Slide 28
Cluster size | Fraction @ 400V [%] | Fraction @ 500V [%]
1-hit | 81 | 78.6
2-hit | 16 | 19.7
3-hit | 1.1 | 1.1
average cluster size
1.17 hits @ 400V
1.2 hits @ 500V
FE-I4 module charge-sharing
F=4x1015 neq cm-2
perpendicular tracks
400V
500V

## Slide 29
Pixel modules glued and wire-bonded to a detector board designed by the University of Bonn in two versions for FE-I3 and FE-I4
Measurements performed with the ATLAS USBPix read-out system
Set-up for the pixel module characterization

## Slide 30: Process steps development
19.02.2013
TSV preparation from back side
  Additional CMP process necessary to cut down isolation trench
TSV preparation results in specific topology due to CMP selectivity:
trench height: 375 nm
TSV height: < 1.0 µm

## Slide 31: Through Silicon Vias processing
Bonding to handling substrate, thinning to 50 mm
SACVD Pad Planarization, TSV Litho, Etching with Bosch process, cross section ~4x10 mm2, depth=60 mm
Electroplating of Cu on the front side
handling substrate
TSV Isolation with SACVD SiO2 ~ 300 nm
TSV Filling with TiN seed + CVD W
Exposure of W in TSV and Alu spattering for creation of pads on the back-side
handling substrate
handling substrate

## Slide 32
Processing status on the first hot wafer: etching of the dielectric layers accomplished
MPP 3D R&D Program: Through Silicon Vias
total view pad array & test field
total view pad array
8.4 µm (resist on top)
total view pad
8.34 µm (resist on top)
Very narrow TSV allows for their possible use to connect every single pixel

## Slide 33
Connection strength – Pull out tests
FE-I3 mechanical dummies used in the pull tests
Connection strength of the order of 0.01N per pad  similar to bump-bonding and other pixel interconnection technology
X 
y
Pull out test performed with “mechanical” chips placed below the hot chips