## Slide 1
D. Henry / CEA-Leti-Minatec
Contibuting authors : A. Berthelot / R. Cuchet / G. Simon / Y. Lamy / P. Leduc / J. Charbonnier
AIDA Meeting / 08 & 09th of April 2013
TSV vertical based interconnections, overview, state of the art

## Slide 2
Introduction
TSV definitions & process flows
TSV (brief & non-exhaustive) state of the art
Applications examples
Conclusions / prospects
Outline
Introduction
TSV definitions & process flows
TSV (brief & non-exhaustive) state of the art
Applications examples
Conclusions / prospects

## Slide 3
CEA - Leti at a Glance
Founded in 1967 as part of CEA
1,700 researchers
40 start-ups & 265 industrial partners
Over 1,700 patents
210 M€ budget
CEO Dr. Laurent Malier
190 PhD students + 34 post PhD with 70 foreign students (30%)
~ 40M€ CapEx
265 generated in 2010 40% under license
is one of the largest research organizations in Europe, focused on energy, health, information technologies, and national defense
Commissariat à l’Énergie Atomique
et aux Énergies Alternatives
10
16,037
People (10% PhD and Post Doc)
Research centers

## Slide 4
In electronics, a 3D integrated circuit is a chip in which two or more layers of active electronic components are integrated vertically into a single circuit, component or system.
Introduction : What is 3D Integration ?
3D Integration key drivers :
  Form factor decrease
  Performances improvement
  Heterogeneous integration
  Cost decrease
Interposer / substrate
Logic
Memory
passives

## Slide 5
Introduction : Why do we need 3D Integration ?
To solve the following issues :
  Form factor decrease :
    X & Y axis
    Z axis
  Performances improvement
    Decrease R, C, signal delay
    Increase device bandwidth
    Decrease power consumption
  Heterogeneous integration
    Integration of heterogeneous components
    in the same system
  Cost decrese
    Si surface decrease
    Reuse of existing Packaging,
    BEOL & FEOL lines
The key technology of 3D integration is TSV

## Slide 6
Introduction
TSV definitions & process flows
TSV (brief & non-exhaustive) state of the art
Applications examples
Conclusions / prospects
Outline

## Slide 7
Two main families :
  Vias first : vias done before bonding & thinning
  Vias last : vias done after bonding & thinning
TSV definitions
Vias first
Vias last
Pre process
FEOL
Via Exposure
BS process
Via formation
BEOL
Bonding
Middle process
FEOL
Via formation
BEOL
Bonding
Via Exposure
BS process
FEOL
BEOL
Bonding perm. or Temporary
(C2W or W2W)
Via formation
BS process

## Slide 8
TSV families
TSV First (Polysilicon filled)
Trench AR 20, 5x100µm
TSV Middle (Copper or W filled)
AR 7 , 2 x 15µm
AR 10, 10x100µm
W filled
TSV Last (Copper liner or filled)
AR 1 80x80µm
AR 2, 60x120µm
SiO2 flanc
métal RDL
BCB
bulle air sous BCB
60µm
AR 3, 40x120µm
AR 7 , 2 x 15µm

## Slide 9
TSV etching
TSV insulation
TSV planarization
FEOL + BEOL
Bonding
BS Via Exposure
BS Insulation
BS RDL & Passivation
BS Bumping
TSV filling
TSV first / pre process – Detailled process flow

## Slide 10
FEOL
TSV etching
TSV insulation
TSV metalization
TSV planarization
BEOL
Bonding
BS Via Exposure
BS Insulation
BS RDL & Passivation
BS Bumping
TSV Middle – Detailled process flow

## Slide 11
Device thinning
FEOL + BEOL
Bonding
TSV etching
TSV Insulation
TSV metalization + RDL
BS passivation
Under bump metallurgy
BS Bumping
TSV last– Detailled process flow

## Slide 12
Introduction
TSV definitions & process flows
TSV (brief & non-exhaustive) state of the art
Applications examples
Conclusions / prospects
Outline

## Slide 13
TSV first / pre process – State of the art
Silex
  MEMS applications
  Conductive substrate
  TSV Insulation / Si poly
NEC / ELPIDA
  DRAM on logic / 8 levels of memories
  Doped poly TSV
Source : Y. Kurita / NEC – OKI – ELPIDA / ECTC 2007
Source Silex

## Slide 14
LETI
  TSV first for medical application
  SOI substrate
  High voltage
Source : G. Pares / CEA-LETI
TSV after filling & CMP
Final cross section of TSV first + Backside RDL
TSV first / pre process – State of the art

## Slide 15
IBM / 2008
  IR detector
  W filling
TSMC / 2009
  Cu filling
Source : D.Y. Chen / TSMC / IEDM 2009
TSV formation
M1 on TSV
Source : F. Liu / IBM / IEDM 2008
Source : K. Sakuma / IBM / ECTC 2008
TSV Middle – State of the art

## Slide 16
TSV Middle – State of the art
IMEC / 2013
  TSV formation after FEOL / before BEOL
  Cu filling
  AR 10 : 1
Source : E. Beyne / IMEC

## Slide 17
TSV Middle – State of the art
ST Micro - LETI / 2013
  TSV formation after FEOL / before BEOL
  Cu filling
  TSV diameters : 10 µm & 6 µm  AR ~ 9 : 1
Source : J. Michailos / ST Micro

## Slide 18
Source : D. Tezcan / IMEC / ECTC 2007
Source : E. Beyne / IMEC / ITF 2009
TSV last - state of the art
State of the art for TSV last / AR from 1:1 to 3:1
  TSV last approach with temporary bonding
  Low temperature process (< 260°C)
IMEC (Belgium - 2009)
  Tapered via / TSV AR from 2:1 to 3:1
  Cu liner + parylène insulation
  Donut structure

## Slide 19
TSV last - state of the art
Allvia (USA - 2011)
  TSV diameter : 50µm / Thickness : 100 µm / AR 2:1
  Cu liner
Source : Allvia / 2011

## Slide 20
ITRI (Singapore - 2011)
  TSV diameter from 55 to 70 µm / AR from 1.3 to 3:1
  Cu liner
Source : ITRI / 2011
TSV last - state of the art

## Slide 21
Xintec (Taiwan - 2011)
  TSV diameter 60 µm / AR 2:1
  Cu liner
  CIS applications
Source : Xintec / 2011
TSV last - state of the art

## Slide 22
LETI / ST Micro (2008  2013)
  CIS application
  Cu liner
  TSV AR 1 : 1
Production mode since 2009
300 mm production line @ STM Crolles
TSV last - state of the art
Source LETI / 2009 & J. Michailos 2013

## Slide 23
LETI RF & detectors Applications (2012-2013) :
  RF platform development & HEP applications
  AR 1.5 : 1 and 2:1
AR = 2
AR = 1.5
Ni/Au finishing
From: “A Silicon Platform With Through-Silicon Vias for
Heterogeneous RF 3D Modules”, EuMW2011 P. Bar et al.
TSV last - state of the art
TSV AR 2:1
Thin wafer on tape
Redistibution layer

## Slide 24
Introduction
TSV definitions & process flows
TSV (brief & non-exhaustive) state of the art
Applications examples
Conclusions / prospects
Outline

## Slide 25
| 25
Product example : Passive interposer / TSV first
Chip A Chip B
Organic substrate
Chip
Si-IP
Si-IP
TSV
Cu Pillar
Features
  Cu TSV, AR10
  2 to 4 layers routing, Damascene thick copper, L/W 0.5/0.5 x 1.4μm
  Temporary bonding
  Thinning, Stress Monitoring, Warp Management
Under-fill
Ken Miyairi, Masahiro Sunohara, Jean Charbonnier et al, IMAPS, San Diego 09/2012

## Slide 26
| 26
Product example : Active interposer – Partitioning / TSV middle
Cu RDL
Cu TSV
BEOL
Cu TSV
 TSV



Top - Digital
Bottom - Analog
BGA
 Die - die connection
 Die - BGA connection
3D Integration of a Wireless product with Design Partitioning
G. Druais et al., 3DIC 2012
Wide I/O
  SDRAM JEDEC memory standard released Jan. 2012
TSV’s
  Ø 10 μm, AR 8, Pitch 40 μm, Number 1016
  Compatible with FD-SOI
Chip to Chip Cu Pillars
  Ø20 μm, Height 20 μm, Pitch 40 μm, Number 1016
SoC to Substrate Cu Pillars
  Ø55 μm, Height 40 μm, Pitch >200 μm, Number 933
FBGA Package
  Size 12x12mm, Ball Pitch 0.4mm,Ball Matrix 29x29, 1.2 mm thickness

## Slide 27
| 27
Product example : memory on application processor – TSV middle
Source : J. Michailos / ST Micro / 2013

## Slide 28
| 28
Product example : Ultra thin 3D capacitors stacking – TSV last
Thinned 3D capacitors interposer
TSV
PCB or Si wafer
<100µm
Stack target: 4µF/mm2
solder
Sample of IPD of 250nF/mm2 thinned at 60µm
Low profile 3D-IPD for Advanced Wafer Level Packaging
S. Bellenger,et al.IMAPS Minapad 2011
Courtesy of IPDIA

## Slide 29
| 29
Product example : TSV for ATLAS Readout chip – TSV last
Source : J. Wolf / TSV summit / January 2013
Tapered TSV with Cu liner

## Slide 30
| 30
Product example : TSV for Medipix project – TSV last
Product : XRay detector for medical applications
Project started On June 2011
First wafers delivered on January 2012
Single chip
Design
Wafer view
TSV
Back side UBM
Medipix wafer after front side UBM
Technology
TSV
Electrical Tests

## Slide 31
Introduction
TSV definitions & process flows
TSV (brief & non-exhaustive) state of the art
Applications examples
Conclusions / prospects
Outline

## Slide 32
Conclusions / Prospects
Conclusions :
  There are 3 TSV families with differents properties, applications and maturity levels :
    TSV pre-process : R&D level
    TSV Middle : consumer / High end - pre-industrialization level
    TSV last : CIS / Imaging – Mass production
  Lot of companies & R&D centres are working on TSV developments and industrialization
  The 3D & TSV supply chain is starting to be available
  Some industrial products have been already achieved with TSV
Prospects
  For TSV community : to find the “killer application” for TSV adoption in the consumer market
  To disseminate the TSV technologies on other markets :
    Medical
    Spatial / aerospace
    HEP
    …

## Slide 33: Thank you for your attention