## Slide 1
L’amélioration en luminosité du LHC : le projet HL-LHC
AFF Commission Cryogénie et Supraconductivité. Les Journées Thématiques au CERN: LHC, premiers résultats et perspectives.
June 6th-7th, 2013
L’amélioration en luminosité du LHC : le projet HL-LHC
Lucio Rossi
CERN
High Lumi LHC Coordinator

## Slide 2: 10 y plan of LHC
Luminosity L  Nevents/cross section ; Nevents = L * 
Luminostiy will continue to increase in LHC thanks to better understanding of the operations and thanks to interventions during LS
Around 2021 we expect to meet few limitations:
Radiation damage and general wear in the machine and detector
Limitation of the increase in luminosity, which is necessary for physics

## Slide 3: Lumi: main ingredients
energy
Unit of lumi through the talk
Beam current and emittance: involve Inj chain and whole ring
β involve «only» 2 IRs, 600 m.
Beam size
Beam current
Small *  big c

## Slide 4: How to do small *
Quadrupole triplet and D1

## Slide 5: Goals of the HL-LHC established in autumn 2010
Working at levelled luminosity:
Lconst= 5 L0(5 1034) limit pileup and heat depo
Produce 250 fb-1/year 3000 fb-1 by 2035
  Before LHC;  10-15 fb-1
  LHC 2012:  25 fb-1 with extended year
  LHC design : 300 (700) fb-1
Lumi (L0)
Time (h)

## Slide 6: The LHC region(s) to change
1.2 km of LHC !!

## Slide 7: Here the region of low-*

## Slide 8: LHC low-β quads: steps from present LHC toward HL-LHC
LHC (USA & JP, 5-6 m)
70 mm, Bpeak 8 T
1992-2005
LARP TQS & LQ (4m)
90 mm, Bpeak 11 T
2004-2010
LARP HQ
120 mm, Bpeak 12.5 T
2008-2014
LARP & CERN
MQXF
70 mm, Bpeak 8 T
2013-2020

## Slide 9: SC Magnets: evolution with projects

## Slide 10: LSQ of LARP
Target:
200 T/m gradient at 1.9 K
LQS01a: 202 T/m at 1.9 K
LQS01b: 222 T/m at 4.6 K
227 T/m at 1.9 K
LQS03: 208 T/m at 4.6 K
210 T/m at 1.9 K
1st quench: 86% s.s. limit
3.3 m coils
90 mm aperture

## Slide 11: HQ – 1 m long - 120 mm
S. Caspi , H. Felice, G. Sabbi, LBNL
HiLumi
Present LHC

## Slide 12: New collimation in the DS for off-momentum particles: 11 T dipole!
5.5 m Nb3Sn
5.5 m Nb3Sn
3.5 m Collim.
5.5 m Nb3Sn
3.5 m Collim
5.5 m Nb3Sn

## Slide 13: 11 T results and issue
Very good progress
steady state issue still tehre
2nd model

## Slide 14: Beating the geometric reduction factor: Crab Cavity

## Slide 15: Really compact to fit into LHC
Lancaster cavity

## Slide 16: Present design of CCs
RF-Dipole Nb prototype
DQWR prototype (17-Jan-2013)
4-rod in SM18 for RF measurements
BNL
Cockroft Institute
& Lancaster Univ.
ODU (Old Dominion Univ.)
and JLAB (USA)

## Slide 17: First test of RF dipole Apr 2013 (ODU-SLAC at J-LAB)
Courtesy A. Ratti, LBNL

## Slide 18: Thinking to cryomodule and test in SPS (2015-16)
D2
Q4
Q4
D2
IP
11 meters

## Slide 19: Reducing radiation risk at 3000 fb-1 and increase availbility: SC links
1. New Magnets in the IRs and interface to detectors; relocation of Power Supplies via use of SC links
Power convertes are very vulnerable to radiation (SEU)
Interface warm-cold requires intervention for maintenance  remove on surface
ATLAS
CMS

## Slide 20
2150 kA
1 pair 700 m 50 kA – 2016-17
4 pairs 300 m 150 kA – 2018
4 pairs 300 m 150 kA – 2021 Many 6-18 kA HTS Cur.Leads

## Slide 21: MgB2 baseline
27 cables 6000 A
48 cables 600 A
Itot = 190 kA (2 × 95 kA)
Cable structure using MgB2 wires
3 × 6 kA
7 kg/m
900 mHTS/mcable
 = 75
Courtesy A. Ballarino, CERN

## Slide 22: HTS possible for 600 A
“smaller cable”: 24 × 2 × 600 A (2 × 15 kA)
@ 25 K MgB2
@ 65 K (YBCO and Bi-2223)
2 kg/m
200 mHTS/mcable
Novel cable concept using tapes (MgB2, YBCO or YBCO)
A. Ballarino, CERN

## Slide 23: A unique tool: the CERN test station: 20 kA, variable temper.
Completion of 20 m long prototype superconducting link for P7 (50600 A @ 25 K, MgB2)

## Slide 24: Overall new cryo HL-LHC layout
HL-LHC cryo-upgrade:
  2 new cryoplants at P1 and P5 for high luminosity insertions
  1 new cryoplant at P4 for SRF cryomodules
  New cooling circuits at P7 for SC links and deported current feed boxes
  Cryogenic design support for cryo-collimators and 11 T dipoles at P3 and P7

## Slide 25: Low-* and MS region (LSS) cryo
2 new plants for : 18 kW (4.2 K equiv.) delivering 1.8 K to:
2x (4xMQX,D1,D2,CC, Q4,Q5,Q6)
Providing redundancy with the arc
Liberating more cryopower for e-clouds and other effects

## Slide 26: P4 Layout: new cryogenics for SRF module
With interconnection for partial redundancy
(Accepted as baseline)
P4
S34
S45

## Slide 27: P4 cryogenic process & flow diagram
UCB:
6-7 kW @ 4.5 K
cryoplant (tbc)
UX45

## Slide 28: EU strategy update document: approved 30 May 2013by Council
High-priority large-scale scientific activities
After careful analysis of many possible large-scale scientific activities requiring significant resources, sizeable collaborations and sustained commitment, the following four activities have been identified as carrying the highest priority.
c) The discovery of the Higgs boson is the start of a major programme of work to measure this particle’s properties with the highest possible precision for testing the validity of the Standard Model and to search for further new physics at the energy frontier. The LHC is in a unique position to pursue this programme. Europe’s top priority should be the exploitation of the full potential of the LHC, including the high-luminosity upgrade of the machine and detectors with a view to collecting ten times more data than in the initial design, by around 2030. This upgrade programme will also provide further exciting opportunities for the study of flavour physics and the quark-gluon plasma.

## Slide 29: Required Budget
 | Improving Consolidation | Full performance | Total HL-LHC
Mat. (MCHF) | 476 | 360 | 836
Pers. (MCHF) | 182 | 31 | 213
Pers. (FTE-y) | 910 | 160 | 1070
TOT (MCHF) | 658 | 391 | 1,049
Performance Improving Consolidation (PIC): Equipment for which upgrade is a plus but change is a must