## Slide 1: Fils et câbles supraconducteurs du futur
Luca.Bottura@cern.ch
AFF Commission Cryogénie et Supraconductivité. Les Journées Thématiques au CERN: LHC, premiers résultats et perspectives.
June 6th-7th, 2013

## Slide 2: Overview
The drive from the LHC
  LTS wires and cables at 50
  HTS conductors at 25
Beyond the LHC
Summary and conclusions

## Slide 3: Overview
The drive from the LHC
  LTS wires and cables at 50
  HTS conductors at 25
Beyond the LHC
Summary and conclusions

## Slide 4: At 50, LTS’s have reached maturity ?
Data by courtesy of J. Parrell (OST)
ITER wire
HL-LHC wire

## Slide 5: Typical HEP-grade Nb3Sn wires
Micrographs by A. Bonasia (CERN)
Strand diameter: 1.0 mm
Cu:non-Cu: 1.25
Filament diameter: 58 m
Number of filaments: 132
JC (15 T. 4.2 K) > 1575 A/mm2
RRR > 150
UL > 400 m … 800 m
Strand diameter: 1.0 mm
Cu:non-Cu: 1.25
Filament diameter: 48 m
Number of filaments: 192
JC (15 T. 4.2 K) > 1350 A/mm2
RRR > 150
UL > 400 m … 800 m
NOTE: procurement assisted by the special in-kind contribution from France

## Slide 6: Material needs – Nb3Sn
Approximately 26 tons of HEP-grade Nb3Sn will be needed in the coming 5 years
FReSCa-II
DS 11 T MB
MQXF

## Slide 7: Cabling challenges
14 strands, 1.25 mm Powder-in-Tube (PIT) SMC cable
Cabling by A. Bonasia, L. Oberli; graphics by M. Brice (CERN)

## Slide 8: Range of Cabling Parameters
NbTi
Nb3Sn
mechanically unstable
Data by courtesy of R. Scanlan, D. Dietderich, H, Highley (LBNL, Berkeley)
and L. Oberli (CERN)
Notes: Petals were pre-shaped (CRPP found scratches on cable and some strands’ Cr plating was damaged). Final stage conductor was compressed.

## Slide 9
The case of the FRESCA2 cable
Data by courtesy L. Oberli (CERN)
3 years of work
Notes: Petals were pre-shaped (CRPP found scratches on cable and some strands’ Cr plating was damaged). Final stage conductor was compressed.

## Slide 10
Compaction vs. Degradation
Data by courtesy L. Oberli (CERN) and E. Barzi (FNAL)
Lowest degradation is obtained when the compaction is in the range of 85%...86%
This is a delicate, lengthy and difficult optimization
FRESCA2
VLHC
Notes: Petals were pre-shaped (CRPP found scratches on cable and some strands’ Cr plating was damaged). Final stage conductor was compressed.

## Slide 11: DS 11 T MB models
Courtesy of D. Mitchell, FNAL and M. Karppinen, CERN
Fermilab MBHSP02
CERN coil

## Slide 12: MBHSP02 Performance
Test completed in April 2013
  Bmax= 11.7 T – 97.5% of design field B=12 T (78% of SSL at 1.9 K)
Issues to be addressed
  Long training
  Conductor degradation
  Negative ramp rate dependence at dI/dt<20 A/s and 4.5 K
Magnet training
Ramp rate dependence
Tests at Fermilab, reported by courtesy of M. Karppinen, CERN

## Slide 13: From HQ to MQXF
HQ, US-LARP
MQXF, joint development US-LARP and CERN

## Slide 14: LARP HQ performance
The test of HQ02 is on-going, but we see very promising results !
HQ01
Courtesy of G. Chlachidze, FNAL
HQ02a

## Slide 15: Effect of magnetization in dipoles
Nb3Sn magnetization is large, and affects field quality at injection: reduce filament diameter !
Measurement by D. Richter, CERN
Tests at Fermilab, reported by courtesy of M. Karppinen, CERN
150/169
108/127

## Slide 16: Sub-element diameter vs. counts
Small sub-elements (filament diameter) implies complex, costly and risky stacking
Sub-element count
Filament diameter

## Slide 17: A Nb3Sn dream wire for the LHC
JC (kA/mm2)
Dfil (m)
RRR (-)
Performance
Peak field
Cost
Stability Protection
Magnetization Field Quality
Stability
2.5
2
1.5
3
3.5
1
4
200
150
100
50
10
20
50
100
PIT
RRP
target
Dream wire
target performance:
Jc > 3 kA/mm2
Dfil < 20 m
RRR > 100

## Slide 18: Longitudinal strain effects
University of Geneva
Bruker PIT, 1mm
4.2 K
B Bordini et al 2013 Supercond. Sci. Technol. 26 075014 doi:10.1088/0953-2048/26/7/075014
University of Geneva

## Slide 19: Transverse strain effects…
Measurements from University of Geneva

## Slide 20: … more on transverse stress…
Measurements from University of Twente
No irreversible degradation till 200 MPa

## Slide 21: … and even more
Transverse stress sample holder in construction for the FReSCa-1 test facility, at CERN, 200 MPa capability in 10 T field and 32 kA (60 kA) current.
By courtesy of B. Bordini (CERN)

## Slide 22: Overview
The drive from the LHC
  LTS wires and cables at 50
  HTS conductors at 25
Beyond the LHC
Summary and conclusions

## Slide 23: From materials to applications
Superconductors as seen by the eye of a physicist
The grand challenge of today is to find the room temperature superconductors

## Slide 24: From materials to applications
Superconductors as seen by the eye of an engineer
The grand challenge of today is to develop the technology of high-field superconductors

## Slide 25: From materials to applications
Superconductors as seen by the eye of a manager
The grand challenge of today is availability of long lengths of reasonably priced commercial materials
≈100
≈10
≈10
≈1
≈20
≈4

## Slide 26: A future for HTS at the LHC
SC links for the LHC
  Quasi-DC operation
  GHe operation (5 K … 25(35) K)
  Single cables operated at up to 20 kA
  Multi-cable ( 50 high-current cable) assemblies
  Horizontal + Vertical ( 80 m) configuration
  2 kV electrical insulation
Potential for use of MgB2, or other HTS materials in specific location demanding for more margin and/or tolerance
More details in the talk of L. Rossi on HL-LHC
A model of link by A. Ballarino and the TE-MSC-SCD team (CERN)

## Slide 27: Superconductors for the LHC SC Links
 |  |  (mm) | W (mm) | Th (mm) | Tmax (K) | Ic (‡) (A)
(†)MgB2 | wire | < 1 | - | - | 25 | ≥ 400
MgB2 | tape | - | 3.7 | 0.67 | 25 | ≥ 400
YBCO | tape | - | 4 | 0.1 | 35 | ≥ 400
BSCCO 2223 | tape | - | 4 | 0.2 | 35 | ≥ 400
(†) bending radius RB ≤ 80 mm
(‡) applied field B ≤ 0.5 T
Reacted wires
Ltot  1000 km of conductor for series production
By courtesy of A. Ballarino (CERN)
Within reach today

## Slide 28: SC Link cables
+ 600 A
- 600 A
5.6 mm
3 kA @ 25 K
20 kA @ 25 K
Twisted wires for high current
(Dummy cables)
Insulated and twisted tapes, for cables of modest amperage (can be assembled into larger cables for higher current)
Work in TE-MSC-SCD, by courtesy of A. Ballarino (CERN)

## Slide 29: SC Link prototype test
New feed-box for supercritical helium (10 g/s) variable temperature (5 K … > 77 K) and high current (13 kA)
Flexible cryostat to host various cable types and materials, up to 20 m length

## Slide 30: Overview
The drive from the LHC
  LTS wires and cables at 50
  HTS conductors at 25
Beyond the LHC
Summary and conclusions

## Slide 31: BSCCO-2212
Voids in 2212 are a clear issue, that has been recently understood, but not yet mastered
  Is it originated by intrinsic or extrinsic sources ?
  What is a practical means to overcome it ?
As drawn
Quenched at 888 C
Fully processed
In-situ tomography
F. Kametani, et al., Superconductor Science and Technology, 24, 075009(7pp) (2011)

## Slide 32: Improvement by CIPping
15 T, 4.2 K
0.1 µV/cm
1.2 mm diameter
1 meter sample
470 A/mm2
@ 15 T
Core densification result in double JE values to ~470 A/mm2 at 15 T
Wire JE improvement by CIPing
The Business of Science®
By courtesy of Y. Huang (OIST)

## Slide 33: Improvement by OPHT
J. Jiang, E. Hellstrom, D. Larbalestier et al., NHMFL-FSU

## Slide 35: BSCCO-2212, “easy” to cable
R. Scanlan, D. Dietderich, A. Godeke, LBNL
High strength
alloy wire
Oxide
protection
layer
Bi-2212 round wire
High Strength 6+1 Bi-2212 cable
T. Shen, Strand and Cable Engineering Group, Fermilab
nGimat/NCSU

## Slide 36: REBCO – how do you cable tapes ?
Stacks in Conduit Conductor
M. Takayasu, MIT
Cable-On-Round-Core
D. van der Laan
Roebels, W. Goldacker, KIT
Stacked tapes conductors, EuCARD WP7 Task 4, Very High Field Dipole Insert

## Slide 37: Roebel cables measured @ 4.2 K
MEM13, 12 March 2013
Applied trans. = 40 MPa
Roebel cable
2  Nb-Ti Rutherford cables
CERN, Superconductors Lab
J. Fleiter, CERN,
PhD thesis of the University of Grenoble

## Slide 38: Roebel cables results
MEM13, 12 March 2013
Measurements @ CERN in the FReSCa-1 Test Station
Ic (B=9.6 T, 4.2 K) = 3.4 kA
Je (B=9.6 T, 4.2 K) = 400 A/mm2
J. Fleiter, CERN, PhD thesis of the University of Grenoble

## Slide 39: Beyond the LHC
EuCARD2: Develop 10 kA class HTS accelerator cable using Bi-2212 and YBCO. Test stability, magnetization, and strain tolerance
WP10: a 5 T, 40 mm bore
HTS dipole
YBCO

## Slide 40: Summary - LTS
Is Nb3Sn mature ? Yes, and no
  performance of Nb3Sn wires has seen a great boost in the past decade (factor 3 in JC w/r to ITER)
  However, Nb3Sn magnets were never built nor operated in accelerators. Manufacturing, quench, training, protection, strain tolerance, field quality are the focus today to make this new technology a reality
  A dream wire will pave the way for the next step in circular accelerators

## Slide 41: Summary - HTS
Can HTS displace LTS ? Not today
  Much needs to be done to bring this technology to a point where it can be sold as “mature”
    Materials have potential that can be exploited
      OPHT for BSCCO-2212
      Thicker layer for YBCO tapes
      The Holy Grail of a round YBCO wire
  Production quantities, homogeneity and cost need to evolve
  Step-up application demands, from self-field (SC-link is an ideal test-bed) to high-field accelerator magnets (feasibility)