## Slide 1: TowerJazz High Performance SiGe BiCMOS processes

## Slide 3: Comprehensive Technology Portfolio
Mixed-Signal
Digital CMOS
0.35
µm
0.50
µm
BiCMOS, SiGe
Power/BCD
BCD
RFCMOS
RFCMOS and SOI CMOS
BCD
RFCMOS and SOI CMOS
Power/BCD
0.13µm
SiGe
SiGe
SiGe
0.25
µm
0.18/0.16/0.152
µm
0.13
µm
Mixed-Signal
Digital CMOS
Mixed-Signal
Digital CMOS
Mixed-Signal
Digital CMOS
Mixed-Signal
Digital CMOS
eNVM
Image Sensor
(X-Ray & Visible)
Image Sensor
(X-Ray & Visible)
eNVM
Image Sensor
(X-Ray & Visible)
RFCMOS and SOI CMOS
Notes: 3

## Slide 4: RF and HPA Applications and Technology
RF CMOS and SiGe BiCMOS
Cell Phone, WiFi TxRx
Basestation, Specialty Wireless
TV, Satellite, STB Tuners
High Performance SiGe
Optical Fiber Networks
Automotive Radar
60 GHz WiFi, 24GHz Backhaul
Light Peak and Thunderbolt
GPS LNA
SOI Switch and SiGe Power Amplifiers
Power Amplifiers
Antenna Switch
PA Controllers
Complementary BiCMOS
Line Drivers DSL, HomePlug, ATE
HDD PreAmp
DAC, ADC
4
Best-in-class SiGe, RF CMOS, RF models and Design Enablement
RF and Tuners
Front-End Modules
mmWave
High Performance Analog

## Slide 5: Front-End Module Technology
RF CMOS Controller Platform
5V, 0.18um optimized CMOS
Up to 50% die size shrink vs. 0.25um
1.8V Logic, Bipolar, LDMOS options
SiGe PA, through-silicon-via (TSV), IPD
SiGe PA cells for WiFi and Cellular
TSV for low-inductance ground
1.8/3.3/5V CMOS, high res options
IPD (5um dual-Cu in development)
Platform for integration of FEM
Thin-Film SOI (best in class Ron-Coff)
Thick-Film SOI for ease of integration
5V control, LNA, PA/Driver options
Models, design tools and IP
Example: PA Design Library (PADL)
Example: 4T, 6T, 9T SOI Switch IP
Analog / RF Design Services
5
Best-in-class SiGe, RF CMOS, RF models and Design Enablement
Controller
SOI Switch
Power Amplifier
Design Services and IP

## Slide 6: Schematic of Key Features in SiGe BiCMOS platform
The SiGe HBJTs are embedded into complimentary BiCMOS platforms offering high performance RF , analog and digital performances.

## Slide 7: SiGe HBJT device structure
The high-performance bipolar transistors are built “vertically” meaning that the n-p-n structure is created perpendicularly from the top of the wafer down.

## Slide 8: TowerJazz High Speed SiGe Processes
 |  | SBC18HA | SBC18H2 | SBC18H3 | SBC13HA | SBC13H3
Status |  | Prod. | Prod. | Proto. | Proto. | Devel.
CMOS | Voltages | 1.8/3.3V | 1.8/3.3V | 1.8/3.3V | 1.2/3.3V | 1.2/3.3V
HS Bipolar | FT (GHz) | 150 | 200 | 240 | 200 | 240
 | FMAX (GHz) | 190 | 200 | 270 | 200 | 270
 | BVCEO (V) | 2.2 | 1.9 | 1.6 | 1.9 | 1.6
Capacitor | fF/µm2 | 2.8/5.6 | 2/4 | 2.8/5.6 | 2.8/5.6 | 2.8/5.6
Varactor | Q at 20 GHz | 10 | NA | 15 | NA | 15
LPNP | Beta | 32 | 7 | 30 | 7 | 30
There are numerous other SBC18 flavors in production with variations in back end configuration, selection of available devices etc.
Presented data mainly from the SBC18H2/H3 flavors.

## Slide 9: SiGe HBJT’s current and power gain
240 GHz Ft / 270 GHz Fmax devices in mass production.
High frequency performances sustained for wide collector current range.

## Slide 10: SiGe HBJT’s gain vs DC power density
TowerJazz Devices are optimized for low power consumption.

## Slide 11: SiGe HBJT’s Noise
SBC18H4 minimum noise figure at 20Ghz is measured less than 1dB and at 40GHz at only 2dB.
NFMIN is flat across various frequency ranges.

## Slide 12: Circuit examples at ~100GHz: LNAs
SBC18H3
SBC18H2
SBC18H3
SBC18H2
Broad band mm-wave LNAs fabricated in SBC18H2 and SBC18H3
4 identical LNAs built for a 4-channel W-band phased-array receiver
Nearly 30dB of gain above noise floor at 85GHz
Almost perfect matching between LNAs

## Slide 13: RF Grounding: Deep Silicon Vias vs. Through Silicon Vias
Deep Silicon Vias and Through Silicon Vias are available for enhanced RF grounding.
Metal 1
Backside Metallization
Through-Silicon Vias
~100um
Deep Silicon Vias
~10um
Metal 1
Backside Metallization
p++ handle wafer
p- Epi
emitter
collector
~150um

## Slide 14: Bipolar Roadmap
next generation (SBC18H4) is in final development stage ,Fmax=350Ghz , improved noise figure.
SiGe NPN on thick film SOI under development.

## Slide 15: Summary
TowerJazz offer SiGe HBJT devices on 0.35µm, 0.18µm and 0.13µm technology nodes.
TowerJazz SiGe HBJT offers Best in class SiGe Speed / Power and Best in class Noise.
The SiGe HBJTs are embedded into complimentary BiCMOS platforms offering high performance RF, analog and digital performances.

## Slide 17: Complete SBC18H3 Device Roster
Family | Device | Characteristics
CMOS | 1.8V CMOS | Model-exact copy of all other TJ 0.18um CMOS
 | 3.3V CMOS | 
Bipolar | HS NPN | 240 GHz FT / 280 GHz FMAX
 | STD NPN | 55GHz FT / 3.2V BVCEO
 | LPNP | b=35
Resistors | Poly | 235 W/sq and 1000 W/sq
 | Metal | 25 W/sq TiN on M3
Capacitors | Single MIM | 2 or 2.8 fF/µm2
 | Stacked MIM | 4 or 5.6 fF/µm2
Varactors | 1.8V MOS | Q @ 20GHz = 20
 | Hyper-abrupt junction | Q @ 20GHz =15, Tuning Ratio = 21%
RF Diodes | p-i-n | Isolation <-15dB, Insertion loss > -3.5dB at 50GHz
 | Schottky | FC > 800 GHz

## Slide 18: SiGe HBJT basic layout-122 configuration
AA, EP
BP
SC
AREA2
XN
AA
WN
EW
WN
N+ for Nsub
WN
N+ for Nsub
STI
STI
SC Implant
SiGe-Based layer
EW
Emitter Poly
Collector
Collector
Emitter
Base
Base
Native P-sub
WN
N+ for Nsub
WN
N+ for Nsub
STI
STI
SC Implant
SiGe-Based layer
EW
Emitter Poly
Collector
Collector
Emitter
Base
Base
Native P-sub