## Slide 1: Status of H0/H- dumps
M. Delonca – LIU meeting
Thanks to:
C. Maglioni,
A. Patapenka,
C. Pasquino,
A. Perez,
N. Mariani

## Slide 2: Outline
Layout and constraints (reminder)
Numerical results
Brazing tests
Conclusion & next steps

## Slide 3: Layout and constraints (reminder)

## Slide 4: Dump space and layout
KSW4 Magnet
Ceramic chamber
H0/H- dump
EDMS 1163508
New baseline for vacuum chamber: Inconel.
Possibility of using the vacuum chamber for supporting the dump?
Development of the chamber in collaboration with EN-STI.

## Slide 5: Dump space and layout
Area to be modified for dump support and cooling.
What should be integrated within this area?
Cooling system
Support system
Beam monitoring instrumentation
In FRONT
At the BACK
Use of the vacuum chamber?
Mechanical solution with shrinking?
Brazing?

## Slide 6: Loading cases
3 type of beams:
  H-: injected or foil failure
  H0: unstripped particles (depend on foil efficiency)
      98% efficiency (operational case)
      90% efficiency (degraded case)
  H+: stripped particles
¼ Linac 4 pulse, interlock after one pulse.
Steady state, 2% of all H0 .
Steady state, 10% of all H0 .
H- impact angle: assumed ~33mrad (J. Borburgh)

## Slide 7: Material considerations
From specification EDMS 1069240, the material should:
  Be completely non-magnetic
  Induces little eddy current
  Be at least slightly conductive (to not electrically being charged)
Ceramic materials are considered as good candidates.
8 ceramics were individuated and compared taking into account:
    Mechanical properties
    Thermal properties
    Electrical properties
    Degassing
    Activation
Silicon Carbide appears to be the most suitable candidate.

## Slide 8: Actual dump design
Brazing
Reminder:
Internal height of vacuum chamber ≈ 63 mm:
  Only 3.5 mm are available all around the dump for:
    Wires for dump monitoring
    Support (if needed)

## Slide 9: Support (baseline)
Fixation by brazing:
Detailed design starting soon with EN/MME.
Stainless Steel Flange
Cooling channels
SiC dump
Brazed part
Mo piece
In this case, the support and the cooling are guaranteed by the brazing.

## Slide 10: Support (back-up solution)
Fixation by shrinking:
Stainless Steel Flange
Cooling channels
SiC dump
Shrinking
Cu piece (clamped)
In this case, the support is ensured thanks to the shrinking and the cooling is ensured by the Mo piece.
Shrinking ring
A clamping system would be positioned behind the Cu piece to press it onto the SiC dump.

## Slide 11: Numerical results

## Slide 12: Instantaneous ∆T - SiC
Case 3
H- beam
Service Temperature = 1900 °C
Half dump BOTTOM view, T due to 1/4 Linac4 pulse (3)
33mrad

## Slide 13: Instantaneous eq. Stassi – SiC
Half dump BOTTOM view, T due to 1/4 Linac4 pulse (3)
Static Limit in tension: 390 Mpa Safety factor tension: 7.9
Static Limit in compression: 3900 Mpa Safety factor compression: 5.1
Case 3
Fixed support from the back.
H- beam
33mrad

## Slide 14: Steady operation - SiC
Active cooling zone
Analysis done considering the ceramic chamber geometry. Results should remain similar with the Inconel chamber.
Water inlet
Water outlet

## Slide 15: Steady operation - SiC
Half dump BOTTOM view, T due to steady-state operation
Circulating H+ beam
H0 beam
Case 2
Case 1
T acceptable for vacuum? To be confirmed.
Contact for brazing considered as perfect!

## Slide 16: Steady operation - SiC
Half dump TOP view, T due to steady-state operation
T acceptable for vacuum? To be confirmed.
Contact for brazing considered as not perfect (TCC=1000 W/m2.K)
For comparison, TCC for brazed jaws for collimators in two different type of Cu:
10 000 W/m2.K

## Slide 17: Brazing tests

## Slide 18: Brazing tests
The brazing between the dump core and the metallic insert should allow:
  The dump to be supported (totally or in part),
  The good heat exchange for an efficient cooling.
Brazing tests already have been conducted at CERN to braze SiC with Copper (2009, EN/MME, N. Mariani et all):
 | Echantillon 1 | Echantillon 2
Cu | 65*50*12 mm3 | 55*20*12 mm3
SiC | 40.5*24.7*8 mm3 | 24.7*9.6*8 mm3
“small” size
“big” size
In both cases: Ag-Cu-Ti brazing alloy used (840 °C).
Similar (smaller) than our case

## Slide 19: Results “big” size
Visual inspection
Ultrason
Ultrason
Joint braze -> OK except on sides
Cracking visible of SiC and propagation in 55% of the material.

## Slide 20: Results “small” size
Ultrason
Ultrason
Joint braze -> OK
No cracking visible on SiC.
Even thought the CTE of SiC and Cu are different, a joint braze is possible with “small” size (25*10 mm2 for SiC)

## Slide 21: Brazing test: numerical results
Sources: FEM Modeling of Phase II Collimators Jaw’s SiC inserts for brazing Tests – N. Mariani
Analysis with Molybdenum and copper.
Size for Mo sample: 40*20*10+ t mm3 (similar to “big size” one).
Our case: thickness=30 mm
Failure
Safe
2009 results were OK for small size for Cu/SiC but shown breaking for big size.
There are planning good results for Mo/SiC.

## Slide 22: New brazing test
For this project, a campaign of tests has been started:
  Vacuum tests
  Brazing tests
  Characterization of material tests
Choice of the company for the samples of SiC:
  Able to provide the final piece
  Properties of the different SiC
  Price
ESK
Our baseline uses Mo (better than Cu for SiC brazing). Study in collaboration with EN/MME.

## Slide 23: Brazing test: numerical results
Crack initiation
Propagation
Tensile Strength SiC: 250 MPa
Benchmark of 2009 tests (Cu-SiC, 2009 sizes)

## Slide 24: Brazing test: numerical results
Preliminary results.
Limit in tension for SiC: 250 Mpa:
  Safety Factor: 4.8.
To be confirmed with appropriated properties for brazing alloy.
New size (dump size)

## Slide 25: Next steps and conclusion

## Slide 26: Conclusion & next steps
Vacuum tests to be done (samples received)
Brazing tests to be performed (SiC samples received, Mo samples to be delivered)
Dynamic analysis
Cooling circuit integration
Integration of beam instrumentation

## Slide 27: Thanks for your attention

## Slide 28: Backup slides

## Slide 29: Material considerations
From specification EDMS 1069240, the material should:
  Be completely non-magnetic
  Induces little eddy current
  Be at least slightly conductive (to not electrically being charged)
Ceramic materials are considered as good candidates.
8 ceramics were individuated:
    Graphite (CNGS/TDE)
    Boron Nitride (TDI)
    Boron Carbide
    Alumina (used for the ceramic chamber)
    Aluminum Nitride
    Al300 (97,3% of Alumina)
    Silicon Nitride
    Silicon Carbide

## Slide 30: Material considerations
Thermal consideration:
Mechanical consideration:
Electrical consideration:
Beam Charge: parallel RC model
t = cycle length
NO Beam Discharge: series RC model

## Slide 31: Material considerations
Chart: Accumulated charged during 9 seconds
| 1E-4 | 0.9 | 0.90010000000000001 | 1.8 | 1.8001 | 2.7 | 2.7001000000000004 | 3.6 | 3.6001000000000003 | 4.5 | 4.5000999999999998 | 5.4 | 5.4001000000000001 | 6.3 | 6.3000999999999996 | 7.2 | 7.2000999999999999 | 8.1 | 8.1000999999999994 | 9
Graphite | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0 | 1.0675e-07 | 0
silicon carbide | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0 | 1.9789 | 0
Al300 | 22488.6592 | 22173.8327 | 44662.4919 | 44160.8969 | 66649.556 | 65901.029 | 88389.6881 | 87397.0022 | 109885.6614 | 108651.5587 | 131140.2179 | 129667.4098 | 152156.069 | 150447.2363 | 172935.8955 | 170993.689 | 193482.3481 | 191309.3887 | 213798.0479 | 211396.9272
Boron Nitride | 63515.6431 | 5731.478 | 69247.1211 | 6298.4285 | 69814.0716 | 6349.9959 | 69865.6391 | 6354.6863 | 69870.3294 | 6355.1129 | 69870.756 | 6355.1517 | 69870.7948 | 6355.1552 | 69870.7984 | 6355.1555 | 69870.7987 | 6355.1556 | 69870.7987 | 6355.1556
Boron Carbide | 145.6992 | 33.342 | 179.0412 | 41.2982 | 186.9975 | 43.1335 | 188.8327 | 43.5568 | 189.256 | 43.6544 | 189.3537 | 43.6769 | 189.3762 | 43.6821 | 189.3814 | 43.6833 | 189.3826 | 43.6836 | 189.3829 | 43.6837
Alumina | 21377.9967 | 7752.4224 | 29130.4191 | 10647.8446 | 32025.8413 | 11706.1887 | 33084.1854 | 12093.038 | 33471.0347 | 12234.4405 | 33612.4371 | 12286.1263 | 33664.123 | 12305.0187 | 33683.0154 | 12311.9243 | 33689.921 | 12314.4485 | 33692.4452 | 12315.3711
Aluminum Nitride | 24647.2669 | 7843.7853 | 32491.0522 | 10422.3404 | 35069.6073 | 11249.4783 | 35896.7452 | 11514.8041 | 36162.071 | 11599.9141 | 36247.181 | 11627.2153 | 36274.4822 | 11635.9729 | 36283.2398 | 11638.7821 | 36286.049 | 11639.6833 | 36286.9502 | 11639.9723
Silicon Nitride | 21992.5453 | 7887.3873 | 29879.9326 | 10801.4445 | 32793.9898 | 11854.8614 | 33847.4067 | 12235.6663 | 34228.2116 | 12373.3254 | 34365.8706 | 12423.0884 | 34415.6337 | 12441.0775 | 34433.6227 | 12447.5805 | 34440.1257 | 12449.9312 | 34442.4765 | 12450.781
limit 50 V | 50 | 50
Chart: FOMS summary: to be minimized
Boron Nitride | 1.0123
Boron Carbide | 0.87816
Alumina (Al2O3) | 1.3381
Aluminum nitride | 1.4718
Al300 (97.6 % of Al2O3) | 1.4432
Silicon Nitride | 1.5027
Silicon Carbide | 1.3545
Graphite | 2.5821
Only Graphite and Silicon Carbide fulfill the electrical requirements BUT graphite is bad for vacuum.

## Slide 32: Brazing test
Sample dimensions:
2 samples of each dimensions and each SiC type + 4 samples of each dimensions for Mo:
12 samples of SiC,
12 samples of Mo.

## Slide 33: Brazing test
For this project, a campaign of tests has been started:
  Vacuum tests
  Brazing tests
  Characterization of material tests
First step: choice of materials for metallic part:
  CTE as close as possible from the SiC one (to minimize cracking risk when cooling down after brazing)
  Thermal conductivity to be maximize (for an efficient cooling)
Chosen material: Molybdenum

## Slide 34: Brazing test
Second step: choice of company producing the SiC:
  Able to produce the final part with the required dimensions and specifications

## Slide 35: Brazing test
Chart: FOM - Comparison of Silicon Carbide
Hexoloy SG | 0.16438
Ekasic T | 0.16979
Ekasic C | 0.17653
Ekasic G | 0.17267

## Slide 36: Brazing test
Second step: choice of company producing the SiC:
  Price for sample order
Companies able to provide dump piece:
  ESK
    EkaSiC G
    EkaSiC T
  St Gobain
2 samples of each dimensions and each SiC type (ESK SiC only)