## Slide 1: BISMV & H0-H- psb injection VACUUM REQUIREMENTS
C. Pasquino, P. Chiggiato, J. Hansen

## Slide 2: Outline
BISMV vacuum layout;
Graphite outgassing tests;
Simulation results;
PSB injection vacuum layout;
Simulation results;
SiC outgassing rate measurements;
Conclusions and actions.

## Slide 3: BISMV – vacuum layout
3 Sputter Ion pumps Starcell 500
2 Sputter Ion pumps Starcell 300

## Slide 4: Bismv – gas loads
Unbaked tank = water vapor outgassing
Magnets outgassing, measured by I. Wevers (EDMS 1097059)
Graphite dumps:
thermal outgassing

## Slide 5: Graphite outgassing test: pumpdown and thermal outgassing
R4450 LHC collimator graphite
Furnace treatment, 2 hours at 950 ◦C
Bakeout ≈ 24 hours at 200 ◦C
Measurement procedure:
Pumpdown of 24 hours
Bakeout
Step of ∆T = 25 ◦C from room temperature to 200 ◦C
Same procedure is followed for the background signal measurement.
In a second measurement campaign a thermocouple was inserted directly to the graphite block to check the effective temperature reached by the latter.

## Slide 6: Graphite outgassing test: pumpdown
The more the graphite is exposed to air the more it outgas.
1st time: | A few hours only after the vacuum firing treatment;
2nd time: | Following the first measurement and 24 h exposure to the lab air;
3rd time: | Following the second measurement and weeks of exposure to lab air.
1st and 2nd measurement | ≤4*10-10 mbar l/s cm2
3rd measurement | 2*10-09 mbar l/s cm2
Outgassing at 10 hours of pumpdown
EDMS DOCUMENT : 1254422

## Slide 7: Graphite outgassing test at different temperatures
with BG subtracted
Thermal outgassing at 200 ◦C is 4 orders of magnitude higher than at 50 ◦C
Equivalent to 2500 cm2 of SS at RT
TEMPERATURE
PRESSURE

## Slide 8: Electrical network – vacuum analogy simulations
Water vapor outgassing at 100 hours of pumpdown;
Outgassing at 50 ◦C and at 200 ◦C from the graphite;
H2 outgassed from the bulk metal & magnets;
Scrapers or pickups are calculated as equivalent to a dump outgassing
NO HEATING OF THE SURROUNDING CONSIDERED.
P tot = 3*10-9 mbar
P tot = 1*10-8 mbar
+
+

## Slide 9: PSB H- Injection: vacuum layout
Linac 4 H-
PSB ring
SIP 1
SIP 2
RF shield
Stripping foil
Internal dump
Gate Valve

## Slide 10: Electrical network – vacuum analogy simulations
Ptot = 6*10-9 mbar
Ptot = 3*10-9 mbar
Water vapor outgassing at 100 hours of pumpdown;
Outgassing at 50 ◦C and at 175 ◦C from the graphite;
NO HEATING OF THE SURROUNDING CONSIDERED.
H2O driven
H2 driven
If the graphite is treated at the furnace, baked and actively cooled (50 ◦C) the 75 l/s SIP can cope with this extra gas load.

## Slide 11: SiC outgassing rate measurements: pumpdown
EkaSiC T plus and EkaSiC G tested in pumpdown:
No cleaning
No heat treatment
Tested as received (vacuum fired by the company?)
It outgasses as a metallic surface!
No difference between the two different grades.

## Slide 12: SiC outgassing rate measurements: accumulation measurements 1/2
After a bake-out at 150 ◦C, the system is cooled down at room temperature: the variable leak valve is closed in order to isolate the sample from the system.
It is possible to measure the outgassing as a function of the heating temperature.
The evaluation of the background is mandatory.

## Slide 13: SiC outgassing rate measurements: accumulation measurements 2/2
By heating the sample, we can evaluate the outgassing as function of different heating temperatures: the last heating steps on the EkaSiC G are on-going.
The evaluation of the background as function of the heating temperature is needed to calculate the samples outgassing..
 | Q H2 | Q CH4 | Q CO | Q CO2
 | Torr l/s cm2 | Torr l/s cm2 | Torr l/s cm2 | Torr l/s cm2
EkaSiC G | 1.2*10-13 | 1.7*10-15 | 3.5*10-15 | 9.9*10-15
Degassing values at room temperature (20 ◦C) with BG subtracted!
We are background limited…

## Slide 14: Conclusions and actions
The BISMV and the PSB H – injection area have been considered from the vacuum point of view;
The R4450 graphite outgassing has been tested at different temperatures from room temperature up to 200 ◦C;
The results of the simulations show that the graphite is compatible with UHV systems only IF:
Vacuum firing at 950 ◦C for 2 hours;
In – Situ bake out at 200 ◦C for 24 hours;
Working temperature of the graphite block T = 50 ◦C.
Outgassing rate measurements of the SiC are on going but from the very first results, it looks very promising for UHV applications.