## Slide 1
Introduction, Past Work and Future Perspectives:
A Concise Summary
CERN, 18.02.2013
Arno E. Kompatscher
CiS Forschungsinstitut für Mikrosensorik und Photovoltaik GmbH
Erfurt, Germany

## Slide 2: Contents
Personal Introduction
Diploma Thesis
  General outline
  Crystallography
  Martensite
  Preparation
  Analysis and results
    TEM bright field
    TEM selected area diffraction (SAD)
    DSC
  Conclusions

## Slide 3: Contents
Present Work and Future
  4’’ wafer layout
  6’’ wafer layout
  Comparison
    Quad vs. FE-I4 vs. FE-I3
    Ganged & long pixels (Quad, center)
    With and without long pixels (edge)
    Bias grid variations
  Prospects

## Slide 4: Personal Introduction
Arno E. Kompatscher
Born June 4, 1984 in Hall in Tirol
Hometown: Feldkirch, Vorarlberg
Studied physics at University of Vienna
Thesis: Electron microscopy of Ni-Mn-Ga alloys
Mag.rer.nat. (= M.Sc.) on August 28, 2012

## Slide 5: Personal Introduction Home & Education

## Slide 6: Personal Introduction Current Work
Since November 1, 2012:
Early Stage Researcher
  CiS Forschungsinstitut für Mikrosensorik und Photovoltaik GmbH
  Erfurt, Thuringia
Ph.D. via
  Prof. Claus Gößling
  Lehrstuhl Experimentelle Physik IV
  TU Dortmund, North Rhine-Westphalia

## Slide 7: Diploma Thesis
“Phase transformations in Ni-Mn-Ga shape memory alloys subjected to severe plastic deformation”
Supervisor:
Prof. Thomas Waitz
Group:
Physics of Nanostructured Materials (PNM)
Faculty of Physics, University of Vienna
physnano.univie.ac.at

## Slide 8: Diploma Thesis General Outline
Material:
  Ni54Mn25Ga21
  Tetragonal martensite (2M) in initial state
Preparation:
  High pressure torsion (HPT)
  Annealing (heat treatment)
Analysis
  Transmission electron microscopy (TEM)
  Differential scanning calorimetry (DSC)
  X-ray diffractometry (XRD)

## Slide 9: Diploma Thesis Crystallography
Austenite
(L21 Heusler)
Martensite
(I4/mmm, bct)

## Slide 10: Diploma Thesis Martensite
Martensitic phase transformation
Displacive, diffusionless, 1st order
Low temperature martensite
High temperature austenite

## Slide 11: Diploma Thesis Martensite
Different variants of martensite
Unmodulated (2M, initial state), Modulated (7M and 5M)

## Slide 12: Diploma Thesis Preparation
High pressure torsion (HPT):
8 GPa, 50 and 100 turns
d = 0.4±0.1
Degree of deformation :
2.2 · 105 % and 6.5 · 105 %

## Slide 13: Diploma Thesis Analysis
Transmission electron microscopy (TEM)
  Microstructure, grain size, lattice structure, lattice parameters
Differential scanning calorimentry (DSC)
  Heat treatment, ID of phase transitions and respective enthalpies
X-Ray diffractometry (XRD)
  Confirmation of lattice structures and parameters

## Slide 14: Diploma Thesis Analysis
Initial Material: w/o HPT, w/o heat treatment
As deformed: after HPT, w/o heat treatment
After HPT, heat treatment to 420°C
After HPT, heat treatment to 500°C

## Slide 15: Diploma Thesis TEM bright field
Each martensitic variant is internally twinned; grain size several hundreds of m
Strong grain fragmentation due to severe plastic deformation (SPD)
Initial state
As deformed

## Slide 16: Diploma Thesis TEM bright field
Beginnings of grain nucleation; small polygonized grains start to form due to heat treatment (arrows)
Grain nucleation completed, clearly identifyable polygonized grains; grain size 140±6 nm
HT 420°C
HT 500°C

## Slide 17: Diploma Thesis TEM SAD
Tetragonal martensite
Disordered tetragonal (fct), face centered cubic (fcc), no martensite
Initial state
As deformed

## Slide 18: Diploma Thesis TEM SAD
HT 420°C
HT 500°C
Intermediade structure detected: disordered body centered cubic (bcc)
7M martensite observed to be predominant

## Slide 19: Diploma Thesis DSC, initial state
AP = 208 °C
MP = 190 °C

## Slide 20: Diploma Thesis DSC, progression
Change of martensite and austenite peak temperatures (AP, MP) due to heat treatment
Sample 1: short annealing time (10 min at 500 °C, almost directly after HPT)
Sample 7: long annealing time (505 min at temperatures from 500 to 675 °C)

## Slide 21: Diploma Thesis Conclusions
HPT induces strong grain refinement
  Hundreds of m before HPT
  140±6 nm after HPT
HPT causes disordering and suppression of martensitic transformation
Upon heat treatment to 500 °C the adaptive 7M martensitic structure forms

## Slide 22: Diploma Thesis Acknowledgement
Prof. Thomas Waitz, supervisor
Dr. Clemens Mangler, assistant supervisor
Physics of Nanostructured Materials (PNM) Group
Faculty of Physics, University of Vienna
Materials Center Leoben (MCL)
Fonds zur Förderung der wissenschaftlichen Forschung (FWF)

## Slide 23: Present Work and Future

## Slide 24: Present Work & Future Motivation
Past: development of new sensors for insertable B-layer (ATLAS Upgrade Phase I, happening now)
Development of new detectors for
ATLAS Upgrade Phase II (2022)

## Slide 25: Present Work & Future 4‘‘ Wafer
2 x Quad
3 x FE-I4
  Bias grid variants
  Long pixels (old)
  No long pixels (new)
8 x FE-I3
  Several variants
  Special: w/o bias grid
Test structures
  Diodes
  Temp. resistors
  etc.

## Slide 26: Present Work & Future 6‘‘ Wafer
4 x Quad
12 x FE-I4
  Bias grid variants
  Long pixels (old)
  No long pixels (new)
16 x FE-I3
  Several variants
  Special: w/o bias grid
Test structures
  Diodes
  Temp. resistors
  etc.

## Slide 27: Present Work & Future Comparison

## Slide 28: Present Work & Future Comparison
 | Columns | Rows | No. of Pixels
Quad | 160 | 680 | 108.800
FE-I4 | 80 | 336 | 26.880
FE-I3 | 18 | 164 | 2.952
Benefit:
Larger area of active pixels
Problem:
Higher risk of fracture
+
–

## Slide 29: Present Work & Future Ganged & long pixels

## Slide 30: Present Work & Future Ganged & long pixels

## Slide 31: Present Work & Future Comparison
w/ and w/o long pixels
Long pixels
  Removed
Guard rings
  Readjusted
  Now below standard pixels
Benefits:
  Slimmer design
  Precision to the very edge

## Slide 32: Present Work & Future Bias grid variations
Problem:
High leakage currents at HV
Possible Source:
Bias grid (dots)
Proposed Solution:
Varying bias grid layout
Var. 1: bias dots unchanged, grid per column
Var. 2: bias dots unchanged, grid at pixel center
Var. 3: bias dots and grid at pixel center
Control: no bias grid

## Slide 33: Present Work & Future Prospects
Processing of 6‘‘ Wafers (CiS)
Characterization and Analysis (TU Dortmund)
Test beam (DESY, Hamburg)
Increasing radiation hardness

## Slide 34: Thank You for your attention