## Slide 1
Outlook
SM & MM fibres have been qualified Rad. Hard
Standard COTS small-form factors LC connectors have also passed the test.
  [D. Hall, et al., JINST 7 P04014]
Bandwidth of MM fibres shows very little effect due to ionizing doses. [F.J. Achten, et al., 2012 JINST 7 P10021]
Full Cable prototype has been bend tested.
Ready for Pre-Production Testing!
Optical Fibre for HL-LHC
Qualifying optical fibres for high Radiation enviroments
Poster ID: | P17 – 1st Day
Title: | Optical Fibre at HL-LHC
Author: | Dr. B. Todd Huffman (University of Oxford on behalf of the Versatile Link Group)
E-Mail | t.huffman1@physics.ox.ac.uk
Fibre optical test details
In-situ measurment of Radiation Induced Absorption (RIA)
Use 60Co array at RITA (SCK·CEN, Belgium)
  Provides γ radiation at ~0.7 kGy(Si)/hr
  Large water heat bath
  A dose of 200 kGy(Si) was accumulated over 2 weeks
Liquid CO2 evaporative cooling system kept fibres cold
Correct RIA for Temperature-related effects
Ionizing Radiation
+
=
Optical Fibres
→
Test Fibres in Gamma Ray sources
Type | Wavelength | Fibre name
SM | 1310 nm | Corning SMF-28e
SM | 1310 nm | DrakaElite Super RadHard SMF
MM | 850 nm | Corning ClearCurve OM4
MM | 850 nm | DrakaElite Super RadHard GI-MMF
Radiation Qualified Fibres
D. Hall, et al. JINST 7 C01047
Ionizing Radiation
+
=
Optical Fibres
→
Test irradiated Fibres for Tensile Strength
Fibre mechanical test details
“Before-and-After” test. Fibres sent away, irradiated, returned.
Use Mega Curie 60Co array at Inst. Nuclear Energy Research, Taiwan
  Provides γ radiation at ~8.0 kGy(Si)/hr
  Highly uniform exposure of fibre spool.
  Control spool travels with spool under test
Irradiated and un-irradiated spools simultaneously tested
Tensile strength of fibres tested with 2pt Bend Tester
Compare tensile breaking stresses and try to fit an “n-value”
Fibre crushing jaws
Linear precision
motion stage
“weakest-link” hypothesis leads to a
Weibul distribution. The breaking stress
of the fibres follows a statistical distribution
Fit this distribution to find “m” (a nuisance parameter) and the median breaking stress (sm). Repeat this for three jaw closure speeds.
The mean time to fibre failure is related to the “n-value” above and this is fit in the graph to the right. .
B. Arvidsson, et al., 2013 JINST 8 P05011