## Slide 1: Monolithic Active Pixel Sensor Development for the Upgrade of the ALICE Inner Tracker System CERN/INFN/WUHAN ALICE ITS team C. Cavicchioli, P. L. Chalmet, P. Giubilato, H. Hillemanns, A. Junique, T. Kugathasan, A. Lattuca, M. Mager, C. A. Marin Tobon, P. Martinengo, S. Mattiazzo, G. Mazza, H. Mugnier, L. Musa, D. Pantano, J. Rousset, F. Reidt, P. Riedler, W. Snoeys, J. W. van Hoorne, P. Yang

## Slide 2: ALICE Inner Tracking System at present
2 layers of hybrid pixels (SPD)
2 layers of silicon drift detector (SDD)
2 layers of silicon strips (SSD)

## Slide 3: ITS upgrade
Objectives
record collisions:
  Pb-Pb at 50 kHz
  pp at 1MHz
improve impact parameter resolution by a factor 3
improve standalone tracking efficiency and pT resolution
fast insertion/removal for yearly maintenance
installation 2017-2018
New layout
7 layers (3 inner, 4 middle+outer)
reduce:
  X/X0 per layer from 1.14 to 0.3 %
  pixel size from 400x50 to O(30x30) μm2
  first layer radius from 39 to 22 mm
beam pipe outer radius: 19.8 mm
“Upgrade of the Inner Tracking System Conceptual Design Report” http://cds.cern.ch/record/1475244

## Slide 4: SPECIFICATIONS
Lowering integration time would significantly reduce background
Lowering power would significantly reduce material budget
UPPER LIMIT
lower much better !
Nr of bits to code a hit : 35
Fake hit : 10-5 /event

## Slide 5: Starting point : ULTIMATE CHIP in STAR
Developed by IPHC Strasbourg
0.35 μm OPTO process
Rolling shutter and correlated double sampling
20.7x20.7 μm2 pixel size
Power consumption 130 mW/cm2
Deeper submicron technology + development to meet ALICE specifications

## Slide 6: Monolithic detector in TowerJazz 180 nm CMOS
Deep Pwell
Pwell
P-substrate
Nwell
Nwell
Collection Electrode
Pwell
Nwell
P-epitaxial layer
Gate oxide < 4 nm => better transistor radiation tolerance
6 metal layers
Epitaxial layer between 1 and 5 kΩcm, 15-18 μm
Deep Pwell shields Nwell with PMOS transistors from the epitaxial layer and allows full CMOS within the pixel without efficiency loss
  Difficult to deplete epitaxial layer under Pwell far from Nwell collection electrode, but radiation tolerance sufficient (see below)
  Stitching possible up to 200mm wafer scale
NMOS
PMOS

## Slide 7: WAFER SCALE INTEGRATION by STITCHING
Courtesy: N. Guerrini, Rutherford Appleton Laboratory
Vth School on detectors and electronics for high energy physics, astrophysics, and space and medical physics applications, Legnaro, April 2013

## Slide 8: Radiation tolerance example: low voltage NMOS transistor
I0 = 100 nA . W/L
TID (Mrad)
W/L = 0.22 um / 0.18 um -> I0 = 122.2 nA
Curves do not change significantly with irradiation
Extensive testing campaign on transistors now complete and radiation tolerance in excess of ALICE needs

## Slide 9: Developments and plan
3 Developments:
MISTRAL & ASTRAL by IPHC Strasbourg
  Rolling shutter with discriminator at the end of the column or in the pixel
  See presentation earlier this afternoon
CHERWELL by RAL
  Rolling shutter with strixel architecture: “end of column” circuitry
  integrated in pixels
ALPIDE by CERN, INFN, CCNU(China)
  Low power front-end (20.5nA/pixel) with data-driven readout, integration time of a few μs determined by shaping time of the front end
2013 : optimize pixel structure and study different options for the readout architecture to obtain medium/large scale demonstrator
2014 : decide & finalize full scale to be ready for volume production

## Slide 10: Last engineering run (April 2013) back from foundry
CERN/INFN/WUHAN: several matrices and test structures, LVDS driver
RAL: three matrices
IPHC: many matrices, also significant work on zero suppression circuitry.
23.5x31 mm2 total
Several starting materials
Type | epi thickness [µm] | resistivity [Ω cm]
1 | 12 | 30
2 | 18 | > 1k
3 | 30 | > 1k
4 | 40 | > 1k
5 | 20 | 6.2 k
6 | 40 | 7.5 k
7 | CZ | > 700

## Slide 11: EXPLORER : PIXEL SENSOR OPTIMIZATION and MEASUREMENTS

## Slide 12: Starting point MIMOSA32 chips: Variation of Vdiode
Vdiode up to 1.3 V:
  Shift of the spectrum towards higher ADC values
Vdiode larger than 1.4 V:
  No big differences observed
Example:
- Chip: 9B
- Structure: P00
~1V
~1.6V

## Slide 13: Prototype July 2012 submission: Explorer-0
Analog readout for pixel characterization
Readout time decoupled from integration time
Possibility to reverse bias the substrate
Sequential readout with correlated double sampling
Contains two 1.8x1.8mm2 matrices of 20x20 and 30x30 micron pixels with different geometries
PULSED ROWS

## Slide 14: More detail on the collection electrodes

## Slide 15: Charge collection efficiency in Explorer-0
response to 55Fe X-rays for :
  seed (highest signal in 5x5 matrix)
  cluster (5x5 pixels around seed)
55Fe calibration peak  charge calibration (1640 electrons in single pixel)
Seed
Cluster

## Slide 16: Test beam explorer-0
4 layers of explorer-0, modified setup of LePix
6 GeV/c pions
Reverse substrate bias gives extra margin
Penalized by too large input capacitance, corrected for Explorer-1.

## Slide 17: Explorer-1 vs Explorer-0
Comparison of 55Fe cluster signal for Explorer-0 and Explorer-1
Explorer-1 shows ~ 2x signal increase, and similar noise level
Confirms correction on input capacitance, circuit contribution reduced from ~4.6 fF to ~2 fF

## Slide 18: Efficiency & fake hit rate (Explorer-0)
High efficiency at low fake hit rates
Reverse substrate bias gives extra margin

## Slide 19: Efficiency & fake hit rate (Explorer-1)
Explorer-1 results after tests with electrons at DESY, averaged on all diode geometries
after irradiation drop of 10 - 20% in CCE, recovered with back bias
better performance of larger diodes with larger spacing to electronics
wider distance  wider depletion volume  lower input capacitance
better performance of 20 x 20 µm2 at low back bias voltage
detection efficiency above 99% up to 10σ cut, also after irradiation

## Slide 20: (p)ALPIDE FRONT END AND READOUT

## Slide 21: IN-PIXEL HIT DISCRIMINATION
VRESET
Low power (20.5 nA) in-pixel hit discrimination allows other readout architectures
Large gain amplifier/comparator discharges ~ 80fF storage capacitor when the sensor receives a particle hit
Storage capacitor instead of full flip-flop to save space
AMPL/COMP
ENABLE
RESET

## Slide 22: Priority Encoder readout
valid
select
a[0]
a[1]
ADDR[0:1]
ADDR[2:3]
VALID
SELECT
v[0]
v[1]
v[2]
v[3]
sel[0]
sel[1]
sel[2]
sel[3]
Periphery
logic
CLOCK
valid
select
a[0]
a[1]
v[0]
v[1]
v[2]
v[3]
sel[0]
sel[1]
sel[2]
sel[3]
valid
select
a[0]
a[1]
v[0]
v[1]
v[2]
v[3]
sel[0]
sel[1]
sel[2]
sel[3]
valid
select
a[0]
a[1]
v[0]
v[1]
v[2]
v[3]
sel[0]
sel[1]
sel[2]
sel[3]
valid
select
a[0]
a[1]
v[0]
v[1]
v[2]
v[3]
sel[0]
sel[1]
sel[2]
sel[3]
TRIGGER
hierarchical readout
4 inputs basic block repeated to create a larger encoder
1 pixel read per clock cycle
forward path (address encoder) in gray
feed-back path (pixel reset) in red
asynchronous (combinatorial) logic
clock only to periphery, synchronous select only to hit pixels
PIXEL COLUMN

## Slide 23: ALPIDE: ALice PIxel DEtector
Priority encoder
Pixel front-end
512
512
STATE
RESET
512
512
STATE
RESET
0
1023
…
10
VALID
SELECT
ADDR
10
VALID
SELECT
ADDR
Periphery
Data
Bias
Clock
Control
+ trigger
Pulser
Pixel front-end
Priority encoder
Pixel front-end
512
512
STATE
RESET
512
512
STATE
RESET
Pixel front-end
low power in-pixel discriminator
current comparator (bias of ~20 nA)
storage element for hit information
in-matrix address encoder
tree structure to decrease capacitive load of lines
outputs pixel address and resets pixel storage element
loss-less data compression de-randomizing circuit
compresses cluster information in the column
multi-event memory

## Slide 24: Prototype ALPIDE or pALPIDE (512x64 pixels)
~ 1.6 mm
12 µm + 10 µm
22 µm
Part of Priority Encoder
Analog
Front End
Memory
cell
Collection electrode
pALPIDE
~ 12 mm

## Slide 25: pALPIDE first results
Minimum detectable charge <130 e-
At nominal bias (20.5 nA/pixel) and threshold setting:
  Threshold spread 17 e-
  Noise ~ 7 e-
Analog output of one pixel under 55Fe
Noise
Threshold

## Slide 26: Beam test at DESY … now

## Slide 27: CONCLUSIONS
Pixel sensor
  100mV distributed over a few pixels
  Could we get to digital signal by further optimization?
Analog front end design: 40nW*250 000 pixels = 10 mW/cm2
  Promising results, but more work and checking needed.
Digital: looking at solution around 10mW/cm2
Off-chip data transmission ~ 30-50mW/chip or <10mW/cm2
Trying to approach strip level power consumption per unit area and stay below 50mW/cm2
Radiation tolerance sufficient for Alice
Significant work in progress in design and in test

## Slide 28
THANK YOU !