## Slide 1
ATLAS Inner detector upgrade
Small size Fitting developments @ LAPP - Annecy
LAPP ATLAS ID cooling team
Jacques Ballansat, Patrick Baudin, Pierre Delebecque, Nicolas Massol, Thibaut Rambure, Theodore Todorov,
A - Why a small custom fitting ?
B - The development story
C - How to reach industrial standards ?
D - How to go forward ?
Notes: * To start: illustration
* Photo tank which flamed
* Not D ' similar examples for the LAPP
* Drawing: result D ' a simulation
* Simulation carried out afterwards

## Slide 2
A very small fitting
1 – Introduction
The fitting is here

## Slide 3
A very small fitting
1 – Introduction

## Slide 4
A very small fitting
Handling is not so easy !
1 – Introduction

## Slide 5
A very small fitting – the 3 components
Female
Male
Nut
1 – Introduction
Mass=2.2g (IBL version)
Tightening torque ~2N.m
f 8mm

## Slide 6
Fitting welded on a titanium pipe (sample for qualification)
Pipes outer diameters : f 1.77 mm and f 2.27mm (IBL)
Pipes wall thickness: 130 mm (IBL) 70 mm (prototyping)
1 – Introduction
Electron Beam welds

## Slide 7
General view of one pixel detector end
2 – Context

## Slide 8
General view of one pixel detector end (zoomed)
2 – Context

## Slide 9
Zoom on IBL end region
2 – Context

## Slide 10
10
Front view of the IBL end region
2 – Context

## Slide 11
11
Small fitting, less than 8 mm :
  Minimize material budget
  Fit inside a limited volume
Maximum leak rate (He) : 10-5 mbar.l.s-1 @ 1bar (10-8 mbar.l.s-1 @ 20bar retained for validation)
Working temperature : mini -40 °C  maxi +20 °C
Pressure (bar):
Radiation level : 1 Grad
Pipe material : Titanium grade 2
20 mountings / dismountings at least
10
2 – Context - specifications
Specifications

## Slide 12
  Problems and questions :
Leaks on the current disks,
Uncertainties on the disassembly capability
We want to use of titanium instead of aluminium
  Why not using the current end-of-stave Pixel aluminium fittings for IBL ?
  Lessons from pixel detector ? :
Need real quality management
Need qualifications
Need procedures for tests, manufacturing controls and mounting
Need tightening control
3 – Why a custom fitting?
The ATLAS tracker community didn’t want any custom fittings !!

## Slide 13
No industrial standard solution was complying with the IBL specifications (especially the envelope)
  Swagelok: not interested in reducing the size of their connectors
  Staübli : specific design proposed but very costly
………………………………but
3 – Why a custom fitting?

## Slide 14
14
Custom developments was the only solution
So what could we do ?
BUT…it had to be developed according to industrial standards
3 – Why a custom fitting?

## Slide 15
Step 0 : Copy of Luer lock pixel aluminium fitting
  Leak rates [2.10-7 - 10-5 ]mbar.l.s-1 @ 2bar He
  Need to put strength to dismount the fittings
  Same material (aluminium EN AW-6063), same design
Chart: Luer lock tration tests
4 – Custom fitting @ LAPP : a brief history

## Slide 16
  Increasing the angle from 3.5 degrees to about 30 degrees
  Changing the nut/female contact
Step 1 : Aluminium Cone/Cone
  Leak rates : no major changes comparde to Luer lock
  Higher torque needed
  Improve dismounting
4 – Custom fitting @ LAPP : a brief history

## Slide 17
  Material changes Aluminium to Ti grade 2
  Design chosen from first tests on aluminium custom fittings
  Tests done with samples Electron beam welded
Step 2 : Titanium grade 2 (not alloyed) Cone/Cone design 1
  Not sufficiently reliable (some leak tight, some not)
4 – Custom fitting @ LAPP : a brief history

## Slide 18
  Analysis of the behavior:
  Extremity of the male too flexible
  Gap between female and nut induces high stresses
Gap
Step 2 : Titanium grade 2 (not alloyed) Cone/Cone design 1
4 – Custom fitting @ LAPP : a brief history

## Slide 19
  Change of surface contact between the nut and the female part
  Not sufficiently reliable (some leak tight, some not again)
  Problem of surface quality or/and hardiness suspected (material torn from the surface)
Step 2 : Titanium grade 2 (not alloyed) Cone/Cone design 2
  Use of electropolishing, « tribofinition » and Balinit C (carbon+tungten) coating on the cone surfaces
4 – Custom fitting @ LAPP : a brief history
  Did not improve the leak tightness

## Slide 20
  Change material to Ti grade 5 (same hardness as stainless steel used for some commercial fittings)
Step 2 : Titanium grade 5 (alloyed) Cone/Cone design 3
4 – Custom fitting @ LAPP : a brief history
  Some samples made of 316 L stainless steel
  Better results but still do not fit the specs
  Good results (need at least to be tightened at 7N.m

## Slide 21
4 – Custom fitting @ LAPP : a brief history

## Slide 22
  Machining of a toroid shape instead of a cone
  Improve the friction of the threads and the nut/female contact
Step 3 : Titanium grade 5 Toroid/Cone
4 – Custom fitting @ LAPP : a brief history
  Very good results obtained on about 50 combinations
  Hybride assembly male/TA6V – Female 316L
  good results obtained on few combinations

## Slide 23
23
  A spherical shape is less sensitive to angular misalignment
  Same conical female parts as for toroid but a different contact point
Why a sphere ?
Toroïde
Sphere
4 – Custom fitting @ LAPP : a brief history

## Slide 24
24
  MOS2 (molybdenum disulphide) coating on friction surfaces (threads, back of female and nut)
  3 times more efficient compared to raw surfaces
  Graphite treatment proposed by the same company is far from being so convincing
  MOS2 is projected at high speed on the surface and remain attached
  Rad-Hard
Major improvement of the tightening efficiency
MOS2 coating
4 – Custom fitting @ LAPP : a brief history

## Slide 25
25
  After 50 CO2 cool down/warm up in the range of +30°C -50°C / and 6 to 60 bars
5 – Test reception criteria
What is a “good” fitting ?
Leak rate < 10-8mbar.l.s-1
After 20 mountings/dismountings
@ 20 bars He and -50°C
@ 70 bars He / 20°C after a 150 bars pressure test

## Slide 26
26
We are able to manage the R&D phases
Industrial validation and qualification must be carried out according to specific rules/standards
How to obtain an “industrially qualified” fitting ?
Experts (quality management and leak tightness) were asked to audit our project and give advice to define and implement the industrialisation and qualification procedures
6 – Validation of the design – Qualification of the procedures
Production operations (machining, geometrical and dimensional controls, coating, marking) are made by industrial companies

## Slide 27
27
A plan must be defined and written to make sure all aspects are considered. This plan has to be checked and validated by an external authority.
Quality control is different from quality management : defining controls is not enough to unsure a good quality product
Tests devices and procedures must be first themselves qualified to be used for tests operations. Devices must be periodically controlled to check their capabilities.
International standards should be used. They can be adapted to the specific context but it has to be validated.
Parameters ( qualification and production) must be strictly recorded and managed. Any detail must be discussed and formalised with subcontractors. All “strategic” elements must be marked and their life must be tracked.
The requirement levels must be adapted in order to be efficient.
Main rules for an “industrially qualified” fitting
6 – Validation of the design – Qualification of the procedures

## Slide 28
28
Pollution and damages-> at any step of operations (cleaning and protection procedures)
Main technical parameters related to fitting quality
6 – Validation of the design – Qualification of the procedures
Material characteristics – hardness >
Careful with the thermal treatments
Tightening must be carefully managed
Cone and sphere surface quality and geometry-> machining / control

## Slide 29
29
Helium leak test
P
T
20
-50
20
150
30
2
3
4
5
6
1
He
t
t
6 – Final validation and qualification – main tests/ Helium leak test

## Slide 30
30
Helium leak test :
  8 samples tested together (9 sphere/cone junctions, 16 weldings)
7 – Final validation and qualification – main tests/ Helium leak test
  32/50 samples tested
  31/32 validated
  2013-06-17

## Slide 31
31
CO2 cycling:
  50 pressure/ temp cycles
  Samples are leak tested before and after cycling
  Temperature are between 20°C and -40°C
  Pressures are between 60 bars and 10 bars
7 – Final validation and qualification – main tests/ Helium leak test
  15/50 samples tested
  15/15 validated
2012-06-17

## Slide 32
32
  Break test : find the ultimate pressure
  Pressure cycle tests : 1 million pressure cycle tests @ 100 bars (done =>leak test to be performed)
  LN2 shock test
  Repair test : "Repair test : damage a fitting by scratching to create a big leak, repair with glue
  Frost test : cool down of a wet fitting
  20 mountings / dismountings test
Chart: 
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20
 | 1e-09 | 3e-09 | 3.3e-09 | 3.4e-09 | 3.8e-09 | 4e-09 | 5e-09 | 5.5e-09 | 4.1e-09 | 4.1e-09 | 3.6e-09 | 3.9e-09 | 4.1e-09 | 4.2e-09 | 4.1e-09 | 4.6e-09 | 4.6e-09 | 4.9e-09 | 4.9e-09 | 4.7e-09
Break test
Repair test
Multi mountings dismountings test
7 – Final validation and qualification – other tests

## Slide 33
33
  About 300 fittings produced for validation/qualification and production
  200 EB weldings
  All the elements are marked and well protected
  10 different types of tests
8 – Status - Summary
  Qualification in progress
  First cooling lines part (detector side - PP0 to PP1) to be delivered beginning of july
  Second cooling lines part (PP1 to manifold) to be delivered end of 2013
  Installation in the pit spring 2014
Programme
IBL status
Industrial production from “INSTRUVIDE”

## Slide 34
34
  Male fitting and electrical isolator brazed together
  Passed the standard leak test (even at 150 bar pressure)
  Too fragile for IBL (ceramic too thin)
New developments
Male
Ceramic
Ti pipe
9 – New and further developments

## Slide 35
35
9 – Possible applications beyond IBL

## Slide 36
36
10 – Conclusions
  Qualification according to industrial standards almost complete
  Fitting exists in 8mm OD (IBL) and 10mm OD
  Any pipe diameter below ~3mm can be used
  Any pipe wall thickness below ~300 microns can be used (70 microns- ID 1.2mm pipe prototype under test)
  Hybrid Titanium/stainless steel is possible (first tests are OK)
  Integrated ceramic electrical break promising
Perspectives
A small fitting for LHC tracking detectors was successfully designed and produced

## Slide 37
37
9 – Further developments
Thank you

## Slide 38
38
9 – Further developments
Backup slides

## Slide 39
39
New titanium sealed fitting
M14 thread
Seal
Nominal torque : 30 N.m (can probably be reduced)
All elements are made of Titanium

## Slide 40
40
Tightening issues
  Torque applied on the nut can be different from the set value
Torque application center
Torque limitation center
Strengh
Additionnal torque
Use this instead
6 – Validation of the design – Qualification of the procedures