## Slide 1: Progress in EuCARD and plans for EuCARD2
Gijs de Rijk
11th June 2013
CERN

## Slide 2: Contents
EuCARD HFM progress for magnets
  Why this dipole and insert ?
  High field dipole magnet: Fresca2
  Very high field dipole insert
EuCARD2 plans for magnets
  Conductors
  A 5 T accelerator quality HTS dipole magnet : the core of a 20 T magnet
Conclusions

## Slide 3: EuCARD HFMs
Why build a 13 T, 100 mm aperture dipole ?
We need such a magnet for testing high field cables
  A 13 T ‘nominal’ field means it should run at 80% of the short sample current: you need to design it for an ultimate current (92%) of 15 T
  If you do this at 4.2 K you get a 15 T magnet at 86%ss at 1.9 K
  13 T to 15 T range is targeted for HL-LHC type conductors
  It also opens the way to test cables at 1 T or 2 T self field higher than 15 T  the HE-LHC domain
A 100 mm aperture is very generous for cable tests
  But opens the way for serving as 15 T outsert for a dipole insert
  Fresca2 shall be used to test the EuCARD insert to approach 20 T
  Fresca2 will be used as outsert for the EuCARD2 magnet
B =13 T with a 100 mm aperture asks for more than a simple scale-up of the LHC dipole type due to the stress on the Nb3Sn: prepare for HE-LHC magnets

## Slide 4: EuCARD HFMs (2)
Why build a 6 T racetrack HTS dipole insert ?
There is virtually no experience with 20 T dipolar fields
To get close to 20 T will already gain us a lot of valuable experience
We need to get experience with using HTS in a magnet
We need to get experience with high field usage of HTS
Best strategy: start simple, do things step by step, learn while doing
So:
Don’t try to build a 20 T in one go: but build insert and outsert separately
Make them mechanically independent
Start with a racetrack, with a medium current cable, low inductance, short length (we don’t want a launcher)  build a racetrack insert

## Slide 5: Fresca2, conductor
What strand do we need for Fresca2 ?
Performance: Jc ≥ 1200 A/mm2 @15 T, Cu to nonCu ratio 1.25,
For stability: RRR >150, 1 mm diam.
High I, low L: 40 strand cable with < 10% cabling degradation
We started from the NED strand of 1.25 mm
1.25 mm is risky for stability reasons
Makes for very stiff cables: hard to wind
Development done with/in industry:
PIT with Bruker (D)
RRP with OST (US)
What cable do we need ?
I >12kA@15T
40 strands Rutherford cable
<10% cabling degradation, RRR>120

## Slide 6: Fresca2, conductor (2)
A qualification phase yielded the required performance for both vendors
 |  | FRESCA2 specification | PIT | RRP
Strand diameter | (mm) | 1.00 | 1.00 | 1.00
Strand layout | - |  | 192 filaments | 132/169 stack
Sub-element diameter | (mm) | < 50 | ~ 48 | ~ 57
Copper to non-Copper volume ratio | - | 1.25 +/- 0.1 | 1.28 (s = 0.02) | 1.28 (s = 0.02)
JC(12 T, 4.2 K) | (A/mm2) | 2500 | 2497 | 2842
JC(15 T, 4.2 K) | (A/mm2) | 1250 | 1425 | 1623
n-value @15 T and 4.2 K | - | > 30 | ~ 44 (s = 8) | ~ 50 (s = 10)
RRR (after full reaction) | - | > 150 | 192 (average) | 260 (average)
DM at 3 T and 1.9 K | mT | - | 173 | 323
Effective filament diameter | (mm) | - | 44 | 64
Piece length | - |  | 7% below 1 km | 40 % below 1 km
L. Oberli

## Slide 7: Fresca2, conductor (3)
Stability of the strand was an initial worry: 1 mm strand performs ok for both PIT and RRP
Stability margin at low field is > factor 2
L. Oberli

## Slide 8: Fresca2, conductor (4)
L. Oberli
Fresac2 cable:
40 strands, 20.9 mm wide, 1.82 mm thick, rectangular, pitch 120 mm
After one year of development cabling degradation is now reliably ≤5%
The good stability is maintained for the cables.

## Slide 9: Fresac2 magnet (1), design
13T nominal field at 4.2K, max length 1.6m , diameter 1.03m
Very systematic design effort: 3D models, FE models, all details addressed
After an ‘intense’ conceptual design phase a layout was chosen with:
Block coil with flared ends (LBNL style)
Shell, bladder and keys structure
A. Milanese, P. Manil, P. Ferracin, + the whole collaboration

## Slide 10: Fresac2 magnet (2), Structure
J. Munoz, P. Ferracin, J-C. Perez + the whole collaboration
Structure is completed
Tested at CERN at 77K in the LN2 cryostat using Al dummy coils
Preliminary results show a good correspondence with the FE model: permits us to fine-tune the models and to aim for a precisely calibrate pre-stress on the coils

## Slide 11: Fresac2 magnet (3), coil manufacturing
Do a stepwise approach, testing a maximum of intermediate steps, we addressed a large number of outstanding issues
Results: we claim to know how to make the coils: Very useful feedback to the other Nb3Sn projects
Make racetrack coils with small cable (SMC)
Winding tests
Layer jump tests
Cable reaction tests
Insulation development
Make racetrack coils with Fresca2 cable (RMC)
Furnace and impregnation tank
Design the coil in all details
Design de manufacturing procedure and tooling
Make Cu coils
Make final coils

## Slide 12: Fresca2 magnet (4)
Fresca2 results dd June2013:
We have a conductor design for which measurements have shown it is in specification
We have 2 conductor suppliers, and strand for 1 magnet in-house
We have a tested structure
We have the coil manufacturing infrastructure
We know how to make the coils
We have the tooling for half of the coils in house
We know from scaled-down models that the technology can work
We are manufacturing coils now
So we are learning how to build a 15 T large aperture magnet: this looks very much a HE-LHC outsert magnet. It also points to how to build a 15 T accelerator dipole with small aperture

## Slide 13: EuCARD Insert, Conductor
YBCO conductor
Special cable for Ieng=2800A@20T
Will get the experience with YBCO tape despite the fact that the cable is not the final one
We are gaining experience on
Long length tapes
Angular field Ieng dependence
Splicing connection
Stress sensitivity
‘windability’
Conductor current and mechanical stability
Quench development
P. Tixador at al.

## Slide 14: EuCARD Insert, design
At the start in 2009 the WP did not have an idea how to do it. So, they went into uncharted territory.
Simplifications introduced:
Racetrack coils, no free bore
3 double pancake coils, 700 total length but 2 are shorter
Should fit in the central homogeneous field region to avoid axial forces (no launcher)
2x2 tape cable: 2 core conductors of 2 tapes soldered together face to face
Reinforcement of core conductor with CuBe strips
Insert to be mechanically independent of the outsert
Dry operation for coil and T > Tl (2.17 K) to avoid He infiltration

## Slide 15: EuCARD Insert, design
Results:
Mechanical structure designed
  Steel pads
  Shrinking cylinder
New connection scheme designed
  Transpose poles
  Splices of double core conductors
Insulation scheme
  0.03 mm polyester tape

## Slide 16: EuCARD Insert, quench
“In 2009 HTS coils would mostly burn out at the first quench”
Results of EuCARD:
Model software made for HTS coils
Models compared to small coil tests
Feasible quenching scheme for stand alone developed
Feasible quenching scheme for insert in outsert

## Slide 17: EuCARD Insert, conclusions
Many of the completely open issues in the beginning have been addressed
The stand alone test will tell us already what some of the remaining issues are
The final test in an outsert (Fresca2 ?) will be crucial for continuing with 20 T projects

## Slide 18: EuCARD2 : the next step
What is the next step ?
Build a accelerator compatible 5 T dipole with HTS conductor
What is accelerator compatibility (with the HE-LHC in mind) ?
Field quality (bn < few units 10-4)
Free aperture of 40 mm
Be able to ramp up in a few minutes
Cable with > 10kA@20T (less turns, less inductance)
Compatible with high mechanical stresses
Quenchable
Dynamic field quality

## Slide 19: EuCARD2 : the conductor
There are 2 types of conductors available:
YBCO
Tape, cable concepts to be proven (Roebel, Cork, or ?)
Mechanically strong (700 MPa in tension)
High current density Ieng >250A/mm2 @20T (dream 750A/mm2 )
Some known problems with tape stability (delamination)
Bi-2212
Round wire, can be cabled into a Rutherford cable
Mechanically fragile (ceramic in a silver matrix)
Need to react the coil at 850° with a 1° precision in a O2 atmosphere under pressure
Insulation needs to withstand the treatment

## Slide 20: EuCARD2 : the conductor (2)
Program for EuCARD2
Develop with industry strand for both Bi-2212 and YBCO going towards 750 A/mm2 @20T
Develop YBCO cable for >10kA@20T
Develop Bi-2212 cable for >10kA@20T
Test and characterize the cables
These cables can then be directly used for an HTS dipole (2 versions).
Effort shared by 2 geographical poles Europe and US
This will be a “fly or bust” effort: if we cannot make a viable cable out of HTS we will probably have a hard time getting a 20T HE-LHC

## Slide 21: EuCARD2 : the magnet
The EuCARD 2 magnet program:
Construct 5 T HTS magnets
Using a Bi-2212 cable (probably in the USA)
Using a YBCO cable (probably in Europe)
Pull all experience from NED, EuCARD, LARP, LBNL, FNAL, BNL, etc together and build the 2 magnets.
Test the magnets in stand-alone: The YBCO magnet is to be tested at LASA (the USA has >3 stations available)
This will be a “fly or bust” effort: if we cannot make a viable dipole magnet out of HTS we will probably have a hard time getting a 20T HE-LHC.
Once the magnet works in standalone mode other accelerator applications will immediately be attracted to this type of magnet.

## Slide 22: EuCARD2 : the magnet as an insert
The successful magnet(s) will be modified into a smaller structure (no yoke) to be tested as an insert in a high field large aperture magnet (the outsert).
The possible candidate outserts are:
Fresca2 at CERN 13 T – 15 T in a 100 mm bore (under construction)
LD1 at LBNL 15 T in a 150 mm x 100 mm bore (planned)
EDIPO (PSI-CCRP) 12.5 T in a 140 mm x 91 mm bore (operational)
This test should bring us to a real 20 T range dipole

## Slide 23: conclusions
The NED, EuCARD and EuCARD2 HFM projects are a logical chain of projects leading from 8T Nb-Ti magnets to 15 T Nb3Sn magnets and after that to 20 T HTS-Nb3Sn magnets.
We have to watch out not to try and jump stages as history has shown us that SC magnet development is a road full of holes and bumps.
The EuCARD2 stage will tell us whether we got close or we still have to interject additional development stages.