## Slide 1
Polarized Photocathode
SRF Guns
EuCARD´13
June 10-14, 2013, CERN, Geneva, Switzerland
Jochen Teichert
for the Rossendorf SRF gun collaboration
Arnold, P. Lu, P. Murcek, H. Vennekate, R. Xiang (HZDR)
T. Kamps, J. Rudolph (HZB)
P. Kneisel (Jlab), I.Will (MBI)

## Slide 2
1. Introduction
2. Previous GaAs PC activities for RT and SC RF photo guns
- RT RF photo gun test at Novosibirsk
- BNL activities
- HZDR
3. Status and Future of the HZDR SRF gun
- Operation status and Cs2Te PC
- Gun upgrade with improved cavity
4. GaAs PC preparation with new concept and hardware
5. Summary
OUTLINE

## Slide 3
Why GaAs Photocathodes ?
Introduction
cesiated GaAs
is a NEA
(negative electron affinity)
material
with high quantum efficiency
>15 % @ green light
for high currents
One candidate for ERL guns
JLab FEL: 10 mA
Cornell Univ.: 50 mA
Other high-current cathodes:
CsK2Sb
Diamond Amplifier
cesiated GaAs
is the only material
for
polarized electrons
with
GaAs/GaAsP
superlattice crystals
95 % polarization
Used at
CEBAF (Jlab),
MAMI Mainz,
ELSA Bonn, etc.
in DC photoguns

## Slide 4
Introduction
Up to now all the guns of
polarized electrons
are DC guns
since GaAs PCs need
excellent ultra-high vacuum
p < 10-11 mbar
“suitcase”
Loading chamber
Preparation/activation chamber
HV chamber
example: CEBAF load-locked gun (100 kV)
ADVANTAGES OF SRF GUNS
superconducting: low RF losses -> high rep. rates in CW
laser and RF field: short pulses & high gradient -> high brightness
very good vacuum: GaAs -> polarized electrons?
M. Poelker, ERL´07, Daresbury

## Slide 5
Introduction
MOTIVATION up to now: for Future Light Source (ERLs):
Cs2Te (UV) -> GaAs (green) in SRF guns:
allows higher currents and simplifies the drive laser
SRF gun of
high-brightness,
high bunch charge,
polarized electron beams
for
particle physics
ILC, eRHIC, …

## Slide 6
Introduction
Application of the ELBE SRF Gun
high peak current operation for CW-IR-FELs with 13 MHz, 80 pC
high bunch charge (1 nC), low rep-rate (<1 MHz) for pulsed neutron and positron beam production (ToF experiments)
low emittance, medium to high charge with short pulses for THz-radiation and x-rays by inverse Compton backscattering
Parameter | ELBE |  | High Charge
final electron energy | ≤ 9.5 MeV |  | 
RF frequency | 1.3 GHz |  | 
operation mode | CW |  | 
Photo cathode | Cs2Te |  | 
bunch charge | 77 pC | 1 nC | 
repetition rate | 13 MHz | 500 kHz | 
laser pulse (FWHM) | 4 ps | 15 ps | 
transverse rms emittance | 1 mm mrad | 2.5 mm mrad | 
average current | 1 mA | 0.5 mA | 
SAPPHiRE
GaAs
1.6 nC
200 kHz
1.5 µm

## Slide 7
gun half-cell
choke filter
cathode
cathode cooler
LN2 reservoir
cathode transfer rod
Photo cathodes must be
exchangeable without
- breaking the vacuum
warming-up the gun
no particle generation
During exchange
Separate support and
cooling with liquid N2
- Vacuum gap, electrically and thermally isolated
Introduction
Normal-conducting
photocathode in
superconducting cavity

## Slide 8
Transfer
chamber
Transport
chamber
Lock
Cathode transfer rod
linear & rotation
Places for
6 cathodes
Use of semiconductor photo cathodes like
Cs2Te requires a UHV (<109 mbar) exchange
system
Introduction

## Slide 9
Previous GaAs PC activities at RT and SC RF photo guns
Problems with GaAs Photocathodes:
experiment failed due to
- worse vacuum of > 10-9 mbar,
high dark current,
electron backbombardment
BINP activity with a copper (RT) RF photo gun

## Slide 10
GunBNL Polarized SRF Photocathode
Previous GaAs PC activities at RT and SC RF photo guns
Test set-up with ½-cavity installed,
GaAs (Cs,O) preparation system exists,
NEA GaAs PC prepared, QE=10%,
First tests with cavity,
Experiments ongoing
Problems:
- transport of PC from preparation chamber
to gun: vacuum only ~10-9 mbar
- RF heat load in the GaAs crystal
- Solution to prevent e- back bombardment
J. Park, et al., PAC´11, New York, p.385
E. Wang, et. al., PAC´11, New York, p. 388

## Slide 11
R. Xiang, et al., FEL´10, Malmö, p. 449
R.Xiang, et al., IPAC´12, New Orleans, p. 1524
Previous GaAs PC activities at RT and SC RF photo guns
Inside view of the Cs2Te
preparation system
HZDR GaAs PC preparation system for ELBE SRF Gun
Compact GaAs
preparation system (developed within EuCARD)
should be later integrated in the existing
Cs2Te chamber
Problems:
Preparation of GaAs failed
- To many compromises in design
- Low QE, very short storage time

## Slide 12
R. Xiang, Phys. Rev. Special Topics AB 13 043501 (2010)
Transport
chamber
Load-lock
Cs2Te
Pb/Nb
Mo
Mo
Cs2Te
SRF Gun
GaAs
Previous GaAs PC activities at RT and SC RF photo guns
GaAs
Modified PC design for GaAs
With Pierce cone
Inside ɸ 4.75 mm
Outside ɸ 10 mm
Test of non-activated GaAs PC

## Slide 13
No detectable dark current from GaAs-crystal.
time (hh:mm)
Gun with GaAs crystal (0.35mm) and holder
Without RF, PN2=34.52W
With RFmax=5.5MV/m on surface , PN2=35 W
R. Xiang, Task 10.7, EuCARD-SRF Annual Review 2012
Previous GaAs PC activities at RT and SC RF photo guns
HZDR design:
Higher RF field than at BNL, but no dark current or heat load problems

## Slide 14
FEL spectra
FEL detuning curve
stabilty
before
first lasing
optimized
Ekin at gun exit | 3.3 MeV
Micro pulse repetition rate | 13 MHz
Macro pulse repetition rate / length | 1.25 Hz / 2 ms
Beam energy at FEL | 27.9 MeV
Bunch charge / beam current | 20 pC / 260 µA
Photo cathode | Cs2Te
RMS bunch length | 1.6 ps
Normal. RMS emittance | 1 mm mrad
ELBE infrared FEL (20 – 250 µm)
April 11, 2013
Status and future of the HZDR SRF gun
First lasing with the SRF Gun at ELBE – Successful proof of the basic design

## Slide 15
Requirements for Transfer:
Load lock system with < 10-9 mbar to preserve QE ≥ 1 %
Exchange w/o warm-up & in short time and low particle generation
Cathode | Operation days | Extracted charge | Q.E. in gun
#090508Mo | 30 | < 1 C | 0.05%
#070708Mo | 60 | < 1 C | 0.1%
#310309Mo | 109 | < 1 C | 1.1%
#040809Mo | 182 | < 1 C | 0.6%
#230709Mo | 56 | < 1 C | 0.03%
#250310Mo | 427 | 35 C | 1.0%
#090611Mo | 65 | < 1 C | 1.2%
#300311Mo | 76 | 2 C | 1.0 %
#170412Mo | From 12.05.2012 | 236 C | ~ 0.6 %
fresh QE 8.5%, in gun 0.6%
total beam time 575 h
extracted charge 236 C
05.06.2013
problems: multipacting, QE drop-down during storage
Status and future of the HZDR SRF gun
Excellent lifetime of Cs2Te PC in SRF gun
Notes: After preparation the cathodes needs to be stored and later moved into the gun, this is done by a transfer system with the requirements shown above.
What we see at every cathode is an early q-drop right after preparation were we do not know were it comes from
But this is stabilized at about 1% which is enough and can be preserved in the gun
The table shows the operation days and the QE in the gun of the cathode being used in the gun
The best one was in operation for more than 400 days, with an QE of at least 1%
The total beam time was 1013h and the total extracted charge was 35C
Unfortunately the cathode died during a vacuum problem

## Slide 16
fine grain
RRR 300
Nb cavity
large grain
Nb cavity
Fabrication of two new cavities in collaboration with Jlab
(fabrication, treatment and tests)
New cryomodule with
SC solenoid (2 K)
Niowave Inc. (NPS, HZB)
remote controlled xy-table for alignment (77 K)
Status and future of the HZDR SRF gun
Version II gun with high-performance cavity & SC solenoid
JLAB_fine grain-cavity
43 MV/m peak field
in vertical test @ JLab
after He tank welding

## Slide 17
GaAs PC preparation with new conception and hardware
- Preparation has to be performed near the gun
movable system, commissioning and tests in preparation lab
connected to gun during GaAs PC beam time
design of the system based on existing successful systems
(BNL, Daresbury Lab, Univ. Mainz)
- in the prep. system only small plug is handled
(new unified cathode/plug design of HZB, HZDR, Uni Mainz)
financial support of GaAs project:
(not by EuCARD2)
German Helmholtz Society / ARD program:
> 100 k€ investment/year since 2012
new photo cathode labaratory (class 100 clean room)
BMBF collaboration project “photocathodes”
HZB, HZDR, Uni. Mainz, MSU Moscow, SPSPU St. Petersburg
GaAs supper lattice supplier

## Slide 18
preparation and transfer system for GaAs (Cs,O)
Close to SRF gun
XHV chamber 10-11 mbar
Green light
Commissioning planned in 2013
Interesting points:
QE / lifetime
dielectric loss on crystal
temporal response
thermal emittance
potential field emission
dark current
1. GaAs Prep-
system
3. Connect to gun
2. Storage and transport
Status and future of the HZDR SRF gun

## Slide 19
Cathode 106 mm long
plug ɸ10mm x 6mm (HZB, HZDR, Mainz standard)
Easier for transport
Easier for heat-cleaning
GaAs
VG Scienta sample handling
Transport only small plugs (up to 6 plugs)
fixed on VG Scienta
holders for storage
and transport
Status and future of the HZDR SRF gun

## Slide 20
topic | discussion | risk
GaAs cathode preparation | successfully demonstrated at many places | low
e-polarision | using GaAs super lattices | low
SRF gun concept | demonstrated at HZDR/ELBE | low
PC lifetime in gun | vacuum ok; ion back bombardment low new unexpected problems? | medium
PC compatible with SC RF field | dark current, RF losses etc. degradation of cavity performance | medium
Beam brightness, emittance | high performance cavity Laser shaping, advanced emittance compensation | medium
QE, thermal emitt. time response, etc. | Experiences and solutions from DC guns | low
Summary

## Slide 21
Acknowledgement
We acknowledge the support of the European Community-Research Infrastructure Activity under the FP7 programme since 2009 (EuCARD, contract number 227579) as well as the support of the German Federal Ministry of Education and Research grant 05 ES4BR1/8.
THANK YOU FOR ATTENTION