## Slide 1: EucARD Annual Meeting 11 June 2013, CERN
WP10 - SRF
“SC RF technology for higher intensity proton accelerators & higher energy electron linacs”

## Slide 2: WP10-SRF Task ‘Patchwork’

## Slide 3: WP10-SRF Fifteen Institutes
Krakow
Swierk
IN2P3
Les deux infinis

## Slide 4
High Gradient barrier (ILC, SPL, ESS, etc…)  Task 10.2, 10.4
High Q0 barrier (efficiency, duty cycle)  Task 10.4
High RF Power barrier (HPPAs)  Task 10.2, 10.8
High Stability and Reliability barriers (ILC, XFEL, ADS)  Task 10.5, 10.6
Low Beta barrier (e.g. Spiral2 =0.07)  Task 10.4
Industrialization and cost barrier (ILC)  Task 10.8
New Applications barrier:
  Crab cavities (LHC, ILC)  Task 10.3
  SC-RF Gun (electrons)  Task 10.4, 10.7
  Energy Recovery Linac (ALICE, BERLinPro)  Task 10.5, 10.7
Pushing Accelerator Performance Barriers
R&D is needed to advance the Superconducting RF Technology for Accelerator applications

## Slide 5: WP10-SRF 1st Annual Review 7-9 April 2010, Cockcroft Institute, Daresbury
45 Participants = 47 Registrants – 2 Visa Problems (@ LAL and FZD)
14/15 Partner Institutes represented
https://espace.cern.ch/EuCARD/AnnualMeeting2010/default.aspx

## Slide 6: WP10-SRF 2nd Annual Review 4-5 May 2011, IN2P3 – Inst. Phys. Nucl. Orsay
42 Participants, including the 2 Coordinators + 7 Task Leaders
14/15 Partner Institutes represented
http://indico.cern.ch/internalPage.py?pageId=7&confId=115634

## Slide 7: WP10-SRF 3rd Annual Review 29-30 March 2012, HZB, Berlin
45 Participants, including the 2 Coordinators + 6 Task Leaders (1 excused)
13/15 Partner Institutes represented
http://www.bessy.de/indico/conferenceDisplay.py?confId=380

## Slide 8: WP10-SRF PhD Students
Ben Hall, Lancaster University T10.3
Ben Woolley, Lancaster University T10.3
Pei Zhang, Manchester University, working at DESY T10.5
Thomas Fligsen, Rostock University T10.5
Nawin Juntong, Manchester University T10.5
Chris Glasman, Manchester University T10.5
Jeniffa Rudolph, HZ Berlin, working partly at Rossendorf T10.7
André Arnold, HZD Rossendorf T10.7

## Slide 9
Proposal to link to TTC Infrastructure database under construction
+ Database on SRF Accelerators in Europe, linked to the TTC server.
WP10.1: Coordination and Communication
Deliverable:

## Slide 10
SRF Accelerators
in Europe
or involving EU labs:
6 de-commissioned,
11 in operation,
4 in construction,
10 under design.
Name | Particles | # cavities |  | Type | Material | Gradient | Mode | T | Status | Location
HERA | electrons, positrons | 16 | 500 MHz | b=1 elliptical 4-cell | Nb | 4.0 MV/m | CW | 4.2 K | de-commissioned | DESY
LEP200 | electrons, positrons | 16 272 | 352 MHz | b=1 elliptical 4-cell | Nb Nb/Cu | 5 MV/m 7 MV/m | CW | 4.5 K | de-commissioned | CERN
LISA | electrons | 4 | 500 MHz | b=1 elliptical 4-cell | Nb | 6 MV/m | pulsed | 4.2 K | de-commissioned | LN Frascati
MACSE | electrons | 5 | 1.5 GHz | b=1 elliptical 5-cell | Nb | 10 MV/m | CW | 1.8 K | de-commissioned | CEA-Saclay
Tandem PA | ions | 16 34 | 81 MHz 135 MHz | b=0.085 helix l/2 b=0.085 helix l | Nb | 2.2 MV/m | CW | 4.2 K | de-commissioned | CEA-Saclay
Tandem PA | ions |  |  |  |  |  |  |  | de-commissioned | Daresbury
ALICE | electrons | 2 2 | 1.3 GHz | b=1 elliptical 9-cell b=1 elliptical 9-cell | Nb | 3-5 MV/m 13.5 MV/m | pulsed | 2 K | operation | Daresbury
ALPI | ions | 2 12 50 58 | 80 MHz 80 MHz 160 MHz 160 MHz | b=0.0255 RFQ b=0.055 QW b=0.13 QW b=0.13 QW | Nb Nb Pb/Cu Nb/Cu | 2-3 MV/m 4 MV/m 2.7 MV/m 4.8 MV/m | CW | 4.5 K | operation de-commissioned | LN Legnaro
DIAMOND | electrons | 2 | 500 MHz | b=1 elliptical 1-cell | Nb | 6.5 MV/m | CW | 4.5 K | operation | Oxford
ELBE | electrons | 1 4 | 1.3 GHz | b=1 elliptical 3½-cell b=1 elliptical 9-cell | Nb | 8 MV/m 9 MV/m | CW | 2 K | operation | HZDR
ELETTRA | electrons | 1 | 1.5 GHz | b=1 elliptical 2-cell | Nb | 5 MV/m | CW | 4.5 K | operation | Trieste
FLASH | electrons | 56 4 | 1.3 GHz 3.9 GHz | b=1 elliptical 9-cell | Nb | 20-30 MV/m 14.5 MV/m | pulsed | 2 K | operation | DESY
ISOLDE | ions | 12 20 | 101 MHz | b=0.063 QW b=0.103 QW | Nb/Cu | 6 MV/m | CW | 4.5 K | operation | CERN
LHC | protons, ions | 16 | 400 MHz | b=1 elliptical 1-cell | Nb/Cu | 6 MV/m | CW | 4.5 K | operation | CERN
S-DALINAC | electrons | 1 1 10 | 3 GHz | b=0.85 elliptical 2-cell b=1 elliptical 5-cell b=1 elliptical 20-cell | Nb | 5 MV/m 5 MV/m 5 MV/m | CW | 2 K | operation | Darmstadt
SLS | electrons | 1 | 1.5 GHz | b=1 elliptical 2-cell | Nb | 5 MV/m | CW | 4.5 K | operation | PSI
SOLEIL | electrons | 4 | 352 MHz | b=1 elliptical 1-cell | Nb/Cu | 6 MV/m | CW | 4.2 K | operation | SOLEIL
BERLinPro | electrons | 1 3 3 | 1.3 GHz | b=1 elliptical 1½-cell b=1 elliptical 2-cell b=1 elliptical 7-cell | Nb | 20 MV/m 18 MV/m | CW | 2 K | construction | HZB
E-XFEL | electrons | 808 8 | 1.3 GHz 3.9 GHz | b=1 elliptical 9-cell | Nb | 24 MV/m 15 MV/m | pulsed | 2 K | construction | Hamburg
IFMIF-EVEDA | D+ | 8 | 175 MHz | b=0.094 HW | Nb | 4.5 MV/m | CW | 4.5 K | construction | Rokkasho
SPIRAL2 | D+, ions A/Q = 3 | 12 14 | 88 MHz | b=0.07 QW b=0.12 QW | Nb | 6.5 MV/m 6.5 MV/m | CW | 4.2 K | construction | GANIL
ESS | protons | 28 64 112 | 352 MHz 704 MHz 704 MHz | b=0.5 double spoke b=0.7 elliptical 5-cell b=0.9 elliptical 5-cell | Nb | 8 MV/m 15.5 MV/m 18.2 MV/m | pulsed | 4.5 K | design | Lund
EURISOL Driver | protons, deutons, H-, 3He2+ | 16 56 36 45 40 24 | 176 MHz 176 MHz 352 MHz 704 MHz 704 MHz 704 MHz | b=0.09 HW b=0.15 HW b=0.3 triple spoke b=0.47 elliptical 5-cell b=0.65 elliptical 5-cell b=0.76 elliptical 5-cell | Nb | 4.7 MV/m 5.2 MV/m 5.8 MV/m 12 MV/m 15 MV/m 18 MV/m | CW | 2 K | design | -
EURISOL PA | ions, A/Q from 2 to 8 | 15 27 80 154 | 88 MHz 88 MHz 176 MHz 264 MHz | b=0.065 QWR b=0.14 QWR b=0.27 HWR b=0.39 single-spoke | Nb | ? | CW | 4 K | design | -
ILC 500 | electrons, positrons | 16 900 | 1.3 GHz | b=1 elliptical 9-cell | Nb | 35 MV/m | pulsed | 2 K | design | -
LUNEX5 | electrons | 16 | 1.3 GHz | b=1 elliptical 9-cell | Nb | 25 MV/m | pulsed | 2 K | design | SOLEIL
LHeC ERL | electrons | 944 | 721 MHz | b=1 elliptical 5-cell | Nb | 20 MV/m | CW | 2 K | design | CERN
MYRRHA | protons | 8 48 34 60 | 176MHz 352 MHz 704 MHz 704 MHz | CH DTL b=0.35 single spoke b=0.47 elliptical 5-cell b=0.65 elliptical 5-cell | Nb | 4 MV/m 6 MV/m 8 MV/m 11 MV/m | CW | 2 K | design | SCK Mol
POLFEL | electrons | ? | 1.3 GHz | b=1 elliptical 9-cell | Nb | 25 MV/m | pulsed | 1.8 K | design | -
SPL | protons, H- | 60 192 | 704 MHz | b=0.65 elliptical 5-cell b=1 elliptical 5-cell | Nb | 19 MV/m 25 MV/m | pulsed | ? | design | CERN
TRASCO | protons |  | 704 MHz |  | Nb |  | pulsed |  | design | -
The TTC started this
work for
SRF Accelerators
in America and Asia

## Slide 11
WP10.2: SC Cavities for Proton Linac

## Slide 12
WP10.2: SC Cavities for Proton Linac

## Slide 13
WP10.2: SC Cavities for Proton Linac

## Slide 14
WP10.2: SC Cavities for Proton Linac

## Slide 15
WP10.2: SC Cavities for Proton Linac

## Slide 16
WP10.2: SC Cavities for Proton Linac

## Slide 17
WP10.2: SC Cavities for Proton Linac
FABRICATION SCHEDULES
Cavity  = 0.65 (IPN) :
  Week 13 : reception of the cavity without He tank
  Week 14-15: resonant frequency measurements, vacuum tests, chemical etching and field flatness tuning at IPN
  Week 16: cavity shipped back to RI for He tank welding
  Week 23-26: reception of the cavity with He tank
  September 2013: Test in vertical cryostat
Cavity  = 1 (CEA) :
  Week 12 : resonant frequency measurements of dumbbells at ZANON before final welding
  Week 22: reception of the cavity without He tank
  Week 23 to 29: controls, resonant frequency measurements, vacuum tests, electropolishing, and field flatness tuning at CEA
  Week 30-31: Clean room assembly, HPR
  End of August 2013: Test in vertical cryostat
  September 2013: cavity shipped back to ZANON for He tank welding

## Slide 18
WP10.2: SC Cavities for Proton Linac
β=1 cavity after final welding at equators @ EZ in May 2013
β=0.65 cavity ready for field flatness tuning at IPN Orsay

## Slide 19
Clean room preparation
(with CARE  = 0.5 cavity)
Vertical EP cabinet
with ILC cavity from FNAL (courtesy C. Ginsburg))
WP10.2: SC Cavities for Proton Linac

## Slide 20
ELECTROPOLISHING
WP10.2: SC Cavities for Proton Linac

## Slide 21
Ventilated acid cabinet
Ventilated cavity cabinet
H2 detection
Automated process
Ventilated acid transfer area
N2 blowing in tank
N2 blowing in cavity
H2 detection
WP10.2: SC Cavities for Proton Linac

## Slide 22
WP10.2: SC Cavities for Proton Linac
Top: RF vertical test on a single cell cavity
 Eacc = 42 MV/m limited by quench
Bottom: RF vertical test on a 9-cell cavity
Eacc = 23 MV/m limited by field emission
new EP and RF test will be done.

## Slide 23
WP10.3: LHC and CLIC Crab Cavities
Deliverables:
Goals:
Design, build and test a single LHC and CLIC crab cavity structure, including input coupler, mode couplers and tuners.
Design, build and test a LLRF and synchronization system that meets the crab cavity phase and amplitude control specifications for LHC and CLIC.
All deliverables are completed.

## Slide 24
WP10.3: LHC and CLIC Crab Cavities

## Slide 25
WP10.3: LHC and CLIC Crab Cavities
Motivation for crab-crossing ccheme at HL-LHC

## Slide 26
WP10.3: LHC and CLIC Crab Cavities
Four-Rod Crab Cavity (4RCC) geometric and RF parameters
The LHC cavity is a four rod structure which makes it ultra-compact and appropriately applicable for local crab crossing on LHC, which has been optimised for low surface fields and a very high shunt impedance. The rod shape has been specially configured to minimise the sextupole component of the deflecting voltage to provide a uniform deflecting field as a function of transverse beam offset.

## Slide 27
WP10.3: LHC and CLIC Crab Cavities
R/Q spectrum of LHC-4RCC
The input power coupler is a coaxial type coupler with a T-section which interfaces to a cavity coupler design which is identical to that of the existing LHC accelerating mode 400 MHz SRF cavities.
A special loop type coupler has been developed for damping the LOM and HOM impedances, with optimisation still being performed for the HOM coupler solutions.
LOM coupler
Input coupler

## Slide 28
WP10.3: LHC and CLIC Crab Cavities
Geometry of the LHC 4RCC and magnitude of the electric field

## Slide 29
WP10.3: LHC and CLIC Crab Cavities
Assembled prototype Niobium cavity, fabricated at Niowave Inc.

## Slide 30
A prototype cavity has been manufactured in UK, which achieved machining tolerances of 1-2 µm. This is the first demonstrated X-band structure in the UK.
A 2nd structure is manu-factured by CERN for breakdown testing using the same manufacturing process as for the main linac.
CERN end and mid cells
UK built CLIC crab cavity
Dual feed coupler design
Horizontal and vertical waveguide damped cell with integrated SiC dielectric loads
WP10.3: LHC and CLIC Crab Cavities

## Slide 31
Target luminosity loss fraction | f (GHz) | sx (nm) | qc (rad) | frms (deg) | Dt (fs) | Pulse Length (ms)
0.98 | 12.0 | 45 | 0.020 | 0.0188 | 4.4 | 0.156
RF path lengths need to be equal to better than cDt = 1.3 µm
travelling wave crab cavity
quadrupoles
quadrupoles
Detector
20 mrad crossing
WP10.3: LHC and CLIC Crab Cavities
Crab cavity to cavity synchronisation requirement ~5 fs.
Crab cavity to beam synchronisation requirement ~ 100 fs.

## Slide 32
WP10.3: LHC and CLIC Crab Cavities

## Slide 33
Goals:
Development of magnetron sputtering for the HIE-ISOLDE QW cavities
Build and test Pb coated phtocathodes on 1 ½ cell SRF gun
Facilitate communication about new thin film tehcniques
WP10.4: Thin Films
Deliverables:

## Slide 34
WP10.4: Thin Films

## Slide 35: Completed cold mass inside cryomodule of HoBiCaT HZB).
WP10.4: Thin Films

## Slide 36: Beam test: drive laser and electron beam diagnostics
0.26 µm, 30 kHz, 2…3 ps, 0.15 µJ pulses from Yb:YAG oscillator + regen. amp. + 4th harm conv.
Stripline BPM,
ICT
THz diagnostics
Viewscreens
Dipole magnet
WP10.4: Thin Films

## Slide 37: T10.4 + T10.7 : Pb/Nb SC-RF Gun Operation
First beam of photoelectrons from Pb cathode generated and accelerated at 21st April 2011, < 2 years after project approval
WP10.4: Thin Films
Lead coated photocathodes in 1 ½ SRF gun
achieving QE of 3.3x10-3
(NCBJ, DESY, Jlab)

## Slide 38
WP10.4: QWR for HIE Isolde

## Slide 39
WP10.4: Thin Films

## Slide 40
WP10.4: Thin Films

## Slide 41
WP10.4: Thin Films
The RRR of our Nb sputtered samples was increasing when increasing the power of sputtering.
We got progressive improvements. The film is uniform all over within the cavity. We can sputter over 1 micron in about 15 minutes.
Today we got RRR values of 22, that means we are ready for sputtering the cavity.
In this situation, we could try the miracle to sputter and test it for the beginning of June, but we need the cavity, and the ancillary equipment (coupler, pickup, bottom plate and closing system).
Communication from E. Palmieri (15/05/2013)
Magnetron sputtering facility
at INFN/Legnaro

## Slide 42
WP10.4: Thin Films
Monograph touching upon
New Thin Film Techniques
by C. Antoine
(cf. EuCARD2 KoM)

## Slide 43
WP10.5: HOM Distribution

## Slide 44
WP10.5: HOM Distribution
Deliverables:

## Slide 45
WP10.5: HOM Distribution

## Slide 46
WP10.5: HOM Distribution

## Slide 47
WP10.5: HOM Distribution

## Slide 48
WP10.5: HOM Distribution

## Slide 49
WP10.5: HOM Distribution

## Slide 50
WP10.5: HOM Distribution

## Slide 51
WP10.5: HOM Distribution

## Slide 52
WP10.5: HOM Distribution

## Slide 53
WP10.5: HOM Distribution

## Slide 54
WP10.5: HOM Distribution

## Slide 55
WP10.5: HOM Distribution

## Slide 56
WP10.5: HOM Distribution

## Slide 57
WP10.5: HOM Distribution

## Slide 58
Deliverables:
WP10.6: LLRF at FLASH
Goals:
Develop components of LLRF system using µTCA technology.
Improve the reliability and functionality of the LLRF at FLASH
Improve the energy stability of the beam in FLASH

## Slide 59
WP10.6: LLRF at FLASH

## Slide 60
WP10.6: LLRF at FLASH

## Slide 61
Downconverter optimization
Vector modulator improvements
Downconverter
Vector modulator
It has been optimized for an input frequency of 1.3 GHz, a heterodyne of 1.354 GHz and an intermediate frequency of 54 MHz.
After extensive tests and requests for new features a second revision of the board with two output channels has been developed. The second channel will be used in the future to perform system calibration.
WP10.6: LLRF at FLASH

## Slide 62
Synthesis and distribution of clock and reference signals in xTCA system (RF Backplane)
RF backplane for the MTCA crate increases reliability and maintainability and reduces the limitations external RF cabling. It generates and distributes high-quality synchronization and reference signals as well as low-jitter clock signals.
There is a patent application for RF Backplane requested and beeing processed.
The patent requiest for RF Backplane was filled in (June 2012).
WP10.6: LLRF at FLASH

## Slide 63
Development of an AMC module with fast radiation sensors
FMC board with RadMon mezzanine
The neutron radiation sensors developed with support of CARE project has been patented (EP 1 729 149 B1, Solid State Neutron Detection System, 09.01.2013) – this work was a base for current developments.
WP10.6: LLRF at FLASH

## Slide 64
Calibration of the radiation sensors in FLASH
Extracted calibration factors
WP10.6: LLRF at FLASH

## Slide 65
The developed LLRF system has been installed in the FLASH accelerator and commissioned during maintenance periods. The system was tested with and without beam.
RF field stability (with beam) is of order of 10-4
WP10.6: LLRF at FLASH

## Slide 66
Goals:
Slice emittance measurements on the SRF gun of ELBE
Development of GaAs photocathodes in SRF gun
Evaluation of critical Issues of SRF guns
WP10.7: SC RF Gun at ELBE
Deliverables:

## Slide 67
WP10.7: SC RF Gun at ELBE

## Slide 68
WP10.7: SC RF Gun at ELBE
Zero Phasing Measurement Principle (PhD Thesis J. Rudolph)

## Slide 69
WP10.7: SC RF Gun at ELBE
Browne-Büchner Spectrometer realizes point to point imaging

## Slide 70
WP10.7: SC RF Gun at ELBE
Quad scan method applied to slice profiles

## Slide 71
WP10.7: SC RF Gun at ELBE
Report of the GaAs activity will be presented by J. Teichert this week.
The conclusion of the project results is to develop a more advanced system which includes the experience of the previous work and state-of-the-art technique in this field:
• split of the cathode body and the new plug,
• only the plugs are treated in the preparation system,
• design of preparation system which can installed near the electron gun,
• using different chambers for cleaning, transfer and preparation.
Furthermore a standard design of the photocathodes, plugs and storage chambers was fixed between the German institutes HZB, HZDR and University of Mainz. This required a further redesign but will allow the exchange of photocathodes for tests and characterization between these institues in the future.
HZDR gives additional funds for investment for this project in 2012 and 2013.

## Slide 72
WP10.7: SC RF Gun at ELBE
New design of the exchangeable cathode plug for GaAs (left) and the new preparation chamber with the interface to the gun and the transport chamber

## Slide 73
Deliverables:
Goals:
Demonstrate new coupler cleaning procedures suitable for
mass production of 1.3 GHz couplers
short RF conditioning time.
Three methods have been investigated:
1. High Pressure Water rinsing
2. Argon plasma discharge
3. Automatic cleaning
WP10.8: RF Coupler Cleaning at LAL

## Slide 74
WP10.8: RF Coupler Cleaning at LAL

## Slide 75
WP10.8: RF Coupler Cleaning at LAL
The man-made preparation procedure: E-XFEL case for 800 couplers

## Slide 76
WP10.8: RF Coupler Cleaning at LAL
The EuCARD automated reparation procedure

## Slide 77
WP10.8: RF Coupler Cleaning at LAL
(Automate de Lavage Intégré pour Coupleur Electromagnétique)

## Slide 78
WP10.8: RF Coupler Cleaning at LAL
Evolution of the concept of automatic coupler washer, over the 4 past years

## Slide 79
WP10.8: RF Coupler Cleaning at LAL
ALICE design v2
The studies of ALICE are complete enough to give us a complete overview and estimation of the feasibility, the process and the costs: the efficiency of the process, as far as the large mass production is concerned, is undisputed.
The cost of a such machine as ALICE is estimated at 150 k€.
All the technical functions can be respected to clean couplers automatically and correctly without any damage for them.

## Slide 80
WP10-SRF: The fifteen deliverables

## Slide 81
Thank You for Your Attention
Many thanks to:
Olivier Brunner
Stéphane Chel
Frank Peauger
Peter McIntosh
Sergio Calatroni
Roger Jones
Nicoleta Baboi
Mariusz Grecki
Jochen Teichert
Walid Kaabi