## Slide 1: Pixel detectors in High Energy Physics experiments: present systems and upgrade plans
Petra Riedler/CERN

## Slide 2: Outline
A short historical excursion
Present pixel systems at LHC
  ATLAS
  CMS
  ALICE
Future pixel systems
  Upgrades: ATLAS, CMS, ALICE
  NA62
  STAR
  CLIC

## Slide 3: Thanks
to many colleagues who provided me with material for this presentation:
Paula Collins
Dominik Danheim
Leo Greiner
Roland Horisberger
Flavio Marchetto
Heinz Pernegger
ALICE ITS team
And apologies to those who I might have forgotten in this list!

## Slide 4
This presentation is a very personal view on the world of pixel detectors.
It is not intended as a complete summary. And if you can read this your eye-sight is definitely better than mine.
Disclaimer

## Slide 5: The “World of Pixels” …
Monolithic Pixels
Charge generation volume integrated into the ASIC
Hybrid Pixels
Sensor and ASIC are independent units
See talk by I. Peric
“Monolithic Pixel Detectors”
June 3, 2013
See talk by T. Fritzsch
“Microintegration of Electronics”
June 3, 2013

## Slide 6: …and why use them in HEP experiments
ATLAS Experiment © 2012 CERN
Event display of a H -> 4e candidate event

## Slide 7
Events recorded by the ALICE experiment from the first lead ion collisions, at a centre-of-mass energy of 2.76 TeV per nucleon pair.
© 2010 CERN

## Slide 8: Pixel Detectors in HEP Experiments
Are high granularity tracking detectors which provide unambiguous and precise hit information in the harsh environment close to the interaction point.
Position resolution down to few microns
Unambiguous hit information in high track density region
Improved primary and secondary vertex resolution
Fast readout (depending on technology)
High level of radiation hardness (again technology dependent)
Pixels are used at the heart of the trackers in ALICE, ATLAS and CMS and are key elements for the upgrades.

## Slide 9: Short Historical Excursion
CCD (1969 Bell Labs)
First use of “pixel”-like silicon detector in a physics experiment (SLD/SLAC and NA11/32, from ~1981)
Charges are shifted through potential wells to the edge of the detector to the anodes
Small pixel sizes (O(10 µm), matrix readout slow, low radiation tolerance

## Slide 10: …moving on to the late 80’s
1980 first application of planar technology to produce silicon sensors (strips) >> produce highly segmented silicon sensors (prerequisite for hybrid pixel detectors)
1987/88 First pixel prototype sensors for SLAC/SSC, Shapiro and Galema, no special pixel electronics yet
1989 LAA project, CERN, first development of dedicated pixel electronic, no bump bonding yet
~1987-90 first monolithic detectors proposed
1990 Omega D chip and sensor, first hybrid pixel detector, tested in testbeam, CERN

## Slide 11: Key ingredients for pixels
Main ingredients required for first silicon pixel detectors (after planar process allowed to produce pixel sensors):
VLSI (Very Large Scale Integration) technology to produce complex ASICs (Application Specific Integrated Circuit) – Hybrid, Monolithic
Interconnect technology based on flip-chip bonding (connections of ~20µm between each sensor pixel cell and the corresponding readout cell in an ASIC) - Hybrid
“recent” development (from ~1990)

## Slide 12: Short Historical Excursion
1947
1958
1959
1961
1970
Flip chip bonding:
Controlled collapse chip connection – C4 by IBM ~1969 (e.g. mainframe computers)
Studies in automotive for voltage regulators (GM Delco)
Miller, IBM, 1969
www.chiphistory.com
www.chiphistory.com
http://smithsonianchips.si.edu/
www.chiphistory.com
http://smithsonianchips.si.edu/

## Slide 13: Flip Chip Bonding
The great wall of bump bonds by N. Ishikawa, Fujitsu Ltd.
See talk by T. Fritzsch
“Microintegration of Electronics”
June 3, 2013

## Slide 14: Omega 2 and Omega3
Early 1990s, CERN’s RD19 collaboration develops the Omega2 and Omega3 chips
Omega2:
16 col x 63 row
cell size 500 x 75 µm2
overall sensitive area 8.0 x 4.7 mm2
Omega3:
16 col x 127 row
cell size 500 x 50 µm2
overall sensitive area 8.0 x 6.4 mm2

## Slide 15: First use in WA94/97 and NA57
Study of the strange and multi-strange particle production in Pb-Pb collisions at the CERN SPS
1992 the first fully operational hybrid silicon micropattern detector was succesfully tested in a fixed target experiment environment
  WA94 heavy ion experiment at the OMEGA spectrometer of the CERN SPS
  WA94 pre-decessor of the WA97/NA57 heavy ion experiment
[A hybrid silicon pixel telescope tested in a heavy ion experiment”, Nucl. Instr. and Meth. A 332 (1993) 188-201)]
beam
L
p
p-

## Slide 16: Omega 2 and 3 Ladders
Omega 2
Omega 3
Omega 3
6 readout ASICs connected to 1 silicon pixel sensor

## Slide 17
© 1995 CERN

## Slide 18: Pixel Detectors at LHC
ALICE
CMS
ATLAS

## Slide 19: ATLAS Pixel Detector
Three barrel layers:
  R= 5 cm (B-Layer)
  R=9 cm (Layer-1)
  R=12 cm (Layer-2)
  1456 barrel modules
Two endcaps:
  three disks each
  288 forward modules
80 million channels
sensitive area of 1.7 m2
Three precise measurement points up to 2.5:
  R resolution:10 m
   (R or z) resolution: 115 m
Environmental temperature about -10 ºC
2 T solenoidal magnetic field.

## Slide 20: ATLAS Pixel Detector

## Slide 21: ATLAS Pixel Module
Sensor
  47232 n-on-n pixels with moderated p-spray insulation
  250 m thickness
  50 m (R) × 400 m ()
  328 rows (xlocal) × 144 columns (ylocal)
16 FE chips
  bump bonded to sensor
Flex Hybrid
  passive components
  Module Controller Chip to perform distribution of commands and event building.
Radiation-hard design:
  Dose >500 Gy
  NIEL >1015 neq/cm2 fluence

## Slide 22: CMS Pixel Detector
Three barrel layers:
R=4.4 cm
R=7.3 cm
R=10.2 cm
Forward disks:
2 forward disks on either side
66 mio. channels
Area ~1 m2
1440 modules
15840 readout chips
Environmental Temperature: -8°C
4T magnetic field
NIM A, 2013
http://dx.doi.org/10.1016/j.nima2013.04.001

## Slide 23: CMS Pixel Detector

## Slide 24: CMS Pixel Module
N-in-n Silicon Sensor
t=285m
100m x 150m pixels
16 x Readout Chips
(CMOS) 175m thick
4160 pixels/chip
Alu-power cable
6 x 250m ribbon
High Density Print
3 Layers, 48m thick
SiN base strips
250m thick, screw holes
Kapton signal cable
21 traces, 0.3mm pitch

## Slide 25: ALICE Pixel Detector
Two barrel layers:
R= 3.9 cm
R= 7.6 cm
No forward disks
9.8 mio channels
Area 0.21 m2
120 modules
1200 pixel chips
Environmental temperature ~ 27°C
0.5 T magnetic field

## Slide 26: ALICE Pixel Detector

## Slide 27: ALICE Pixel Module
2 p-in-n sensors
200 µm thick
70 mm x 14 mm
Pixel size: 50 µm x 425 µm
5 ASICs connected to one sensor
8192 pixels/chip
Chips thinned to 150 µm
Multi-chip module
    3 ASICs
    max. height: 5 mm
Multilayer Al flex cable
1200 pixel chips
9.83 x 106 pixels
1.14% X0 per layer

## Slide 28: Spatial Resolution
 | [μm] | pixel cell size z x Rφ [μm2]
ALICE | 100 (z); 12 (Rφ) | 425 x 50
ATLAS | 115 (z); 10 (Rφ) | 400 x 50
CMS | ~ 15-20 | 150 x 100
Intrinsic resolution
CMS and ATLAS have analog information
ALICE uses binary readout
Operated in magnetic field:
  ALICE: 0.5 T
  ATLAS: 2 T
  CMS: 4T
Different sensor thicknesses (200-285 µm)

## Slide 29: Impact Parameter Resolution
sb ≈ sdetector resolution ⊕ smultiple scattering
smultiple scattering dominated
sdetector resolution dominated

## Slide 30: Sensor and ASIC Thickness…..
 | Si sensor [μm] | X0 [%] | ASIC [μm] | X0 [%]
ALICE | 200 | 0.21 | 150 | 0.16
ATLAS | 250 | 0.27 | 180 | 0.19
CMS | 285 | 0.30 | 180 | 0.19
X0 (Si) = 9.36 cm

## Slide 31: ..enter into the material budget
Example: ALICE
… but are not the only contributions!
Support, services, cooling need to be optimized in terms of material budget.
Yes, the pixel contribution is small, BUT: it also the closes layers to the IP which are crucial for the impact parameter resolution.

## Slide 32: Radiation Levels …..
 | TID [kGy] | Fluence 1MeV n eq. [cm-2] | Time
ATLAS Pixel* | 500 | 1 x 1015 | 10 years
ATLAS Strips | 100 | 2.0 x 1014 | 10 years
CMS Pixels | 840 | 3 x 1015 | 10 years
CMS Strips | 70 | 1.6 x 1014 | 10 years
ALICE Pixel | 2.7 | 1 x 1013 | 10 years
LHCb VELO | 50 | 1.3 x 1014** | 1 year
** inner part, inhomogeneous irradiation
ATLAS and CMS values cited for innermost layers for pixels and strips for 500 fb-1
* averaged (B-layer to be replaced)

## Slide 33: …impact on technology choices
 | Sensor [μm] | ASIC | Temp.
ALICE | P-in-n | 0.25 µm | ~27°C
ATLAS | N-in-n ox | 0.25 µm | -10°C
CMS | N-in-n | 0.25 µm | -8°C

## Slide 34: Future Pixel Detectors
Many new projects using pixel detectors in production and being planned. Pixels are increasingly important for new projects and upgrades of existing ones:
  ATLAS IBL
  STAR vertex detector
  NA62 Gigatracker
  Belle upgrade
  ATLAS pixel upgrade
  CMS pixel upgrade
  ALICE inner tracker upgrade
  ILC/CLIC
  …
Hybrid pixels AND monolithic pixels
Some of them taking place right now!

## Slide 35: Experimental Requirements
Requirements drive the technology choice:
  Radiation levels (1011neq (ILC/CLIC) – 1015/16neq (SLHC))
  Pixel size
  Readout speed
  “Added” functionality, eg. trigger information
  Material budget
  Cost …
…technology decisions for the upgrades at LHC in LS2 will be taken now!

## Slide 36: LHC Upgrade Schedule

## Slide 37: ATLAS IBL – LS1
New pixel layer around smaller, new beam pipe (r=24 mm, was 29 mm)
IBL mounted on beampipe
14 staves arraged at average r=33 mm
Radiation levels: ~5 x 1015 neq cm-2

## Slide 38: ATLAS IBL
3D
3D
Planar
Based on hybrid pixel detectors
New FE (FE-I4) in 0.13 µm CMOS technology (intrinsically more radiation resitant)
  19 x 20 mm2, 26880 channels
Pixel size reduced: 50 µm x 250 µm
2 sensor types per stave:
  Double chip planar sensors (200 µm thick, n-in-n ox, reduced edge region by guard rings shifted underneath pixels)
  Single chip 3D sensors (250 µm thick, vertical electrodes through the bulk)
Each stave:
  8 single chip modules (3D) and 12 double chip modules (planar)
  12 mio channels
Reduced material budget: ~1.9 % X0

## Slide 39: ATLAS Phase II
All new silicon tracker
  Radiation levels will increase up to 2-3 x 1016 neq cm-2
  4 barrel layers, 6 x 2 forward disks
  Smaller pixel size (O (25 µm))
  Robust tracking, by having at least 14 silicon hits everywhere
Forward pixel
Long Barrel Strips
Short Barrel Strips
Forward Strips
Barrel pixel

## Slide 40: ATLAS Phase II Pixels
Prototypes being developed to optimize:
Radiation hardness, small pixel size, large area coverage, minimize material,….
Pixel sensors in several technologies proved to high doses (planar/3D/diamond shown to 2×1016neq/cm2)
IBL pixel (50×250µm) OK for outer pixel layers, but can go down to 25µm×125µm pixels with 65 nm CMOS
Larger area sensors for quads/sextuplets modules
Quad module prototype

## Slide 41: CMS Pixel Upgrade
Pixel upgrade planned for phase II based on hybrid pixels:
Smaller pixels, higher granularity
Radiation hardness
Reduce material budget

## Slide 42: CMS Pixel Upgrade
Parameter of Pixel System
# layers (tracking points)
beam pipe radius (outer)
innermost layer radius
outermost layer radius
pixel size (r-phi x z)
In-time pixel threshold
cooling
material budget X/X0 (h=0)
pixel data readout speed
1st layer module link rate (100%)
ROC pixel rate cabability
Present
3
29.8 mm
44 mm
102 mm
100m x 150m
3400 e
C6F14 (monophase)
6%
40MHz (analog coded)
13 M pixel/sec
~120 MHz/cm2
Upgrade
4
22.5 mm (LS1)
29.5 mm
160 mm
100m x 150m
1800 e
CO2 (biphase)
5.5%
400Mb/sec (digital)
52 M pixel/sec
~580 MHz/cm2
79 mio pixels (barrel) + 44 mio pixels (forward)

## Slide 43: CMS Pixel Upgrade
In LS1 install 2 assemblies with 4 new pixel modules (2 blades) each (Pilot-run)
Present FPIX allows partially equipped 3rd disk with new ROC & digital readout system
Cooling by old C6F14 monophase cooling, use existing extra cables & fibers
Integration and operations of new pixel system in CMS under LHC conditions
Study performance of new ROC
Installation in the experiment in summer 2014
FPIX with space for 3rd disk

## Slide 44: ALICE Inner Tracker Upgrade
All pixel tracker (presently pixel-drift-strips) based on monolithic silicon pixel detectors for LS2
7 layer barrel tracker, no forward disks
~ 10 m2
Layer | Radius [cm] | +/- z
1 | 2.2 | 11.2
2 | 2.8 | 12.1
3 | 3.6 | 13.4
4 | 20 | 39.0
5 | 22 | 41.8
6 | 41 | 71.2
7 | 43 | 74.3
Inner barrel
Outer barrel

## Slide 45: ALICE Inner Tracker Upgrade
Cell size for inner barrel layers: 20μm (r,φ) x 20μm (z); can be relaxed for outer barrel layers (< O(100 µm)) >> pointing resolution ~ 4 µm
Binary readout
Material Budget X/X0 /layer ~ 0.3%, up to ~ 0.8% for the outer layers
  power density < 300 mW / cm2
Readout rate and bandwidth
  Interaction rate (Pb-Pb): 50 kHz (LOI), 100kHz (design value)
  Interaction rate (pp): 500 kHz
  Data throughput < 200 Mbit / sec × cm2 (innermost layer) and < 6Mbit/sec x cm2 (outer layers), total data throughput 200 Gbit/s
Removal/insertion during winter shutdown (all services on one side (A))
Radiation tolerance to: ~700 krad and 1013/cm2 1 MeV neq (safety factor 4)

## Slide 46: ALICE Inner Tracker Upgrade
Monolithic silicon pixel detectors based on wafers with high resistivity (1-2 kWcm) epi layer (~ 20 µm thick)
0.18 µm CMOS technology offered by TowerJazz (improved radiation resistance confirmed by test-structures)
Special quadruple-well available to shield PMOS transistors (allows in-pixel truly CMOS circuitry)
R&D on chip architecture ongoing
Figure Stanitzki, M. (2010). Nucl. Instr. and Meth. A doi:10.1016/j.nima.2010.11.166

## Slide 47: ALICE Inner Tracker Upgrade
Prototype chips developed in 0.18 µm process: MIMOSA32, Explorer
Engineering run with different architectures submitted in March 2013
Charge in seed pixel
Equivalent noise charge
Signal to Noise Ratio
after 1 Mrad+1013 neq
MPV ~ 20-25
Detection eff. ~99.8%

## Slide 48: ALICE Inner Tracker Upgrade
Module:
15 mm x 30 mm chip, 50 µm thin
Al flex cable (2 layers)
Laser soldered BGA type connections between flex and chips
Ultra-light support structure (CF)
Diffent cooling concepts under study (PI tubes, PI microchannels, Si microchannels)
See talk by C. Gargiulo
June 3, 2013

## Slide 49: NA62 – Gigatracker GTK
Measure O(100) K+p+nn events with ~10% background at the CERN SPS in two years of data taking (2014)
π/K/p (~6% K+)
  Precise momentum and direction measurement of kaon and pion
  Precise timing measurement to associate the outgoing pion to the correct incoming parent kaon
3 GTK pixel stations
Hybrid pixels: 1 sensor+10 FE chips
18000 pixels/station

## Slide 50: NA62 - GTK
Pixel size: 300 µm x 300 µm
Precise timing information: s(t)~ 150 ps rms on single track
Material budget per station: 0.5% X0 to preserve beam divergence for precise downstream measurement and to limit beam hadronic interactions
High and non-uniform rate (~1.5 MHz/mm2 in hot center, ~0.8-1.0 GHz total)
High fluence levels: ~2 1014 neq cm-2 in 100 days (~1 year)
Operation in beam vacuum
Estimated power dissipation per readout chip ~ 2W/cm2
Microchannel cooling (~ 130 µm Si)
See talk by A. Mapelli
“Microtechnologies for particle detectors”
June 4, 2013

## Slide 51: CLIC
e+
e-
Large background hit rates from Beamstrahlung in vertex and forward regions:
  2-3% maximum pixel occupancy / train (incl. clustering + safety factors)
  Time stamping with ~10 ns accuracy, to reject background
Moderate radiation exposure:
  NIEL: < 1011 neq/cm2/y
  TID: < 200 Gy / year
CLIC e+e- linear collider:
  √s up to 3 TeV, L=6×1034cm-2s-1
  156 ns bunch trains, 312 bunch crossings each
  20 ms gaps between trains
  trigger-less readout
  power pulsing
156 ns
20 ms
312 bunches
Time structure of collisions (not to scale)
June 3, 2013
TALENT Summer School - CERN
51

## Slide 52: CLIC
Efficient tagging of heavy quarks through precise determination of displaced vertices:
Single point resolution: σSP~3 μm
  Small pixels ~25x25 μm, analog readout
Material budget: X ⪅ 0.2% X0 / layer
  Low-power ASICs (~50 mW/cm2) + air-flow cooling
  50 µm sensor + 50 µm ASIC
VXD parameters | CLIC
Material X/X0 (90o) | ~1% (5-6 layer)
Pixel size | 25 x 25 μm2
# pixels | ~2 G
Time slicing resol. | ~10 ns
Avg. power/pixel | <~0.3 μW

## Slide 53: CLICpix
65 nm CMOS hybrid r/o chip, targeted to CLIC vertex detectors
Demonstrator chip produced with fully functional 64 x 64 pixel matrix
25 μm pixel pitch
Simultaneous 4-bit time (TOA) and energy (TOT) measurement per pixel
 Front-end time slicing < 10 ns
Selectable compression logic:
  pixel, cluster + column-based
 Full chip r/o in less than 800 μs (at 10% occup.) with 320 MHz r/o clock
power pulsing scheme  Pavg< 50 mW/cm2
CLICpix
demonstrator chip
P. Valerio
14 μm
25 μm
Preamp
leakage compensation
+ return to baseline circuit
discriminator
DAC output

## Slide 54: STAR HFT at RHIC
Direct topological reconstruction of Charm (200 GeV Au-Au collisions)
  Detect charm decays with small c, including D0  K 
HFT – Heavy Flavor Tracker
SSD – Silicon Strip Detector
  r = 22 cm
IST – Inner Silicon Tracker
  r = 14 cm
PXL – Pixel Detector
  r = 2.5, 8 cm
Installation: December 2013
3 sectors installed May 8, 2013

## Slide 55: STAR HFT at RHIC
Pointing resolution | (12  19 GeV/pc) m
Layers | Layer 1 at 2.5 cm radius Layer 2 at 8 cm radius
Pixel size | 20.7 m X 20.7 m
Hit resolution | 6 m
Position stability | 6 m rms (20 m envelope)
Radiation length per layer | X/X0 = 0.37%
Number of pixels | 356 M
Integration time (affects pileup) | 185.6 s
Radiation environment | 20 to 90 kRad / year 2*1011 to 1012 1MeV n eq/cm2
Rapid detector replacement | ~ 1 day
356 M pixels on ~0.16 m2 of Silicon
Monolithic silicon pixel detectors

## Slide 56: STAR HFT at RHIC
Air cooling
Thinned silicon sensors (50 μm thickness)
MAPS (Monolithic Active Pixel Sensor) pixel technology
  Sensor power dissipation ~170 mW/cm2
  Sensor integration time <200 μs (L=8×1027)
Quick detector installation or replacement (1 day)
Aluminum conductor Ladder Flex Cable
Ladder with 10 MAPS sensors (~ 2×2 cm each)
carbon fiber sector tubes (~ 200 µm thick)
20 cm

## Slide 57: STAR HFT at RHIC
ULTIMATE chip (IPHC Strasbourg)
Reticle size (~ 4 cm²)
  Pixel pitch 20.7 μm
  928 x 960 array ~890 k pixels
Power dissipation ~170 mW/cm² @ 3.3V
Integration time 185.6 μs
In pixel CDS
Discriminators at the end of each column (each row processed in parallel)
2 LVDS data outputs @ 160 MHz
High Res Si option – significantly increases S/N and radiation tolerance.

## Slide 58: Summary
Silicon pixel detectors gain increasing importance in HEP experiments. All upgrades of LHC experiments consider or have already decided to use pixel detectors.
Present pixel systems in HEP experiments are based on hybrid pixel detectors. The new generation of pixel detectors will see hybrid and monolithic pixel detectors.
Severe challenges lie ahead to achieve higher granularity, low mass and to sustain high radiation environment and data rates.
Pixels are very popular outside HEP experiments (not only in your camera..) – see the next talk!
See talk by M. Campbell
“Hybrid pixels – from HEP to imaging and other applications and back again”

## Slide 59: SPARE

## Slide 60: The upgrade of the ALICE Inner Tracker
Performance - 1
Layout A (7 pixel layers) | 
srf = 4 µm | sz=4 µm
X/X0 | 0.3 %
Layout B (3 pixel + 4 strip layers) | 
srf = 4 µm (pixel), 20 µm (strips) | sz=4 µm (pixel), 830 µm (strips)
X/X0 | 0.3% (pixel), 0.8 % (strips
~3x

## Slide 61: The upgrade of the ALICE Inner Tracker
Performance - 1
Layout A (7 pixel layers)
Layout B (3 pixel + 4 strip layers)
Tracking efficiency
Momentum resolution