## Slide 1
Simulations of irradiated detectors: E(x) & parameterization
RD50 Simulation Working Group Meeting
March 27th - 28th 2013
T. Peltola1) , J. Härkönen1)
1)Helsinki Institute of Physics, CMS Tracker Project.

## Slide 2
Outline
Status of irradiated Si detector simulations with Synopsys TCAD
  Results of E(x) simulations
  Parameters and parameterization
  p-type device: EVL and Petasecca defect models
SiBT measured and simulated p-type detector CCE
Future plan / work in progress
  edge-TCT

## Slide 3
n-type device,
1 μm x 1 μm x 300 μm
α (290K)= 4·10-17 A·cm-1
Ф =1014 cm-2
I = V·α·Ф ~ 1.2·10-12 A
Current cannot be introduced by adding the suggested "trap" E = EC - 0.65eV
Current introduction rates GDD and GDA modified to match experimental value of leakage current
EVL:
Type of defect | Activation energy, eV | Trapping cross section, cm2 | Introduction rate, cm-1
Deep donor (DD) | EV + EDD = 0.48 | se = sh = 4e-14 | GDD = 1
Deep acceptor (DA) | EC - EDA = 0.525 | se = sh = 4e-14 | GDA = 1
Modified:
Type of defect | Activation energy, eV | Trapping cross section, cm2 | Introduction rate, cm-1
Deep donor | EV + EDD = 0.48 | se = sh = 4e-14 | GDD = 0.285
Deep acceptor | EC - EDA = 0.525 | se = sh = 4e-14 | GDA = 0.285
Tuning of EVL-defect model: GDD, GDA

## Slide 4
Tuning of GDD , GDA: Neff , E(x)
E(x) simulated on Synopsys-TCAD
Neff conc. simulated on Synopsys-TCAD
Neff conc. simulated by V. Eremin
E(x) simulated by V. Eremin
Synopsys model not matching with Eremin’s simulation:
No double peak behaviour at Φ = 3e14 cm-2
~90 μm difference in Neff sign change at
Φ = 5e14 cm-2
The missing bulk generated current level is not compensated by simply tuning GDD, GDA at Φ > 1e14 cm-2
GDD and GDA = 0.285
GDD and GDA = 0.285
290K, 300V
290K, 300V

## Slide 5
EVL defect model, tuned to T = 253 K by Robert Eber, KIT
Type of defect | Activation energy, eV | Trapping cross section, cm2 | Introduction rate, cm-1 | Acceptor/donor conc. cm-3
Deep acceptor | EC - EDA = 0.525 | se = sh = 1e-14 | GDA = 1.189 | 1.189*F + 6.454e13
Deep donor | EV + EDD = 0.48 | se = sh = 1e-14 | GDD = 5.598 | 5.598*F – 3.959e14
Tuning of EVL-defect model: Defect concentrations
Method produces correct leakage current & DP behaviour
253K, 300V

## Slide 6
se = sh = 0.9e-14 cm2
Tuning of defect concentrations: Neff , E(x)
se = sh = 0.9e-14 cm2
V. Eremin
V. Eremin
Synopsys model differences with Eremin’s simulation:
Double peak behaviour already at Φ = 3e14 cm-2
~60 μm difference in Neff sign change at
Φ = 5e14 cm-2
Amplitude differences of Neff and E(x)
Synopsys
Synopsys
260K, 300V
260K, 300V

## Slide 7
Simulated and measured leakage currents
Tuning of defect concentrations: Leakage currents
Hardness factor | 24 GeV proton fluence [cm-2] | 1 MeV neqv fluence [cm-2]
0.56±0.01 [1] | 1.16e15 | (6.50±0.12)e14
0.56±0.01 | 1.92e15 | (1.08±0.02)e15
0.56±0.01 | 4.39e15 | (2.46±0.04)e15
0.56±0.01 | 5.05e15 | (2.83±0.05)e15
0.56±0.01 | 8.05e15 | (4.51±0.08)e15
[1] D. Bechevet et al. NIM A 479 (2002) 487-497.
IV data from VTT 24GeV irradiated minisensors
Part of the fluence region > 1e15 neqv cm-2
300N @ T = -20°C
Improved match with measurement by Qox(Φ)
Good agreement even at high fluencies
253K
253K
E(x) of the simulated fluencies
Fluence conversion to simulator input

## Slide 8
P-type detector: Petasecca & EVL models
Effective Petasecca defect model for p-type, modified to match leakage current @ T=253K
Type of defect | Activation energy, eV | Trapping cross section, cm2 | Introduction rate(253K), cm-1
Deep acceptor | EC - EDA = 0.42 | se = 2e-15, sh = 2e-14 | GDA = 10.818
Deep acceptor | EC - EDA = 0.46 | se = 5e-15, sh = 5e-14 | GDA = 7.305
[2] M. Petasecca et al.
NIM A 563 (2006) 192-195
Level [eV] | σn [cm-2] | σp [cm-2] | Introduction rate [cm-1]
EC - 0.42 | 2e-15 | 2e-14 | 1.613
EC - 0.46 | 5e-15 | 5e-14 | 0.9
EV + 0.36 | 2.5e-14 | 2.5e-15 | 0.9
Three-level defect model for p-type @ T = 290 K [2]
EV + 0.36 level was not found to contribute to the performance of an irradiated detector
Petasecca model
Modified EVL-model
253K, -300V
253K, -300V
Expected DP behaviour observed only with EVL-model

## Slide 9
5-strip structure
5-120 region
wp = 14 μm
Np = 5e16 cm-3
T=273K
F = 1e14 – 1e16 cm-2
P-type MSSD: Petasecca & EVL models
Electric field distributions @
y = center of the strip 3:
Petasecca
Petasecca
Modified EVL
Modified EVL
Level, eV | Introduction rate (273K), cm-1
EC - 0.42 | GDA = 7.733
EC - 0.46 | GDA = 4.314
Petasecca tuning @ T=273K
Level, eV | Trapping X section, cm2
EC - 0.525 | se = sh = 1.3e-14
EV + 0.48 | se = sh = 1.3e-14
Modified EVL tuning @ T=273K
Leakage current matching:

## Slide 10
5-120 region, T = 273 K
FTH300P and 320P active area ≈ 290 μm
Simulated results matching with measured CCE of FTH190P and 320P
Difference in CCE of 200P due to definition of deep diffusion doping profile?
P-type MSSD: SiBT CCE data
Simulated deep diffusion doping profile
Measured and simulated CCE vs Φ

## Slide 11
Goal: extract electric field from drift velocity measurements using eTCT
Collected eTCT generated charges as a function of injection distance
First MSSD simulations produce matching behaviour with measurement
Work in progress: edge-TCT
MIP trajectories in 300N device:
FZ320N nonirr. eTCT-measurement (M. Fernandez 2013). Vfd ~ 210 V
Vfd ~ 800 V
10 μm
100 μm
250 μm
mip direction
Irradiated 300N eTCT pulses, F = 1e15 cm-2,
T=-20°C

## Slide 12
Summary
Tuning of defect concentrations succesful way to modify EVL-model for Synopsys-TCAD
  Double peak formation
  Correct leakage currents
  Promising CCE results compared with SiBT data
Petasecca model for p-type device does not produce the expected double peak
First edge-TCT simulations match the measured behaviour