## Slide 1
PTI results on I(T) and E(x) simulations
with two midgap energy levels
E. Verbitskaya, V. Eremin,
Ioffe Physical-Technical Institute of Russian Academy of Sciences
St. Petersburg, Russia
RD50 simulation group meeting
CERN, March 27-28, 2013

## Slide 2
Earlier results of RD50 collaboration
Linear fit of I(F) is a strong argument to use linear dependence of the concentration of radiation induced defects which act as generation centers on F
a = 3.7x10-17 A/cm
G. Lindström, NIM A 512 (2003) 30

## Slide 3
Modeling of bulk generation current
Modeling is based on Shockley-Read-Hall statistics
Emission rates ee,h:
Generation rate:
Et = Et – Ev; s - carrier capture cross section, Nt – deep level concentration
G is determined by a larger energy gap
Assumption for s(T):
s(T) = so(T/To)-m m = 02
(V. Abakumov, et. al., Sov. Phys. Semicond. 12 (1978) 1)
Presented: E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012

## Slide 4
Reverse current simulation
1. Carrier generation via single level (SL): macroscopic approach
Igen = esvthniNgenexp(-Ea/kT)
vth~T3/2; ni~T1/2; s(T) = so(T/To)-2
 Igen ~ exp(-Ea/kT)
Activation energy Ea = 0.65 eV for both radiations and all F
d = 200 mm

## Slide 5
Reverse current simulation
1. Carrier generation via single level
Ngen vs. fluence dependence
Linear dependence of Ngen
vs. F - agrees with data on Ib(F)
Simple and direct approach

## Slide 6
Reverse current simulation
2. Carrier generation via two levels (TL simulation)
– microscopic approach; two independent processes
DD: Ev + 0.48 eV; DA: Ec – (0.5250.005) eV
– midgap levels used in all PTI simulations and fits
NB!
Variables: introduction rates K, s, Nt

## Slide 7
Reverse current simulation
2. Carrier generation via two levels (TL simulation)
KDA/KDD = 1; KDD = 0.8
DD: Ev + 0.48 eV; DA: Ec – (0.5250.005) eV
KDA/KDD = 2; KDD = 0.8, KDA = 1.6
NB!

## Slide 8
Parameters of two level simulation
protons
neutrons
Generation via two midgap levels,
DDs and DAs, adequately describes Ig(T)
Generation rate is determined by a larger energy gap
se – sensitive for DD
sh – sensitive for DA
G. Kramberger, NIM A 515 (2004) 109 – parameters of dominant traps are defined at continuous injection
DDs: se = (0.8-1)x10-13 cm2, sh = 1x10-15 cm2
DAs: se = 1x10-14 cm2, sh = (0.7-2)x10-14 cm2

## Slide 9
Contribution of DDs and DAs to Ib
Contribution from DAs prevails
Contributions to current from DDs and DAs are close
KDA/KDD = 1; KDD = 0.8
KDA/KDD = 2; KDD = 0.8

## Slide 10
Reverse current simulation
How many levels?
I(T), neutrons, F = 1x1012 cm-2  Additional generation level?
Contribution from E-center
3rd level: DA2, Ec – 0.43 eV
kDD = 0.5
NDA1/NDD = 1 NDA2/NDA1 = 5
Contribution from DA2 prevails
- agrees with [E. Borchi and M. Bruzzi, NIM A 310 (1991) 273]

## Slide 11
Whether DLs with Ea ~ 0.4 eV can affect Igen (occupancy of DLs vs. T)
Feq ~ 1014 cm-2 DLs: DD, DA, VV-
NVV = 1x1014 cm-3
NVV = 1x1016 cm-3
In plots: concentration of charged DLs and total Neff
Deep levels with Ea ~ 0.4 eV (VV, Ci-Oi) hardly affect I(T) dependence
DLs with Ea ~ 0.4 eV affect:
♦ space charge region depth (at very high F);
♦ trapping time constant
NVV = 1x1017 cm-3
Neff

## Slide 12
I(T) and E(x) simulation using parameters
of two level approach
2.3x1014 n/cm2; 200 V; 200 mm
Double peak is less pronounced at lower T

## Slide 13
Impact of parameter variation on E(x)
DDs: Ev + 0.48 eV; DAs: Ec – 0.52 eV
E(x) has DP shape
1: KDA = 1; KDD = 1
2: KDA/KDD = 2; KDD = 0.8, KDA = 1.6

## Slide 14
E(x) profile vs. V and F
DDs and DAs parameters as extracted from Ib(T) dependences

## Slide 15
Impact of Ig on E(x) profile
Key parameters for adequate E(x) description: deep levels and generation current
Impact of Igen – double peak (DP) E(x) Simulation without current – no DP E(x)
Igen gives correct E(x) reference
to other characteristics (CCE, tdr)
Alternative approach:
Generation may be considered via lifetime
– used by M. Moll,
Delhi University group
Presented E. Verbitskaya, et al., 21 RD50 workshop, CERN, Nov 14-16, 2012
F = 1e15 n/cm2; 500 V, 300 mm

## Slide 16
Relationship between generation lifetime and trapping time constant
Ibgen = eniVol/tgen; Ibgen = aFVol
tgen = (eni /a)F-1
tgen  15ttr
E. Verbitskaya, et al., 20 RD50 workshop, Bari, May 30 – June 1, 2012
tgen = 4.32x107/Feq
ttr_e = 3.1x106/Feq
ttr_h = 2.9x106/Feq
Feq = 1x1015 cm-2
tgen = 40 ns
ttr_e,h ≈ 3 ns
I. Mandić, et al.,
NIM A 612 2010) 474
be = 3.2x10-16 cm2s-1; be = 3.5x10-16 cm2s-1
Trapping: all levels with Ea>0.2 eV contribute to t
Generation: only midgap levels contribute

## Slide 17
In PTI simulations:
 Ibgen may be described as:
- carrier generation in Ibgen via effective level with Ea = 0.65 eV;
- independent generation via midgap DDs and DAs
 Two level approach gives microscopic parameters of DDs and DAS
E(x) profile formation in irradiated Si detectors may be described as:
Carrier generation + trapping to midgap DDs and DAs.
 Two level model with a consideration on bulk generation current gives adequate description of irradiated Si detector characteristics
Conclusions