## Slide 1
Summary of Simulation Work for HPK Campaign
Ranjeet Singh, Ashutosh Bhardwaj, Kirti Ranjan
Center for Detector & Related Software Technology (CDRST)
Department of Physics and Astrophysics,
University of Delhi (DU), Delhi, INDIA
RD-50 Simulation group meeting
27-28 March 2013

## Slide 2: Contents
Introduction
Simulations for p-type MSSD,s
  For non-irradiated MSSDs
  For irradiated MSSDs
Simulation for n-type
  With P-stop isolation structure
  With P-spray isolation structure
Diode Simulation
  non-irradiated Diodes
  irradiated Diodes
Summary

## Slide 3
Most of the volume of a future Tracker will be equipped with planar silicon sensors
  A survey of available silicon materials has been started
  One wafer layout has been developed and the various materials are processed with this mask by the same producer, which allows well defined comparisons
  Investigation of the properties of several layout options for strip, strixel and pixel sensors is going on
  A well defined measurement plan has been worked out and participating institutes have been inter-calibrated to guarantee comparable measurements
  For the test wafers a producer was chosen
  that can provide the large quantity and high
  quality we need  “HPK campaign”
  Measurements are
  complemented by device simulations
The CMS HPK campaign & motivations
HPK wafer layout

## Slide 4: 17 institutes currently involved in HPK campaign
Firenze
Bari

## Slide 5: Simulations for p-type of MSSD (Non-irradiated & Irradiated)

## Slide 6
12 Configurations of Multi-SSD in HPK
Strip length = 3.0490 cm
Experimental results of Cint taken from Lyon Tracker Upgrade Database http://ikcms02.fzk.de/probe/lyon2/login.php
P+-N--N+ configuration chosen for these results.
For each design, three separate results for non-irradiated sensors and one result for irradiated sensor is given.

## Slide 7
Simulation of Cint for Multi-SSD – Previous Results
First results on Cint comparison was shown in Sensor Upgrade Meeting – “MSSD Simulation Results “ on 17 Feb. 2011
P+-N--N+ configuration
Two P+ neighboring strips
Cint results were ~ 30% lower than experimental values
TWO HALF-STRPS
DC-ELECTRODES
AC-ELECTRODES
Metal-Overhang
SiO2
Si-Substrate
https://indico.cern.ch/getFile.py/access?contribId=1&resId=0&materialId=slides&confId=125774

## Slide 8
Simulated Structure – zoomed region
Simulation of Cint for Multi-SSD
Instead of Two adjacent half- P+ neighboring strips, we have considered five strips in which Cint is evaluated by sending AC signal to central electrode and measuring it w.r.t. two adjacent strips (which are dc-shorted).

## Slide 9
Simulation of Cint for Multi-SSD
We also performed “sensitivity studies” for Substrate Doping Concentration (NB), Metal Overhang Width(WMO), Oxide Thickness (tox) , Junction Depth (XJ), Coupling Oxide Thickness, Strip pitch (P), Strip Width (W), Surface charge density (Qf).
We varied NB (range: 1.0x1012 cm-3 - 5.0x1012 cm-3 ) and Qf (range: 1x1010 cm-2 - 2x1012 cm-2 ) keeping other parameters fixed (which have minor impact).
We compared various set of (NB , Qf) for one structure, keeping other parameters fixed. Once we compared it with one design, we kept the same values of NB and Qf for all other designs.
2.5x1011 cm-2
1.5x1011 cm-2
1.0x1011 cm-2
2.5x1012 cm-3
3.5x1012 cm-3
3.0x1012 cm-3
Rise point of Cint curve
was used to fix NB
slop of Cint curve
was used to fix QF

## Slide 10
1.Substrate Doping Conc. (NB) = 3.0x1012 cm-3
2. Surface Charge Density (Qf) = 1.0x1011 cm-2
3. Temp = 21deg C corresponding to 294 K.
4) n+ implant of 30 micron from the back side
5) Junction depth of 1.5 micron
6) Strip length for normalization = 3.0490 cm
7) Total device depth is 320 micron.
8.) Frequency = 1MHz
Simulation Parameters – Same for all 12 configurations
2. Other than Width and Pitch, nothing else is changed in 12 Configurations.

## Slide 11: Non Irradiated
In all the plots shown on next page :
Colors – Red, Blue and Green show the three Cint measurements
Color – Magenta show the simulated result

## Slide 12: Non Irradiated MSSD
One of the Expt. result
Excellent agreement
Excellent agreement
Excellent agreement
Excellent agreement
– Red, Blue and Green show the three Cint measurements
Magenta show the simulated result
A good agreement was obtained for other detectors also

## Slide 13: Simulations for irradiated p-type MSSDs
Nb=3e12 cm-2, and QF=1e11 cm-2
(Measurements by Marco Meschini, The sensors have been irradiated at a fluence of 5e14 neq/cm² with annealing of 24h at 25°C + 5h at 20°C + 10 minutes at 60°C )
Cint simulation using the following radiation damage model: 1. T = -20 degC ( 253.15 K)
2. Use of improved EVL model
(“Simulation of Heavily Irradiated Silicon Pixel Sensors and Comparison with Test Beam Measurements”, Vincenzo Chiochia, et. al., 2004 IEEE Nuclear Science Symposium, October 18-21 2004, Rome, Italy.) A.) Donor: EV + 0.48 eV; introduction rate, gint = 9.25; sigma e = 1e-15 cm2 and sigma h = 0.25 e-15 cm2
B.) Acceptor: EC - 0.525 eV; introduction rate, gint = 3.7; sigma e = 1e-15 cm2 and sigma h = 0.25 e-15 cm2
But simulations with EVL model parameters also gave similar results

## Slide 14: Irradiated MSSD
Excellent agreement
Excellent agreement
Red Color – Measurement
Green – Simulated Result
These results were presented in 20th RD50 Workshop on Radiation hard semiconductor devices for very high luminosity colliders (30 May 2012 to 01 June 2012 (Europe/Zurich) Bari )
A good agreement between experimental and simulation results was observed.
Similar agreement was obtained for other detectors also

## Slide 15
Simulation of Cint for Multi-SSD with Double P-stops
Instead of two adjacent half- n+ neighboring strips, we have considered five strips in which Cint is evaluated by sending AC signal to central electrode and measuring it w.r.t. two adjacent strips (which are shorted).
Simulated Structure – zoomed region
Double P-stops
4µm wide separated by 6µm

## Slide 16
Effect of QF on Cint
For QF = 0
No initial bump !
For QF = 3x 1010 cm-2
Initial dip in Cint along with slow rise and finally plateau region
For QF = 5x 1010 cm-2
Small initial bump (Initial dip have gone)
For QF = 1x 1011 cm-2
Large initial bump which decrease to plateau
Finally, for QF = 2x 1011 cm-2
--- Initial bump have spread upto ~ 350V and it look like that there is no initial bump but only a slow decrease in Cint !

## Slide 17: Cint Simulations for Pstop Isolation structure
No initial bump

## Slide 18: Cint Simulations for Pspray isolation structure
Simulation vs. Measurement for FZ320Y
  All 12 N+-P--P+ configurations (non-irradiated)
  For FZ320Y, Peak P-spray doping density =
  4x1016cm-3, P-spray doping depth = 0.2µm
  Only FIRENZE Probe station measurements
  are used for comparison

## Slide 19
FZ 320 N Diode L
(non-irradiated)

## Slide 20
Simulation structure
For Large Diode
Periphery
mm
Total implant area mm x mm
Guard
Diode center
Zoomed view
Zoomed view
mm
Total implant area 4.893 mm x 4.893mm
Diode center
Guard
Periphery

## Slide 21
CV comparison for large diode
Full depletion ~ 200V for measurements and simulations
Slightly lower Capacitance
for simulations?
(pF-2)

## Slide 22
IV comparison
293K

## Slide 23
Irradiated diode simulations

## Slide 24
Irradiation Simulations
Three flux irradiation data( 1.1e14cm-2, 5e14cm-2 and 1e15cm-2) for large diode
(Thanks to Robert Eber for data and alpha calculator link!)
For flux = 1.1e14cm-2 and 1e15cm-2 , Annealing time = 50.23 Hours
For flux = 5e14cm-2 , Annealing time = 33.16 Hours
Irradiation parameterization is carried out by using two trap model (Modified EVL)
The following parameters are used in two trap model A.) Donor: EV + 0.48 ev; introduction rate (gint) = 9.25; Sigma e =1e-14 cm2 and
Sigma h = 1.5e-14 cm2
B.) Acceptor: EC - 0.525 ev; introduction rate (gint) = 3.7; Sigma e = 1e-14 cm2 and
Sigma h = 1.5e-14 cm2

## Slide 25
IV comparison for Large diode (FZ320N)
Flux = 1.1e14 cm-2
Temp = 253K
Simulation & Measured values are ~ 10%

## Slide 26
IV comparison for Large diode (FZ320N)
Flux = 5e14 cm-2
Temp = 253K
Simulation & Measured values are ~ 10%

## Slide 27
IV comparison for Large diode (FZ320N)
Flux = 1e15 cm-2

## Slide 28
CV comparison for Large diode (FZ320N)
Flux = 1e14 cm-2
Significantly different VFD

## Slide 29
CV comparison for Large diode (FZ320N)
Flux = 5e14 cm-2
Significantly different VFD for Simulations and Experiments

## Slide 30
CV comparison for Large diode (FZ320N)
Flux = 1e15 cm-2
Similar VFD for Simulations and Experiments

## Slide 31
CV comparison for Large diode (FZ320N)
Flux = 5e14 cm-2 & 1e15 cm-2
VFD for Simulations increases with flux as trap density is taken proportional to flux but for measurements it saturates quickly
No way to incorporate this effect in simulations!
F=5e14cm-2 Simulation
F=1e15cm-2 Simulation

## Slide 32
IV & CV comparison for Large diode Flux = 1e14 cm-2
Full Depletion Voltage using IV ~ 50V
Full Depletion Voltage using CV ~ 110V
Full depletion voltage is considerable different for IV and CV plots !
How to reproduce it !

## Slide 33
IV & CV comparison for Large diode Flux = 5e14 cm-2
Full Depletion Voltage using IV ~ 270V
Full Depletion Voltage using CV ~ 680V
Full depletion voltage is considerable different for IV and CV plots !

## Slide 34
IV & CV comparison for Large diode Flux = 1e15 cm-2
Full Depletion Voltage using IV ~ 660V (Difficult to say) ?
Full Depletion Voltage using CV ~ 660V
Full depletion voltage is considerable different for IV and CV plots !

## Slide 35
Simulation results of Cint of n-type MSSD of HPK are in good agreement for all the designs for both non-irradiated and irradiated Sensors.
Simulation study for Cint of n+- p-- p+ MSSD with double P-stops has been carried out. Most of the simulated Cint values are within 20% of the experimental values. Simulation indicate presence of the of Oxide charge density ~ 3e10cm-2
CV and IV comparison is done between simulation and measurements for large non-irradiated as well as irradiated diodes.
-- CV & IV comparison for Non-irradiated Diode seems good
-- Leakage current is tuned with Tau0=1.6x10-2sec.
-- CV and IV comparison for irradiated diodes can be carried out by two trap model.
-- Leakage current for irradiated diodes is reproduced well.
-- Full depletion voltage obtained by CV plots is significantly lower for flux = 1e14 cm-2 and flux =5e14cm-2.
Full depletion voltage obtained from measurements by IV and CV plots are inconsistent but consistent in simulation plots.
Simulations for TCT and CCE are in progress.
Summary/Future plan

## Slide 36
Thanks!

## Slide 37
Backups!

## Slide 38
Diode center
2.4465mm
Total implant area 4893mm x 4893mm
22.5µm
12.5µm
17µm
90µm
Dimensions from masks for DiodeL
660µm
Implant
Guard
Periphery