## Slide 1
Influence of HTS Wire and Coil Configuration on Quench Propagation Guillaume Escamez
Clement Lorin,
Denis Netter,
Philippe J. Masson. University of Houston Department of Mechanical Engineering Texas Center for Superconductivity October 10th, 2013

## Slide 2: NASA’s Distributed Propulsion Aircraft

## Slide 3: Distributed Propulsion – LH2 Cooling Network
LH2 can be used to cool-down superconducting components and power converters
Network dynamic simulation is used to determine the requirements of energy storage devices and reconfiguration
Turboshaft

## Slide 4: Project Objectives
Develop a high fidelity sizing tool for fully superconducting rotating machines.
  Accurate 3D geometry represented
    Electromagnetics, mechanical and thermal
  Portable code in Python and C
Develop model for quench propagation
  Address detection and protection
Develop new model for AC losses for superconducting stators
  Based on FEA simulations
Validate AC losses model experimentally

## Slide 5: Sizing Model “Amber” Version 0.9
Electromagnetic model
  Geometry accurately represented
  No mesh in air
  Based on integral methods (GFUN – Biot Savart)
Mechanical model
  Geometry accurately represented
  Steel and composite materials
  Thermal and force induced stress
Thermal model
  Total cryogenic heat load and temperature distribution estimated using finite differences
  Cryogenic system based on LH2 or Ghe and Reversed Turbo-Brayton cryocoolers
Zeroth order analytical sizing model (2D) used for preliminary optimization

## Slide 6: Winding Geometry
Symmetry planes
Simulations performed on 1/4th of the geometry
Backiron
Stator winding
Rotor winding
First step focuses on quench in the rotor winding
Objective is to evaluate the impact of quench protection on the machine design

## Slide 7: Quench in Superconductors
*
Hot Spot
I
T
V
Stabilizer
Superconductor

## Slide 8: Quench model
Model
Conductor topology/materials
Winding geometry
NZPV
MQE
Peak temperature
versus τdischarge
NZPV: Normal zone propagation velocity
MQE: Minimum quench energy
τdischarge : time constant of the discharge
Detection parameters (Voltage)
Protection parameters (τdischarge )
YBCO Tapes
MgB2 conductors
Cu
Hastelloy
Cu
YBCO

## Slide 9: YBCO Tape Configuration
2 mm Ag
20mm Cu
20mm Cu
50mm Nickel Hastelloy substrate
1 mm YBCO - HTS (epitaxial)
~ 50 nm Buffer
x
z
y
< 0.1 mm
20mm Cu
50mm Hastelloy
20mm Cu
Kapton Insulation

## Slide 10: Electrical Properties
Anisotropic model
Infinite transversal equivalent resistivity (insulator)
  Resistivity on x-axis
  Infinite resistivity on y-axis and z axis (Use of Katpon)
Kapton
Kapton
Cooper
Silver
YBCO
Nickel
Rkapton
Rcopper
Rsilver
RYBCO
Rnickel
Rbuffer
Rkapton
x
z
econductor
estack
L
Current

## Slide 11: Flux and Temperature Distribution in Superconducting Machine
Need to consider field distribution and temperature gradient in winding for YBCO equivalent resistivity

## Slide 12: YBCO Layer Critical Current
Jc data from SuperPower – 2G HTS Tape w/ Advanced Pinning
YBCO Jc(B,T) Scaling Law
A/m2
with
and
 | YBCO T<50K | YBCO T≥50K
Tc(K) | 92 | 92
p | 0.95 | 0.73
q | 2.568 | 1.69
m | 1.98 | 1.98
λ | 1.98 | 1.54
Birr0 (T) | 88 | 91
C0 | 3.5e7 | 1e7
Ec (V/m) | 10-6 | 10-6
n | 30 | 30
Chart: Magnetic Field (T)
| 0 | 0.5 | 1 | 2 | 3 | 4
exp-77k | 250000000 | 110000000 | 74250000 | 46750000 | 33000000 | 26250000
exp-60K | 692250000 | 423000000 | 313250000 | 225250000 | 178500000 | 148250000 | 126250000
exp-50K | 980750000 | 717000000 | 588000000 | 456000000 | 379000000 | 332500000 | 296750000
exp-40K | 1329750000 | 1131750000 | 997250000 | 860000000 | 780250000 | 700500000 | 645500000
exp-30K | 1741750000 | 1626250000 | 1516500000 | 1371000000 | 1280250000 | 1200500000 | 1099000000
exp-20K | 2186750000 | 2126250000 | 2027500000 | 1895500000 | 1794000000 | 1664750000 | 1533000000
fit-20K | 2386267838.2773 | 2294049926.9379 | 2237327959.5525 | 2194877145.7205 | 2160172139.5475 | 2130340727.1211 | 2103863771.8643 | 2079840354.8933 | 2057692338.2569 | 2037026603.0758 | 2017563699.3717 | 1999097863.9703 | 1981473195.2338 | 1964568736.0897 | 1948288746.8242 | 1932556142.1461 | 1917307932.9099 | 1902491980.0956 | 1888064632.4355 | 1873988973.9573 | 1860233501.7692 | 1846771113.2693 | 1833578319.7696 | 1820634628.3924 | 1807922050.7968 | 1795424708.7352 | 1783128514.399 | 1771020909.1567 | 1759090648.3298 | 1747327622.6005 | 1735722708.8128 | 1724267644.543 | 1712954922.0338 | 1701777698.0113 | 1690729716.6097 | 1679805243.1823 | 1668999007.2021 | 1658306152.7929 | 1647722195.6983 | 1637242985.7073 | 1626864673.7257 | 1616583682.8213 | 1606396682.6775 | 1596300566.9877 | 1586292433.3895 | 1576369565.6065 | 1566529417.5092 | 1556769598.8545 | 1547087862.4946 | 1537482092.8772
fit-30K | 1756175304.9802 | 1685533589.62 | 1641144994.5469 | 1607337743.7538 | 1579289537.0997 | 1554876016.8349 | 1532972668.9555 | 1512912053.822 | 1494265505.4096 | 1476741296.5079 | 1460131874.8093 | 1444284284.0683 | 1429082531.0944 | 1414436541.3589 | 1400274954.1994 | 1386540259.8221 | 1373185420.3756 | 1360171462.8095 | 1347465726.321 | 1335040561.7592 | 1322872349.9444 | 1310940749.4221 | 1299228112.1526 | 1287719024.0497 | 1276399939.6536 | 1265258888.6904 | 1254285238.1762 | 1243469497.9 | 1232803160.1187 | 1222278566.4836 | 1211888796.8228 | 1201627575.6054 | 1191489192.8139 | 1181468436.6367 | 1171560535.9222 | 1161761110.7394 | 1152066129.7116 | 1142471873.0357 | 1132974900.3018 | 1123572022.382 | 1114260276.785 | 1105036905.9749 | 1095899338.2361 | 1086845170.7324 | 1077872154.4647 | 1068978180.8766 | 1060161269.8959 | 1051419559.2299 | 1042751294.7606 | 1034154821.9055
fit-40K | 1223558073.3784 | 1171197842.1011 | 1137283892.8446 | 1110838826.7556 | 1088480018.7932 | 1068715280.1709 | 1050753646.6238 | 1034125000.5933 | 1018526980.689 | 1003753519.2927 | 989657791.2301 | 976131429.6395 | 963092127.731 | 950475868.124 | 938231850.368 | 926319064.9622 | 914703911.354 | 903358499.8993 | 892259414.7768 | 881386795.3266 | 870723642.2004 | 860255285.3252 | 849968970.3725 | 839853533.3718 | 829899141.8188 | 820097086.59 | 810439613.1338 | 800919783.3504 | 791531361.6906 | 782268720.5391 | 773126761.0862 | 764100846.7341 | 755186746.7239 | 746380588.1519 | 737678814.9169 | 729078152.4269 | 720575577.1203 | 712168290.0309 | 703853693.769 | 695629372.3985 | 687493073.784 | 679442694.0499 | 671476263.8552 | 663591936.2336 | 655787975.7893 | 648062749.0697 | 640414715.9635 | 632842421.9966 | 625344491.4132 | 617919620.9493
fit-60K | 678908085.2003 | 557695068.4605 | 495099680.6641 | 453707503.6336 | 423061060.5089 | 398834443.3393 | 378844534.647 | 361844836.7991 | 347060560.4798 | 333979180.916 | 322245092.0516 | 311602061.1035 | 301859704.2078 | 292872919.246 | 284528719.575 | 276737499.7675 | 269427063.1896 | 262538430.1038 | 256022827.8541 | 249839486.2081 | 243953993.6466 | 238337052.38 | 232963521.913 | 227811674.8195 | 222862610.8816 | 218099790.9867 | 213508662.6919 | 209076356.7382 | 204791439.0426 | 200643706.4818 | 196624017.5455 | 192724150.9826 | 188936687.089 | 185254907.4386 | 181672709.7381 | 178184535.1592 | 174785306.0264 | 171470372.1445 | 168235464.3756 | 165076654.3225 | 161990319.1871 | 158973111.0265 | 156021929.7671 | 153133899.4399 | 150306347.1885 | 147536784.6711 | 144822891.5384 | 142162500.7157 | 139553585.2593 | 136994246.589
fit-70K | 154594226.7969 | 124273179.8212 | 107904760.9807 | 96660900.609 | 88055068.6384 | 81051163.7295 | 75122573.871 | 69966501.3619 | 65393424.9274 | 61277113.2388 | 57529388.5351 | 54086289.9379 | 50899982.8069 | 47933776.895 | 45158925.5154 | 42552494.4557 | 40095899.5021 | 37773876.2992 | 35573738.0956 | 33484830.1701 | 31498121.6999 | 29605895.6265 | 27801509.6622 | 26079209.7883 | 24433983.0563 | 22861440.2203 | 21357721.292 | 19919418.9144 | 18543515.7406 | 17227332.9304 | 15968487.5673 | 14764857.3014 | 13614550.9072 | 12515883.7385 | 11467357.2861 | 10467642.2222 | 9515564.4625 | 8610093.8916 | 7750335.5078 | 6935522.8364 | 6165013.5616 | 5438287.4342 | 4754946.6419 | 4114719.0033 | 3517464.589 | 2963186.7451 | 2452049.084 | 1984401.0048 | 1560816.0943 | 1182151.1726
fit-50K | 970000000 | 910000000 | 843923414.4739 | 775954580.88 | 725984092.6011 | 686743222.025 | 654567729.9999 | 627367704.0831 | 603845509.7748 | 583143680.9987 | 564667918.3964 | 547990456.9212 | 532793802.5266 | 518836234.2066 | 505929732.2802 | 493925344.6795 | 482703186.1608 | 472165422.9431 | 462231238.4557 | 452833147.8712 | 443914251.9017 | 435426157.9294 | 427327383.85 | 419582116.7613 | 412159236.3394 | 405031538.2853 | 398175110.8449 | 391568829.7508 | 385193945.7221 | 379033744.9897 | 373073267.9456 | 367299074.4287 | 361699046.7181 | 356262223.2256 | 350978657.352 | 345839297.094 | 340835881.8649 | 335960853.6725 | 331207280.3335 | 326568788.8296 | 322039507.2457 | 317614014.0054 | 313287293.3349 | 309054696.0646 | 304911905.0233 | 300854904.3961 | 296879952.5165 | 292983557.6441 | 289162456.3428 | 285413594.1358

## Slide 13: YBCO Jc Dependence on Field Direction
Incidence magnetic field
Bi
θ
y-axis
Anisotropic critical current, magnetic field dependency
Jc: Critical current density (A/m2)
Bi: Incidence magnetic field (T)
Fit values for 0% Zr doping
A=5.97 γ=7
B=21.39 β=0.438
J
Percentage of improved pinning by Zr in YBCO tape

## Slide 14: Electrical Equivalent Properties
Example of electrical resistivity of material and coil for J/Jc = 0.6, no field

## Slide 15: Equivalent Thermal Properties
Kapton
Kapton
Cooper
Silver
YBCO
Nickel
x-axis
Rthkapton
Rthcopper
Rthsilver
RthYBCO
Rthnickel
Rthbuffer
Rthkapton
x
y
Kapton
Kapton
Cooper
Silver
YBCO
Nickel
z-axis
R’thkapton
R’thcopper
R’thsilver
R’thYBCO
R’thnickel
R’thbuffer
R’thkapton
z
y
Kapton
Kapton
R’’thkapton
R’’thcopper
R’’thsilver
R’’thYBCO
R’’thnickel
R’’thbuffer
R’’thkapton
y-axis
R2thkapton
R’’thkapton

## Slide 16: Thermal conductivities
Equivalent conductivities versus temperature

## Slide 17: Equivalent Heat Capacity
Heat capacity:
Ceq: equivalent heat capacity (J/Kg/K) C: heat capacity of layers (K/Kg/K)
m: mass of layers (Kg)

## Slide 18: COMSOL Computational Model
Input
Geometry Operation current
Compute magnetic flux density
Compute equivalent properties ρeq, keq, Ceq , Qj at magnetic field and Temperatures
Affect equivalent properties ρeq, keq, Ceq to the windings
Solve
for small time step
Use temperature distribution
Parameterized model implemented in COMSOL
Winding properties are calculated in COMSOL

## Slide 19: Magnetic Flux Density Distribution

## Slide 20: Coil heat source
Joule losses versus temperature at constant magnetic field (1T)
Superconducting state
With: - Joperating: operating current density (A/m2)
- σcoil: equivalent conductivity of the coil (S/m)
- Pj: Joule losses in the coil (W/m3)
- Vi: specific volume (m3)

## Slide 21: Thermal model
Cooling from inner pole surface (heat exchange coefficient)
Joule losses in the winding as Heat source
Heat pulse
Heat source:
- Rectangle pulse
- Start time: 0.1s
- Duration 220 ms
- Value ≈ 5 W at 77K
t(s)
0.1 0.32
Power (W)
5
0

## Slide 22: Example of Quench Simulation at 77 K
Heat pulse (W)
Heat pulse (W)
Propagation mainly along x-axis
Chart: maximal temperature versus time
| 0.09 | 9.1410000000000005E-2 | 9.282E-2 | 9.5640000000000003E-2 | 9.9269999999999997E-2 | 0.1036 | 0.10742 | 0.11123 | 0.11885999999999999 | 0.12648999999999999 | 0.13411999999999999 | 0.14939 | 0.16464999999999999 | 0.19517000000000001 | 0.22264 | 0.25011 | 0.27757999999999999 | 0.29810999999999999 | 0.31512000000000001 | 0.32979000000000003 | 0.34187000000000001 | 0.35394999999999999 | 0.36603000000000002 | 0.37809999999999999 | 0.40226000000000001 | 0.42399999999999999 | 0.44574000000000003 | 0.46748000000000001 | 0.51097000000000004 | 0.55445 | 0.64141000000000004 | 0.71967999999999999 | 0.79795000000000005 | 0.87622 | 0.95448 | 1.09548 | 1.23648 | 1.37748 | 1.5184800000000001
Top=77K | 77 | 77 | 77 | 77 | 77 | 77.9659 | 79.0117 | 79.9009 | 81.5632 | 83.0794 | 84.4737 | 87.0535 | 89.3905 | 94.8164 | 100.1684 | 105.192 | 109.8977 | 113.1989 | 115.8193 | 117.0408 | 117.674 | 118.1428 | 118.3194 | 118.3775 | 118.186 | 117.8589 | 117.4109 | 116.9103 | 115.8841 | 114.8845 | 113.3819 | 112.7296 | 112.622 | 112.9697 | 113.6966 | 115.787 | 118.6363 | 122.0736
Chart: Voltage drop versus temperature
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9
 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2
Top=77K | 5.3229e-07 | 5.3229e-07 | 5.3229e-07 | 5.3229e-07 | 5.3229e-07 | 5.3229e-07 | 5.3229e-07 | 5.3229e-07 | 5.323e-07 | 5.3232e-07 | 8.8824e-06 | 0.00337 | 0.01 | 0.01902 | 0.0292 | 0.03983 | 0.05049 | 0.05839 | 0.06538 | 0.07109 | 0.07556 | 0.07971 | 0.08364 | 0.08738 | 0.09503 | 0.10189 | 0.10916 | 0.11686 | 0.1323 | 0.14984 | 0.19178 | 0.23747 | 0.29524 | 0.3665 | 0.45524 | 0.67556 | 0.9945 | 1.4609 | 2.1606

## Slide 23: Normal Zone Propagation Velocity
Quench Propagation velocity (x-axis)
Getting value during post processing

## Slide 24: Quench detection
Voltage probe
if V< Vthreshold
then 0
else
then 1
Integration
of the voltage probe
t(s)
Voltage
during detection
Voltage probe
t1
t1+ε
Step to trigger coil discharge
t(s)
a
a
1
Total heat source time exponential
decrease:
With the discharge time constant
L the inductance of the winding, R: the dump resistance
And
t(s)
τdischarge
t6
t2

## Slide 25: Example of Quench Simulations
Voltage detection
  Threshold: 400 mV
  Current discharge time constant: 0.5 s
Pulse of heat induces quench in winding
Top: 50 K I/Ic=0.7
*

## Slide 26: Minimum Quench Energy

## Slide 27: Temperature Profiles for Different Discharge 

## Slide 28: Impact of Detection Threshold on Peak Temp.

## Slide 29: Impact of I/Ic on the Discharge Time Constant

## Slide 30: Peak Temperature vs. Je
Chart: Winding engineering current density (A/mm2)
| 115 | 153.33333333333334 | 317.76315789473682
20 K | 220 | 250 | 700
30 K | 300 | 225 | 210
40 K | 365 | 235 | 215 | 208 | 197 | 180
50 K | 300 | 220 | 190.4 | 166.4 | 150.4
60 K | 195 | 177 | 147.8 | 135 | 129.2 | 125
70 K | 122.4 | 113.2

## Slide 31: Influence of Copper Content on Coil Performance
Chart: Highest admissible engineering current density (peak temperature at 300 K) versus operating temperature
| 20 | 30 | 40 | 50 | 60 | 70
eCu:200um | 168 | 172 | 180 | 175 | 146.0317 | 65.71
eCu:100um | 218 | 223 | 240 | 235 | 217 | 108.94
eCu:50um | 270 | 290 | 312 | 308 | 295 | 162

## Slide 32: Influence of Copper Content on Coil Performance (40K)
Chart: Copper layer thickness (μm)
| 200 | 100 | 50 | 25 | 10 | 0 | 15 | 20 | 5
Top40 | 180 | 240 | 312 | 340 | 345 | 272 | 352 | 348 | 308
15 μm copper layer thickness leads to the highest engineering. current density in the winding

## Slide 33: Summary and Perspectives
Parameterized model developed for YBCO
  Quench behavior can be estimated from
    Materials composing winding
    Jc(B,T) characteristic of the superconductor
    Voltage detection threshold
    Discharge time constant
Python code is being generated based on simulation results and will be implemented in Amber
    Quench protection will be used as additional constrains for the machine design
  More data needs to be generated to extract response surface
  Need coupling with external electric circuit model
    magnetic coupling, quench back
  Development of an in house flexible tool independent from FEA commercial packages is being considered