## Slide 1: Quench modelling for accelerator magnets
L. Bottura and S. Izquierdo Bermudez
CERN TE-MSC
Boston
October 9th-11th, 2013
A Case Study and Various Other Considerations relevant to

## Slide 2: Outline
Motivation
Scaling analysis
Quench modeling and issues
A “real-life” example
An attempt to transpose experience gained in quench modelling for fusion to the domain of accelerator magnets

## Slide 3: Motivation: MQXF for HL-LHC
Aperture | (mm) | 150
Gradient | (T/m) | 140
Current | (A) | 17500
Temperature | (K) | 1.9
Peak field | (T) | 12.1
Shell-based support structure (aka bladder-and-keys) developed at LBNL for strain sensitive material
HQ image by courtesy of H. Felice (LBNL)

## Slide 4: More motivation: 11 T dipole
Aperture | (mm) | 60
Field | (T) | 10.8
Current | (A) | 11850
Temperature | (K) | 1.9
Peak field | (T) | 11.3
Integrated pole loading
Removable pole loading
By courtesy of A. Zlobin (FNAL) and M. Karppinen (CERN)
Jop ≈ 800 A/mm2
em ≈ 150 MJ/m3

## Slide 5: Scaling: adiabatic heat balance
The simplest (and conservative) approximation for the evolution of the maximum temperature during a quench is to assume adiabatic behavior at the location of the hot-spot:
Average heat capacity:
Average resistivity:

## Slide 6: Scaling: hot spot temperature
adiabatic conditions at the hot spot :
can be integrated:
cable operating current density
total volumetric heat capacity
stabilizer resistivity
B.J. Maddock, G.B. James, Proc. IEE, 115 (4), 543, 1968
The function G(Tmax) is a cable property quench capital
The integral of J depends on the circuit quench tax

## Slide 7: Material properties
copper resistivity
Useful power approximation
copper G(Tmax)
B=0 T
Wilson’s Gamma

## Slide 8: Quench Capital vs. Tax
The real problem is to determine the integral of the current waveform: how much is the quench time tquench ?
Two limiting cases:
  External-dump: The magnet is dumped externally on a large resistance (Rdump >> Rquench) as soon as the quench is detected (e.g. ITER)
  Self-dump: The circuit is on a short circuit and is dumped on its internal resistance (Rdump = 0) (e.g. LHC)

## Slide 9: “Self dump”
The magnetic energy is completely dissipated in the internal resistance, which depends on the temperature and volume of the normal zone
In this case it is not possible to separate the problem in quench capital and quench tax, but we can make approximations
Assume that:
  The whole magnet is normal at tdischarge (perfect heaters)
  The current is constant until tquench then drops to zero
  Wilson’s Gamma and the power resistivity
L
Rquench
D
normal operation
quench
S1

## Slide 10: Scaling for “self dump”
Temperature
Quench time
magnet bulk
hot-spot
Details as from M. Wilson, Superconducting Magnets, Clarendon Press, 1986

## Slide 11: Scaling study for “self dump”
Cu/Nb3Sn
fCu ≈ 0.55
fSC ≈ 0.45
Iop ≈ 10 kA
tdischarge ≈ 0.1 s
Tmax
em limited
Jop limited
Jop ≈ 800 A/mm2
em ≈ 150 MJ/m3
Remember…
for the 11 T dipole:
LHC
11 T
ITER

## Slide 12: Detection, switch and dump
precursor
propagation
detection
detection threshold
trigger (t=0)
fire heaters
switch
magnet quenched
tdetection
tvalidation
theater
tdump
tquench ≈ tdetection + tvalidation + theater +f tdump
tdischarge
Example of an LHC dipole magnet training quench
≈ 50…100 ms

## Slide 13: Quench (modeling) issues
What is the time needed to detect a normal zone ? Longitudinal quench propagation speed
What is the time needed to induce a distributed quench, using quench heater or comparable mechanism ? Heater delay
What is the time needed for the quench to “invade” the whole magnet cross section (and the magnet tu dump) ? Transverse quench propagation speed

## Slide 14: Quench model for a 11 T dipole
Turns 1…9
10…17
18..20
21,22
Turns 1…16
17…34
40 Nb3Sn strands
14.7 mm x 1.25 mm
0.1 mm insulation
ANb3Sn = 7.2 mm2
ACu = 8.2 mm2
Aepoxy-glass = 5.5 mm2
6 blocks coil
2 layers/pole
56 turns
Outer layer
Inner layer
Heater
Iop = 11850 A
L/l = 6.8 mH/m
wedge

## Slide 15: Quench modeling – unfolding
Identify in the winding the longitudinal and transverse (principal) directions
The longitudinal
cable is a continuum
“relatively easy” to solve
with accurate (high order) and
adaptive (front tracking) methods

## Slide 16: Longitudinal propagation speed
≈30 m/s
Adaptive mesh tracking fronts
≈600 m/s
Adaptive mesh: minimum element size 1 mm
Static mesh: 100 mm
Example of a quench in a Nb3Sn 11 T cable triggered over 10 cm in a high field (11 T) zone (uniform field assumed)
Small mesh size and/or adaptive meshing are a must for quench analysis

## Slide 17: Longitudinal propagation
Conductor only
Conductor/insulation
Conductor+insulation
Appropriate subdivision is important to resolve relevant temperature gradients

## Slide 18: Quench model – thermal coupling
Continuum models
  3-D mesh of the magnet system allows for a natural treatment of geometry
  Examples:
    OPERA-quench (MICE)
    ANSYS (e.g. LBNL, FERMILAB)
    COMSOL (e.g. TUT)
X.L. Guo et al., Cryogenics 52 (2012) 420–427
Network models
  Simplified connectivity and thermal resistances
  Examples:
    SARUMAN and following (LB)
    Gavrilin, 1992
    ROXIE (S. Russenschuck, B. Auchmann, N. Schwerg)
    …
L. Bottura, O.C. Zienkiewicz, Cryogenics 32 (1992) 659-667

## Slide 19: First order thermal coupling
Convection not considered -> cooling by helium mass flow can not be taken into account
Finite volumes and linear approximations:
Transverse direction
Longitudinal direction
Heat capacity:
includes conductor + insulation
Thermal conductance and heat fluxes:
Conductor without insulation. Uniform temperature in the conductor and linear temperature distribution in between them
Implementation in ROXIE, N. Schwerg, B. Auchmann, S. Russenschuck

## Slide 20: Higher order thermal coupling
Thermal resistance
Heat capacity
cable
insulation
Refine the 1-D thermal resistance
A. Gavrilin, Cryogenics, 32 (1992), 390-393
Hybrid model (DOF<->FEM)
SUPERMAGNET
VINCENTA
4C
FE mesh
Coupling
This would be great, but how to make it work in case of quench ?!?

## Slide 21: Coupling to circuit model
From MT-23 4OrCa-01

## Slide 22: Case study: simulations performed
ROXIE
  3-D slice simulation, scaled by the length
    1-D model of the cable
    2-D thermal network, first order thermal coupling
  Self-consistent current and field model
  Case 1: QH powered with nominal power (LF: 70.5 W/cm2; HF: 45.5 W/cm2)
  Case 2: OL temperature raised above Tcs after measured QH delay
SUPERMAGNET
  3-D model of the complete magnet
    1-D simulation of cable, adaptive mesh
    2-D thermal network, second order coupling
  Self-consistent current calculation, scaled field
  Quench triggered at the HF pole turn, detected (100 mv, 10 ms)
  QH modelled as power input to OL with 25 ms delay
Quench of MBPS01, 1 m long, single aperture, 11 T dipole model
Magnet running at 11850 A, quench triggered by QH
case | IT tins (mm) | IL tins (mm) | QH power (W/m)
1 | 0.2 | 0.2 | 400
2 | 0.2 | 0.4 | 400
3 | 0.2 | 0.2 | 100
4 | 0.2 | 0.4 | 200

## Slide 23: Quench simulation – 1
Current vs. time
The current waveform is reproduced fairly well within a relatively broad range of (quite uncertain) parameters

## Slide 24: Quench simulation – 2
Temperature vs. time (at the QH)
Temperatures suffer from much greater uncertainty, but no data is available for direct comparison

## Slide 25: Quench simulation – 2
Temperature vs. time (at the QH)
≈ 350 K
Peak temperature hidden by overall behaviour !!!
150…200 K
IL-OL delay ≈25 ms vs. 13 ms measured

## Slide 26: Lots of further details
Transverse heat transfer (geometry, properties, anysotropy) – measure !
Numerical stability, convergence, consistence
Quench heater efficiency (geometry, heat diffusion)
Effect of cooling (helium bath, superfluid, flows ?)
Quench-back (AC loss distribution in the coil and structure)
Resistive, inductive, capacitive effects in the circuit (non-linear components such as cold diodes, internal voltages)
A daunting problem ?
A wonderful playground

## Slide 27: Conclusions
New accelerator magnets based on Nb3Sn are pushing the boundary of protection
Accurate simulation of quench transients in these magnets is crucial to the design choices, definition of priority R&D and to prove that the magnets are fit for operation
We have today large uncertainties in the simulation results, depending on the hypotheses (inputs). It is essential to establish a good understanding of the dominating physics, and collect (new ?) data in well controlled and heavily instrumented experiments
This is a challenge for the CHATS community !!!

## Slide 28: Typical quench sequence (case 4)

## Slide 29: Typical quench sequence (case 4)

## Slide 30: ROXIE Quench Module
Fourth-order Runge-Kutta algorithm.
Adaptive time stepping
Field computation
(computationally more demanding, weak coupling, magnetic field updated a number of times that can be defined by the user)
Electrical network
Thermal network
Critical surface model
B
Ploss
L
I
POhm
I
R
T
Explicit Runge-Kutta solver: Conditionally stable
Adaptive time stepping: Necessary, high non-linear problem
Static mesh: computationally “expensive”

## Slide 31: Simulation : Test bench conditions
Manual trips with the two operating protection heaters
  Dump delay 1000 ms  Self-dump (non-linear inductance and resistance)
  I0 = 11850 A, Tbath = 1.9 K
 | MIITs after heater effective [MA2s] | MIITs from heater fired until effective [MA2s] | OL-IL delay [ms] | PH delay [ms]
Experimental data | 10.9 | 3.4 | 13.4 | ≈27
CASE1: OL heaters fired @ t=0 (computed heat transfer from heater to coil) | 12.3 | 2.9 | 42.5 | 21
CASE2: OL quenched @ PH measured delay (OL fully quenched at PH measured delay) | 11.4 | 3.8 | 33.8 | 27
Max. Temperature [K]
Heaters fired @ t=0
OL quenched @ measured delay

## Slide 32: Heaters delay
Chart: I/Iss (%)
| 71.4085690282834 | 63.00756090730888 | 49.00588070568464
measured MBSHP02 | 29.6 | 33.9 | 48
roxie MBSHP02 | 27.05 | 33.86 | 48.16
measured MBSHP01 | 42.8 | 59.6 | 78.3
roxie MBSHP01 | 44.3 | 59 | 75