## Slide 1
Losses Scaling Law for Superconducting Filaments Magnetized by an Elliptical Field. Clement Lorin,
Denis Netter,
Philippe J. Masson. University of Houston Department of Mechanical Engineering Texas Center for Superconductivity October 11th, 2013

## Slide 2: NASA’s Distributed Propulsion Aircraft

## Slide 3: Project Objectives
Develop a high fidelity sizing tool for fully superconducting rotating machines.
  Accurate 3D geometry represented
    Electromagnetics, mechanical and thermal
  Portable code in Python and C
Develop model for quench propagation
  Address detection and protection
Develop new model for AC losses for superconducting stators
  Based on FEA simulations
Validate AC losses model experimentally

## Slide 4: Frequency Dependence of AC Losses
3 sources of AC losses in superconductors:
  Magnetization losses Pmagα B, f, Jc
  Coupling losses Pcoupl α B2, f2
  Eddy current losses PEddy α B2, f2
Magnetization losses are dominating at low frequency

## Slide 5: Magnetization (Hysteresis) Losses Calculation
Assumes AC field (alternating)
  Limited to self field
Transport current and applied field are in phase
Jc: filament critical current density
s: fraction of superconductor
d: filament size
B0: flux density variation
F: I/Ic

## Slide 6: Stator Peak Field at Full Load
Non uniform flux density distribution
Flux density contribution from both rotor and stator

## Slide 7: Introduction (1/3)
Magnetization losses in stator wires of rotating machines:
  Stator: Rotating field generated by temporal variation of currents inside the windings.
  Rotor: Rotating and Alternating field produced by rotation of the spatial distribution of the currents.
   Local field = rotating field + alternating field

## Slide 8: Introduction (2/3)
Peak field
Probe #
Rotating/pulsating
Phase angle rotating-pulsating
In 1 pole, each stator conductor is in a unique magnetic configuration

## Slide 9: Introduction (3/3)
Armature
Cross-Section
Filaments are twisted and magnetically decoupled
  Analysis can be done on 1 filament
  Model implemented in COMSOL Multiphysics
  Sc. Modeled using a power law
  No current yet

## Slide 10: Model description (1/2)
Geometry and model description:
H-Formulation:
Boundary conditions:
k = [0,1] → field configuration: “ellipticity”
f frequency
B0 field amplitude
φ = [-π,π]
Electrical behavior, power-law:
n n-value
Jc critical current @ Ec = 100 μV/m
r filament radius
7 variables

## Slide 11: Model description (2/2)
Loss [J/m/cycle]:
Filament cross-section (πr2)
Over 1 cycle

## Slide 12: Dimensional Analysis (1/2)
Dimensional Analysis:
Variable | Usual unit | [kg] | [m] | [s] | [A] | 
Jc | A.m-2 | 0 | -2 | 0 | 1 | n1
μ0 | H.m-1 | 1 | 1 | -2 | -2 | n2
r | m | 0 | 1 | 0 | 0 | n3
Ec | V.m-1 | 1 | 1 | -3 | -1 | n4
Q (per cycle) | J.m-1 | 1 | 1 | -2 | 0 | n5
B0 | T | 1 | 0 | -2 | -1 | n6
f | Hz | 0 | 0 | -1 | 0 | n7
ϕ | rad | 0 | 0 | 0 | 0 | 
k | adim | 0 | 0 | 0 | 0 | 
n | adim | 0 | 0 | 0 | 0 | 
3 dimensionless numbers
f* , b* , q*
This number must be dimensionless.
Remark: adding a current It would lead to an additional dimensionless number.

## Slide 13: Dimensional Analysis (2/2)
Our parameters:
with
with
and n, k, φ
5 variables
instead of 7
with
Those parameters can be called invariants since the reduced losses q do not change if they do not change.
Reduced losses:
with
b*
f*

## Slide 14: Alternating field losses – SL (1/5)
b*
f*
k=0
n

## Slide 15: Alternating field losses – SL (1/5)
n = 20
q* versus f* for various b*
We need to reorder the charts to explain the thought process which led to a semi-analytical formula for AC losses under alternating field or rotating field
b* = 20
b* = 10
b* = 2
b* = 1
b* = 0.5
b* = 0.25

## Slide 16: Alternating field losses – SL (2/5)
n = 20
b* = 20
b* = 10
b* = 2
b* = 1
b* = 0.5
b* = 0.25
A curve seems to be revealed.
We try to scale the ordinate to get reduced losses values in the same order of magnitude, to do so we divide q* by b*2
 Then we try to adjust the abscissa values for each values of b* so as to create a curve with all the dots looking like the black curve above.
q*/b*2 versus f* for multiple b*
(bp = b* former notation)

## Slide 17: Alternating field losses (n=20) – SL (3/5)
If we divide the abscissa by b*2 
If we divide the abscissa by b*4 
If we divide the abscissa by b*10 
If we divide the abscissa by b*19 

## Slide 18: Alternating field losses (n=10) – SL (4/5)
If we divide the abscissa by b*2 
If we divide the abscissa by b*4 
If we divide the abscissa by b*9 
We did the same for n = 2, n= 3, n = 5, n = 40, n = 50
Dividing by b*n-1 aligns the data points. Instead of an abscissa f*/b*n-1 we can use (f*/b*n-1)1/n
to match Critical State Model (i.e. no frequency dependency when n).
b*(n-1)/n
f*1/n
q
b*2

## Slide 19: Alternating field losses – Scaling Law (5/5)
Data can be normalized with respect to a function of n
with
with
with

## Slide 20: Losses in Rotating field Scaling Law
b*
f*
k=1
n

## Slide 21: Losses in Rotating field Scaling Law
Data can be normalized with respect to a function of n
with
with
with
Rotating field: k = 1
Same method
Coefficients α1 α2 α3 α4 α5 are different

## Slide 22: Elliptical field
b*
f*
k
n

## Slide 23: Elliptical field
k = 0.25, 0.5, 0.75
k
1
1
1
1
0
alt
ell
rot
Q*
X*
Same method

## Slide 24: Fit(b*,f*,n,k) or fit (cn,n,k)
Fit curves
General expression:
Q*
X*
Error on data used to get the fit (~600):

## Slide 25: Elliptical field – with phase angle
b*
f*
k
n


## Slide 26: Elliptical field – with phase angle
Ratio between losses with and without phase angle can be approximate by:

## Slide 27: Elliptical field – with phase angle
Transform to
k1 must be in [0,1] to use our previous fit.
Based on geometrical considerations on the applied field.
So is known.
 Lorin C. , Masson P.J., Numerical Analysis of the Impact of Elliptical Fields on Magnetization Losses, IEEE TAS, 23, 3, 8201405 (2013)

## Slide 28: Random test
Results
60 simulations randomly taken in the whole domain

## Slide 29: Conclusion
Investigation of elliptical field losses in smooth power-law electrical behavior round-shaped filaments:
  Reveal a fundamental variable:
  Semi-analytical formulae give fast and reliable magnetization losses values depending on:
k = [0,1] → field configuration: “ellipticity”
f frequency
B0 field amplitude
φ = [-π,π]
n n-value
Jc critical current @ Ec = 100 μV/m
r filament radius

## Slide 30: Next Steps (1/2)
Electrical behavior, power-law:
where
H-Formulation:
Boundary conditions:
k = [0,1] → field configuration
φ = [-π,π] → rotor load angle
bp penetration field ratio
ip = [0,1] → penetration current ratio
θ = [0,2π] → current/field phase angle
Transport current constrain:
where A = filament area

## Slide 31: Next Steps (2/2)
Implement model in Amber HTS Machine Sizing Code
Perform experimental validation
  Tests will start in January 2014
    AC field
    Transport current
  Upgrade to include elliptical field scheduled for 2015
Sample Cryostat
GHe Transfer Line
Cooling System