## Slide 1: GEM and Micromegas production Rui De Oliveira TE/MPE/EM

## Slide 2: Summary
GEM Single mask process
Micromegas
  Bulk
  Classical
  resistive

## Slide 3: GEM process step by step

## Slide 4
5um Copper
5um Copper
50um Polyimide
Base material
50um adhesiveless copper clad Polyimide
Rolls of 100m x 600mm
Polyimide : APICAL NP or AV
2 suppliers :
Sheldhal (US)
Nippon steel (Jp)
CR layer 10nm

## Slide 5
Photoresist deposition
15um dry resist (KL 1015 – Korea)
15um resist
15um resist
Maximum size 100m x 600mm
Dupont manual laminators

## Slide 6
Photoresist holes patterning
15um resist
15um resist
70um

## Slide 7
Top copper etching

## Slide 8
Resist stripping

## Slide 9
Polyimide anisotropic etching

## Slide 10
Bottom resist protection deposition

## Slide 11
Bottom copper etch by chemical reaction
Top copper protected by galvanic connection
etchant

## Slide 12
Resist stripping

## Slide 13
Soft Polyimide etching
The hole become double conical

## Slide 14: cross section pictures

## Slide 15: Comparison with std GEM from external supplier

## Slide 16: examples
Large GEM already produced:
ILC Dhcal: 1m x 33cm (5 pieces)
Kloe: 750mm x 40cm (30pieces)
CMS: 1m x 45cm (40 pieces)

## Slide 17: GEM single mask process summary
Chemical Polyimide etching
Second Polyimide etching
Copper electro etching
Stripping
Reality

## Slide 18
PCB
lamination
Mesh deposit
lamination
development
Bulk Micromegas
BULK Technology
DUPONT PC 1025 coverlay
BOPP Meshes
SERITEC stretching

## Slide 19
19
Pad read-out 1cm², thickness 8mm for ILC Hadronic calorimetry
Tested in the RD51 1 kHz beam.
The BULK is made on a populated PCB
Bulk Micromegas ILC DHCAL first m2
LAPP Annecy
Pad read-out large TPC
Neutrino detector
10 sqr meter in service
T2K experiment
Japan (CEA Saclay)

## Slide 20
Resistive Bulk MicroMegas

## Slide 21
PCB
PCB
PCB
-Not compatible with pitches
smaller than 0.4mm
-Thixotropic paste
Screen printing of for the resistive strips

## Slide 22
Double sided Board
Resistive strip deposit
Bulking
Test before closing
Closing

## Slide 23
Rohacell
Aluminum support plate
Stiffening panel
Drift electrode
Pillars (128 µm)
PCB1
PCB2
Classical MicroMegas resistive or not
1 x 1m2 not to scale detector opened

## Slide 24
Stiffening panel
Rohacell
Aluminum support plate
5.00
PCB1
PCB2
1 x 1m2 not to scale detector closed

## Slide 25
flat gluing
< 10um error
Flat board < 30um error
Mesh on drift (10Ncm )