## Slide 1: Mechanical analysis of Foam and plastic honeycomb panels
Simon Gonzalez

## Slide 2: Foam Panel
Composition of Foam Panel
  FR4 skins
  Blue plastic mesh
  Glued with Araldite 2011 (side 1) and Araldite AY-103 (side 2)
  Aluminum frame
Scans of the panel were done on both sides along the length and width of the panel.

## Slide 3: Results From Side 1
Standard deviation from measurements (in mm)
  0.16411 for Z(136)
  0.11056 for Z(288)
  0.06977 for Z(527)
  0.05125 for Z(688)
Chart: 
Standard deviation from measurements (in mm)
  0.05451 for Z(200)
  0.07511 for Z(400)
  0.05545 for Z(715)
  0.05803 for Z(900)
Chart: 

## Slide 4: Results From Side 2
Chart: 
Standard deviation from measurements (in mm)
  0.0387 for Z(108)
  0.0439 for Z(511)
Chart: 
Standard deviation from measurements (in mm)
  0.03568 for Z(400)
  0.03909 for Z(715)
  0.03947 for Z(900)
  0.02269 for Z(200)
The graphs is generated by subtracting the panel form the marble reference.

## Slide 5: Large Honeycomb Panel
Consist of a plastic honeycomb.
Scans of the panel were done on both sides along the length and width of the panel.

## Slide 6: Results From Side 1 Edge and Side 2 Edge A to B
Chart: 
Standard deviation from measurements (in mm)
  0.05247 for Z(117)
  0.0846 for Z(441)
  0.08411 for Z(791)
  0.09544 for Z(1163)
Chart: 
Standard deviation from measurements (in mm)
  0.0999 for Z(52.64)
  0.07321 for Z(771.36)

## Slide 7: Results From Side 1(edges C to D and D to C), Side 2 (edges C to D and D to C)
Chart: 
Standard deviation from measurements (in mm)
  0.1965 for Z(401.82)
  0.14259 for Z(986.5)
  0.25678 for Z(400.72)
  0.22024 for Z(987.4)
Chart: 
Standard deviation from measurements (in mm)
  0.2421 for Z(403.57)
  0.19152 for Z(984.18)
  0.17784 for Z(402)
  0.11398 for Z(983)

## Slide 8: Results From Curve Side 1(edges C to D and D to C), Side 2 (edges C to D and D to C)
Chart: 
Standard deviation from measurements (in mm)
  0.0348 for Z(401.82)
  0.0513 for Z(400.72)
  0.0439 for Z(986.5)
  0.0317 for Z(987.4)
Chart: 
Standard deviation from measurements (in mm)
  0.0379 for Z(403.57)
  0.0255 for Z(402.00)
  0.0340 for Z(984.18)
  0.0379 for Z(983)