## Slide 1: MM mechanical prototype
Work progress at CERN

## Slide 2: Purpose
Demonstrate feasibility
Setup of basic infrastructure
Gain experience with
  Materials
  Construction/assembly ideas/schemes
  Procedures
  Precision (panel planarity, parallelism of skins, …)
Produce objects that can be measured
Establish an Assembly Manual

## Slide 3: CERN mechanical prototype (1)
Full-wedge small sector quadruplet
  Eta and stereo doublet
Drift gap spacers: 5 mm
Total thickness: ~80 mm
Gas distribution
Mesh?

## Slide 4
All panels of equal thickness – 12 mm
  Frame of standard t=10 mm Al profiles
  0.4 mm plastic mesh
  9.5 mm foam panels
  Skins – 0.5 mm FR4
  Glue – Araldite 2011 – Araldite AY 103-1 + HY 991 – Araldite AY 103-1 + HY 951
CERN mechanical prototype (2)

## Slide 5: The table
Size: 4 x 2.5 m
Flatness: ≤ 20 µm
Location: Bld. 153

## Slide 6: Stiff-back (1)
Vacuum
Clarinet gas
Skin (G10)
Precision insert
Rohacell honeycomb
Vacuum
Using Skin suction Tool
Vacuum
Expansive glue
Vacuum
Precision shim

## Slide 7: Stiff-back (2)
Simple stiff-back structure with suction heads (following small test structure) used for 2 x 1 m2 prototype
CERN-DT group is working on a final system using a perforated honeycomb structure with a perforated lower skin
Work in progress
  Small 50 x 50 cm2 prototype ready for the test
  Large, full wedge size, if prototype successful
60 mm

## Slide 8
Gluing (1)
Step 1 – FR4 skins were placed and sucked
on the table
Step 2 – Plastic mesh was wetted with
the glue and placed on the FR4
Step 3 – Frame foam panel were placed on the mesh

## Slide 9
Gluing (2)
Second skin was placed and sucked on the table
Glue was distributed on the surface
Plastic mesh was wetted by glue and placed on the skin
Prepared “half panel” picked up with the stiff-back structure and placed on the mesh
Calibrated shims were placed under the stiff-back

## Slide 10: First experience (1)
Two full-wedge size drift panels were glued
The planarity of the panels seems good – to be measured on the laser interferometer
  Araldite AY103 + HY991 seems the optimal
Some problems with the gluing
  Some regions where mesh is not glued to the skin
  Use other type of glue?
  Change the gluing procedure?
  Increase the glue gap?

## Slide 11
First experience (2)
Full panel view
Inner structure
Problematic regions

## Slide 12: Collaborative effort
CERN, Dubna, Lecce …
Drawings and calculations: Lecce and CERN
Infrastructure and tooling: CERN
Technical work: CERN, Dubna, Lecce + 3 summer students (2 physicist + 1 engineer)