## Slide 1: In situ SEM DC experiments in Uppsala – update 01 July 2013
Tomoko Muranaka

## Slide 2: Preparation
Cathode: Copper (SLAC etching + 1040deg H2 heating)
  EBSD analysed
Anode: Tungsten 7um

## Slide 3: Experiments
Grain dependent field emission measurement
  5 measurements on (111), (101), (001)
Field emission stability measurement
  1 measurement (for 2000 points, about 30minuites) on (111), (101), (001)
Breakdowns for warm-like feature observation
  1 BD on (111), (101), (001)
  Supply 1kV at 5um gap then make the anode closer step by step until the current constantly over 1uA.

## Slide 4: Measurement area
101
111
001

## Slide 5: Field emission onset voltage
The onset voltage varies 700-1000V except three spots (two on (101), one on (111)).
Chart: onset voltage (measured current exceeded 10nA)
| 1 | 2 | 3 | 4 | 5
(001) | 893 | 878 | 932 | 755 | 791
(111) | 825 | 900 | 556 | 1000 | 912
(101) | 501 | 1000 | 658 | 699 | 828
Chart: onset voltage (measured current exceeded 0.5pA)
| 1 | 2 | 3 | 4 | 5
(001) | 867 | 870 | 912 | 716 | 785
(111) | 824 | 852 | 554 | 1000 | 910
(101) | 488 | 931 | 656 | 695 | 825

## Slide 6: Emission stability (001), 800V
Chart: Step (0-2000 measurement point)
Ramping up from 600V, “stay” if the current once exceeded 0.5pA (background was 0.2pA). 2000 meas. points ~ 30minuites

## Slide 7: Emission stability (101), 600V
Chart: Step (0-2000 measurement point)

## Slide 8: Emission stability (111), 990V
Chart: Step (0-2000 measurement point)

## Slide 9: Breakdown site (001)

## Slide 10: Breakdown site (101)

## Slide 11: Breakdown site (111)

## Slide 12: Breakdown site (111)

## Slide 13: Anode tip after three BD