## Slide 1: Talk Over View - LHC Insertion history - MQXC magnet special features - Test over view - Training MQXC0 & MQXC2 - Heat extraction. - Quench heater Delays - New superconducting magnet protection system!
LHC IR Upgrade Nb-Ti, 120mm Aperture Model Quadrupole Test Results at 1.8K
G.A. Kirby
B. Auchmann, M. Bajko, V.I. Datskov, M.Durante P. Fessia, J. Feuvrier, M.Guinchard, C. Giloux, P.P. Granieri, P. Manil, J.C. Perez, E. Ravaioli, J.M.Rifflet, S. Russenschuck,
T. Sahner, M. Segreti, E.Todesco, G. Willering.

## Slide 2: Triplet Upgrade

## Slide 3
MQXC phase 1 Upgrade,
fallback solution, & technology transfer MQXD
Today's LHC insertion magnets 70mm
KEK’s - MQXA and FERMI- Lab’s-MQXB
Phase 1 upgrade MQXC cross section 120mm
120 T/m Nb-Ti high cooling capability
CERN-OXFORD Ins. LHC
1989
D1 Nb-Ti separation dipole
Nb-Ti out line proposal at KEK
Q4 Nb-Ti Quad
Nb-Ti out line
proposal at CEA Saclay
All the data for most of the magnets are in www.cern.ch/hilumi/wp3
MQXF Nb3Sn 150mm, 140T/m
Previous talk!
MQY / LHC Q4
1998
1996
2009
2012

## Slide 4: The Enhanced Cable Insulation
Enhanced insulation system from Davide TOMMASINI
Heat extraction plot from Pier Paolo Granieri PhD theses

## Slide 5
Open Ground Insulation
Closed ground insulation
Open ground insulation
Closed ground insulation
Open collaring shoe
Open Ground Insulation
Thermal plots thanks to : E. Bielert

## Slide 6: MQXC High Heat Extraction Design
Open cable insulation, open ground insulation

## Slide 7: Electrical checks
We performed electrical checks at each stage of production.
1KV pulse test looking for shorts in the coils.
5KV ground insulation tests.
Resistance and inductance of coils
Insulation between all circuits.
Quench heater firing at full 850V, 80A

## Slide 8: Test lab. For Model magnets at CERN
20KA Power Supply Current Transducer Control Room data racks Test Cryostat
Dump resistor Switch
Magnet in
transport frame
8

## Slide 9: Magnet Circuit

## Slide 10: Test Over View

## Slide 11: MQXC2 training comparison with MQXC0
Chart: Training MQXC0 & 2
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45
MQXC2 Training Quenches | 10850 | 11485 | 11733 | 12146 | 12404 | 12802 | 12911 | 12791 | 13118 | 13458.7 | 13450
MQXC2 De-training | 12218 | 13366
MQXC0 Training | 11385 | 11859.8 | 12300 | 12226 | 12538 | 13249

## Slide 12: Heat Extraction Beam Simulation Heaters
Chart: 
| 2 | 2.5 | 3 | 3.3 | 6
Coils 1-3 | 1.0111 | 1.5833 | 2.2833 | 2.8233 | 9.1333
Coils 3-2 | 1.1 | 1.7222 | 2.4833 | 3.08 | 10.2
Coils 3-2 | 1.1 | 1.7222 | 2.4833 | 3.08 | 10.2
Coils 2-4 | 1.0156 | 1.5833 | 2.2833 | 2.8233 | 9.1667
Coils 1-4 | 1 | 1.5694 | 2.25 | 2.805 | 9.1
Total power W/m from heaters | 4.1267 | 6.4583 | 9.3 | 11.5317 | 37.6
Initial observations
MQXC2 ~ 5W/m
MQXC0 ~ 10W/m

## Slide 13: Quench heater performance
Chart: 
| 0.8 | 1 | 3 | 5 | 7 | 9 | 11 | 12.8
MQXC0 40A Quench heater current | 160 | 148 | 117 | 77 | 20 | 12 | 6
MQXC 2 40A Quench heater current | 160 | 97 | 62 | 51.8 | 10

## Slide 14: Coil Resistance during Quench.
Two curves are plotted, giving the circuit resistance needed to limit the hot spot temp. One limiting the cable hot spot to 300K and the second limiting, HS. to 100K. With a 0.012 s detection delay.
We see from the tests that the internal coil resistance is insufficient at all currents to protect the magnet.
With 60% quenched cable we could protect the magnet!
100K max hot spot
300K max hot spot
Hotter hot spots
Without Dump adiabatic calculated Hot Spot 1200K

## Slide 15: New Coupling Loss Induced Quench Protection System for Superconducting Accelerator Magnets “CLIQ”
“AC-Current Induced Quench Protection system”, application has been filed with the European Patent Office on June 28, 2013 under the application number EP13174323.
3OrCB-03

## Slide 16: Magnet Circuit
CLIQ lead
3/4
1/4

## Slide 17: CLIQ set up & PSU modification

## Slide 18: Simulation of a Quench induce by a Capacitive Discharge

## Slide 19: 9KA comparison Quench heaters and CLIQ
9KA, QH @40A +EE
9KA, CLIQ + EE @150ms
(capacitor voltage at 400V)

## Slide 20: Simulation v Measurements
CLIQ possibilities :
- Fast repair to existing systems
- Nb-Ti, Nb3Sn and HTS protection
- Fast protection
- Uses no real-estate in magnet
- Good prediction of effects.
Best performance: (symmetric, 500 V, 12.8 kA)
In 20 ms 50% coil quenched
In 50 ms 80% coil quenched

## Slide 21: Special thanks to the rest of CLIQ team
Mk2
Mk1
1st Signals
Vladimir Datskov
Emmanuele Ravaioli
Francois-Olivier Pincot
Marta Bajko, Jerome Feuvrier

## Slide 22: Thanks to the teams.
The many people that have worked on the Nb-Ti MQXC over last 5 years.

## Slide 23
Any Questions