## Slide 1: MBW-MQW in the LHC
Considerations on expected life and available options
Presented by P. Fessia
Fluka analysis: Francesco Cerutti, Anton Lechner, Eleftherios Skordis
Collimation input: Rodrick Bruce, Stefano Redaelli , Belen Maria Salvachua Ferrando , Elena Quaranta
MNC team: Paolo Fessia, Pierre Alexandre Thonet, D. Tommasini
Power Converter: Hugues Thiesen
Optics: Massimo Giovannozzi
MME design office: L. Favre, T. Sahner
VSC: Eric Page, N. Zelko

## Slide 2: Summary
The magnets
The expected dose
Evaluation of the magnet lifetime
Protective actions
  Shielding
  Optics changes
The present “final” picture
Actions, planning and risks

## Slide 3: MQW point 7 and 3
Characteristics | RQ4.LR7 | RQ5.LR7 | RQT4.L7 | RQT5.L7 | RQT4.R7 | RQT5.R7 | RQ4.LR3 | RQ5.LR3 | RQT4.L3 | RQT5.L3 | RQT4.R3 |  | RQT5.R3
I ultimate (from layout database) [A] | 810 | 810 | 600 | 600 | 600 | 600 | 810 | 810 | 600 | 600 | 600 |  | 600
Voltage I ultimate [V] | 381 | 383 | 29 | 31 | 27 | 29 | 451 | 452 | 38 | 34 | 42 |  | 39
I 7 TeV (Fidel report) [A] | 598 | 610 | 151 | 17 | 151 | 17 | 561 | 593 | 313 | 441 | 313 |  | 441
Voltage I 7 TeV [V] | 282 | 289 | 8 | 2 | 8 | 2 | 313 | 331 | 20 | 31 | 22 |  | 29
Number magnet in series in circuit | 10 | 10 | 1 | 1 | 1 | 1 | 10 | 10 | 1 | 1 | 1 |  | 1
Turn/magnet | 171 |  |  |  |  |  |  |  |  |  |  |  | 
Estimated ultimate inter-turn voltage [V] | 0.22 | 0.22 | 0.17 | 0.18 | 0.16 | 0.17 | 0.26 | 0.26 | 0.22 | 0.2 |  | 0.25 | 0.23
Estimated inter-turn voltage at 7 TeV [V] | 0.16 | 0.17 | 0.05 | 0.01 | 0.05 | 0.01 | 0.18 | 0.19 | 0.12 | 0.18 |  | 0.13 | 0.17
Estimated inter layer voltage | Same as inter turn |  |  |  |  |  |  |  |  |  |  |  | 
Insulation thickness inter turn | 2X(2X0.25) mm=1 mm glass tape |  |  |  |  |  |  |  |  |  |  |  | 
Circuit energy ultimate [Kj] | 154 | 164 | 9 | 9 | 9 | 9 | 154 | 164 | 9 | 9 |  | 9 | 9
Circuit energy 7 TeV [Kj] | 84 | 93 | 0.6 | 0.01 | 0.6 | 0.01 | 74 | 88 | 2.5 | 5 |  | 2.5 | 5
Ground insulation | 1X(2X0.25) mm+3X(2X0.25)=2 mm |  |  |  |  |  |  |  |  |  |  |  | 
Resin used | EPN1138 42%+ GY 6004 42% + CY 221 16% + HY 905 100 %+ 30ml DY 073 |  |  |  |  |  |  |  |  |  |  |  | 
Dielectric resin | > 20 kV/mm |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 4: MBW point 7 and 3
Characteristics | RD34.LR7 | RD34.LR3
I ultimate [A] (layout database) | 810 | 810
Voltage I ultimate [V] | 440 | 700
I 7 TeV (Fidel report) | 643 | 643
Voltage I 7 TeV | 350 | 556
Number magnet in series in circuit | 8 | 12
Turn/magnet | 84 | 
Estimated ultimate inter-turn voltage [V] | 0.65 | 0.7
Estimated inter-turn voltage 7 TeV [V] | 0.52 | 0.55
Estimated ultimate inter layer voltage [V] | 9.2 | 9.7
Estimated inter layer voltage 7 TeV [V] | 7.2 | 7.8
Circuit energy ultimate [Kj] | 472 | 793
Circuit energy 7 TeV [Kj] | 297 | 500
Insulation inter turn [mm] | 2X(2X0.15)=0.6 glass tape | 
Insulation inter layer [mm] | 2X(2X0.15)+2X(2X0.15)+1(glass cloth) =1.6 glass tape | 
Ground insulation | 2X(2X0.15)+1.5(0.15Xx)=1.8 glass tape | 
Resin used | EPC-1: resin ED-16 100 Hardener MA 2.28  K Plasticizer MGF-9 20 TEa accelerant 0.5 | 
Dielectric resin | Unknwown (>>15kV/mm) | 

## Slide 7: Analysis exp. data point 3 and point 7
RP survey IP3
RP survey IP7
7R/7L=B2/B1
3R/3L=B2/B1
297.4 kGy
8.0 kGy
1.6 kGy
6.7 kGy
81.7 kGy
1.3 kGy
2.3 kGy
fallen off
(487.3 kGy)
25.7 kGy
100.4 kGy
59.6 kGy
> 500 kGy
43.7 kGy
19.1 kGy
1/6
1/10
1/3
1
397.5 kGy
119.8 kGy
> 500 kGy
106.3 kGy
487.3 kGy
469.1 kGy
297.4 kGy
329.4 kGy
15.7 kGy
6.3 kGy
18.0 kGy
9.2 kGy
4.4 kGy
5.5 kGy
2.3 kGy
1/100
1/20
1
1

## Slide 8: Point 3 and 7 coil magnet damage estimation
MQW | MBW
From 10 to 20 MGy | From 40 to 60 MGy
From 20 to 50 MGy | From 60 to 80 Mgy
Larger than 50 MGy | Larger than 80 MGy
IP 7
IP 3

## Slide 9: Screen design
- For max effectiveness we have to target the higher possible density candidate therefore W, or better the alloys for machining
- Magnetic properties can be an issue. Measurement being performed
- Possible material staging along the MQW magnet length under study
 | Inermet IT180
Nominal density | 18
W content % | 95
Balance | Ni,Cu
E-modulus | 360 GPa

## Slide 10: MQW shielding effect
Normalization: 1.15 1016 p (50 fb-1 )
Beam 2
Beam 2
Beam 2
Beam 2

## Slide 11: MBWA - MBWB Peak Dose profile
MBW.B6R7 Flanges + Protection
Beam 2
MBW.A6R7
Flanges + Protection
Beam 2
MBW.A6R7 with Flanges
Beam 2
Normalization: 1.15 1016 p (50 fb-1 )
MBW.B6R7
With Flanges
Beam 2

## Slide 12
ABS
Optic change proposal point 7 discussed and agreed as possible with M. Giovannozzi
(it needs verification)

## Slide 13: Magnet damage with shielding point 3 and 7, W shielding peak dose scaling
 | Action LS1 |  | Dose [MGy] for integrated luminosity 150 fb^-1 |  | Action LS2 |  | Dose [MGy] for integrated luminosityy350 fb^-1 |  | Action LS3 |  | Dose [MGy] for integrated luminosity3000 fb^-1 |  | Action during HL-LHC exploitation | 
 | R | L | R | L | R | L | R | L | R | L | R | L | R | L
MQWA.A4 |  |  | 0.4 | 0.5 |  |  | 0.9 | 1.2 |  |  | 7.4 | 11 |  | 
MQWA.B4 |  |  | 0.3 | 0.8 |  |  | 0.7 | 1.9 |  |  | 6.4 | 16 |  | 
MQWB.4 |  |  | 0.5 | 1.3 |  | S | 1.2 | 1.8 |  | S | 10.1 | 9 |  | 
MQWA.C4 |  |  | 4.0 | 4.0 | S | S | 5.8 | 5.8 | S | S | 30 | 30 |  | 
MQWA.D4 |  |  | 2.7 | 2.7 | S | S | 3.8 | 3.8 | S | S | 20 | 20 |  | 
MQWA.E4 |  |  | 5.0 | 10.0 | S | S | 7.2 | 14 | S | S | 37 | 73 |  | R
MQWA.A5 |  |  | 2.6 | 2.6 | S | S | 3.7 | 3.7 | S | S | 19 | 19 |  | 
MQWA.B5 |  |  | 3.5 | 3.5 | S | S | 5.0 | 5.0 | S | S | 25 | 25 |  | 
MQWB.5 |  |  | 4.1 | 4.1 | S | S | 5.9 | 5.9 | S | S | 30 | 30 |  | 
MQWA.C5 |  |  | 1.9 | 4.9 | S | S | 2.8 | 7.0 | S | S | 14 | 36 |  | 
MQWA.D5 | S | S | 1.4 | 2.0 | done | done | 3.3 | 4.7 | done | done | 27.9 | 39.9 |  | 
MQWA.E5 | S | S | 12 | 4.1 | done | done | 29 | 10 | done | done | 246 | 82 | R | R
MBW.A6 | S | S | 7.8 | 5.5 | done | done | 18 | 13 | done | done | 155 | 111 | R | R
MBW.B6 | S | S | 12 | 6.2 | done | done | 30 | 14 | done | done | 248 | 124 | R | R
Limit reached in | 7R | 7L
MQWA.E4 |  | 1500 fb^-1
MBW.B6 | 1500 fb^-1 | 2400 fb^-1
MBW.A6 | 1000 fb^-1 | 2000 fb^-1
IP 7
IP 3
Remove
 | Action LS1 |  | Dose [MGy] for integrated luminosity 150 fb^-1 |  | Action LS2 |  | Dose [MGy] for integrated luminosity 350 fb^-1 |  | Action LS3 |  | Dose [MGy] for integrated luminosity 3000 fb^-1 |  | Action during HL-LHC exploitation | 
 | R | L | R | L | R | L | R | L | R | L | R | L | R | L
MQWA.A4 |  |  | 0.0 | 0.1 |  |  | 0.1 | 0.2 |  |  | 1.0 | 1.9 |  | 
MQWA.B4 |  |  | 0.1 | 0.1 |  |  | 0.1 | 0.2 |  |  | 1.0 | 2.1 |  | 
MQWB.4 |  |  | 0.1 | 0.1 |  |  | 0.1 | 0.3 |  |  | 1.1 | 2.2 |  | 
MQWA.C4 |  |  | 0.1 | 0.1 |  |  | 0.2 | 0.3 |  |  | 1.4 | 2.8 |  | 
MQWA.D4 |  |  | 0.2 | 0.3 |  |  | 0.4 | 0.8 |  |  | 3.5 | 6.9 |  | 
MQWA.E4 |  |  | 0.9 | 1.7 | S | S | 1.2 | 2.5 | S | S | 6.3 | 12 |  | 
MQWA.A5 |  |  | 0.6 | 1.1 | S | S | 0.8 | 1.6 | S | S | 4.0 | 7.5 |  | 
MQWA.B5 |  |  | 0.7 | 1.4 | S | S | 1.0 | 2.0 | S | S | 5.1 | 9.4 |  | 
MQWB.5 |  |  | 1.7 | 3.3 | S | S | 2.4 | 4.8 | S | S | 12 | 23 |  | 
MQWA.C5 |  |  | 3.9 | 7.7 | S | S | 5.6 | 11 | S | S | 29 | 53 |  | 
MQWA.D5 |  |  | 0.9 | 1.9 | S | S | 1.3 | 2.7 | S | S | 6.8 | 13 |  | 
MQWA.E5 |  |  | 1.7 | 3.5 | S | S | 2.5 | 5.0 | S | S | 13 | 24 |  | 
MBW.A6 |  |  | 1.0 | 2.0 | S | S | 1.4 | 2.9 | S | S | 7.3 | 14 |  | 
MBW.B6 |  |  | 1.2 | 2.3 | S | S | 1.7 | 3.3 | S | S | 8.4 | 16 |  | 
MBW.C6 |  |  | 1.6 | 3.3 | S | S | 2.3 | 4.7 | S | S | 12 | 3 |  | 

## Slide 14: Conclusions I
 |  | IP3 |  |  |  |  |  | IP7 |  |  |  |  | 
 |  | L |  |  | R |  |  | L |  |  | R |  | 
 |  | Broken units no int | Units to be modified | Broken units | Broken units no int . | Units to be modified | Broken units | Broken units no int | Units to be modified | Broken units | Broken units no int . | Units to be modified | Broken units
LS1 | MQW | NA | 0 | NA | NA | 0 | NA | NA | 2 | NA | NA | 2 | NA
 | MBW | NA | 0 | NA | NA | 0 | NA | NA | 2 | NA | NA | 2 | NA
LS2 | MQW | 0 | 7 | 0 | 0 | 7 | 0 | 0 | 7 | 0 | 0 | 8 | 0
 | MBW | 0 | 3 | 0 | 0 | 3 | 0 | 0 | NA | 0 | 0 | NA | 0
LS3 | MQW | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 0 | 0
 | MBW | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 0 | 0
HL-LHC | MQW | 4 | 0 | 0 | 1 | 0 | 0 | 9 | 0 | 1 | 9 | 0 | 0
 | MBW | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 0 | 2 | 2 | 0 | 2

## Slide 15: Conclusion II
The proposed screen allow reducing of a factor 3 the dose and limit the number of magnet at risk or surely damaged, see previous slides. Hp. to achieve the same reduction factor on the spacers
The change of the optic in point 7 installing a long absorber is key to complete the protection
The lifetime of these units could be affected by the new environmental condition of point 7 not discussed here

## Slide 16: Conclusion III: actions
The proposed shielding campaign should start in LS1 for effectiveness and ALARA
Very high dose dosimeter shall be installed systematically in point 3 and 7 to check better benchmark computations and symmetry effect
A campaign of irradiation of resins shall be performed with the real used resins and the relevant fillers in order to real know when the magnet will reach damage level
For HL LHC 4 MBW shall be reassembled with saddle type heads. This will solve the issue without needing special development
I suggest that we launch the program to build a NC magnet with extremely high radiation resistance (>300 MGy). It is and it will be more and more needed and today we do not have it in our capabilities and it will be key for future target areas development
We need to check
  For HL-LHC the MBW radiation dose along the straight part of the coil
  The level of accumulated dose of the MBXW units
  If any protecion can be added to on the beam line for the MQWA.E4 in point 7 R and 7 L

## Slide 17: Long version

## Slide 18: MQW coil resins
Resin used |  |  |  |  | 
component | EPN1138 | GY 6004 | CY 221 | HY 905 | 30ml DY 073
percentage | 50 % | 50 % | 20 % | 120 % | 0.03
EPN 1138 | Novolac
GY 6004 | DGEBA
CY 221 | DGEBA
HY 905 | HPA
DY 073 | flexibilizer

## Slide 19
1
2
3
4
5
6
7
8
9
10
11

## Slide 21: Different epoxy
Resins |  | Hardeners | Additives | Composition (p.p.) | Mix Temp (°C) | Viscosity (cPs) | Service life (mn) | Fig | Dose for 50% flex. (MGy) | Dose Range (MGy)
EDBAH |  | MA |  |  |  |  |  | 5.4 | 1.4 | 1 - 3
EDBAH |  | MA | BDMA | 100-105-0.2 | 80 | 45 | >180 | 5.1 | 1.6 | 
BECP |  | MA |  |  |  |  |  | 5.4 | 2.5 | 
BECP |  | MA | BDMA | 100-110-0.2 | 80 | 40 | >180 | 5.1 | 2.3 | 
ECC |  | MA |  | 100-72 | 80 | 20 | >240 | 5.5 | 1.8 | 1 - 6
VCD |  | MA | BDMA | 100-160-05 | 60 | 20 | >180 | 5.4 | 3.7 | 
DADD |  | MA |  | 100-65 | 80 | 180 | >240 | 5.4 | 5.5 | 
DGEBA + | EDGDP | TETA |  | 100-20-12 | 25 |  |  | 5.21 | 1.3 | 1 - 2
DGEBA |  | TETA | DBP | 83-9-17 | 50 | 500 | few | 5.22 | 1.2 | 
DGEBA |  | DADPS |  | 100-35 | 130 | 60 | 180 | 4.2 | 5.1 | 5 - 15
DGEBA + | EDGDP | MDA |  | 100-20-30 | 80 |  |  | 5.21 | 8.2 | 
DGEBA |  | MDA |  | 100-27 | 80 | 100 | 50 | 5.9 | 13.0 | 
DGEBA |  | MPDA |  | 100-14.5 | 65 | 200 | 30 | 5.7 | 23.5 | 23
DGEBA |  | AF |  | 100-40 | 100 | 150 | 30 | 5.26 | 45.2 | 45
DGEBA |  | DDSA | BDMA | 100-130-1 | 80 | 70 | 120 | 5.2 | 4.2 | 5 - 15
DGEBA |  | NMA | BDMA | 100-80-1 | 80 | 80 | 120 | 5.2 | 5.9 | 
DGEBA |  | MA |  | 100-100 | 60 | 69 | >1440 | 5.23 | 7.1 | 
DGEBA |  | MA | BDMA |  |  |  |  | 5.1 | 12.0 | 
DGEBA |  | MA | BDMA + Po. Gl. | 100-100-0.1-10 | 60 | 65 | 300 | 5.23 | 12.1 | 
DGEBA |  | AP |  | 100-70 | 120 | 26 | 180 | 5.2 | 13.0 | 
DGPP |  | DADPS |  | 100-28 | 130 |  |  | 5.6 | 8.2 | 5 - 15
DGPP |  | MA |  | 100-135 | 120 |  |  | 5.3 | 13.0 | 
EDTC |  | MDA |  | 100-20 | 80 |  | 40 | 5.9 | 10.0 | 
TGTPE |  | DADPS |  | 100-34 | 125 | >20000 |  | 5.6 | 12.1 | 
TGTPE |  | MA | BDMA | 100-100-0.2 | 125 | >15000 |  | 5.3 | 10.6 | 
EPN |  | DADPS |  | 100-35 | 100 |  | 30 | 5.6 | 23.5 | 20 - 40
EPN |  | MDA |  | 100-29 | 100 |  | 35 | 5.10 | 37.2 | 
EPN |  | HPA | BDMA | 100-76-1 | 80 |  | 40 | 5.10 | 13.0 | 10 - 20
EPN |  | MA | BDMA | 100-105-0.5 | 80 |  | 100 | 5.3+5.25 | 15.0 | 
EPN |  | NMA | BDMA | 100-85-1 | 100 |  | 80 | 5.10 | 20.6 | 
TGMD |  | DADPS |  | 100-40 | 80 |  | 50 | 5.6 | 20.6 | 10 - 25
TGMD |  | MA | BDMA | 100-136-0.5 | 60 |  | 30 | 5.3 | 11.4 | 
TGMD |  | NMA | BDMA | 100-110-1 | 80 | 500 | 20 | 5.8 | 18.0 | 
TGPAP |  | NMA |  | 100-137 | 80 | <20 |  | 5.8 | 23.5 | 
DGA |  | MPDA |  | 100-20 | 25 |  | 120-420 | 5.7 | 23.5 | 20 - 30
DGA |  | NMA |  | 100-115 | 25 | 5 - 20 | 30-5760 | 5.8 | 28.6 | 
Legend | 
Resin | 
 | Linear aliphatic
 | Cycloaliphatic
 | Aromatic
Hardener | 
 | Aliphatic Amine
 | Aromatic Amine
 | Alicyclic Anhydride
 | Aromatic Anhydride
Aromatic > Cycloaliphatic > Linear Aliphatic
Aliphatic amine harderner  poor radio-resistance
Aromatic amine hardener >
Anhydride hardener
H: Too high local concentration of benzene may induce steric hindrance disturbation
Good radio-resistance even if Cl (tendence to capture nth)
Novolac: HIGH Radio-resistance
Large nb of epoxy groups  Density + rigidity
Glycidyl-amine: HIGH R.-resistance
Quaternary carbon  weakness
Ether group (R – O – R’)  weakness
 Repl. by amina

## Slide 22
EPN 1138 | CY 222 (similar to CY221)
MY745 replaced by GY6004 | 

## Slide 23: Filler contribution
Resins | Hardeners | Additives | Filler | Composition (p.p.) | Fig | Dose for 50% flex. (MGy) | Dose Range (MGy)
DGEBA | MDA |  | Papier | 100-27-200 | 5.14 | 1.3 | 1 - 2
DGEBA | MDA |  | Silice | 100-27-200 | 5.14 | 10 | 10 - 15
DGEBA | MDA |  | Silice | 100-27-200 | 5.18 | 11.4 | 
DGEBA | MDA |  | Silice (5 micron) | 100-27-20 | 5.16 | 14.8 | 
DGEBA | MDA |  | Silice (20 micron) | 100-27-20 | 5.16 | 14.8 | 
DGEBA | MDA |  | Silice (40 micron) | 100-27-20 | 5.16 | 14.6 | 
DGEBA | MDA |  | Silice (40 micron) | 100-27-200 | 5.17 | 12.1 | 
DGEBA | HPA | BDMA | Silice (40 micron) | 100-80-2-200 | 5.17 | <10 | <10
DGEBA | MDA |  | Aérosil + Sulphate de Barium | 100-27-2-150 | 5.14 | 15.8 | 15
DGEBA | MDA |  | Magnésie | 100-27-120 | 5.14 | 18 | 18
DGEBA | MDA |  | Graphite | 100-27-60 | 4.6 | 26.8 | 25 - 30
DGEBA | MDA |  | Graphite | 100-27-60 | 5.14 | 30.5 | 
(DGEBA | MDA |  | Alumine | 100-27-220 | 4.7 | 23.5) | 20 - 50
DGEBA | MDA |  | Alumine | 100-27-220 | 5.14 | 51.7 | 
DGEBA | MDA |  | Alumine | 100-27-100 | 5.15 | 20.6 | 
DGEBA | MDA |  | Alumine | 100-27-220 | 5.15 | 42.5 | 
DGEBA | MDA |  | Fibre de verre | 100-27-50 | 5.19 | 82 | 80 - 100
DGEBA | MDA |  | Fibre de verre | 100-27-60 | 5.18 | 100 | 
EPN | MDA |  | Fibre de verre | 100-29-50 | 5.19 | >100 | >100
TGMD | MDA |  | Fibre de silice | 100-41-50 | 5.20 | >100 | >100
TGMD | DADPS |  | Fibre de silice | 100-40-50 | 5.20 | >100 | 
Legend | 
Resin | 
 | Linear aliphatic
 | Cycloaliphatic
 | Aromatic
Hardener | 
 | Aliphatic Amine
 | Aromatic Amine
 | Alicyclic Anhydride
 | Aromatic Anhydride
Paper [cellulose (C6H10O5)n]
 Strong decrease of radio-resistance
2 Categories of fillers:
Powder fillers
Glass/Silice fibers
The bigger the powder, the more radio-resistant
Hardener choice not influenced by filler
High r.-resistance for Graphite and Alumina
The more fillers, the more radio-resistant
Best Radio-Resistant materials are obtain with Glass/Silice (influence of boron) fibers and aromatic resins (Novolac and glycidyl-amine)

## Slide 24
EPN 1138 with filler | CY 222 (similar to CY221) with filler
MY745 replaced by GY6004 with filler | Other DGBA with filler
MQW
The pure resin mix used shall keep substantial mechanical properties at least till 15-20 MGy
Presence of glass fibre shall increase the substantial mechanical properties at least to 40-50 MGy

## Slide 25: Spacers resins
Composition
  HD polyethylene pipes filled with
Ingredient | Quantity | Description
EPON 826 | 22 kg | Low viscosity, liquid bisphenol A based epoxy resin.
RP 1500 | 3kg | Tetramine hardener
MIN-SIL 120 F | 17 kg | Fused silica particles 50% diameter smaller than 0.044 mm
Assume a limit of
20 MGy

## Slide 26: MBW BINP used resin. We looked at molecule and there is good indication that it should radiation hard as witnessed by the tests and we assume stresses of the order of 10 MPa
MBW
The pure resin mix used shall keep substantial mechanical properties at least till 50-60 (10 MPa)
Presence of fibre glass should probably extend life till 70-80 MGy

## Slide 27: Type of deposition map
Dose (MGy)
Normalization: 1.15 1016 p (30-50 fb-1 ).
Computations with E 6.5 TeV relaxed collimator settings
Dose (MGy)

## Slide 28: Analysis exp. data point 3 and point 7
RP survey IP3
RP survey IP7
7R/7L=B2/B1
3R/3L=B2/B1
297.4 kGy
8.0 kGy
1.6 kGy
6.7 kGy
81.7 kGy
1.3 kGy
2.3 kGy
fallen off
(487.3 kGy)
25.7 kGy
100.4 kGy
59.6 kGy
> 500 kGy
43.7 kGy
19.1 kGy
1/6
1/10
1/3
1
397.5 kGy
119.8 kGy
> 500 kGy
106.3 kGy
487.3 kGy
469.1 kGy
297.4 kGy
329.4 kGy
15.7 kGy
6.3 kGy
18.0 kGy
9.2 kGy
4.4 kGy
5.5 kGy
2.3 kGy
1/100
1/20
1
1

## Slide 29: Point 3 and 7 coil magnet damage estimation
MQW | MBW
From 10 to 20 MGy | From 40 to 60 MGy
From 20 to 50 MGy | From 60 to 80 Mgy
Larger than 50 MGy | Larger than 80 MGy
IP 7
IP 3

## Slide 30: Screen design
- For max effectiveness we have to target the higher possible density candidate therefore W, or better the alloys for machining
- Magnetic properties can be an issue. Measurement being performed
- Possible material staging along the MQW magnet length under study
 | Inermet IT180
Nominal density | 18
W content % | 95
Balance | Ni,Cu
E-modulus | 360 GPa

## Slide 31: MQW shielding effect
Normalization: 1.15 1016 p (50 fb-1 )
Beam 2
Beam 2
Beam 2
Beam 2

## Slide 32: MBWA - MBWB Peak Dose profile
MBW.B6R7 Flanges + Protection
Beam 2
MBW.A6R7
Flanges + Protection
Beam 2
MBW.A6R7 with Flanges
Beam 2
Normalization: 1.15 1016 p (50 fb-1 )
MBW.B6R7
With Flanges
Beam 2

## Slide 33
ABS
Optic change proposal point 7 discussed and agreed as possible with M. Giovannozzi
(it needs verification)

## Slide 34: Magnet damage with shielding point 3 and 7, W shielding peak dose scaling
 | Action LS1 |  | Dose [MGy] for integrated luminosity 150 fb^-1 |  | Action LS2 |  | Dose [MGy] for integrated luminosityy350 fb^-1 |  | Action LS3 |  | Dose [MGy] for integrated luminosity3000 fb^-1 |  | Action during HL-LHC exploitation | 
 | R | L | R | L | R | L | R | L | R | L | R | L | R | L
MQWA.A4 |  |  | 0.4 | 0.5 |  |  | 0.9 | 1.2 |  |  | 7.4 | 11 |  | 
MQWA.B4 |  |  | 0.3 | 0.8 |  |  | 0.7 | 1.9 |  |  | 6.4 | 16 |  | 
MQWB.4 |  |  | 0.5 | 1.3 |  | S | 1.2 | 1.8 |  | S | 10.1 | 9 |  | 
MQWA.C4 |  |  | 4.0 | 4.0 | S | S | 5.8 | 5.8 | S | S | 30 | 30 |  | 
MQWA.D4 |  |  | 2.7 | 2.7 | S | S | 3.8 | 3.8 | S | S | 20 | 20 |  | 
MQWA.E4 |  |  | 5.0 | 10.0 | S | S | 7.2 | 14 | S | S | 37 | 73 |  | R
MQWA.A5 |  |  | 2.6 | 2.6 | S | S | 3.7 | 3.7 | S | S | 19 | 19 |  | 
MQWA.B5 |  |  | 3.5 | 3.5 | S | S | 5.0 | 5.0 | S | S | 25 | 25 |  | 
MQWB.5 |  |  | 4.1 | 4.1 | S | S | 5.9 | 5.9 | S | S | 30 | 30 |  | 
MQWA.C5 |  |  | 1.9 | 4.9 | S | S | 2.8 | 7.0 | S | S | 14 | 36 |  | 
MQWA.D5 | S | S | 1.4 | 2.0 | done | done | 3.3 | 4.7 | done | done | 27.9 | 39.9 |  | 
MQWA.E5 | S | S | 12 | 4.1 | done | done | 29 | 10 | done | done | 246 | 82 | R | R
MBW.A6 | S | S | 7.8 | 5.5 | done | done | 18 | 13 | done | done | 155 | 111 | R | R
MBW.B6 | S | S | 12 | 6.2 | done | done | 30 | 14 | done | done | 248 | 124 | R | R
Limit reached in | 7R | 7L
MQWA.E4 |  | 1500 fb^-1
MBW.B6 | 1500 fb^-1 | 2400 fb^-1
MBW.A6 | 1000 fb^-1 | 2000 fb^-1
IP 7
IP 3
Remove
 | Action LS1 |  | Dose [MGy] for integrated luminosity 150 fb^-1 |  | Action LS2 |  | Dose [MGy] for integrated luminosity 350 fb^-1 |  | Action LS3 |  | Dose [MGy] for integrated luminosity 3000 fb^-1 |  | Action during HL-LHC exploitation | 
 | R | L | R | L | R | L | R | L | R | L | R | L | R | L
MQWA.A4 |  |  | 0.0 | 0.1 |  |  | 0.1 | 0.2 |  |  | 1.0 | 1.9 |  | 
MQWA.B4 |  |  | 0.1 | 0.1 |  |  | 0.1 | 0.2 |  |  | 1.0 | 2.1 |  | 
MQWB.4 |  |  | 0.1 | 0.1 |  |  | 0.1 | 0.3 |  |  | 1.1 | 2.2 |  | 
MQWA.C4 |  |  | 0.1 | 0.1 |  |  | 0.2 | 0.3 |  |  | 1.4 | 2.8 |  | 
MQWA.D4 |  |  | 0.2 | 0.3 |  |  | 0.4 | 0.8 |  |  | 3.5 | 6.9 |  | 
MQWA.E4 |  |  | 0.9 | 1.7 | S | S | 1.2 | 2.5 | S | S | 6.3 | 12 |  | 
MQWA.A5 |  |  | 0.6 | 1.1 | S | S | 0.8 | 1.6 | S | S | 4.0 | 7.5 |  | 
MQWA.B5 |  |  | 0.7 | 1.4 | S | S | 1.0 | 2.0 | S | S | 5.1 | 9.4 |  | 
MQWB.5 |  |  | 1.7 | 3.3 | S | S | 2.4 | 4.8 | S | S | 12 | 23 |  | 
MQWA.C5 |  |  | 3.9 | 7.7 | S | S | 5.6 | 11 | S | S | 29 | 53 |  | 
MQWA.D5 |  |  | 0.9 | 1.9 | S | S | 1.3 | 2.7 | S | S | 6.8 | 13 |  | 
MQWA.E5 |  |  | 1.7 | 3.5 | S | S | 2.5 | 5.0 | S | S | 13 | 24 |  | 
MBW.A6 |  |  | 1.0 | 2.0 | S | S | 1.4 | 2.9 | S | S | 7.3 | 14 |  | 
MBW.B6 |  |  | 1.2 | 2.3 | S | S | 1.7 | 3.3 | S | S | 8.4 | 16 |  | 
MBW.C6 |  |  | 1.6 | 3.3 | S | S | 2.3 | 4.7 | S | S | 12 | 3 |  | 

## Slide 35: MQW Shielding strategy Bring the coil below 50 MGy, trying to get uniform and below that level (useless to have points at 10 MGy if your peak is at 50 MGy)
 | Peak dose reduction factor to reach 3000 fb^-1 |  | Shielding strategy | 
 | R | L | W | Steel/Copper/Bronze
MQWA.A4 | Not needed | Not needed |  | 
MQWA.B4 | Not needed | Not needed |  | 
MQWB.4 | Not needed | Not needed | none | full length
MQWA.C4 | 1.6 | 1.6 | 50 cm | rest of length
MQWA.D4 | 1.1 | 1.1 | none | full length
MQWA.E4 | 2.0 | 4.0 | 100 cm | rest of length
MQWA.A5 | 1.0 | 1.0 | none | full length
MQWA.B5 | 1.4 | 1.4 | none | full length
MQWB.5 | 1.6 | 1.6 | 50 cm | rest of length
MQWA.C5 | Not needed | 1.9 | 50 cm | rest of length
MQWA.D5 | 1.7 | 2.4 | 100 cm | rest of length
MQWA.E5 | 14.8 | 4.9 | 100 cm | rest of length
IP 7
 | Peak dose reduction factor to reach 3000 fb^-1 |  | Shielding strategy | 
 | R | L | W | Steel/Copper/Bronze
MQWA.A4 |  |  |  | 
MQWA.B4 |  |  |  | 
MQWB.4 |  |  |  | 
MQWA.C4 |  |  |  | 
MQWA.D4 |  |  |  | 
MQWA.E4 | Not needed | Not needed |  | 50 cm
MQWA.A5 | Not needed | Not needed |  | 50 cm
MQWA.B5 | Not needed | Not needed |  | 50 cm
MQWB.5 | Not needed | 1.4 | 50 cm | rest of length
MQWA.C5 | 1.7 | 3.3 | 100 cm | rest of length
MQWA.D5 | Not needed | Not needed |  | 50 cm
MQWA.E5 | Not needed | 1.5 | 50 cm | rest of length
IP 3

## Slide 37
ABS
Optic change proposal point 7 discussed and agreed as possible with M. Giovannozzi
(it needs verification)

## Slide 38: Estimated MQW spacer damage with screens (extrapolated red. factor 3)
Need to modify screen design
IP 7
IP 7

## Slide 39: Conclusions I
 |  | IP3 |  |  |  |  |  | IP7 |  |  |  |  | 
 |  | L |  |  | R |  |  | L |  |  | R |  | 
 |  | Broken units no int | Units to be modified | Broken units | Broken units no int . | Units to be modified | Broken units | Broken units no int | Units to be modified | Broken units | Broken units no int . | Units to be modified | Broken units
LS1 | MQW | NA | 0 | NA | NA | 0 | NA | NA | 2 | NA | NA | 2 | NA
 | MBW | NA | 0 | NA | NA | 0 | NA | NA | 2 | NA | NA | 2 | NA
LS2 | MQW | 0 | 7 | 0 | 0 | 7 | 0 | 0 | 7 | 0 | 0 | 8 | 0
 | MBW | 0 | 3 | 0 | 0 | 3 | 0 | 0 | NA | 0 | 0 | NA | 0
LS3 | MQW | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 0 | 0
 | MBW | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 0 | 0
HL-LHC | MQW | 4 | 0 | 0 | 1 | 0 | 0 | 9 | 0 | 1 | 9 | 0 | 0
 | MBW | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 0 | 2 | 2 | 0 | 2

## Slide 40: Conclusion II
The proposed screen allow reducing of a factor 3 the dose and limit the number of magnet at risk or surely damaged, see previous slides. Hp. to achieve the same reduction factor on the spacers
The change of the optic in point 7 installing a long absorber is key to complete the protection
The lifetime of these units could be affected by the new environmental condition of point 7 not discussed here

## Slide 41: Conclusion III: actions
The proposed shielding campaign should start in LS1 for effectiveness and ALARA
Very high dose dosimeter shall be installed systematically in point 3 and 7 to check better benchmark computations and symmetry effect
A campaign of irradiation of resins shall be performed with the real used resins and the relevant fillers in order to real know when the magnet will reach damage level
For HL LHC 4 MBW shall be reassembled with saddle type heads. This will solve the issue without needing special development
I suggest that we launch the program to build a NC magnet with extremely high radiation resistance (>300 MGy). It is and it will be more and more needed and today we do not have it in our capabilities and it will be key for future target areas development
We need to check
  For HL-LHC the MBW radiation dose along the straight part of the coil
  The level of accumulated dose of the MBXW units
  If any protecion can be added to on the beam line for the MQWA.E4 in point 7 R and 7 L

## Slide 42: Long version

## Slide 43
The doses

## Slide 44: Dose evaluation process for each point
Fluka model results with 1.15 1016 p lost per interaction point E 6.5 TeV.
Scale to 7 TeV (linearly)
Scale to the dosimeter readings as benchmark (TS2)
Scale to the increase slope dose/luminosity after TS2
Normalise to a total losses (adding the 2 points) of 1.15 1016
Scale to the Left and Right using RP survey
IP 3
IP 7
1.077
1
(Fluka esti. already 7 TeV)
1
1
Scale to the LS1, LS2 LS3 and HL-LHC integrated luminosity
150 fb-1 ->3
350 fb-1 -> 7
3000 fb-1 ->60
150 fb-1 ->3
350 fb-1 -> 7
3000 fb-1 ->60
2
2
0.23
0.98->1
L=1
R=0.5
L=1
R= (0.4->2)

## Slide 45: Relationship dose vs. luminosity and point 7 vs. point 3
2
196.7/(697+196.7)=0.23
1357/(1357+30)

## Slide 46
100-400 kGy
60 kGy
one would get
by normalizing to
1.4 1015 beam 1 protons lost in P7
IP7
TCP.D C B 6L7.B1
v
h
s
MBW
MQW
beam 1
s
TCAP
assuming a horizontal halo
for 1.15 1016 lost protons per beam
MEASUREMENTS VS EXPECTATIONS
(different collimation settings and before change of slope losses vs. luminosity )
peak dose
for intermediate
collimator settings
taking for 4 TeV
with tight settings
2 250kGy
0.5 60 kGy
measured
F. Cerutti 03/09/2012

## Slide 47: Point 3 vs. point 7
397.5 kGy
119.8 kGy
> 500 kGy
106.3 kGy
487.3 kGy
469.1 kGy
297.4 kGy
329.4 kGy
15.7 kGy
6.3 kGy
18.0 kGy
9.2 kGy
4.4 kGy
5.5 kGy
2.3 kGy

## Slide 48
297.4 kGy
8.0 kGy
1.6 kGy
6.7 kGy
81.7 kGy
1.3 kGy
2.3 kGy
fallen off
(487.3 kGy)
25.7 kGy
100.4 kGy
59.6 kGy
> 500 kGy
43.7 kGy
19.1 kGy
Point 3 vs. point 7

## Slide 49: Estimated dose point 3 and point 7
IP 3
IP 7

## Slide 50
Magnet lifetime

## Slide 52: Different scenarios agreed with M. Giovannozzi
Other operating scenario
Reconfigure the MQWA in pos. C5 as MQWB
Remove MQWA.E5
Connect new MQWB.C5 in the circuit RQ5.LR7
Substitute MQWA.E5 with an absorber at least effective as previous MQWA.E5
    In IR3 no MQWB can be removed without changing the optical conditions at the collimators.
    In IR7 the MQWB modules in the two Q5 may be removed without changing the optical conditions at the collimators (2 spare magnets

## Slide 53: Power deposition

## Slide 54: Power deposition
 | MQW |  | MBW | 
Ultimate current | 810 | A | 820 | A
Electrical dissipated power ultimate current | 25 | kW | 41 | kW
Delta T measured ultimate current on cooling water | 16 | C | 30 | C
New operational current | 620 | A | 650 | A
New dissipated electrical power operational current | 15 | kW | 26 | kW
Worst dissipated power due to radiation losses (including dissimetry and new loss rate) | 3 | kW | 4 | kW
New total power to be dissipated (Pel+Prad+Pconv) | 19 | kW | 30 | kW
New Delta T necessary to evacuate the power | 12 | C | 22 | C
New magnet working temperature | 38 | C | 48 | C
Remark
Due to small lifetime (load case 1h) we do not take into account the coefficient 2linked to the ratio losses/luminosity nor the discrepancy B1/B2 (L/R)

## Slide 55: MQWA.E Energy Deposition on various elements
5770
5670
2310
1780
1670
50
70
2030
2130
2230
1950
50
110
500
110
1250
720
370
210
290
570
4550
640
1290
Values are in pJoule/proton lost in the collimators
60
2020
90
With Protection over 50 c m

## Slide 56: Peak power adiabatic (wrong) approximation in shielding
Baking vacuum chamber
T->230 C
Necessary 4 KW to get to the temperature along several hours
 | MQW shielding |  | MQW beam pipe |  | MBW shielding | 
Env Temp | 50 | C | 50 | C | 50 | C
Integral proton energy lost | 1012 | pJ/proton | 4550 | pJ/proton | 256 | pJ/proton
symmetry, loss rate and 7 TeV factor | 1.0775 |  | 1.0775 |  | 1.0775 | 
Proton losses | 9.00E+10 | proton/s | 9.00E+10 | proton/s | 9.00E+10 | proton/s
Loss time | 3600 | s | 3600 | s | 3600 | s
Total integral power | 98 | W | 441 | W | 25 | W
Assumed ratio Pmax/Pmin along magnet | 4 |  | 4 |  | 1 | 
Adiabatic Delta T Pmax | 170 | C | 750 | C | 224 | C
Adiabatic Delta T Pmin | 43 | C | 190 | C |  | 

## Slide 57: Installation issues and planning

## Slide 58: Installation/planning/risks
To reduce radiation aging intervention on most exposed magnets shall performed in LS1 (also for ALARA reasons ). The initial foreseen modus operandi directly on the magnet in the tunnel is not feasible because of the interference with the backing equipment. Due to the limited number of vacuum chambers available and also field quality sorting it is better to modify the magnets presently installed in LHC and replace them in the same slot. It will help in saving non radioactive spares.
The backing strips power wiring and the related thermocouples need to be rewired. VSC (N. Zelko) performed test and it looks feasible. Possible back up strategy with screen modification is available
Possible planning sequence
  From 18/11/2013 till 30/11/2013 removal of 8 magnets and transport to point 6
  From 20/11/2013 modification of 1st unit in 867 workshop
  From 01/02/2014 start re-installation
  01/03/2014 complete re-installation
Risks | Solutions/Consequences
Screens not available on time | Install steel screen or re-install without screen
W-Ni-Cu alloy cause no acceptable field distortion | Install reduce effectiveness copper or steel screens
Difficult installation on MBW | Possibility to machine the shielding to ease installation and close the hole with W tap
Damage of backing strip | One magnet not backed out

## Slide 59: MBW

## Slide 60: MQW

## Slide 61
LHC Point 7
Ambient dose equivalent rates in µSv/h at 40cm
measured on Dec 20, 2012
(last “good” fill on Dec 5, i.e. cooling time >1week)
tcool | Scaling factor
One hour | 1.4
One day | 1.0
One week | 0.73
One month | 0.45
4 months | 0.20
Scaling factors
based on generic
Studies for IR7:

## Slide 63
ISR~MQW
SPS

## Slide 67: Electrical Properties Changes 2
Volumetric Resistivity r (Ω·cm)
1010
1011
1012
1013
1014
1015
1016
1017
0
20
40
60
80 100 120 140 160 180 200 Temp. (°C)
○ DGEBA + MDA
x EPN + MDA
∆ TGMD +MDA
_______ Non irradié
_ _ _ _ _ 2.7x109 rad
T ↑ => r ↓
r = ~1016 Ω·cm @RT
High mechanical radio-resistance  High electrical resistance (mechanical degradation occurs first)
Example of low mechanical-resistance system:
DGEBA-DBP-TETA  r = ~1013 Ω·cm @RT for 6.8x108 rad

## Slide 68: DGEBA considerations

## Slide 69: PROPOSALS I
 | Traction test | Flexural test | Leakage current in air humid | Dielectric in air humid | Leakage current in air humid after 1 month in water | Dielectric in air humid after 1 month in water
0 MGy | Y | Y | (Y) | Y | (Y) | Y
10 Mgy |  | Y | (Y) | Y | (Y) | Y
20 Mgy | Y | Y | (Y) | Y | (Y) | Y
40 Mgy | Y | Y | (Y) | Y | (Y) | Y
50 MGy |  |  | (Y) | Y | (Y) | Y
60 MGy | Y | Y | (Y) | Y | (Y) | Y
70 MGy | Y | Y | (Y) | Y | (Y) | Y
Wafer 1 and 2 mm thickness resin and glass fibre

## Slide 70: PROPOSALS II
 | Shear test | Leakage current in air humid | Dielectric in air humid | Leakage current in air humid after 1 month in water | Dielectric in air humid after 1 month in water
0 MGy | Y | (Y) | Y | (Y) | Y
10 Mgy |  | (Y) | Y | (Y) | Y
20 Mgy | Y | (Y) | Y | (Y) | Y
40 Mgy | Y | (Y) | Y | (Y) | Y
50 MGy |  | (Y) | Y | (Y) | Y
60 MGy | Y | (Y) | Y | (Y) | Y
70 MGy | Y | (Y) | Y | (Y) | Y
Insulated cables, 2 resins, 3 samples