## Slide 1
3D Silicon and 3D Diamond Detectors for Future Upgrades of LHC Experiments
Particle Physics
IOP 2014
7-9.04.14
Presented by Iain Haughton
..

## Slide 2
Overview
Motivation
Material Properties
Geometry
Silicon
Diamond
Conclusion

## Slide 3
Motivation
LHC Increasing Luminosity
Jose Bernabeu, “Silicon Strip Detectors for the ATLAS HL-LHC Upgrade”.
Expected fluence @ HL-LHC innermost layer: 2E16 1MeV neq/cm^2
LHC equivalent to 6000 fb^-1
2 x target luminosity

## Slide 4
Property | Silicon | Diamond
Band Gap (eV) | 1.12 | 5.5
Dielectric Constant | 11.9 | 5.7
Breakdown Field (V/m) | 107 | 107
Thermal Conductivity (Wcm-1k-1) | 1 | 22
Displacement Energy (eV) | 20 | 43
Material Properties

## Slide 5
Charge Collection
Silicon
MIP
h
e
p+
p+
n+
MIP
h
e
Diamond

## Slide 6
Charge Collection
Radiation Damage
MIP
+
-
+
+
+
+
+
+
+
+
-
-
-
-
-

## Slide 7
Geometry
Planar
3D
MIP
h
e
p+
p+
n+
MIP
h
e
n+
n+
p+
Δ
L
Δ
L

## Slide 8
Silicon
3D Silicon Fabrication
Wafer cleaning.
Mask production.
Deep Reactive Ion Etching of column holes.
column hole filling with poly silicon.
Introduction n+ and p+ dopants.
Addition of metallisation layer.
1
2
3
4
5
6

## Slide 9
Silicon
3D Silicon for the HL LHC
IES = 56μm
50% signal efficiency
after 2×1016 1MeV neq/cm2
p+
p+
p+
n+
p+
100μm
50μm

## Slide 10
Diamond
Planar Diamond
Single Crystal Diamond
Polycrystalline Diamond
Planar Diamond Detector
ATLAS Diamond Beam Monitor.
To be installed in Phase 0 upgrade.

## Slide 11
Diamond
3D Diamond Fabrication
Wafer cleaning.
Laser drilling of columns.
Addition of metallisation layer.
1
2
3
1
2
fs Laser
Diamond

## Slide 12
Diamond
Planar versus 3D Diamond

## Slide 13
Conclusion
Aim to produce innermost layer detectors  perform after a radiation fluence of 2×1016 1MeV neq/cm2, as expected at the HL LHC.
3D Silicon, having been proven for the IBL ATLAS project, is a good candidate.
Trying to apply 3D geometry to other semiconductors, specifically diamond.
Generation of first 3D Diamond prototype using a laser for fabrication. Results are promising.